Properties of Glass
    72% Silica + 13% Soda Ash + 13%Limestone +Feldspar all melted at about 1510 degrees C.
- Essentially solid below about 510 deg C.
- Has an average coefficient of expansion (0 - 300 °C) of about 8.6 x 10-6/°C
  - (1m long glass will expand 2.58mm in 300 °C)
Very strong in Compression.
  - (Can withstand 1,000,000 psi. – 6894 MPa)‏
Relatively weak in Tension.
  - (can only take about 4-5000 psi (34 MPa) due to surface micro-flaws. A perfect surface can take about 150,000 psi. (1034 MPa))‏
Therefore, to break, the glass must be in Tension.
Tempered glass has all external surfaces in compression and is therefore very difficult to break compared to raw glass.
[Speaker Notes: 72% sand (silica)‏ 13.6% Soda Ash (sodium carbonate) is used as a flux to help melting. 12.6% Limestone (calcium carbonate) makes glass durable and insoluble. 1.7% Feldspar (alumina) makes glass hard - good weather resistance. Glass is weak in Tension. We cut glass by scoring the surface and then put the scored surface into tension when we ‘break-out’. Soda-Lime Glass:	Has a coefficient of expansion (about 7-8*10-6 /OC). Borosilicate Glass (Pyrex):	Has a lower coefficient of expansion (about 3-4*10-6 /OC).]

---
Glass Exit Temperature
- Why 'well above' the 'Annealing' point?
- When we start quenching, the centre (inside) also starts to cool, and we need time to get a difference of around 100 C to 170 C between surface and centre, before the centre cools below the 'Transition' point.
  Then maintain the temperature difference until the glass is well below the 'Strain Point'
410 C
560 C
410 C

---
Master What We Want
What we must achieve
- A very Uniform temperature in the glass
- At a temperature well above the 'Transition' point
- Keep the glass optically flat whilst soft
- Transfer it to a Quench
- Uniformly cool it at a controlled rate to a temperature below it's 'Transition' point
- Then maintain the cooling rate until well below the 'Strain' point where the glass becomes solid
- Cool it down to a handling temperature
Result:- Perfect Tempered glass

---
Heat-Soaked Glass
- Fully Toughened Glass.
- Soaked at 290 deg C for 2 hrs.
(EN 14179-1)‏
Accelerates ageing of Nickel Sulphide Particles.
    - Where nickel rich contaminants such as stainless steel are present in the glass melt materials, the nickel may combine with sulphur in the batch or furnace fuels to form an impurity called nickel sulphide (NiS).
- Not prone to spontaneous breakage.
- Usually more applicable to thick glass. (10mm and above)‏

---
Uniform Quenching
- Critical to ensure no thermal distortion
- Good Quench box and nozzle design
- Good air release top and bottom
- Good ride into and through the Quench
  - Spiral wrapped rolls and mimics
  - Accurate box alignment
- 100% clear nozzles
- Stable air pressure
- Time in High/Medium Pressure sections to get glass well below 'Strain Point' temperature.

---
Recommended Additional Equipment
Scanning Infra Red Camera – Raytec or LandScan
Stress Measurement
Edge stress – Strain Optics
Surface stress – Toshiba Differential Surface Refractometer
Optical Evaluation
Zebra board at entrance to unload table.
Manual transmitted and reflective optics rig
Automatic 'On-line' rig – LiteSentry Osprey 5

---
Quench Breakage - Causes
- Transient tension breaks or cracks glass in first few seconds.
- High surface tension is caused by glass being too cold for quench pressure being used.
- Normal tension will cause cracks to run from flaws.
  - Poor: cutting, breakout, edgeworking, & handling.
- Flipping in quench can cause shocks and cracks.
- Glass corners damaged during heating.
- Damage from glasses touching during index into quench.
- Water dripping from Ircon camera housing.

---
Sulphur Dioxide SO2
- SO2 Oxidises easily and becomes SO3
- If in contact with Moisture (H2O) becomes H2SO4
(Sulphuric Acid)‏
- In contact with Sodium (Na) in surface of glass becomes a form of Sodium Sulphate NaSO3 which is liquid at furnace temperatures providing a lubricant. Reduces ‘White Marking’.
- Condenses into brown spots which have a coefficient of expansion greater than ceramic rolls.
- Large spots will lift off rolls during cool down – damaging surface of roll.
- Will simply wash off roll using hot water (600C).

---
Quench Pressure Required