(2000, Daimler Chrysler, Moisel)
- Polymer waveguides, 200x200 µm, 0.03 dB/cm @ 780 nm, flexible substrate demonstrated
- Micromirroirs + lenses

---
(2004, IBM Zurich)
- Acrylate polymer on FR4 with doctor blade or spray coating, 50x50 µm – 30x30 µm, UV mask proximity photolithography, 0.04 dB/cm @ 850 nm
- Waveguide crossing 0.02 dB