Thermogravimetric Measurements

Thermogravimetric analysis / differential thermal analysis were performed on a Netzsch STA/QMS STA 449 F1 Jupiter. All measurements of CPs were done prior to any (deliberate) solvent exchange experiments.
It is hardly possible to predict which kind of species develop during a slow thermal decomposition in He flow. Also, the species must be volatile enough to travel through the (heated, > 180 °C) capillary to the MS device. Furthermore, if, and that is likely, radical species are released they may recombine with each other or miscellaneous species and form unpredictable results. Thus MID (multiple ion detection) was set to products that were assumed to be possible during decomposition. Bargraph scanning tries to detect all masses in a preset range but is slower and may miss a signal.

Curves have been smoothened slightly. Sometimes substances that char might start to oscillate the balance slightly by their decomposition. Yet, a material ejection from the crucible would involve a permanent mass loss, and the latter was not detected.
Also starts of the curves may show very light variations due to an unreached buoyancy equilibrium in the helium flow. A mass signal does not strictly correlate with the temperature of measurement at the time (traveling time, detection).

Thermal Properties of TBAPy (C44H26O8, 682.67 g/mol):

Mass loss starts after the 205 °C mark is passed. It is not clear what leaves the molecule in this step. A single decarboxylation would yield a similar result. It might also include small amounts of water leaving over time that were clinging to the structure. It is also not obvious if there are two steps following or just one. And indication for a second step might also come from the DTA curve that show a change in energy consumption. MS delivers signals for 18 (H2O), 28 (CO) and 44 (CO2) only in the late phase of decomposition that left charred remains.
Thermal Properties of TPyPy (C36H22N4, 510.58 g/mol):

Information beforehand: The substance likely included some NaCl, despite multiple washings. Thus the decomposition steps shown should be acceptable in quality but quantity is likely below optimum conditions. EA showed about up to 3 units NaCl for the same bulk this sample was taken from. That would relate to about less than a third of mass. Comparing this with the findings for ACPy4 the remaining ~ 25% here might be the NaCl plus few C.
The compound is stable up to 200 °C where decomposition slowly starts. It seems to take place in two steps - the second starting at about 400 °C. No decomposition products could be detected with a bargraph scan (N2, HCN, pyridine) (intensity too low).