### Silicon dioxide (SiO2) from Dry Oxidation (O2)
Basic configuration
N2, O2
Temperature at 800-1100°C
Dummy wafers (at least 1 on each side of process load), 2 heatbarriers and 1 flowbaffle
Description
Purpose
Dry Oxidation is used to create an insulating SiO2 layer using the mono crystalline Si of the wafer. The silicon dioxide layer is used as a mask during dopant diffusion, as a junction passivation, as an insulating field oxide and as a gate oxide. Due to its low oxidation rate it is typically used for an oxide film thickness up to 1000Å
Chemicals
Oxygen is the basic gas of every combustion reaction and therefore leaks can be dangerous near hot areas.
Process
Oxygen (O2) reacts with the Silicon top layer of the wafer into Silicon dioxide like:
Si + O_{2} rightarrow SiO_{2}

Oxygen must diffuse through the formed SiO2, so the process will slow down in time, because silicon dioxide is a barrier to oxygen diffusion.

###### Figure 1.1-1: Si consumed by the oxidation process
Cross-wafer uniformity is normally very good, since the diffusion process is limited by the surface reaction part. If relatively small wafers are used (compared to the tube diameter) an increased gas flow improves cross-wafer and cross-load uniformity drastically.
Typicalities
To improve cross-wafer uniformity at the front and back of the wafer load it is necessary to apply a set of dummy wafers at each side of the load. A flowbaffle is necessary.
Startup parameters for processing
Available on request.
Process result indication
Available on request.
Gas schematic example: Dryoxidation
Available on request.
Recipe example horizontal tube: silicondioxide using Dryoxidation O2
Available on request.

©Copyright Sep 2015 Tempress Systems, The Netherlands. This document contains information proprietary to Tempress Systems and shall not be used for engineering, design, procurement or manufacture in whole or in part without the consent of Tempress Systems