Light emitting AlOx tunnelling junctions

---
Outline
- Motivation
- Device fabrication
- Measurements
- In-situ oxidation
- Conclusion & Outlook

---
Motivation
- LEIT: fast emittion for optical connections
- Device size scalable to ultimate limit
- 2D materials: no scalable fabrication process (so far)
- Al deposition and patterning: standard process

---
Fabrication
Oxidised Al electrode
Junction Area
Au Counter electrode

---
Results

---
Context: inelastic tunnelling
Electrons tunnelling into Eν<Eμ
Launches SPP
SPP might couple to far field (photons!)
h %omega = E_%mu - E_%nu

---
Corner Emission

---
Context: SPP dispersion
k mismatched
ways to add k:
device edges
surface roughness
optical antennas
Limited propagation

---
Temporal stability

---
In-situ oxidation
Shadow Mask, offset
Evaporation 1
In-Situ oxidation
Evaporation 2
Resulting Tunnel Junction

---
Results

---
Conclusion
- Al – AlOx – Au Tunnel Junctions
- Light emission
- Controlled in-situ oxidation

---
Outlook: Optical Antennas

---
Outlook: Template Stripping

---
Thank you
Lukas, Markus,
Achint, Jan Winkler (OMEL),
2D-Subgroup
- Questions?

---
Spectrum

---
Results