Thread   Test Report

Page no – 480

DN NO - 34885

Supplier Name – New supplier Ningbo xindew pvt LTD

| DESCRIPTION | UNIT | SPECIFICATION | NO.OF PLYS | BREAKING LOAD | RESULT |
| --- | --- | --- | --- | --- | --- |
| TKT 40 White | Kg / N | 4.5 ± 0. 5 | 3 | 4.5 kg | ok |
| TKT 40 Black |  | 4.5 ± 0. 5 | 3 | 4.6 kg | ok |
| TKT 60 White |  | 3.5 ± 0. 5 | 2 | 3.4 kg | ok |
| TKT 60 Black |  | 3.5 ± 0. 5 | 2 | 3.1 kg | ok |
| TKT 15 White |  | 12.0 ± 2. 5 | 3 | 13.0 kg | ok |

* All Test Results is ok.

Rathnayaka– AQO

Date – 12/September/2011

Note: This is an electronically prepared document therefore signature is not necessary

Bonding Test Report

Page No: - 409

DN No: - 35340

Indent No  -  SSL – 11 - 65 M

| ITEM | SOLE MATERIAL | UPPER MATERIAL | APPLIED PRIMER | APPLIED ADHESIVE | TEST RESULTS |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | L | R |
| PF0126 Size – 12 | Gajeendra white Ex : 80 Com : 20 | Toe cap PVC Material 2414 White + Lamicamber White With 1 mm Eva 54 “ others 2414 White | MEK + Cyclo 10 : 90 |  | 16.7 kg | 17.1 kg |

Bonding Specification - 10 Minimum

Note:  Bonding result is ok

Ratnayaka – AQO

Date: 27/October/2011

Note: This is an electronically prepared document therefore signature is not necessary

Bonding Test Report

Page No: -   69

DN NO: -   35103

| ITEM | SOLE MATERIAL | UPPER MATERAL | APPLIED PRIMER | APPLIED ADHESIVE - | USED HARDNER | TEST RESULTS |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | L | R |
| PF0120 Size - 10 O. NO - 11 - 1788 Random test | Rubber Balck | 3514 black | Sole - Eth : Hal 100 g : 3 g Upper - MEK | 5030 1Kg Bostic Bostikure Hardner 20 g | Bostikure Hardner - D Temperature 65 °c | 14.0 kg | 13.1 kg |
| PE0120 Size - 09 O. NO – 11 – 1787 Random test | Rubber Balck | 3514 black | Sole - Eth : Hal 100 g : 3 g Upper - MEK | 5030 1Kg Bostic Bostikure Hardner 20 g | Bostikure Hardner - D Temperature 65 °c | 16.2 kg | 17.7 kg |

Comment:    Bonding result is not ok, due to poor bonding strength

Bonding Specification - 10 Minimum

Bonding result is ok

Ratnayaka-AQO

Date: 01, September, 2011

Note: This is an electronically prepared document therefore signature is not necessary.

PVC   Sample Test Report

DN NO - 34274

PAGE NO -308

| Sample no | Hardness | Specific Gravity |
| --- | --- | --- |
| 1 | 70 – 72 Asker Type C | 1.103 |
| 2 | 70 – 72 Asker Type C | 1.046 |

Ratnayaka – AQO

Date : 09,October, 2010

Note: This is an electronically prepared document therefore signature is not necessary.

PVC   UV Test Report

DN No: - 35057

PAGE NO -475

TEST SAMPLE – pvc material white

| DESCRIPTION | UNIT | SPECIPICATION | TEST RESULT | Remark |
| --- | --- | --- | --- | --- |
| pvc material white 1 – 27 weak no upper component 2414 white + lamicambr white with 1 mm Eva 54" | hours | 3 hours | colour not change | O.K |

Note:    Ucification: 3 hours in UV oven are similar to 6 months in normal atmosphere

Rathnayaka           – AQO

Date: 17/August/2011

Note: This is an electronically prepared document therefore signature is not necessary.

Bonding   Test Report

Page no – 342

DN NO -    319462

| DESCRIPTION | ITEM | SOLE UPPER MATERIAL | UV TEST RESULTS |
| --- | --- | --- | --- |
| Bonding strength | PF0093 size 06 | SPC Ex .8 com-2 EXP.SFC-80209079 (0-50) com . SSL -10-96 m | NOT OK |
| Bonding strength | PF0093 size-07 | Mazda Ex .8 com-2 Exp-Fw-80G D28 com –Fw-65GL-20C | OK |
| Bonding strength | PF0093 Size -07 | Gajeendra Ex .8 com-2 EXP.COM SSL/11-06 M Indent No | NOT OK |
| Bonding strength | PF0093 Size -06 | Gajeendra Ex .8 com-2 EXP.COM SSL/11-07 M Indent No | NOT OK |

Note:    UV Specification: 3 hours in UV oven are similar to 6 months in normal atmosphere.

Rathnayaka– AQO

Date – 11/May/2011

Note: This is an electronically prepared document therefore signature is not necessary

Bonding Test Report

Page No: -385

DN No: - 34758

| ITEM | SOLE MATERIAL | UPPER MATERIAL | APPLIED PRIMR | APPLIED ADHESIVE | USED HARDNER | TEST RESULTS |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | L | R |
| PE-0120 Size - 09 | Rubber | 3514 black | Sole - Eth : Hal 100 g : 3 g upper – M E K | Bostic 5030 1 kg boscoder -10 g Adhesive drying time , 16 hrs heat activation 1 min in 650C | Boscoder D Temperature 650C | 19.3 kg | 15.1 kg |
| PE-0092 Size - 03 | Rubber | 2116 black | Sole - Eth : Hal 100 g : 3 g upper – M E K | Bostic 5030 1 kg boscoder -10 g Adhesive drying time , 16 hrs heat activation 1 min in 650C | Boscoder D Temperature 650C | 23.0 kg | 22.5 kg |

Bonding Specification - 10 Minimum

Note:    Bonding result   ok

Ratnayaka – AQO

Date: 26/July/2011

Note: This is an electronically prepared document therefore signature is not necessary

Bonding Test Report

Page No: - 290, 291, 292, 293, 289

DN No: - 34758

| Sample No | Description | Sole | Upper | Primer | Adhesive | Hardener | Test Result Kg |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | Left | Right |
| 1 | PE0087 Size -02 | TPR Black | Leather Black | Sole – MEK 30 min Eth : Hal 100g : 3 g 30 min | Bostic Black 1 kg Rc 20 g | RC | 40.0 kg | 31.0 kg |
| 2 | PE0087 Size -03 | TPR Black | Leather Black | Sole – MEK 30 min Eth : Hal 100g : 3 g 30 min | Bostic Black 1 kg Rc 20 g Double code | 311FT 3448 ( 4 % ) | 25.6 kg | 29.5 kg |
| 3 | PE0087 Size -03 | TPR Black | Leather Black | Sole Rubber | 5030 1 kg Bostic Rc 20 g Double code | RC | 34.4 kg | 28.1 kg |
| 4 | PE0087 Size -02 | TPR Black | Leather Black | Sole Rubber | 5030 1 kg Bostic Rc 20 g | RC | 36.3 kg | 36.1 kg |
| Q/A Dip | PE0087 Size -02 | TPR Black | Leather Black | Sole – MEK 30 min Eth : Hal 100g : 3 g 30 min | Bostic Black 1 kg Boscodr –D Toluene 10 g | Hardner D | 24.6 kg | 31.6 kg |

* Sample – 04 -     Adhesive applied for Sole one cord & for upper double cord.

Bonding Specification – 10 Kg Minimum

Note:    Bonding result   ok

Ratnayaka – AQO

Date: 20th October 2011

Note: This is an electronically prepared document therefore signature is not necessary

BENDING / UV TEST REPORT

Page no – 67

DN NO - 34946

Expanded Indent No - SSL – 11 – 46 M

Compact Indent No - SSL – 11 – 46 M

| DESCRIPTION | SOLE MATERIAL | SPECIPICATION CYCLE | BENDING TEST RESULTS | UV TEST |
| --- | --- | --- | --- | --- |
| BENDING TEST PVC Sole black Size – 01 | pvc Gajeendra black Ex:80 Com : 20 | 150,000 | OK | - |
| BENDING TEST PVC Sole white size – 06 | pvcGajeendra white Ex:80 Com : 20 | 150,000 | OK | OK |

Note:    UV Specification: 3 hours in UV oven are similar to 6 months in normal atmosphere

* All Test Results is ok.

Rathnayaka– AQO

Date – 01/Sepetember/2011

Note: This is an electronically prepared document therefore signature is not necessary

BENDING / UV   TEST REPORT

Page no – 399

DN NO - 35054

| DESCRIPTION | SOLE MATERIAL | INDENT NO | SPECIPICATION CYCLE | BENDING TEST RESULTS | UV TEST |
| --- | --- | --- | --- | --- | --- |
| BENDING & UV TEST PVC Sole Size - 12 | SPC white Ex : 80 Com : 20 | (Indent no Expanded - SSL -11 – 39 M ) (Indent no compact SSL 11 - 40 M ) | 150,000 | 150,000 | ok |

Note:    UV Specification: 3 hours in UV oven are similar to 6 months in normal atmosphere

* All Test Results is ok.

Rathnayaka– AQO

Date – 22/August/2011

Note: This is an electronically prepared document therefore signature is not necessary

Bonding / Bending Test Report

Page No: -400

DN No: - 34784

Bonding   Left shoes

| ITEM | SOLE MATERIAL | UPPER MATERIAL | APPLIED PRIMER | APPLIED ADHESIVE | TEST RESULTS |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | L | R |
| PE0093 Size – 01 Left | PVC Compound SPC white EX : 75 Nation : White Com : 10 Rec : 30 | 2414 white DSI – 11 – 49 F Bang jyr Enterprices. | MEK : Cyclo 10 : 90 |  | 18.5 kg | - |

Bending Right shoes

| DESCRIPTION | SOLE MATERIAL | UPPER MATERIAL | APPLIED PRIMER | SPECIPICATION CYCLE | BENDING TEST RESULTS |
| --- | --- | --- | --- | --- | --- |
| PE0093 Size – 01 Right | PVC Compound SPC white EX : 75 Nation : White Com : 10 Rec : 30 | 2414 white DSI – 11 – 49 F Bang jyr Enterprices. | MEK : Cyclo 10 : 90 | 150,000 | 150,000 |

Bonding Specification - 10 Minimum

Note:     All Test Results is ok.

Ratnayaka – AQO

Date: 20/August/2011

Bonding Test Report

Page No: - 290, 291, 292, 293, 289

DN No: - 34758

| Sample No | Description | Sole | Upper | Primer | Adhesive | Hardener | Test Result Kg |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | Left | Right |
| 1 | PE0087 Size -02 | TPR Black | Leather Black | Sole – MEK 30 min Eth : Hal 100g : 3 g 30 min | Bostic Black 1 kg Rc 20 g | RC | 40.0 kg | 31.0 kg |
| 2 | PE0087 Size -03 | TPR Black | Leather Black | Sole – MEK 30 min Eth : Hal 100g : 3 g 30 min | Bostic Black 1 kg Rc 20 g Double code | 311FT 3448 ( 4 % ) | 25.6 kg | 29.5 kg |
| 3 | PE0087 Size -03 | TPR Black | Leather Black | Sole Rubber | 5030 1 kg Bostic Rc 20 g Double code | RC | 34.4 kg | 28.1 kg |
| 4 | PE0087 Size -02 | TPR Black | Leather Black | Sole Rubber | 5030 1 kg Bostic Rc 20 g | RC | 36.3 kg | 36.1 kg |
| Q/A Dip | PE0087 Size -02 | TPR Black | Leather Black | Sole – MEK 30 min Eth : Hal 100g : 3 g 30 min | Bostic Black 1 kg Boscodr –D Toluene 10 g | Hardner D | 24.6 kg | 31.6 kg |

* Sample – 04 -     Adhesive applied for Sole one cord & for upper double cord.

Bonding Specification – 10 Kg Minimum

Note:    Bonding result   ok

Ratnayaka – AQO

Date: 20th October 2011

Note: This is an electronically prepared document therefore signature is not necessary