Deterministic Reliability Engineering
Analysis of failure mechanisms/cause
Strongly discipline dependent
VS
Statistical Reliability Engineering
Collection and analysis of statistical failure date
Prediction of system reliability

---
Deterministic Reliability Engineering
(Physics of Failure)
Failure Mechanism
= process that leads to failure
Failure Mode
= Appearance of failure
Stressor
= condition that accelerates failure

---
Important Stressors
Temperature	(most physical/chemical processes)
Temperature steps	(induces thermo-mechanical stress)
Humidity	(corrosion)
Supply voltage	(dielectric breakdown)
Switching on/off	(voltage/current peaks, mechanical stress)
Ionizing radiation	(fatigue, charge generation in MOST)
Load/current intensity	(heat dissipation, wear etc.)

---
Failure Mechanisms in Electronic Components
Corrosion
Electro-Migration
Dielectric Breakdown
Hot Carrier Degradation
Purple plague
Package related failures:
delamination
cracks
“pop-corn”

---
Corrosion of aluminum IC-interconnect
Conditions: moisture + contamination + potential difference
Anodic Corrosion:
Al  Al3+ + 3 e-
2Al3+ + 3 H2O  Al2O3 + 6 H+
Cathodic Corrosion:
2 H2O + 2 e-  2 OH- + H2
2 H2O + 2 Al + 2 OH-  2 AlO-2 + 3 H2 (AlO-2 dissolves)
[Speaker Notes: The three ingredients necessary to establish a corrosive environment for the aluminum metallisation of semiconductor devices are: moisture and halide or alkalic contamination together forming an electrolyte and the presence of voltage bias between the aluminum electrodes. Although different corrosive reactions for aluminum are possible we will introduce only one basic reactions, an anodic reaction and a cathodic reaction. The anodic reaction formula is: Al ──────< Al3+ + 3 e- 2 Al3+ + 3 H2O ──────< Al2O3 + 6 H+ The Al2O3 forms a protective layer that prevents further corrosion at the anode electrode. The cathodic reaction proceeds as: 2 H2O + 2 e- ──────<	2 OH- + H2 2 H2O + 2 Al + 2 OH- ──────< 2 AlO2- + 3 H2 The second reaction makes the corrosion temperature dependent. AlO2- is water soluble and forms Al(OH)3 which has a larger volume than Al hence, leads to cracking of the passivation layer. Corrosion is a electro-chemical process and, therefore, is highly temperature dependent. Observed activation energies for corrosion processes in semiconductor devices range from 0.3 eV to 0.6 eV.]

---
Corrosion
[Speaker Notes: SEM close ups of the surface lift damage shown in . Upper left picture shows the heavily corroded bondpad, upper right the surface lift above the right bondpad, lower left shows close up of the damage exactly above that pad and lower right is a magnification of the single trace marked by the white arrow.]

---
Electro-Migration
= Material transport along conductors
Cause: high current density
domestic
supply
voids
chip
hillock
growth
Cu
Al
6 A/mm2
1 mA/m2
        =
1000 A/mm2
[Speaker Notes: Electro Migration: Electro migration = current induced material transport along conductors. Occurs at high current densities. For comparison: In domestic supply systems the maximum current density is limited to 16A/2.5 mm2 = 6 A/mm2 (otherwise conductors become to warm) while on a chip current densities of 1000 A/mm2 are quite common. These high current densities are possible because at shrinking dimensions the circumference/area ratio of the cross section (and so the cooling efficiency) is increased. The material transport almost quadratic depends on the current density. Therefore no electro migration is observed in domestic supply lines. Apart from that the domestic conductor materal (Cu) is much less sensitive to electro-migration than Al used in IC metallization. When high-density currents (10^5 - 10^6 A/cm^2) are led through metal conductors metal ions which have been thermally activated upto their saddle point (lifted out of their potential well and essentially free of the metal lattice) are acted on by two forces: The electric field that causes the current exerts a force on the positive ion in a direction opposite to the electron flow. However, the "cloud" of conducting electrons shield the metal ion from the electric field and, therefore, the electrical forces acting on the ions are quite small. The exchange of momentum which occurs when conducting electrons collide with the activated metal ions will exert a net force in the direction of electron flow. This "electron wind" is the predominating force on the metal ions.]