ME 354 Tensile Testing Laboratory

by

Tom Titus
Section AB, Wednesday, 2:30pm, October 28
Julio Davis

Date of Laboratory Report: November 12, 2009

Report submitted to: Jiangyu Li

TENSE!

Executive Summary:

The objectives of this laboratory exercise is to get several calculated results such as ultimate tensile strength, yield stress, modulus of elasticity, modulus of resilience, modulus of toughness, the stress-strain curve, true-stress-true-strain curve, and constitutive approximations of four different materials. By meeting these objectives we can characterize the performance and properties of these materials. The tensile test experiment is a basic mechanical test for material properties which is important for design.

The procedure is basically to put each different material specimen into the Instron tensile test machine, clip-on an extensometer, and record the stress-strain data through a computer data aquisition system. Measurements of the dimensions of the specimens, axial gage, and tranverse gage are to be taken as well before and after the tensile test. To perform the test, initiate the computer data aquisition system and run the Instron controller. Continue the test until at the maximum force, remove the extensometer to avoid damage to the extensometer. And then continue the test until the specimen fractures. This summarized procedure will give the raw data of the experiment.

The results of the experiment was the raw data recorded on an spreadsheet of the time, load, extension, strain, axial extensometer strain, and transverse extensometer strain. With these results, the objectives of the experiment can be met. The calculated results shown from the first paragraph give different characteristics of each material.

The final conclusions of the experiment were that the calculations from the results showed that steel was the toughest material with highest ultimate tensile strength and acrylic was the most resilient.Comparing aluminum and steel, steel had a similar yield stress on average and a much higher modulus of elasticity. Materials cannot be characterized by ultimate strength alone. Resilience negatively correlated with toughness. The true-stress and true-strain curve for aluminum excluded data after the point of the removal of the gage which is where a great discontinuity occurs. The percent error between the constitutive relation and the true-stress-true-strain curve were 345.4646%, 1.2128%, and 1.8255% at 0.1% strain, 1% strain, and 5% strain respectively.

OBJECTIVES

The goals of this laboratory exercise is to get several experimental results such as ultimate tensile strength, yield stress, modulus of elasticity, modulus of resilience, modulus of toughness, the stress-strain curve, true-stress-true-strain curve, and constitutive approximations of four different materials. By meeting these objectives we can characterize the performance and properties of these materials.

This laboratory experiment objectives are to gather information about the material properties and performance of 6061-T6 Aluminum, A-36 Steel, Acrylic, and Polycarbonate. By putting a specimen each that are cylindrically shaped into an Instron machine for the tensile test, we can get results that can be used to calculate the goals of the laboratory.

The hypothesis of the experiment is that the tensile tests will show large plastic deformations for the polymers, acrylic and polycarbonate, and less plastic deformation for the metal alloys, steel and aluminum. But the ultimate strength, or stress at point of fracture, for the metals are expected to be high stress values because the metals fracture more abruptly compared to the polymers. Since polymers tend to deform plastically, the fracture points will have smaller stresses. Comparing the steel and aluminum for yield stress and modulus of elasticity, due to prior knowledge, the steel should have a higher modulus of elasticity than aluminum. For yield stress, because the offset method suggests an arbitrary 0.2% offset, the magnitude of yield stress for each metal is hard to predict due to the nature of the deviation from elastic strain.

The hypothesis for modulus of toughness are expected to be high for polymers due to the amount of energy and deformation it can take. For resilience, it is expected that the metals to be better than the polymers because of the high elastic moduli yields a larger area under the curve for smaller strains.
For the true-stress-true-strain analysis on the aluminum, the hypothesis is that there should be a discontinuity in the curve because the the tranverse gage is taken out towards the point of maximum force. The discontinuity is because the true-stress is based on the current area of the specimen which depends on the transverse gage. Therefore readings taken after the gage is taken out are considered invalid. A final hypothesis on the power fit constitutive approximation of the true-stress-true-strain curve is that the approximation should give a small percent error for large strains and large percent error for small strains. Because the power fit is meant to be a good approximation for large plastic strains.

The mechanics of materials subject provides basic equations and concepts regarding the analysis for tensile tests on different materials. Such analysis deals with the concepts of stress and strain. Stress is defined as the force per unit area which is:

 (1)

Where σ is the stress, F is the force, and A is the cross-sectional area. This distribution of loading is of primary importance for understanding material behavior. The concept of strain shows the change of length over the original length to characterize how much the material has deformed due to the stress in the same direction. Strain is defined as:

(2)

Where L is the current length and L0 is the original length. Stress and strain are related together by Hooke's Law which is:

(3)
Where E is the elastic modulus and is the property of the material. The elastic modulus defines how well the material resists deformation. With this relationship, the given data can be used to calculate the stress for each recorded strain from the data.

Stress and strain of the material observed over time gives many more additional properties according to a stress-strain curve. In most most metals, take aluminum for example, the stress-strain curve has different points corresponding to the behavior of the material under stress. In Figure 1, the stress-strain curve for 6061-T6 Aluminum is given.

Figure 1: The stress-strain curve for 6061-T6 Aluminum.

As can be observed from the graph, there are two primary regions of deformation. The linear portion of the graph corresponds to elastic deformation and can be defined by Hooke's Law. In this region, stress is linearly proportional to strain. As the stress-strain curve nears the point where the curve is no longer linear, the proportional limit is reached and the material begins to plastically deform. The elastic deformation region has the property that if the stress is suddenly released, the material returns to the original length. So no permanent deformation is made if stress is under the proportional limit. As the curve passes the proportional limit, the material begins yielding or the curve deviates from linearity. If the material is unloaded past this limit, the material will not return to the original length. The material has permanently been deformed. The yield point or yield stress is different for every material so a simple method to define the yield stress is to use the offset method. The offset method shows the yield stress by taking a typical 0.2% strain and drawing a straight line with the same slope as the elastic modulus from the linear region. The intersection of the point is where the yield stress value is given. The final point on the curve is the ultimate tensile strength or the point of fracture. The area under this entire curve defines the amount of energy the material can absorb which is known as the modulus of toughness. The area under the curve up to the proportional limit is known as the modulus of resilience. The resilience is defines the the amount of energy the material can absorb up to the proportional limit and can recover the energy once unloaded at the proportional limit.

For aluminum alloy, several more properties can be observed. In Figure 1, the maximum load is where the highest amount of stress is applied to the speciemen. This is defined as the tensile strength which is the highest point on the graph. Another type of stress and strain is true stress and true strain. True stress and true strain gives a more accurate description of the stress on the material because it considers the force on the current area of the specimen. As the specimen elongates from tensile stress, the cross-sectional area of the specimen decreases. This is why the transverse extensometer gage is used to measure the decreasing diameter of the specimen. By taking the force divided by the current area, the true stress is given:

(4)

Where the tilde indicates true stress and Aj is the current area of the specimen. Similarly true strain is defined to be an infinitesimal length divided by the current length of the material. This can be manipulated to give the formula for true strain as:

(5)

The relationship between strain and true strain is taken to be:

(6)

This relationship is valid up to the tensile strength of the material. After that point, the material begins necking where the relationship holds for true strain:

(7)

Where for the circular specimens, d is the diameter and dj is the current diameter. An approximation for large true plastic strain can be approximated by the constitutive relation(relation between true stress and true strain in this particular case) by:

(8)

This is the power fit relationship and values for H and n can be found by doing a least squares fit on the true stress and true strain curve. How well the constitutive relation can approximate the true stress and true strain curve is by taking a percent error defined as:

(9)

where X is the actual measured true stress and Xapprox is the value given by the constitutive relation. All of the above equations are taken from Mechanical Behavior of Materials[1].

TEST DESCRIPTION

The following items are needed to fully replicate the experiment.

The materials tested were
- 6061-T6 Aluminum
- A-6 Steel
- Acrylic
- Polycarbonate

 The equipment used for the test includes:
- a clip-on extensometer
- a tensile test machine with grips, controller, and data acquisition system

The laboratory data did not give any information about the Intron machine. The same exact experiment can be replicated from the following information taken from the ME 354 sample formal laboratory[2]. The specimen and setup of the tensile test are shown in Figures 2 and 3 respectively.
"A servo-hydraulic, universal test machine (Instron Model 8511) with a digital controller and computer interface was used to conduct the tests as shown in Figure 3. Force capacity was 20 kN. The stroke range was ±50 mm. The clip-on extensometer had a range of ±40% with a 12.7 mm initial gage length. Manually-operated, wedge grips with V-grooved faces were used to grip the specimens. Digital data (force, stroke and strain displacement) were acquired at a rate of 5 points per second from 1 to 5 minutes of test time for different materials."[1].

Figure 2: Test specimen reduced gage section.
Figure 3: A schematic of the tensile test setup.

RESULTS
According the objectives that were met, the following results are presented The stress-strain plots of all four materials are presented in the following Figures 4 through 7. The raw data gave force values recorded for every tenth of the second. These force values and the original diameter of the specimens were all that were necessary to get the stress every tenth of a second for a corresponding strain in the data. With the strain from the data and the calculated stress, the points were plotted together to give the entire stress-strain curves for all four materials.
Figure 4: Stress-strain curve for 6061-T6 Aluminum
Figure 5: Stress-strain curve for A-36 Steel
Figure 6: Stress-strain curve for Acrylic.
Figure 7: Stress-strain curve for polycarbonate.

The results of the ultimate tensile strengths for all four materials of the experiment are given in Table 1. The ultimate tensile strength is taken to be the final point on the stress-strain curve which is the fracture point and no more stress can be taken from the material.

Table 1: Ultimate tensile strength and corresponding strains for all four materials.

Next, the three steel raw datasets and the three aluminum raw datasets are analyzed by plotting the stress-strain curves for each dataset. The plots were observed. And in the analysis of finding the modulus of elasticity for the steel, the dataset RawData_3 was found to be a bad dataset because the results differed greatly compared to the other two datasets for steel. This was found by looking at the first 200 or so points of the curves for each dataset, and the third dataset was found to yield earlier than the other two datasets. So in finding the yield stress and modulus of elasticity, RawData_3 was omitted from the calculations. See Appendix B for the three compared plots.

The results of the average and standard deviation of the yield stress are shown in Table 2 on the next page. The yield stress from the steel's stress-strain curve:

Average = 350.3689 MPa; Standard Deviation = 23.0044

The yield stress from the aluminum's stress-strain curve:

Average = 369.8039 MPa; Standard Deviation = 0.4796

The yield stress was found using the offset method as explained earlier in the objectives section. The analysis of finding the yield stress are given in Appendix A for all five curves.

Table 2: Average and standard deviation of yield stress for aluminum and steel.

The results of the average and standard deviation of the modulus of elasticity are shown in Table 3. The modulus of elasticity (E) is the slope of the stress-strain curve in the linear region. Since these materials exhibit elastic strain early in the tensile test, the first 200 points were taken and a linear least squares (LSQ) fit equation was applied to the points. The slope of the LSQ is then taken to be the modulus of elasticity. The plots of the first 200 points of all six curves including the omitted steel plot are given in Appendix B.

Table 3: Average and standard deviation of modulus of elasticity for aluminum ans steel.

To complete the analysis of all four materials, a single stress-strain plot for each material was chosen to find the moduli of resilience and the moduli of toughness. The modulus of resilience and modulus of toughness to reiterate are defined to be the amount of energy the material can absorb and in particular the modulus of resilience is the amount of energy the material can absorb up to the proportional limit.

In finding the modulus of resilience, a similar method was used to that of find the modulus of elasticity. Instead this time, the points were taken up to the proportional limit. This proportional limit again is the point where the stress-strain curve deviates from elastic strain. To find the proportional limit, it was an eyeball judgement as to when the slope suddenly starts to drop off due to yielding. So all the points leading up to the proportional limit were taken and another LSQ was made to the points yielding different but similar equations as for steel and aluminum in finding the modulus of elasticity. The LSQ was then integrated up to the strain of the proportional limit yielding the area under the curve which is the modulus of resilience. These results for all four materials are given in Table 4. The hand calculations of the integrations are given in Appendix B.

Table 4: The modulus of resilience, fit equation integrated, and proportional limit values.

Finding the modulus of toughness also used a similar approach to finding the modulus of resilience. This time, the entire curve is considered. Finding the area under the entire curve is difficult because the curve cannot be represented by an exact formula that one can integrate. So in OpenOffice.org Calc, the spreadsheet program used, cannot just give the area under such complex stress-strain curves. So again, an LSQ is applied to the entire curve for the aluminum, steel, and acrylic. The polycarbonate curve was broken up into two LSQ equations for different portions of the curve. The most suitable curve that yielded the highest R2 value(the coefficient of determination which defines how well an LSQ fits a curve) were LSQs that were logarithmic. Although these are not perfect appproximations, the R2 values are reasonable. These equations were taken and integrated to up to the final strain to get the modulus of toughness. The results for all four materials are given in Table 5 on the next page. The hand calculations for the integrations are given in Appendix B.

Table 5: Modulus of toughness, integrated fit equation(s), R2 value, strain, and integrated at strain.

The next analysis is made on aluminum for true-stress and true-strain. The true stress is defined by equation 4. The true strain is defined by equation 6. The true-stress-true-strain curve is shown in the same graph as the stress-stress curve in Figure 8. The true stress and true strain at the maximum load of 47881.905 N was found to be 398.9 MPa and 0.07 mm/mm respectively. This is significant because this is point where necking starts for the material and the formula for true strain changes to equation 7.

The final analysis is again made on aluminum for fitting the true-stress-true-strain curve. The constitutive relation given by equation 8 is a good LSQ for large true strains. The LSQ was made using the power fit in OpenOffice.org Calc for points after the yield stress point and before the point of discontinuity as discussed in the objectives section. The following values were obtained for H and n for the constitutive relation:

H = 432.6, n= 0.04.

 And to make the comparison of this fit to the actual true-stress-true-strain curve, the percent difference was taken at 0.1%, 1%, and 5% strain respectively. These results are given in Table 6.

Table 6: The percent error between the constitutive approximation and measured true stress at different strains.

DISCUSSION / CONCLUSIONS

The ultimate tensile strength for aluminum and steel as expected were very high in comparison to the polymers. But what was unexpected was the low corresponding strain for the acrylic at the fracture. So comparing acrylic and polycarbonate, even though the ultimate tensile strengths are similar, the amount of plastic strain that polycarbonate can undergo is far greater(due to the chemical structure of long chains of atoms connected). In this case, it seems the acrylic polymer is not the type that will undergo large plastic strain before rupturing like most polymers.

The yield stress of aluminum and steel were similar with an average around 300 to 400 MPa. But the modulus of elasticity was far greater for steel than aluminum. This means that far greater force is required to elongate the steel compared to aluminum. But at around the same stress they both yield even though aluminum yields at a longer strain than steel.

The modulus of resilience and modulus of toughness should be discussed together for a few reasons. It almost appears from the fit calculations that modulus of resilience negatively correlates with modulus of toughness. Acrylic with the highest amount of resilience at 7.835 has the lowest toughness. And steel that has the highest toughness at 164.812 MPa is one of the lower two of resilience. This can mean that materials that can undergo large plastic deformations that yields greater toughness are not resilient in that they deform and cannot retain the energy as well from linear deformation. Conversely, materials that can't undergo large plastic deformations have great resilience like acrylic because the curve is mostly linear that has a lot of area under it.

The close analysis of aluminum for the true-stress-true-strain curve revealed that there was a great discontinuity around where the maximum force was applied. This was because the tranverse gage was removed to prevent damage to it. Therefore, the results yielded invalid data on the spreadsheet just after the removal. So for the calculations, the true-stress-true-strain curve excluded the invalid points for the power least squares fit/consitutive relation.

The constitutive relation for true strains much larger than at the yield stress point is a very good one according to the low percent errors given in the results Table 6. And for small strains inputing a 0.1% strain into the constitutive relation results in a large percent error of over 300%!.

The final conclusions of this report according to the results are listed here:

1. The ultimate strength itself does not characterize a particular material regardless of what category the material falls under i.e. acrylic, a polymer, has a low ultimate tensile strength with low strain at fracture compared with polycarbonate – high strain at fracture.
2. A particular material can have a very high modulus of elasticity but may begin yielding earlier in terms of strain compared to another material. This can be a major consideration for design of perhaps the frame of a car. In that in an accident, can the frame undergoe deformation such that it does not yield early.
3. The modulus of resilience and modulus of toughness are negatively correlating properties. In design, choosing a resilient material versus a tough material can have its advantages and vice-versa.
4. The point of discontinuity on the true-stress-true-strain curve corresponds to the point where the tranverse gage was removed.
5. The power constitutive relation is an excellent approximation for materials with very large deformations but a terrible relation for very small deformations.