4075.15

TABLE  OF CONTENTS

PREFACE . . . . . . . . . . . . . . . . . . . . . . . . . .

LIST OF FIGURES . . . . . . . . . . . . . . . . . . . . . .

I.    INTRODUCTION  . . . . . . . . . . . . . . . . . . . .    1

II.   ENVIRONMENT AND MOISTURE CONDITIONS . . . . . . . . .    1

A.  General . . . . . . . . . . . . . . . . . . . . .    2

B.  Environment and Shrinkage . . . . . . . . . . . .    2

C.  Environment and Swelling  . . . . . . . . . . . .    2

D.  Climate Studies . . . . . . . . . . . . . . . . .    3

III.   USING THE FHA SOIL PVC METER . . . . . . . . . . . .    5

A.  General . . . . . . . . . . . . . . . . . . . . .    5

B.  Equipment . . . . . . . . . . . . . . . . . . . .    6

C.  Preparation of Sample . . . . . . . . . . . . . .    6

D.  Preparation for Compaction  . . . . . . . . . . .    7

E.  Compaction  . . . . . . . . . . . . . . . . . . .    7

F.  Alternate Method of Compaction  . . . . . . . . .    9

G.  Swelling  . . . . . . . . . . . . . . . . . . . .    9

H.  Reading . . . . . . . . . . . . . . . . . . . . .   10

IV.   FHA SOIL PVC METER SWELL INDEX TEST RESULTS FROM

SELECTED LOCATIONS IN THE UNITED STATES . . . . . . .   17

V.    GLOSSARY  . . . . . . . . . . . . . . . . . . . . . .   30

6/74

_____________________________________________________________________

4075.15

LIST OF FIGURES

FIGURE 1   UNITED STATES WEATHER BUREAU SOIL-CLIMATE RATING MAP .   4

FIGURE 2   PICTURES OF EQUIPMENT  . . . . . . . . . . . . . . . .  12

FIGURE 3   PROVING RING CALIBRATION . . . . . . . . . . . . . . .  13

FIGURE 4   SWELL INDEX VS. POTENTIAL VOLUME CHANGE. . . . . . . .  14

FIGURE 5   SWELL INDEX VS. PLASTICITY INDEX . . . . . . . . . . .  15

FIGURE 6   TABLE FOR CONVERTING PROVING RING READINGS TO

PVC CATEGORY AND APPROXIMATE PLASTICITY INDEX. . . . .  16

6/74

_____________________________________________________________________

4075.15

FOREWORD

In 1960, the FHA Soil PVC Meter was developed under the Federal Housing

Administration Technical Studies Program.  It was developed to provide

a quick and practical method of testing soils for shrink-swell potential.

It also presents a condensed explanation of the relationship between

environment and moisture conditions and their effects on expansive soils.

This guide also contains the significant, hitherto unpublished results

of over 100 FHA Soil PVC Meter tests which were made from samples taken

in selected locations in 15 states.  Although these locations were

primarily in areas of known highly expansive soils, the test results

reflect general characteristics of expansive soils throughout the

United States.

6/74

HUD-Wash., D. C.