CONSTRUCTION SPECIFICATION

NE-83.  TIMBER FABRICATION AND INSTALLATION

1.	SCOPE

This specification covers the quality and installation of plywood and pressure treated structural timber poles, posts, and lumber structures and also timber and lumber portions of composite structures.

2.	MATERIAL

A.	Plywood shall be new and of exterior grade.  Plywood for use underground shall be pressure treated.

B.	Structural timber and lumber shall be structural grade or better.  Structural timber poles and posts shall be sound, uncracked, decay free, and straight.  All lumber shall be treated by any of the following preservatives:

Commercial Coal Tar Creosote

Hot and Cold Bath Creosote

Pentachlorophenol - Commercial Treatment

Pentachlorophenal - Cold Soaking Method

AWPB-FDN Standard Preserving Salts

C.	Bolts, rods, nuts, washers, and other hardware shall be an appropriate grade of steel and shall be galvanized.

3.	INSTALLATION

All framing shall be true and exact.  Timber and lumber shall be accurately cut and assembled to a close fit and shall have even bearing over the entire contact surface.  Holes for machine bolts shall be bored to the same diameter as that of the bolt.

Raw ends of lumber which have been cut after treatment shall be immersed in the preservative solution, or painted with four (4) heavy coats of the treatment solution.  Each application should be allowed to dry before installation.