$$701.00A

Section 701.—CEMENT

Revised 25 January 2005

INCLUDE THE FOLLOWING FOR PROJECTS IN HIGH SULFIDE AREAS

$$701.01A

701.01(a).  Add the following:

Furnish portland cement with a maximum sulphate expansion of 0.040 percent when tested in accordance with ASTM C 452.

INCLUDE THE FOLLOWING FOR SHOTCRETE.  FOR COLORED SHOTCRETE, INCLUDE 711.05

$$701.01B

701.01.  Add the following:

For shotcrete, use low alkali portland cement.  Conform to AASHTO M 85, limiting alkalis according to Table 1A in AASHTO M 85.