DOT/FAA/AR-95/81		Corrosion of Aluminum Alloys in the Presence of 					Fire-Retardant Aircraft Interior   							          Materials

FAA Technical Center

Atlantic City Airport,

NJ  08405

October, 1995

Final Report

This document is available to the public through the 					            National Technical Information Service, Springfield, 					            Virginia 22161

NOTICE

This document is disseminated under the sponsorship of the U.S. Department of Transportation in the interest of information exchange.  The United States Government assumes no liability for the contents or use thereof.

U.S. Department of Transportation

Federal Aviation Administration

1. Report No.

DOT/FAA/CT-94/110

2. Government Accession No.

3. Recipient’s Catalog No.

4. Title and Subtitle

Corrosion of Aluminum Alloys in the Presence of Fire-Retardant Aircraft Interior Materials

5. Report Date

1995

6. Performing Organization Code

7. Author(s)

Dr. J. E. Talia and Dr. J. Chaudhuri

8. Performing Organization Report No.

9. Performing Organization Name and Address

National Institute for Aviation Research/

Mechanical Engineering Department

Wichita State University

Wichita, KS 67260-0035

10. Work Unit No. (TRAIS)

Task C-4

11. Contract or Grant No.

DTFA-03091-C-00044

12. Sponsoring Agency Name and Address

U. S. Department of Transportation

Federal Aviation Administration

Technical Center

Atlantic City International Airport, NJ 08405

13. Type of Report and Period Covered

Final Report

14. Sponsoring Agency Code

AAR-430

15. Supplementary Notes

FAA COTR: Dr. Thomas Flournoy

16. Abstract

This research project was to evaluate the potential for fire-retardant materials used in aircraft interiors to cause corrosion of aluminum structural alloys.  Service Difficulty Reports (SDR’s) were reviewed for several aircraft types, and the most frequent locations for corrosion were identified as fuselage, windows, and frames.

Laboratory experiments were designed and conducted for corrosion testing of common aircraft structural alloys (Al 2024-T3 and Al 7075-T6) in the presence of Ultrasuede, Glenlivit, and Highland Wool, common interior materials. Accelerated corrosion test results showed that, for most test conditions, corrosion was increased for all three fire-retardant materials compared to baseline tests without fire retardants. Chemical composition from EDAX studies of the fire-retardants revealed substantial halogens in Ultrasuede and Glenlivit, but negligible halogens in Highland Wool. Thus, the corrosion results cannot be attributed solely to halogens. Sulfur, which is present in substantial amounts in both Glenlivit and Highland Wool, could be another cause for corrosion observed with these materials.

17. Key Words

Fire Retardant

Corrosion

18. Distribution Statement

This document is available to the public through the National Technical Information Service,

Springfield, VA 22161

19. Security Classif . (of this report)

Unclassified

20. Security Classif. (of this page)

Unclassified

21. No. Of Pages

22. Price

Form DOT F 1700.7 (   )		Reproduction of completed page authorized

TABLE OF CONTENTS

Page

EXECUTIVE SUMMARY	vii

1.	INTRODUCTION	1

2.	CORROSION CASES FROM AIRCRAFT SERVICE

DIFFICULTY REPORTS	1

3.	SUMMARY OF SERVICE DIFFICULTY REPORTS	5

4.	LABORATORY CORROSION EXPERIMENTS	8

5.	EVALUATION OF CORROSION	9

6.	CORROSION RESULTS	12

7.	CHEMICAL COMPOSITION OF THE FIRE-RETARDANT MATERIALS	30

8.	CONCLUDING REMARKS	34

9.	REFERENCES	35

LIST OF FIGURES

Figure											Page

1.	Corrosion Cases from Service Difficulty Reports	6

2.	Corrosion Incidents by Location	7

3.	Assembly of Sandwich Test Specimen	9

4. 	Micrograph of Al 7075-T6 With Ultrasuede, 100oF, 90% RH, 21 Days	10

(Severe Corrosion, 100 Points)

5. 	Micrograph of Al 2024-T3 With Glenlivit, 100oF, 90% RH, 14 Days.	11

(Moderate Corrosion, 50 Points)

6. 	Micrograph of Al 7075-T6 With Highland Wool, 70oF, 50% RH, 7 Days	11

(Minimal Corrosion, 5 Points)

7.	Al 2024-T3 With Ultrasuede, 100oF, 90% RH, 21 Days (50 Points)	12

8. 	Al 2024-T3 With Ultrasuede, 130oF, 90% RH, 14 Days (80 Points)	13

9.	Al 7075-T6 With Ultrasuede, 70oF, 50% RH, 21 Days (40 points)	13

10. 	Al 7075-T6 Alclad With Ultrasuede, 130oF, 90% RH, 21 Days (40 Points)	14

11. 	Al 2024-T3 With Glenlivit, 100oF, 90% RH, 21 Days (65 Points)	14

12.	Al 2024-T3 Alclad With Glenlivit, 130oF, 50% RH, 14 Days (80 Points)	15

13.	Al 7075-T6 Alclad With Glenlivit, 130oF, 50% RH, 21 Days (55 Points)	15

14.	Al 2024-T3 With Glenlivit, 130oF, 90% RH, 21 Days (85 Points)	16

15. 	Al 2024-T3 With Highland Wool, 70oF, 90% RH, 7 Days (40 Points)	16

16. 	Al 7075-T6 With Highland Wool, 130oF, 50% RH, 7 Days (45 Points)	17

17.	Al 2024-T3 Alclad With Ultrasuede, 130oF, 90% RH, 14 Days (Cross Section)	17

18.	Al 7075-T6 With Ultrasuede, 70oF, 90% RH, 14 Days (Cross Section)	18

19. 	Al 7075-T6 With Glenlivit, 70oF, 50% RH, 14 Days (Cross Section)	18

20.	Al 7075-T6 With Glenlivit, 70oF, 50% RH, 21 Days (Cross Section)	19

LIST OF FIGURES (CONTINUED)

Number	Page

21.	Al 2024-T3 Alclad With Highland Wool, 130oF, 90% RH, 21 Days (Cross Section)	19

22. 	Al 7075-T6 With Highland Wool, 70oF, 90% RH, 14 Days (Cross Section)	20

23.	Average Corrosion Rating of Fire Retardants

with Al 2024-T3 (at 70oF/90% RH)	25

24.	Average Corrosion Rating of Fire Retardants

with Al 2024-T3 (at 100oF/50% RH)	25

25.	Average Corrosion Rating of Fire Retardants

with Al 2024-T3 (at 130oF/50% RH)	26

26.	Average Corrosion Rating of Fire Retardants

with Al 2024-T3 (at 130oF/90% RH)	26

27.	Average Corrosion Rating of Fire Retardants

with Al 2024-T3 Alclad (at 130oF/50% RH)	27

28.	Average Corrosion Rating of Fire Retardants

with Al 2024-T3 Alclad (at 130oF/90% RH)	27

29.	Average Corrosion Rating of Fire Retardants

with Al 7075-T6 (at 70oF/50% RH)	28

30.	Average Corrosion Rating of Fire Retardants

with Al 7075-T6 (at 130oF/50% RH)	28

31.	Average Corrosion Rating of Fire Retardants

with Al 7075-T6 (at 130oF/90% RH)	29

32.	Average Corrosion Rating of Fire Retardants

with Al 7075-T6 Alclad (at 130oF/50% RH)	29

33.	Average Corrosion Rating of Fire Retardants

with Al 7075-T6 Alclad (at 130oF/90%RH).	30

34. 	EDAX Analysis of Fire-Retardant Ultrasuede	31

35. 	EDAX Analysis of Fire-Retardant Glenlivit	32

36. 	EDAX Analysis of Fire-Retardant Highland Wool	33

LIST OF TABLES

Table											Page

1.	Reference Specimens	10

2.	Aluminum Control Specimens without Fire Retardant	21

3.	Average Corrosion Rating for Aluminum Specimens with Ultrasuede	22

4.	Average Corrosion Rating for Aluminum Speimens with Glenlivit	23

5.	Average Corrosion Rating for Aluminum Specimens with Highland Wool 	24

6.	Elements Associated with Fire Retardants Present in Ultrasuede, Glenlivit,

and Highland Wool.	34

EXECUTIVE SUMMARY

This research project was to evaluate the potential for fire-retardant materials used in aircraft interiors to cause corrosion of  aluminum structural alloys. This work was initiated based on evidence of some corrosion problems in general aviation, small business jets, and commuter aircraft in areas near fire-retardant interior fabrics.  Service Difficulty Reports (SDR) data were studied to measure the magnitude of the problem. Corrosion incidences were reviewed for several aircraft types, and the most frequent locations for corrosion were identified as fuselage, windows, and frames.

Laboratory experiments were designed and conducted for corrosion testing of common aircraft structural alloys (Al 2024-T3 and Al 7075-T6) in the presence of aircraft interior materials.  Tests were conducted for Ultrasuede, Glenlivit, and Highland Wool, common interior materials. Accelerated corrosion test conditions included ambient and high temperatures and high-humidity conditions. Control specimens of the aluminum alloys were tested as a baseline without exposure to the fire retardants.  Results show that, for most test conditions, corrosion was increased for all three fire-retardant materials compared to the baseline tests without fire retardants. Chemical composition from EDAX studies of the fire-retardants revealed substantial halogens  in Ultrasuede and Glenlivit, but negligible halogens in Highland Wool. Thus the corrosion results cannot be attributed solely to halogens. Sulfur, which is present in substantial amounts in both Glenlivit and Highland Wool, could be another cause for corrosion observed with these materials.

1.  INTRODUCTION.

The purpose of this research was to investigate the potentially corrosive behavior of upholstery, floor, and wall covering material, currently used in the interiors of general aviation and commuter aircraft. Halogen salts have commonly been used to provide such materials a level of fire retardancy. Federal Aviation Regulations (FAR) 23.853 and 25.853 established the requirement for fire retardancy of seat cushions, and Advisory Circular AC 25.853-1 also addresses their flammability requirements. However, service difficulty reports indicate that the fire-retardant products which are currently being used might be responsible for severe corrosion in aircraft interiors [1,2,3].

General corrosion and corrosion due to fire retardants in particular are a strong function of environment. Alert No. 161, 1991[4], states:

"Reports continue to be received concerning rapidly induced corrosion possible from various flame-retardant fabrics used in aircraft interiors. The latest reports involve a Jetstream 3101 and the Gulfstream Commander 900, both of which had Ultrasuede 357 installed in the cabin interior. Extensive corrosion was found on panels and stringers where the material had been attached. Reports have been received on a wide range of aircraft, including amateur-built, with corrosion caused by the salts (usually bromide or chloride salts) which are used to increase the flame retardancy of materials.

Fabrics which have been treated with any of the above salts can be extremely corrosive when exposed to moisture of any nature. Corrosion occurs very rapidly and is difficult to detect without removing the material. In general, the more synthetic material in a fabric, the more salts required to provide the desired flame retardancy. Metal surfaces contacting this type of interior fabric must be properly treated in order to avoid corrosion. Zinc chromate primer will not provide the required corrosion protection. The use of acid etching and wash primer treatment will provide protection."

This Alert and the cited Service Difficulty Reports implicating fire-retardant materials in accelerated metal corrosion suggested that a research program should be conducted to quantify this corrosion problem. The program should include review of SDR's and laboratory experiments to quantify corrosion of typical aircraft metals in the presence of fire-retardant materials currently in use.

2.  CORROSION CASES FROM AIRCRAFT SERVICE DIFFICULTY REPORTS.

Data were obtained from several pertinent sources including  General Aviation Airworthiness, "Alerts," aircraft maintenance logs (Cessna), and the FAA Service Difficulty Report data base for FAR part 23 aircraft [4,5]. An extensive search of the Service Difficulty Report data base was done to identify corrosion attributed to a fire-retardant treatment.

Aircraft that have had corrosion due to the use of fire-retardants and have been cited in the data base are classified below. A brief summary of the description of the corrosion as listed in the narrative is also given.

PIPER

Aircraft model PA28161, serial number 287916185;

A report of corrosion under rear seat. The possible cause was leakage at rear seat window causing wetness of the fire-retardant insulation around fitting.

Aircraft model PA23250, serial number 234405291;

A report of corroded longeron tube. Suspected cause was a water leak at the left window where water soaked the side wall insulation. Fire-retardant insulation resting on the tubing triggered corrosion.

Aircraft model PA23250, serial number 277654176;

A report of corrosion on 17134-44 tube and frame 3039206 at station 153.87 below door. Suspected cause was that the flame retardant insulation had gotten wet and held water against the tubing. Corrosion on the tube was found below the battery box.

Aircraft model PA23250, serial number 277554032;

A report of corrosion on 17134-44 tube at station 153.87 on right and left tubes. Suspected cause was that the corrosion was caused by flame-retardant.

Aircraft model PA23250, serial number 277754158;

A report of corrosion at station 153.87 on right side at cabin step. Holes were put in tubes with scribe. This was probably caused by a window leaking water and trapped by fiber glass insulation against the tube.

Aircraft model PA28140, serial number 2825805;

A report of corrosion under left rear seat in the steel plate and rivet heads; corrosion was found to have extended through half the thickness of the plate. The possible cause was the fire-retardant insulation under the seat holding water.

Aircraft model PA28151, serial number 287415687;

A report of steel fittings corrosion. The possible cause was the wet fire-retardant insulation which was in contact with these steel parts.

Aircraft model PA28161, serial number 288116316;

A report of corrosion on the surface of the fitting P/N 62448-03 behind the fiberglass insulation in the lower cockpit. The possible cause of this corrosion was the moisture retained by the fiberglass insulation in contact with the fittings.

Aircraft model PA28161, serial number 287816067;

Corrosion reported on right rear spar and left rear spar in the fittings 6244803 and 6244802 respectively. Moisture leaking in from a side window caused the fiberglass insulation to become saturated. This insulation contacts the fitting, the worst corrosion was noted under the insulation, but very little corrosion was noted on the exposed portion of the fitting outside the aircraft.

Aircraft model PA28181, serial number 288090326;

A report of corrosion in the fittings 6244802 and 6244803 located at lower fuselage. The fittings were located inside the flap torque tubewell, behind flap pillow blocks, and the submitter suggested that the fire-retardant insulation held water and caused the corrosion.

Aircraft model PA28181, serial number 287890373;

A report of corrosion on plates 6244803 and 6244802 under rear seat. Possible cause was the fire-retardant insulation packed under the rear seat became soaked with water and caused these steel plates to corrode.

Aircraft model PA32300, serial number 327940243;

A report of corrosion on the fitting assembly 6538861 in the right wing attachment. Corrosion had built up on steel rear spar attaching plate and cabin caused by the fiber glass insulation holding water. There were no drain holes forward of this bulkhead.

Aircraft model PA60600, serial number 600016;

Corrosion was reported on longerons 210028510, 210028525, and 210028506 on the extruded H sections. This seemed to have been caused by water leaking through windows and being held by the longerons and fire-retardant insulation materials.

Aircraft model PA23160, serial number 231626;

Corrosion reported in frame 1716206 on the lower fuselage. It appeared that moisture was collecting at the point of contact of insulation on the tube causing the corrosion.

Aircraft model PA23250, serial number 273335;

A report of corrosion on frame 3039205 in the fuselage. The corrosion appeared to be caused by fire-retardant insulation between the fuselage frame and the aircraft skin.

Aircraft model PA34200, serial number 3474T0131;

Corrosion reported on bracket 6252200 on the windshield. During inspection it was found that the sponge type fire-retardant insulation in this area trapped water from a leaking windshield seal.

BEECH

Aircraft model 35A33, serial number CD277;

Corrosion reported on the stringers in the cabin right corner, and pitting was formed on the inside surface of skin and stringers. This was probably caused by a leaking door seal which allowed moisture to enter and then became retained in the fire-retardant insulation.

Aircraft model B60, serial number P336;

Corrosion found extensively on structural fuselage in the cabin. This seemed to have been caused by moisture trapped in the fire-retardant insulation around structural members.

Aircraft model 58, serial number TH513;

Report of corrosion on the floor supports 0024400291, 0024400294, 0024400293, and 0024400292 from FS151-FS171. The corrosion reported was intergranular corrosion. Cause of this corrosion was speculated to be from the floor fire-retardant insulation holding water due to a leaking frame door seal.

MOONEY

Aircraft model M20J, serial number 240210;

Corrosion reported on tubes 340155021 and 340155061 in the frame. The cause for corrosion was water retained by the fire-retardant insulation.

Aircraft model M20J, serial number 241098;

Corrosion reported on tubing 340155 at the window area. It was revealed that the fire-retardant insulation was soaked with moisture from leaking windows caused the corrosion.

Aircraft model M20J, serial number 240839;

Corrosion reported on tubing 340117 at the window area. Corrosion was caused by soaked fire-retardant insulation, caused by leaks around left cockpit windows.

Aircraft model M20J, serial number 240414;

A report of corrosion on the fuselage tube below pilot's window. Corrosion was caused by window leakage soaking the fire-retardant insulation.

Aircraft model M20J, serial number 240712;

Corrosion was reported on the structure in the fuselage. The problem seemed to be caused by water entering the fuselage around the side sections and was retained by the fire-retardant insulation.

Aircraft model M20J, serial number 240318;

Corrosion of tube 340155021 on left fuselage. It was revealed that the fire-retardant insulation soaked with moisture from leaking windows caused the corrosion.

Aircraft model M20J, serial number 240656;

Tubing part number 340155 was corroded through tubing wall and severely pitted. Other tubing was also pitted as far back as left side of the baggage bulk head. It was caused by deteriorated cabin window sealant.

Aircraft model M20J, serial number 240921;

Corrosion in the fuselage tubes was reported along with electrical problems from the wires

and the connectors in this area. The fire-retardant insulation was soaked with moisture and was the probable cause of corrosion.

Aircraft model M20J, serial number 240746;

Corrosion in the fuselage tubing. Water appeared to have entered side panel areas through poor bonding of the sealer along the bottom of the windows. This soaked the insulation and rusted the tubing.

Aircraft model M20K, serial number 250020;

Corrosion in tubings 350155009, 340177141, 350155061, 350155021, and through the upper fuselage. It was found that corrosion was due to water soaked fire-retardant insulation from a leak at angle P/N 320009-083+320013.

Aircraft model M20K, serial number 250047;

Corrosion in tube 340155067 in left hand side of the fuselage. Leaking cabin side windows caused the corrosion of the tube structure.

CESSNA

Aircraft model 337A, serial number 3370297;

There was a report of corrosion in the cabin roof interior from FS 135.45 to 165.09 and LBL 13.75 to RBL 13.75. The possible cause was that three of the stiffeners were lying on the loose fire-retardant insulation thus causing galvanic corrosion.

AEROSPATIAL

Aircraft model ATR42300, serial number 37;

The frame in station 17319 was corroded. The fire-retardant insulation blanket was found saturated with moisture and galley fluids which caused the corrosion.

ROCKWELL

Aircraft model NA26560, serial number 306131;

The main fuselage frame was found to have been corroded at fuselage station 206. The frames are of 7178-T6 extrusion and the corrosion appeared to be caused by moisture entering the fire-retardant insulation around window area during manufacture.

3.  SUMMARY OF SERVICE DIFFICULTY REPORTS.

Figure 1 presents a histographic representation of various corrosion cases from SDR's with respect to the aircraft manufacturers. Figure 2 presents the locations at which corrosion was reported in SDR's.  This graph illustrates that the most frequently observed corrosion was in the fuselage, with especially high occurrences near windows and frames.

The following inferences and recommendations are made based on study of the Service Difficulty Report data base.

Reports stated that most of the corrosion was due to the presence of moisture in the fire-retardant insulation. In many of these cases the presence of moisture was due to window leaks, saturation by galley fluids, deterioration of cabin window sealant, and leaking door seals. Following are a series of suggested practices based on review of the SDR's:

Windows should be leak proof and there should be no deterioration of window sealants.

Insulation should be contained in a plastic bag so that it does not rest directly against the aircraft skin or structure.

Interior of the aircraft should be coated with primer.

Regular visual inspections should be conducted of the insulation in areas that can retain water.

Insulation should be removed and dried if moisture gets in. It should not come in contact with metallic parts [7,8].

The Service Difficulty Report Data Base clearly raised the question concerning the role of fire-retardant treated materials in accelerated metal corrosion. The lack of pertinent data regarding fire-retardant corrosion suggested the need of controlled laboratory experiments to quantify the problem. To evaluate the corrosiveness of various fire retardants, the following experimental program was designed.

4.  LABORATORY CORROSION EXPERIMENTS.

After thorough consideration and research of the existing interiors of small planes, two aircraft structural aluminum alloys, Al 2024-T3 and Al 7075-T6 (bare and clad), were selected to represent the most common materials for floor panels, seats, side wall, and floor tracks [6]. After consultation with local small aircraft manufacturers such as Cessna and Beechcraft, and fire- retardant product manufacturers, three fire-retardant aircraft interior materials were selected for experiments: 1) Ultrasuede, 2) Glenlivit and 3) Highland Wool.  In a generic sense, most fire retardants in current use are halide based (bromides, chlorides or fluorides). Ultrasuede and Glenlivit fire-retardants were provided by the Tapis Corporation, and Highland Wool was provided by Cessna Aircraft Company.

The several experimental approaches available [9,10,20] were thoroughly investigated and the search for appropriate testing procedure was narrowed down to the sandwich test. This test method was also recommended by the Tapis Corporation and United States Testing Company, Inc. for evaluating the corrosiveness of fire-retardant materials on aluminum alloys. Alloys, specimen size and fire-retardant aircraft interior materials used during experiments were:

Alloy:					Al 2024-T3 & Al 7075-T6 bare and clad

Specimen size:			2 x 2 inch x 0.040 inch thick

(51 x 51 mm x 1.02 mm thick)

Fire-retardant aircraft materials:	Ultrasuede, Glenlivit, Highland Wool

Surfaces of the specimens were cleaned using isopropyl alcohol before the tests.  Corrosion test articles consisted of  the fire-retardant material "sandwiched" between two aluminum specimens, with a masking tape wrap to maintain uniform contact between the aluminum and the fire-retardant material.(See Figure 3.)  The sandwich was then placed in the environmental chamber where the desired humidity and temperature were accurately maintained with digital humidistat and thermostat.

Over 288 tests were performed at room temperature (70oF) and at elevated temperatures (100oF and 130oF), with humidity varying from 50% to 90% for the purpose of accelerating the corrosion process.  Time periods used were: 7, 14, and 21 days. These tests included Control specimens for each aluminum alloy which were tested without fire-retardant material applied to determine basic corrosion of the aluminum alloy as a function of temperature and humidity.

FIGURE 3. ASSEMBLY OF SANDWICH TEST SPECIMEN

After the exposure period, the test and control specimens were removed from the chamber and the fire-retardant material was carefully separated from the aluminum test article. Specimen surfaces were cleaned with warm tap water and wiped with a clean, soft cloth. Specimen panels were photographed with an ordinary camera to record the appearance of the corrosion to the un-aided eye. Later each specimen was examined using an optical microscope and micrographs were prepared.  Corrosion characteristics such as uniformity of corrosion and severity of pitting were recorded.

5.  EVALUATION OF CORROSION

In order to grade corrosion, three corroded specimens to be used as references were selected from all the test specimens. The specimens selected were judged to be examples of severe, moderate and minimal corrosion.  An arbitrary corrosion level value of 100 was assigned to the specimen judged to have severe corrosion, a value of 50 was assigned to the specimen judged to have moderate corrosion, and a value of 5 was assigned to the specimen judged to have minimal corrosion.  Table 1 details the specimens selected as references based on an analysis of the specimen micrographs.   Rating for all other specimens was done by comparing the appearance of each specimen with these three reference specimens and interpolating the number to be assigned. Micrographs of the three reference specimens are shown in Figures 4, 5, and 6.

TABLE 1. REFERENCE SPECIMENS

Sample

Material

Temperature

(Deg. F)

Humidity

(%)

Duration

(Days)

Rating

FR7075-T6

(Ultrasuede)

100

90

21

100

FR2024-T3

(Glenlivit)

100

90

14

50

FR7075-T6

(Highland Wool)

70

50

7

5

Detailed results of these evaluations for 288 specimen sets are given in Tables 2 through 5 in the following section.  Each specimen rating listed in the tables indicates the average value for three identical material specimens tested at the same conditions.

6.  CORROSION RESULTS.

Typical optical micrographs for specimens in each category are presented in figures 7 through 16.  Cross sections were cut from the samples and optical micrography was performed where the depth of pitting was the greatest. Figures 17 to 22 present selected cross-sectional micrographs.

The corrosion rating was averaged for each set of three specimens and for the three time durations (average of a total of nine specimens). GB-STAT and STORM [11] software systems were utilized for entry, storage, editing, manipulation, graphics, and statistical analysis of numeric data as they were gathered during corrosion experiments.

Corrosion ratings for each condition with different aluminum alloys, cabin interior materials and various combinations of temperature and humidity for the 288 specimen test sets are shown in Tables 2, 3, 4 and 5, and illustrated graphically in Figures 23 through 33.  The rating for each test condition shown is an average for three distinct specimens at that condition.  An average for the three different time periods (7, 14, and 21 days) at each temperature and humidity condition is also shown in these tables.  In most test conditions, the data show that the intensity of corrosion was increased in the presence of a fire-retardant product.  Figures 23 through 33 present data selected from Tables 2, 3, 4, and 5 to illustrate the relative corrosive behavior of the three fire retardants at different test conditions of temperature and humidity.  The corrosion values presented in these tables are the average of the 7, 14, and 21 day tests for each material at the temperature and humidity conditions noted.

TABLE 2.      ALUMINUM CONTROL SPECIMENS WITHOUT FIRE RETARDANT

Sample

Material

Temperature

(Deg F)

Humidity

(%)

Rating*

Average

Rating

7 Days

14 Days

21 Days

AL2024-T3

70

50

10

12

20

14

+AL2024-T3

70

90

14

15

22

17

+AL2024-T3

100

50

10

15

14

13

AL2024-T3

100

90

8

12

20

13.3

+AL2024-T3

130

50

10

12

15

12.3

+AL2024-T3

130

90

10

20

25

18.3

AL2024A-T3

70

50

6

5

7

6

AL2024A-T3

70

90

8

12

14

11.3

AL2024A-T3

100

50

6

10

10

8.7

AL2024A-T3

100

90

8

14

14

12

+AL2024A-T3

130

50

2

6

7

5

+AL2024A-T3

130

90

5

10

6

7

+AL7075-T6

70

50

2

5

5

4

AL7075-T6

70

90

10

17

25

17.3

AL7075-T6

100

50

15

22

30

22.3

AL7075-T6

100

90

10

18

15

14.3

+AL7075-T6

130

50

15

18

12

15

+AL7075-T6

130

90

12

13

20

15

AL7075A-T6

70

50

3

8

10

7

AL7075A-T6

70

90

8

12

15

11.7

AL7075A-T6

100

50

8

15

9

10.7

AL7075A-T6

100

90

9

15

14

12.67

+AL7075A-T6

130

50

10

18

17

15

+AL7075A-T6

130

90

2

5

5

4

* Rating is the average of 3 specimens.

+ Average rating for these conditions for all fire-retardant materials are graphically displayed in figures 23 through 33.

NOTE:	AL2024-T3 designates Al 2024-T3, AL2024A-T3 designates Al 2024-T3 Alclad, AL7075 designates Al 7075-T6, all tested in the absence of fire-retardant material.

TABLE 3.	AVERAGE CORROSION RATING FOR ALUMINUM SPECIMENS WITH ULTRASUEDE

Sample

Material

Temperature

(Deg F)

Humidity

(%)

Rating*

Average Rating

7 Days

14 Days

21 Days

FR2024-T3

70

50

8

10

16

11.3

+FR2024-T3

70

90

75

85

85

81.7

+FR2024-T3

100

50

40

40

55

45

FR2024-T3

100

90

65

70

50

61.7

+FR2024-T3

130

50

30

80

40

50

+FR2024-T3

130

90

50

80

60

63.3

FR2024A-T3

70

50

5

10

10

8.3

FR2024A-T3

70

90

10

8

15

11

FR2024A-T3

100

50

10

20

55

28.3

FR2024A-T3

100

90

25

60

65

50

+FR2024A-T3

130

50

75

60

85

73.3

+FR2024A-T3

130

90

60

50

95

68.3

+FR7075-T6

70

50

10

10

40

20

FR7075-T6

70

90

80

65

80

75

FR7075-T6

100

50

10

30

65

35

FR7075-T6

100

90

70

70

75

71.7

+FR7075-T6

130

50

30

45

60

45

+FR7075-T6

130

90

5

5

15

8.3

FR7075A-T6

70

50

5

8

20

11

FR7075A-T6

70

90

50

50

60

53.3

FR7075A-T6

100

50

10

10

30

16.7

FR7075A-T6

100

90

10

18

40

22.7

+FR7075A-T6

130

50

15

40

70

41.7

+FR7075A-T6

130

90

40

15

40

31.7

*Rating is the average of 3 specimens.

+ Average rating for these conditions for all fire-retardant materials are graphically displayed in figures 23 through 33.

NOTE:	FR2024-T3 designates Al 2024-T3, FR2024A-T3 designates Al 2024-T3 Alclad, FR7075-T6 designates Al 7075-T6, and FR7075A-T6 designates Al 7075-T6 Alclad, all with Ultrasuede.

TABLE 4.	AVERAGE CORROSION RATING FOR ALUMINUM SPECIMENS WITH GLENLIVIT

Sample

Material

Temperature

(Deg F)

Humidity

(%)

Rating*

Average

Rating

7 Days

14 Days

21 Days

FR2024-T3

70

50

12

15

20

15.7

+FR2024-T3

70

90

50

70

80

66.7

+FR2024-T3

100

50

30

45

75

50

FR2024-T3

100

90

65

75

80

73.3

+FR2024-T3

130

50

20

60

75

51.6

+FR2024-T3

130

90

20

18

85

41

FR2024A-T3

70

50

8

12

18

12.7

FR2024A-T3

70

90

20

32

40

30.7

FR2024A-T3

100

50

15

20

60

31.7

FR2024A-T3

100

90

15

50

60

41.7

+FR2024A-T3

130

50

35

80

85

66.7

+FR2024A-T3

130

90

25

85

75

61.7

+FR7075-T6

70

50

40

70

50

53.3

FR7075-T6

70

90

25

85

80

63.3

FR7075-T6

100

50

20

30

85

45

FR7075-T6

100

90

65

70

85

73.3

+FR7075-T6

130

50

25

47

70

47.3

+FR7075-T6

130

90

50

20

30

33.3

FR7075A-T6

70

50

10

8

25

14.3

FR7075A-T6

70

90

40

45

80

55

FR7075A-T6

100

50

7

15

35

19

FR7075A-T6

100

90

20

25

35

26.7

+FR7075A-T6

130

50

20

40

55

38.3

+FR7075A-T6

130

90

20

40

60

40

*Rating is the average of 3 specimens.

+ Average rating for these conditions for all fire-retardant materials are graphically displayed in figures 23 through 33.

NOTE:	FR2024-T3 designates Al 2024-T3, FR2024A-T3 designates Al 2024-T3 Alclad, FR7075-T6 designates Al 7075-T6, and FR7075A-T6 designates Al 7075-T6 Alclad, all with Glenlivit.

TABLE 5.	AVERAGE CORROSION RATING FOR ALUMINUM SPECIMENS WITH HIGHLAND WOOL

Sample

Material

Temperature

(Deg F)

Humidity

(%)

Rating*

Average Rating

7 Days

14 Days

21 Days

FR2024-T3

70

50

8

40

15

21

+FR2024-T3

70

90

40

75

50

55

+FR2024-T3

100

50

25

50

45

40

FR2024-T3

100

90

30

70

35

45

+FR2024-T3

130

50

35

60

60

51.7

+FR2024-T3

130

90

35

35

80

50

FR2024A-T3

70

50

10

18

20

16

FR2024A-T3

70

90

12

22

18

17.3

FR2024A-T3

100

50

28

20

40

29.3

FR2024A-T3

100

90

20

35

50

35

+FR2024A-T3

130

50

55

40

45

46.7

+FR2024A-T3

130

90

35

65

45

48.3

+FR7075-T6

70

50

15

20

30

21.7

FR7075-T6

70

90

50

90

65

68.3

FR7075-T6

100

50

25

35

65

41.7

FR7075-T6

100

90

30

65

75

56.7

+FR7075-T6

130

50

25

35

75

45

+FR7075-T6

130

90

45

80

50

58.3

FR7075A-T6

70

50

5

8

10

7.7

FR7075A-T6

70

90

8

15

12

11.7

FR7075A-T6

100

50

45

55

35

45

FR7075A-T6

100

90

10

20

18

16

+FR7075A-T6

130

50

50

20

45

38.3

+FR7075A-T6

130

90

15

60

65

46.7

*Rating is the average of 3 specimens.

+ Average rating for these conditions for all fire-retardant materials are graphically displayed in figures 23 through 33.

NOTE:	FR2024-T3 designates Al 2024-T3, FR2024A-T3 designates Al 2024-T3 Alclad, FR7075-T6 designates Al 7075-T6, and FR7075A-T6 designates Al 7075-T6 Alclad, all with Highland Wool.

7.  CHEMICAL COMPOSITION OF THE FIRE-RETARDANT MATERIALS.

Ultrasuede, Glenlivit and Highland Wool are fire-retardant materials commonly used in aircraft seats and wall coverings. In order to identify the specific corrosion-causing element, the chemical composition of the fire-retardant must be known. Due to its proprietary nature, this information is not generally released by the manufacturers. This information was obtained by EDAX (Electron Dispersion Analysis of X-rays) microanalysis. X-ray microanalysis graphs for the three aircraft interior fire-retardant materials are given in Figures 34 to 36. The tests were performed to exclude the majority content of hydrocarbons and other materials usually present in interior fabrics and amplified the ability to detect small levels of elements.   Table 6 summarizes the results of an EDAX analysis for elements usually associated with the fire retardants.  The result given is the mass percent of the given element of the total mass of the elements selected for measurement.  Halogen peaks in the EDAX analysis of Ultrasuede show approximately 32% bromine and 23%  chlorine.  In Glenlivit, negligible bromine and approximately 21% chlorine was found.  A negligible amount of bromine and only 0.2% chlorine was found in Highland Wool.  There was a significant amount of sulfur present in Glenlivit (49.3%) and Highland Wool (46.7%), but none was observed in the Ultrasuede material.  The absence of significant halogen content for Highland Wool and significant sulfur content for Ultrasuede discounts the ideas that either halogens or sulfur are unique causes of increased corrosion.

TABLE 6.  ELEMENTS ASSOCIATED WITH FIRE RETARDANTS PRESENT IN

ULTRASUEDE, GLENLIVIT, AND HIGHLAND WOOL.

Mass Percentage of Total Measurement

Element

Ultrasuede

Glenlivit

Highland Wool

Bromine

32.1

-

-

Fluorine

-

3.6

-

Chlorine

23.0

21.6

0.2

Zirconium

-

22.5

-

Sulfur

-

49.3

46.7

Silicon

10.9

3.0

-

Phosphorus

-

-

40.9

Argon

-

-

8.5

Calcium

18.3

-

3.7

Potassium

15.7

-

-

Totals

100.0

100.0

100.0

8.  CONCLUDING REMARKS.

This research project evaluated the potential for fire-retardant materials used in aircraft interiors to cause corrosion of  aluminum structural alloys. This work was initiated based on evidence of some corrosion problems in general aviation, small business jets and commuter aircraft, in areas near fire-retardant interior materials.

Service Difficulty Reports (SDR) data were studied to identify the frequency of fire-retardant related corrosion. The most frequent locations for corrosion were identified as fuselage and windows and frames.

Laboratory experiments were designed and conducted for corrosion testing of common aircraft structural alloys (Al 2024-T3 and Al 7075-T6) in the presence of aircraft interior materials.  Tests were conducted for Ultrasuede, Glenlivit and Highland Wool, common interior materials.

Results of accelerated corrosion tests show that corrosion was increased for all three fire-retardant materials under most test conditions compared to baseline tests without fire retardants.

Chemical composition from EDAX studies of the fire-retardants reveal substantial halogens  in Ultrasuede and Glenlivit, but negligible halogens in Highland Wool. Thus the corrosion results cannot be attributed solely to halogens.

Sulfur, which is present in substantial amounts in both Glenlivit and Highland Wool, could be another cause for corrosion observed with these materials.

9.  REFERENCES.

1.	Federal Aviation Administration, "Flammability Requirements for Aircraft Seat Cushions, 25.853-1", 1986.

2.	AGARD, "Aircraft Fire Safety", AGARD lectures series No. 123.

3.	G. A. Gehring,  Jr. and C. W. George, "Guidelines for  Preventing Fire Retardant 	Corrosion", U.S. Government Printing Office, 1986.

4.	General Aviation, Airworthiness (FAA), "ALERTS",  Alert No. 161, 1991.

5.	"Service Difficulty Report Data", Prepared by the operational systems branch/AFS-620, 	Oklahoma City, FAA, 1980 to date.

6.	V. M. Bhatnagar, "Advances in Fire Retardant Textiles", Technomic Publishing Co. Inc., 	1975.

7.	L. K. Chew, "Corrosion Experience On Inservice Airplanes", Singapore Airlines, 1991.

8.	M. Atkinson, "Corrosion and its Control", National Association of Corrosion Engineers, 	1982.

9.	S. V. Crume, "A Corrosiveness Test for Fibrous Insulations", ASTM STP 866, p 215, 	1985.

10.	ASTM Standards, G1-81, ASTM STP, 866, p 505.

11.	Emmons, "STORM", H. Holden-Day, Inc, 1993.

12.	ASM International, "Metals HandBook", 13, 1987.

13.	Hanes and Baboin, "Laboratory Corrosion Tests and Standards", ASTM Special Technical Publication 866, 1985.

14.	M. G. Fontana, "Corrosion Engineering", Mc. Graw-Hill Inc., 1986.

15.	J. W. Lysons, "The Chemistry and Use of Fire Retardants", Wiley and Sons Inc., 1970.

16.	AGARD, "Fire Worthiness of Transport Aircraft Interior System", AGARD CP 166.

17.	H. Buchert, E. Koch, et al., "Aircraft Interiors, Flammability Impact Maintenance and 	Refurbishing Technology", Third Conference for NIAR, Wichita State University, 1991.

18.	F. D. Bogar and R. T. Foley, "The Influence of Chloride Ion on the Pitting of Aluminum", J. Electrochem. Soc., 119, 462, 1972.

19.	ASTM, "Standard Method of Salt Spray (Fog) Testing", B117 Annual Book of ASTM 	Standards, 1985.

20.	Sandwich Test Report, United States Testing Company Inc., No. 052281, 1992.

21.	R. S. Treseder, "NACE Corrosion Engineer's Reference Book", National Association of 	Corrosion Engineers, 1980.