November 21, 1997

Contract # TW-0928

SPECIAL SPECIFICATION

SECTION 09720-S

WALL COVERINGS

Page

PART 1- GENERAL

1.01	Description of Work	2

1.02	References	2

1.03	Submittals	2

1.04	Quality Assurance	3

1.05	Test Requirements	3

1.06	Delivery, Storage and Handling	4

1.07	Sequence and Scheduling	4

1.08	Warranty	4

PART 2-  PRODUCTS

2.01	Manufacturers	5

2.02	Materials	5

2.03	Accessories	5

PART 3- EXECUTION

3.01	Examination	6

3.02	Preparation	6

3.03	Installation	6

3.04	Cleaning	7

3.05	Protection	7

SPECIAL SPECIFICATION

SECTION 09720-S

WALL COVERINGS

# PART 1 - GENERAL

## 1.01	DESCRIPTION OF WORK

                - Furnish and install broadloom carpet, vinyl base adhesives and all accessories as shown on Contract documents, required to perform all work indicated.

                - Related Sections:  Refer to the following sections for related work:

1.	Division 9, Section “Painting Materials” for painted wall surfaces.

## 1.02	REFERENCES

A.	American Association of Textile Chemists and Colorists (AATCC)

16A	Colorfastness to Light

B.	American Society of Testing and Materials (ASTM)

D-4157	Abrasion Resistance:  Double Rub Face to Face

D-3597	Abrasion Resistance:  Double Rub Face to Face

E-84	Surface Burning Characteristics of Building Materials (Steiner Tunnel Test)

C.	Uniform Building Code (U.B.C)

42.2	Standard Test Method for Evaluating Room Fire Growth Contribution of 			Textile Wall Covering

## 1.03	SUBMITTALS

A.	General:  Submit the following in accordance with provisions of Section 1300-S, “Descriptive Submittals.”

B.	Product Data:  Submit manufacturer’s product literature and installation instructions for each type of wall covering and installation accessory required.

C.	Samples

1.	Submit manufacturer’s standard size samples showing full range of colors, textures and patterns available for each type of wall covering required.

2.	Submit samples of each type of accessory item showing full range of standard colors.

D.	Shop Drawings:   None required.

E.	Maintenance Manual:  Submit manual or wall covering manufacturer’s recommendations for the care, cleaning and maintenance of wall covering.

F.	Certification

1.	Submit manufacturer’s certificate stating all materials are asbestos-free and lead paint-free.

2.	Submit certificate stating that the manufacturer and installer comply with Quality Assurance requirements.  Include a minimum of five (5) references, complete with addresses, telephone numbers and contact persons for installations within the time period indicated.

3.	Submit manufacturer’s certificate stating that materials furnished comply with specified requirements.  Include supporting independent certified laboratory testing data indicating that material meets specified test requirements.

4.	Submit Material Safety Data Sheet (MSDS) for adhesives, leveling compounds and primers required.

5.	Submit sample warranty showing compliance with requirements.

## 1.04	QUALITY ASSURANCE

A.	Manufacturer Qualifications:  Firm (material producer) with not less than five (5) years of production experience, whose published literature clearly indicates general compliance of products with requirements of this section.

B.	Installer Qualifications:  Firm with not less than five (5) years of experience in installation of commercial carpet of type, quantity and installation methods similar to work of this section.

C.	For each colorway, per floor, furnish wall covering from one dye lot only.

## 1.05	TEST REQUIREMENTS

A.	Flame and Smoke Resistant Standards:  Provide wall covering complying with rating as indicated for the following:

1.	Surface Burning Characteristice of Building Materials:  Class A  (ASTM E84).

2.	Standard Text Method for Evaluating Room Fire Growth Contribution of Textile Wall Covering (Corner Burn):  Meets acceptance criteria  (UBC 42.2).

B.	Lightfastness:  No change  after 100 hours  (AATCC 16A).

C.	Abrasion Resistance:  15,000 Double Rubs  (ASTM D-3597, ASTM D-4157).

## 1.06	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials to site in original factory wrappings and containers, clearly labeled with identification of manufacturer, brand name, quality or grade, fire hazard classification, and lot number.

B.	Store materials in original undamaged packages and containers, inside well-ventilated area protected from weather, moisture, soiling, extreme temperatures, humidity; laid flat, blocked off ground to prevent sagging and warping.  Maintain temperature in storage area above 40 degrees F (4 degrees C).

C.	Comply with instructions and recommendations of manufacturer for special delivery, storage, and handling requirements.

## 1.07	SEQUENCE AND SCHEDULING

Coordinate work of this section with other work to ensure that installed wall covering materials are not damaged or soiled.

## 1.08	WARRANTY

A.	Submit a written warranty signed by the manufacturer, installer, and the general contractor, guaranteeing to correct failures in wall covering which occur within two (2) years after completion, without reducing or otherwise limiting any other rights to correction which Sandia National Laboratories (SNL) may have under the contract documents.  Failures are defined to include faulty workmanship or faulty materials.  Corrections shall include repair or replacement.

# PART 2 - PRODUCTS

## 2.01	MANUFACTURERS

A.	Manufacturers:  Products made by the following manufacturers, provided they comply with requirements of Contract documents, are those considered acceptable.  However, it is the contractor’s responsibility to provide only products compatible with adjacent materials in the assembly.

Koroseal Wallcoverings

B.	Substitutions: only under provisions of Section 1600-S.

## 2.02	MATERIALS

Compatibility:  Provide wall covering, adhesives, and other related materials that are compatible with one another and with substrates under conditions of service and application.

A.	Weight:  7.4 Oz. per square yard.

B.	Construction:  100% Polyolefin

C.	Backing:  Acrylic.

D.	Width:  Untrimmed (Trim to 54”)

E.	Thickness:  0.022 Inches

F.	Pattern:  Gossamer Steel “Napa”

G.	Color:  6712-12

## 2.03	ACCESSORIES

A.	Primer:  Provide pigmented antibacterial primer to provide uniform hanging surface.

B.	Miscellaneous Materials:  As recommended by manufacturers of wall covering and other wall covering products for intended application.

C.	Adhesive for Wall Covering:  Provide first quality, pre-mixed, non-staining clear vinyl type as recommended by wall covering manufacturer which complies with flame spread rating required for the wall covering installation.

# PART 3- EXECUTION

## 3.01	EXAMINATION

A.	Examine substrates for moisture content and other conditions under which wall covering is to be installed. Notify SDR in writing of major conditions detrimental to proper completion of the work.  Do not proceed until unsatisfactory conditions have been corrected.

B.	Field verify all dimensions and other work conditions affecting the installation of wall covering.

## 3.02	PREPARATION

A.	General

1.	Repair minor holes, cracks, depressions or rough areas using wall patching/leveling compound.  Sand repair smooth.

2.	Provide a clean, dry, smooth, structurally sound, and uniformly colored  wall surface.

3.	Prime with manufacturer’s recommended primer.

4.	Sequence wall covering installation with other work to minimize possibility of damage and soiling of wall covering during remainder of construction period.

5.	Maintain room temperature at minimum 60 degrees F (15 degrees C) for at least 24 hours prior to installation and relative humidity at approximately that at which the area is to be maintained.

## 3.03	INSTALLATION

A.	General:  Perform installation in accordance with manufacturer’s instructions, except where more strigent requirements are shown or specified, and except where project conditions require extra precautions or provisions to ensure satisfactory performance of the work.

1.	Visually match  panels for color gradation and shading prior to hanging.

2.	Wrap covering 6”  (15.24 cm) beyond outside corners and at inside corners.

3.	Provide cut-outs where required.

4.	Follow manufacturer’s instructions for cutting wall covering, using tools designed to cut type of wall covering materials being installed.  Inspect material prior to cutting for defects.  Use new, clean, sharp blades and change blades after each cut.

5.	Before applying adhesive to substrate, pre-fit wall covering in area where it is to be installed.  Where cutting is necessary, provide properly prepared, straight, and unfrayed edges.

6.	Apply a full spread of adhesive in an even layer to substrate and allow to become tacky before applying wall covering. Follow MSDS instructions for ventilation requirements.

7.	Install prefitted wall covering from top to bottom between two plumb lines and trim as necessary.  Overlap and double-cut wallcovering, with sufficient  overlap to ensure cut is made through acrylic backing and not the selvedge.  Do not damage substrate when double cutting.  Press panel gently from top to bottom to remove bubbles or wrinkles.   Butt edges snugly at seams and against vertical obstructions.

8.	Immediately remove any excess adhesive from surface of wall covering by method which will not damage wall covering.

## 3.04	CLEANING

A.	Remove and dispose of debris and unusable scraps.  Return excess rolls and usable scraps to SNL.

B.	Vacuum wall covering using commercial quality vacuum cleaner attachment.  Remove spots and trim loose yarns where required.  Blot wet spills with a clean absorbent cloth.  Brush dry spots with a soft bristled brush.  Should any trace of stain remain, a mild household cleaner should be used.

## 3.05	PROTECTION

A.	Protect installation with a nonstaining building paper. Do not use a moisture barrier such as plastic film.

END OF SECTION