# Alternative Beam Tubes

- Material Search

  - Non-Conductive

  - Magnetically Transparent

  - Good Vacuum Properties

  - Radiation Hardness (1 Mrad)

  - Good Manufacturability

- Polyetheretherketone

  - Victrex PEEK™ 450CA30

- Borosilicate Glass

  - Pyrex® (Corning)

# Pyrex® Properties

  - Vacuum properties well known…bell jars etc.

  - Radiation resistance – DOE chose Borosilicate for High Level Nuclear Waste Vitrification (Hanford)

  - ASTM C 158 Modulus of Rupture test ongoing

  - Ability to form long tubes by fusing sections together

# PEEK™ Properties

  - Radiation Resistance:

Gamma Radiation Resistance of Victrex® PEEK™ 450G

Dose Rate 2 MeV, 1/5mQ, tested on film samples

| Dose Rate | Modulus | Yield Stress | Elongation |
| --- | --- | --- | --- |
| (Mrad) | (kg/cm2) | (kg/cm2) | (%) |
| 0 | 6000 | 688 ±32 | 500 ±19 |
| 1000 | 6000 | 635 ±8 | 432 ±22 |
| 2000 | 6000 | 614 ±16 | 261 ±12 |

  - Carbon fiber-filled resin (30%)

    - Improved stiffness

    - Eliminates Aerodag coating

# PEEK™ Vacuum Properties

  - Measured specific out gassing rate (Torr-L/s-cm2) ~ 3e-9  NON-BAKED

  - Assuming a 10 foot long tube with 100 L/s ion pumps on each end, the pressure at the pumps would be:

    - 1.1e-7 Torr for a 3" ID

    - 1.4e-7 Torr for a 4" ID

(Data generated by Terry Anderson 9/12/01)

  - All tests performed on cast material.  Additional testing required on extruded tube.

Pyrex® Vacuum Forming Process

- Rotating Vertical Mandrel

  - 303-304 SS, Graphite

  - High surface finish imparted to tube

  - No taper required

- Mechanized Torch

- Pull vacuum in outer tube

- Fuse Pyrex® rods into rough shape

- Join 2 tubes using alignment mandrel

Pyrex® Vacuum Forming Process

- Grinding to Final Size

  - Horizontal surface grinder

  - Form grind outside corners

  - Straightness ±.010” full length all 4 sides

- Full Polish Tube Exterior

  - Silicon carbide

  - Inspect for bubbles and cracks

  - Polariscope for stress

  - Any flaw and tube is rejected

Optimized Tube Dimensions

- Improved Aperture

  - Kickers & Lambertsons

  - 40 ( mm.mrad/95% full width (1.10”horiz. X .59”vert.)

  - PEEK™ vs. Pyrex®

- Stress Analysis (ANSYS)

  - Modeled uniform external surface pressure (atmospheric)

  - Peak stresses

  - Maximum deflection

Secondary Operations - Pyrex®

- Graded Seal

  - Oxidize kovar flange

  - Housekeeper seal to oxide layer

  - Intermediate sealing glass to Pyrex®

  - Tesla coil test for seal integrity

- Polymer Coating

  - Scratch protection during handling and installation

  - Implosion containment

Secondary Operations - PEEK™

- Mechanical Seal

  - Mill circumferential groove

  - Clamp to groove

  - U-shaped spring seal on tube end

  - Belleville washers

- Coating to reduce permeability

Summary

|  | Ceramic | Pyrex® | PEEK™ |
| --- | --- | --- | --- |
| Mechanical - Dimensional | Fair | Very Good | Good |
| Mechanical – Strength (under vacuum) | Good | Uncertain | Good |
| Mechanical - Durability | Requires Caution | Requires Caution | Good |
| Vacuum Properties | Very Good | Good | Fair |
| Radiation Resistance | Very Good | Uncertain | Good |
| Chemical Resistance | Good | Good | Good |
| Experience in this application | Yes | No | No |