96E01/03/08

S703-96E.doc

Use on all projects with aggregate for concrete, subbase, base, asphalt mix, and asphalt surface treatments is specified.

Section 703. – AGGREGATE

Include Subsection 703.02 for all concrete.

703.02  Coarse Aggregate for Concrete.  Delete the Subsection and substitute the following:

703.02  Coarse Aggregate for Concrete.  Conform to AASHTO M 80 class A including the restriction on reactive materials, except as amended or supplemented by the following:

(a) Los Angeles abrasion, AASHTO T 96	40% max.

(b) Adherent coating, ASTM D 5711	1.0% max.

(c) Grading, AASHTO M 43	All sizes, except  Nos. 8, 89, 9 or 10

For bridge decks or surface courses, do not use aggregate known to polish or carbonate aggregates containing less than 25 percent by mass of insoluble residue as determined by ASTM D 3042.

For lightweight coarse aggregate, conform to AASHTO M 195.

Add the following:

In addition to the requirements under 703.01 and 703.02 the following will also apply to fine and coarse aggregate for concrete.

Fine and Coarse Aggregate for Concrete.

Alkali reactivity of aggregates (Mortar bar method), ASTM C 1260		0.10% max.

Aggregates tested by ASTM C 1260, which exhibit mortar bar expansions less than 0.10 % at 16 days after casting, are considered innocuous and may be used.

Aggregates tested by ASTM C 1260 which exhibit mortar bar expansions between 0.10 and 0.20 % at 16 days after casting may be used if acceptable supplemental information is submitted which confirms that mortar bar expansions are not caused by alkali-silica reactions.  Acceptable supplemental information includes:

• A report of petrographic examination of the aggregate by ASTM C 295 performed within one year from the time of submittal which contains quantifiable data and conclusions verifying that the aggregate is not potentially deleteriously reactive with cement

or

• A report of petrographic examination of the ASTM C 1260 mortar bar samples by ASTM C 856 which contains quantifiable data and conclusions verifying that the aggregate is not potentially deleteriously reactive with cement and that the mortar bar reaction products are not due to alkali-silica reaction.

Aggregates tested by ASTM C 1260 which exhibit mortar bar expansions more than 0.20 % at 16 days after casting or aggregates exhibiting expansions between 0.10 and 0.20 % at 16 days after casting that have been found to be potentially deleteriously reactive by acceptable supplemental information may be used if additional supplemental information is submitted which confirms that effective mitigation measures utilizing supplementary cementitious materials have been used in the concrete mix design.  Acceptable supplemental information includes:

• Data and test results by ASTM C 1567 which confirm that concrete mix design combinations of cement, fly ash, silica fume and/or ground iron blast furnace slag exhibit expansions less than 0.10 % at 16 days after casting.  Lithium compounds shall not be used.

Testing of the reactivity of aggregates by ASTM C 1293 may be substituted for ASTM C 1260.  In such a case, the average concrete prism expansion must be less than 0.04 % at one year.  Aggregates exhibiting mortar bar expansions more than 0.04 % at one year may be used if additional supplemental information is submitted which confirms that effective mitigation measures utilizing supplementary cementitious materials have been used in the concrete mix design.  Acceptable supplemental information includes:

• Data and test results by ASTM C 1567 which confirm that concrete mix design combinations of cement, fly ash, silica fume and/or ground iron blast furnace slag exhibit expansions less than 0.10 % at 16 days after casting.  Lithium compounds shall not be used.

Include Subsection 703.05 when specifying subbase or base aggregate using Section 301. Include Section 301 and the following:

703.05  Subbase, Base and Surface Course Aggregate.

(a) General.  Delete lines (3), (4), (5), and (6) and substitute the following:

(3) Fractured faces, one or more, ASTM D 5821	50% min.

(4) Free from organic matter and lumps or balls of clay

(b) Subbase or base aggregate.

(1) Gradation.  Delete Table 703-2 and substitute the following:

Table 703-2

Target Value Range for Subbase and Base Gradation

| Sieve Size | Percent by Mass Passing Designated Sieve (AASHTO T27 and T 11) |
| --- | --- |
|  | Grading Designation |
|  | A (Subbase) | B (Subbase) | C (Base) | D (Base) | E (Base) |
| 2½ inch | 100 (1) |  |  |  |  |
| 2 inch | 97-100 (1) | 100 (1) | 100 (1) |  |  |
| 1½ inch |  | 97-100 (1) |  |  |  |
| 1¼ inch |  |  |  |  |  |
| 1 inch | 65-79 (6) |  | 80-100 (6) | 100 (1) |  |
| ¾ inch |  |  | 64-94 (6) | 86-100 (6) | 100 (1) |
| ½ inch | 45-59 (7) |  |  |  |  |
| ⅜ inch |  |  | 40-69 (6) | 51-82 (6) | 62-90 (6) |
| No. 4 | 28-42 (6) | 40-60 (8) | 31-54 (6) | 36-64 (6) | 36-74 (6) |
| No. 40 | 9-17 (4) |  |  | 12-26 (4) | 12-26 (4) |
| No. 200 | 4.0-8.0 (3) | 4.0-12.0 (4) | 4.0-7.0 (3) | 4.0-7.0 (3) | 4.0-7.0 (3) |

(1) Statistical procedures do not apply.

( ) Allowable deviations (+/-) from the target values

Include Subsection 703.02(c) when specifying surface course aggregate using Section 301. Include Section 301 and the following:

(c) Surface course aggregate. Delete the text including Table 703-3 and substitute the following:

Furnish hard, durable particles or fragments of crushed stone, crushed slag, or crushed gravel conforming to the following:

(1) Los Angeles abrasion, AASHTO T 96	50% max.

(2) Fractured faces, one of more, ASTM D 5821	50% min.

(3) Free from organic matter and lumps or balls of clay

(4) Liquid Limit, AASHTO T 89	35 max.

(5) Dust ratio:	2/3 max.

(6) Gradation and plasticity index, AASHTO T 90	Table 703-3

Do not use material that breaks up when alternately frozen and thawed or wetted and dried.

Obtain the aggregate gradation by crushing, screening, and blending processes as necessary.  Fine aggregate, material passing the No. 4 sieve, will consist of natural or crushed sand and fine mineral particles.

Do not furnish material that contains asbestos fibers.

Table 703-3

Target Value Ranges for

Surface Course Gradation and Plasticity Index

| Sieve Size | Percent by Mass Passing Designated Sieve (AASHTO T 27 and T 11) |
| --- | --- |
| ¾ inch | 100 (1) |
| No. 4 | 41-71(7) |
| No. 40 | *(5) |
| No. 200 | 9-16 (4) |
| Plasticity Index (PI) | 8 (4) |

(1) Statistical procedures do not apply.

(*) Submit target values for applicable sieves

( ) Allowable deviations (+/-) from the target values

Include Subsection 703.06 when specifying surface course aggregate using Section 308. Include Section 308 and the following:

703.06  Crushed Aggregate.  Add the following to the end of the paragraph:

When aggregate is used as a surface course, furnish an aggregate with a Plasticity Index conforming to Table 703-3a.

Table 703-3a

Surface Course Gradation and Plasticity Index

| Sieve Size | Percent by Mass Passing Designated Sieve (AASHTO T 27 and T 11) |
| --- | --- |
| ¾ inch | 100 |
| No. 4 | 41-71 |
| No. 40 | * |
| No. 200 | 5-20 |
| Plasticity Index (PI) | 4-12 |

(*) Submit target values for applicable sieves

Include Subsection 703.07 when Hot Asphalt Concrete Pavement is specified using Sections 401 (NOT Superpave). Include Section 401 for Hveem or Marshall mix and the following:

703.07  Hot Asphalt Concrete Pavement Aggregate.

(a) Coarse aggregate (retained on a No. 4 sieve).  Delete lines (3) and (4) and substitute the following:

(3) Fractured faces, one or more, ASTM D 5821	75% min.

(4) Liquid limit, AASHTO T 89	25 max.

(5) Adherent coating, FLH T 512	1% max.

(b) Fine aggregate (passing a No. 4 sieve).  Delete lines (1) and (2) and substitute the following:

(1) Liquid Limit, AASHTO T 89	25 max.

Include Subsection 703.08 when an open-graded friction course is specified using Section 404.

703.08  Open-Graded Asphalt Friction Course Aggregate.  Delete lines (a), (b), and (c) and substitute the following:

(a) Fractured faces, two or more, ASTM D 5821	75% min.

(b) Fractured faces, one or more, ASTM D 5821	90% min.

Include Subsection 703.09 when emulsified asphalt pavement is specified.

703.09  Emulsified Asphalt Pavement Aggregate.

(a) Coarse aggregate.  Delete lines (3) and (4) and substitute the following:

(3) Fractured faces, one or more, ASTM D 5821	75% min.

(b) Fine aggregate.  Delete lines (1) and (2) and substitute the following:

(1) Liquid Limit, AASHTO T 89	25 max.

Include Subsection 703.10 when aggregates for asphalt surface treatments are specified.

703.10 Asphalt Surface Treatment Aggregate.  Delete lines (d) through (l) and substitute the following:

(d) Fractured faces, one or more, ASTM D 5821	90% min.

(e) Flat and elongated particles, 1:3 ratio. +⅜ inch sieve,	10% max.

calculated by mass, weighted average, ASTM D4791

(f) Clay lumps and friable particles, AASHTO T 112	1.0% max.

(g) Adherent coating, ASTM D 5711	0.5% max.

Table 703-7.  Delete Table 703-7 and substitute the following:

Table 703-7

Target Value Ranges for

Single and Multiple Course Surface Treatment Aggregate Gradation

| Sieve Size | Percent by Mass Passing Designated Sieve (AASHTO T 27 & T 11) |
| --- | --- |
|  | Grading Designation |
|  | A | B | C | D | E | F |
| 1½ inch | 100 (1) |  |  |  |  |  |
| 1 inch | 90 – 100 (3) | 100 (1) |  |  |  |  |
| ¾ inch | 0 – 35 (5) | 90 – 100 (3) | 100 (1) |  |  |  |
| ½ inch | 0 – 8 (3) | 0 – 35 (5) | 90 – 100 (3) | 100 (1) |  |  |
| ⅜ inch | --- | 0 – 12 (3) | 0 – 35 (5) | 85 – 100 (3) | 100 (1) | 100 (1) |
| No. 4 | --- |  | 0 – 12 (3) | 0 – 35 (5) | 85 – 100 (3) | 85 – 100 (1) |
| No. 8 | --- |  |  | 0 – 8 (3) | 0 – 23 (4) | --- |
| No. 200 | 0 – ½ (½) | 0 – ½ (½) | 0 – ½ (½) | 0 – ½ (½) | 0 – ½ (½) | 0 - 10 (1) |

(1) Statistical procedures do not apply.

( ) The value in parentheses is the allowable deviation (±) from the target value.

Include Subsection 703.17 when Superpave hot asphalt concrete is specified using Section 401 (Superpave). Include Section 401 and the following (including Table 703-14).

703.17  Superpave Hot Asphalt Concrete Aggregate.  Delete the text and substitute the following:

Furnish hard, durable particles or fragments of crushed stone, crushed slag, or crushed gravel conforming to the following:

(a) Los Angeles abrasion, AASTHO T 96	35% max.

(b) Sodium sulfate soundness loss of coarse and	12% max.

fine aggregate, 5 cycles, AASHTO T 104

(c) Fractured faces, one or more, ASTM D 5821	90% min.

(d) Fine aggregate angularity, AASHTO T 304, method A	40% min.

(e) Flat and elongated particles, 1:5 ratio. +⅜ inch sieve,	10% max.

calculated by mass, weighted average, ASTM D4791

(f) Sand equivalent AASTHO T 176, referee method	45 min.

(g) Gradation.  Size , grade, and combine the aggregate fractions inn the mix proportions that result in a composite blend between the control points for the appropriate nominal maximum size aggregate in Table 703-14.  The nominal maximum size is one size greater than the first sieve to retain more than 10 percent of the combine aggregate.  Test according to AASTHO T 11 and T 27.

Table 703-14

Superpave Gradation and Target Value Range

| Sieve Size | Percent by Mass Passing Designated Sieve |
| --- | --- |
|  | Grading Designation |
|  | ¾ inch (1) | ½ inch (1) |
| 1 inch | 100 |  |
| ¾ inch | 90-100 | 100 |
| ½ inch | 90 max | 90-100 |
| ⅜ inch |  | 90 max |
| No. 4 | *(6) | *(6) |
| No. 8 | 23-49 (6) | 28-58 (6) |
| No. 16 |  |  |
| No. 30 | *(4) | *(4) |
| No. 50 | *(3) | *(3) |
| No. 100 |  |  |
| No. 200 | 2-8 (2) | 2-10 (2) |

(1) Submit target values for applicable sieves

(*) Submit target values for applicable sieves

( ) Allowable deviations (+/-) from the target values

Include Subsection 703.18 when Shotcrete is specified. Include Section 566 and the following:

703.18  Shotcrete Aggregate.  For fine aggregate, furnish rounded particles conforming to Subsection 703.01.  For coarse aggregate, conform to AASHTO M 80 class B, except as amended or supplemented by the following:

(a) Los Angeles abrasion, AASHTO T 96	40% max.

(b) Adherent coating, FLH T 512	1.0% max.

Combine the aggregates to meet the designated gradation in Table 703-16.

Table 703-16

ShotCrete Gradation Limits for Combined Aggregates

| Sieve Size | Percent by Mass Passing Designated Sieve (AASHTO T 27) |
| --- | --- |
|  | Grading Designation |
|  | A | B | C |
| ¾ inch |  |  | 100 |
| ½ inch |  | 100 | 80-95 |
| ⅜ inch | 100 | 90-100 | 70-90 |
| No. 4 | 95-100 | 70-85 | 50-70 |
| No. 8 | 80-100 | 50-70 | 35-55 |
| No. 16 | 50-85 | 35-55 | 20-40 |
| No. 30 | 25-60 | 20-35 | 10-30 |
| No. 50 | 10-30 | 8-20 | 5-17 |
| No. 100 | 2-10 | 2-10 | 2-10 |

# Text boxes

% passing #200

% passing #40