MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A16905 | In-Flight Anomaly Number -- | Contractor Report Number P-081 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title HE INJECTION FLEX HOSE RUPTURED DURING VIBRATION QUAL TEST |
| EICN# -- | ELEMENT ET | Contractor LMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE HE INJECTION FLEX HO | PART# 32L20600133BA000 | SER/LOT# 0000026 | MANUFACTURER TITEFLEX COR |
| Test/Operation Q - QAL | Prevailing Condtion V - VIBRATION | F / U F | Fail Mode MS - STRUCT | Cause ET - EI-TEST |
| System PROPULSION | Defect DC - BROKEN | Material S - STRUCT | Work Contact D. O`NEAL | Fail Date 08/13/1996 |
| Received at MSFC 08/16/1996 | Date Isolated 08/13/1996 | FMEA Reference 2.4.9.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MSFC | Symptom MS - STRUCT | Time Cycle -- |
| Effectivity Text ET-80 AND UP |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date 03/09/1997 | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action 09/24/1996 |
| Investigation / Resolution Summary |
| Last MSFC Update 02/13/2001 | CN RSLV SBMT 09/25/1996 | Defer Date -- | Add Date 08/16/1996 | R/C Codes 4 - TEST -- -- |
| Assignee |
| Design J. SANFORD | Chief Engineer M. PESSIN | S & MA M. SMILES | Project -- | Project MGR P. COUNTS |
| Approval |
| Design J. SANFORD | Chief Engineer M. PESSIN | S & MA M. SMILES | Project -- | Project MGR P. COUNTS |
| PAC Assignee R. TUCKER | PAC Review Complete RHT | MSFC Closure Date 10/02/1996 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N012111 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description DURING THE FLEX HOSE DELTA VIBRATION QUALIFICATION TEST FOR SLWT BEING CONDUCTED AT MSFC, THE FLEX HOSE BROKE INTO TWO PIECES (REFERENCE NCD012111 AND TEST PROCEDURE 809-2077) CRITICALITY: THE FLEX LINE IS CRIT. 1; FMEA ITEM CODE 2.4.9.1, "LEAKAGE" AND/OR DAMAGE INFLICTED TO THE ADJACENT WIRING HARNESS DUE TO STRUCTURAL FAILURE OF THE HOSE ASSEMBLY REV. "C", REVISES TASKS I.A, B, C, AND D, II, III AND IV AND CLOSES CAPS. (SEE ASTERISKS) |
| Contractor Investigation/Resolution GENERAL: - THIS FLEX HOSE CONNECTS HELIUM INJECTION TUBE ASSEMBLIES LOCATED IN THE LH2 CABLE TRAY AND VERTICAL STRUT CABLE TRAY AT STATION 2033. THE HOSE IS FABRICATED USING CORRUGATED STEEL, BRAID WIRE REINFORCEMENT AND END FITTINGS. ALL HOSE MATERIAL IS CORROSION RESISTANT STEEL - THE TEST REQUIRES FLIGHT QUALIFICATION RANDOM VIBRATION AND FLIGHT DYNAMIC SINE VIBRATION TESTING TO BE PERFORMED IN Y-AXIS, X-AXIS AND Z-AXIS - THE FAILURE OCCURRED 2 MINUTES AND 52 SECONDS INTO THE 3 MINUTE RANDOM VIBRATION TEST BEING CONDUCTED IN THE Y-AXIS. BOTH THE Z-AXIS AND X-AXIS TESTS (RANDOM AND FLIGHT DYNAMIC) HAD BEEN SUCCESSFULLY COMPLETED TASK I. FAILURE /PROBLEM INVESTIGATION A. REVIEW TEST DATA AND VERIFY ALL TEST PARAMETERS WERE WITHIN SPECIFICATION DURING THE TEST RESPONSIBILITY: J. BLEVINS/4410 - J. DYE/4400 * COMPLETE: 8/29/96 * CLOSURE STATEMENT A REVIEW OF TEST DATA HAS SHOWN THAT THE X AND Z-AXIS QUALIFICATION EXPOSURES REMAINED IN TOLERANCE FOR BOTH VEHICLE DYNAMICS SINE VIBRATION AND FLIGHT RANDOM VIBRATION. THE Y-AXIS FLIGHT RANDOM VIBRATION TEST, HOWEVER, CONTAINED HIGH FREQUENCY HARMONICS WHICH EXCEEDED THE UPPER TOLERANCE. AN EVALUATION DETERMINED THAT THE HOSE ASSEMBLY WAS NOT AFFECTED BY THIS Y-AXIS TOLERANCE EXCEEDANCE. REFERENCE IOM 4410-96-042 B. PERFORM FAILURE ANALYSIS ON FAILED FLEX HOSE RESPONSIBILITY: J. RUSSELL/3741 - D. WESTPHAL/3740 J. MATTHEESSEN/3741 - D. WESTPHAL/3740 R. LEBOEUF/4643 - E. HORAK/4600 * COMPLETE: 9/6/96 CLOSURE STATEMENT SEM AND PHOTOGRAPHIC EXAMINATION SHOWS EVIDENCE CONSISTENT WITH FATIGUE FAILURE; NO UNEXPECTED CONDITIONS WERE NOTED. CHEMICAL ANALYSIS OF ASSEMBLY'S COMPONENTS SHOW THEM TO BE OF THE PROPER MATERIALS. A COMPARATIVE ANALYSIS WITH AN UNDAMAGED HOSE SHOW NO ABNORMAL/UNEXPECTED CONDITIONS. REFERENCE LAB REPORT NO. 96A196 C. EVALUATE LWT ENVIRONMENTS VS. SLWT ENVIRONMENTS RELATIVE TO THE QUALIFICATION REQUIREMENTS FOR THIS FLEX HOSE. DETERMINE IF THIS FAILURE IMPACTS LWT QUALIFICATION RESPONSIBILITY: L. PALERMO/4410 - J. DYE/4400 * COMPLETE: 9/23/96 CLOSURE STATEMENT AN INSPECTION OF THE SLWT ENVIRONMENT SHOWED AN EXCEEDANCE OVER THE HISTORIC LWT TEST. TRANSLATING THE SLWT ENVIRONMENT TO THE LWT LEVEL SHOWED A LOW FREQUENCY EXCEEDANCE STILL EXISTED AFTER EVALUATION BY ENGINEERING, A DECISION WAS MADE TO ADJUST THE TEST ENVIRONMENTS AND UPDATE THE LWT QUALIFICATION FOR THIS HOSE AS WELL AS RETEST FOR SLWT ENVIRONMENTS. REFERENCE TEST PLANS 809-2080 (LWT) AND 809-2078 (SLWT). BOTH HOSES WERE SUCCESSFULLY PASSED. REFERENCE IOM 4410-96-045 D. REVIEW THE BUILD DATA RELATIVE TO THIS FLEX HOSE AND EVALUATE FOR COMPLIANCE TO REQUIREMENTS RESPONSIBILITY: F. RAMSEY/3761 - S. PARIKH/3760 J. RUSSELL/3741 - D. WESTPHAL/3740 * COMPLETE: 9/12/96 CLOSURE STATEMENT ATTEMPTS TO LOCATE THE BUILD DATA AT TITEFLEX WERE UNSUCCESSFUL THIS HOSE WAS MNAUFACTURED IN JULY 1989; TITEFLEX IS CONTRACTUALLY REQUIRED TO RETAIN THE DATA FOR A PERIOD OF SEVEN YEARS. AS THE SEVEN YEARS LIMITATION HAS PASSED, THE SEARCH FOR DATA WAS DISCONTINUED. REFERENCE CCMAIL FROM F. RAMSEY, PROCUREMENT QUALITY; DATED 9/12/96 E. REVIEW THE NONCONFORMANCE DATABASE FOR SIMILAR FAILURES RESPONSIBILITY: J. RUSSELL/3741 - D. WESTPHAL/3740 COMPLETE: 8/20/96 CLOSURE STATEMENT A SEARCH WAS CONDUCTED FOR ALL NONCONFORMANCES WRITTEN AGAINST 32L2XXX AND 32L1XXX FLEX HOSE ASSEMBLIES, BOTH FLEXIBLE METALLIC ASSEMBLIES. NO SIMILAR FAILURES, I.E. STRUCTURAL FAILURE OF THE LINE ASSEMBLIES, WERE FOUND NOTE: ON ET-4 A FINAL LEAK CHECK ON THE HE INJECTION SYSTEM FAILED AS A RESULT OF A LEAKING 32L206026AA000 HOSE ASSEMBLY THE CAUSE WAS FOUND TO BE A HIGH CYCLE FATIGUE CRACK WHICH ORIGINATED FROM A SHARP ROOT RADIUS OF THE FLEX HOSE CONVOLUTE AND A SERIES OF CIRCUMFERENTIAL GROOVES ON THE OUTSIDE SURFACE PROPAGATION STRESSES WERE CAUSED BY HIGH FREQUENCY VIBRATION THAT OCCURRED DURING THE LEAK CHECK. NO STRUCTURAL FAILURE OF THE ASSEMBLY OCCURRED. REFERENCE MATERIALS ENGINEERING F/A REPORT NO. ETFA-50 REFERENCE CCMAIL FROM J. RUSSELL, DATED 8/20/96 CAUSE: FATIGUE FAILURE DUE TO OVER TEST * TASK II. CORRECTIVE ACTION - TEST ENVIRONMENTS WERE EVALUATED AND ADJUSTED AND THE HOSE ASSEMBLY SUCCESSFULLY RETESTED - NO FURTHER ACTION REQUIRED. QUALIFICATION TEST ENVIRONMENTS ARE UNIQUE AND DETERMINED ON A CASE BY CASES BASIS TASK III. CLEARANCE OF EFFECTIVITIES ET-80 AND UP: REQUALIFICATION OF THE 32L2060133BA000 HOSE WAS SUCCESSFUL FOR BOTH LWT AND SLWT ENVIRONMENTS REFERENCE MSFC MEMO EE31(53-96) NOTE: THIS IS ALSO DEFERRAL RATIONALE * TASK IV. CAPS CLOSURE SUMMARY DURING THE FLEX HOSE DELTA VIBRATION QUALIFICATION TEST FOR SLWT BEING CONDUCTED ON THE HE INJ FLEX HOSE ASSEMBLY, THE HOSE BROKE INTO TWO PIECES. THE TEST REQUIRES FLIGHT QUALIFICATION RANDOM VIBRATION AND FLIGHT DYNAMIC SINE VIBRATION TESTS TO BE PERFORMED IN THE Y-AXIS, X-AXIS AND Z-AXIS. THE FAILURE OCCURRED WHILE THE TEST WAS BEING CONDUCTED IN THE Y-AXIS, THE LAST AXIS TO BE TESTED, DURING RANDOM VIBRATION TESTING. THE FAILURE CAUSE WAS DETERMINED TO BE FATIGUE FAILURE DUE TO OVER TESTING THE ASSEMBLY AFTER EVALUATION BY ENGINEERING, IT WAS DETERMINED THAT A LOW FREQUENCY EXCEEDANCE EXISTED FOR BOTH THE SLWT TEST ENVIRONMENTS AND THE PREVIOUS LWT TEST ENVIRONMENTS. CORRECTIVE ACTION CONSISTED OF ADJUSTING THE ENVIRONMENT FOR BOTH LWT AND SLWT AND RETESTING. BOTH TEST WERE SUCCESSFUL. NO FURTHER ACTION WAS NECESSARY THIS CAPS IS CLOSED. NO FURTHER ACTION REQUIRED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A16905 | IFA# -- | Contractor RPT# P-081 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 32L20602133BA000 | Asmnt Part Name FLEX HOSE ASSY | Asmnt Serial/Lot# 0000026 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD ET - EI-TEST | FAIL MODE MS - STRUCT |
| Asmnt FMEA 2.4.9.1 | Asmnt FM 1 | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |