96E03/29/06

S559-96E.doc

Use on projects as appropriate.

Section 559. - WATER PROOFING

Delete the text of this section and substitute the following:

Description

Use the following SCR for waterproof deck membranes on bridges. Edit as required. Also include the appropriate SCR for subsection 702.11. Insert the name of the bridge in the space provided.

559.01  This work consists of preparing for, furnishing, and placing a membrane waterproofing system on ____________ bridges.

Material

559.02  Material shall conform to the following subsections:

Asphalt Cement	702.01

Geotextile, Type VII	714.01(g)

Granulated Rubber	702.11

Pavement Reinforcing Fabric	714.03

Construction Requirements

559.03  General.  At least 14 calendar days before installing the membrane, submit a proposed procedure for installing the membrane system.  Indicate in detail the techniques, equipment, and materials proposed for preparing the bridge deck and installing the membrane.  Also indicate what membrane system (i.e. generic according to Subsection 559.06 or proprietary according to Subsection 559.07) is to be used, the intended dates for installation, traffic control considerations and any other details necessary to control the work.  Do not begin any work on the bridge deck until the procedure has been accepted.  This review and acceptance shall not relieve the Contractor of the responsibility of achieving the desired result of a sound waterproof membrane free from defects.

559.04  Weather Restrictions.  Do not place tack coats, leveling or the membrane system during wet, foggy, or frosty weather.  Apply the membrane system to surfaces which are completely clean and dry before and during application.  If the surfaces have been saturated with moisture before application, dry an additional 24 hours after the surfaces become visibly dry.  Do not apply the membrane system until the temperature of the prepared deck surface is at least 50(F and the air temperature in the shade is at least 50(F and rising.

For new construction, edit 559.05 to remove references to existing overlay. Keep last sentence: "reasonably smooth and clean" statement. On existing bridge decks, include any modifications to paving dams, expansion joints, curbs, etc…

559.05  Preparing the Existing Bridge Deck.  Remove the existing AC overlay from the bridge deck.  Avoid damaging the bridge deck when removing the existing overlay.  Small areas of asphalt and asphalt stain need not be removed if smooth and tightly bonded to the deck.  The deck surface must be reasonably smooth and clean before applying the new membrane.

Eliminate 559.05a if there are not transverse deck joints on the bridge. If waterproofing fabric is needed, include SCR for 714.03. If not, strike from materials list at beginning of this section.

(a) Expansion Joints.  Before installing the waterproof membrane, measure, cut, and install pavement reinforcement fabric over the deck joint at the pier.  Place the fabric such that it is centered over the deck joint.  Install the fabric according to manufacturer's recommendations.  Install the fabric full-width of the bridge in a single piece.

559.06  Asphalt-Rubber Fabric Seal.  This system consists of a one course hot asphalt-rubber seal with a geotextile fabric cover.

Provide a self-powered pressure distributor for mixing and spreading the asphalt and rubber equipped with the following:

• Separate power pump unit capable of pumping the specified material at the specified rate.

• Equipment for heating the bituminous material.

• Distribution bar with nipples and valves bathed in the circulating asphalt to the extent the nipples do not become partially plugged with congealing asphalt upon standing.

• A tachometer, pressure gauges, volume measuring devices and a thermometer for reading temperatures of tank contents.

• Full circulating spray bar controlled by a bootperson riding in such a position that all sprays are in full view and readily accessible for controlling spread widths.

Before adding the ground rubber, bring the temperature of the asphalt to between 390(F and 450(F.  Combine the asphalt and rubber as rapidly as possible in the proportions of at least 2 pounds of rubber to 1 gallon of asphalt (standard at 390(F), then mix until semi-fluid.

Use up to 9% diluent, if needed, to assist in the mixing of the rubber and the spray application of the mixture.  Diluent shall have a boiling point of at least 350(F.

Apply the mixture as soon as it reaches application consistency.  Do not hold the mixture above 350(F for more than 1 hour after it reaches that temperature.

Apply the hot asphalt-rubber mixture at the rate of 0.50 (+0.01) gallons per square yard.  Make transverse joints by placing building paper over the ends of the previous applications, and start the joining application on the building paper.  Once the application process has progressed beyond the paper, remove and dispose of the paper.  Repair any unsatisfactory joint at no expense to the Government.

Align the fabric and carefully roll or broom it into the asphalt-rubber mixture.  If the alignment of the fabric must be changed, cut the fabric and realign it overlapping the previous material and proceed as before.

Overlap all joints a minimum of 6 inches.  Overlap transverse joints in the direction of paving to prevent edge pickup by the paver.  For lapped joints, fold the top fabric back and apply a light (0.005 gallons per square yard) coat of asphalt-rubber mixture.  Fold the top fabric onto the asphalt-rubber mixture, broom and squeegee out smoothly.

Roll or broom the fabric into the asphalt in such a way that any air bubbles under the fabric are removed.  Puncture membrane to release bubbles or pockets of trapped air or vapor and repair in a manner satisfactory to the CO.

Apply the waterproof membrane system across the entire width of the bridges extending it a minimum of 30 inches up the curb faces.

If asphalt sealant bleeds through the fabric, treat the affected areas with blotter.

559.07  Proprietary Membrane Systems.  In lieu of the Asphalt-Rubber Fabric Seal described above, the Contractor may elect to use any of the following proprietary deck seal systems listed in Table 559-1:

Table 559-1

Approved Proprietary Deck Seal Systems

| PRODUCT NAME | LOCAL REPRESENTATIVE | REMARKS |
| --- | --- | --- |
| Bituthene 5000 | W.R. Grace Company 62 Whittemore Avenue Cambridge, MA 02140 617-876-1400 or 206-391-4981 | Rubberized asphalt and mesh. No more than 4% slope. No tack coat required. |
| Boni Fibers Fiber ASP Conc (Type B Fibers) | KAPEJO, Inc. P.O. Box 649 New Castle, DE 19720-0649 800-342-3717 | Polyester fiber asphalt concrete system. |
| CIM 1000 Commercial Industrial Membrane | CIM Industries, Inc. Mfg: 800-543-3458 Local: Ed Cook Special Asphalt Products: 503-295-6490 | No more than 8% slope. |
| Geo Tac | PavePrep Corporation Local: Columbia Storage Inc. 600 SE Assembly , Suite 100 Vancouver, WA 98661 800-426-7976 or 206-699-1426 | No tack coat required. |
| Highway Membrane 125 | American Hydrotech, Inc. Chuck Croneweth 2001 6th Avenue, Suite 3306 Seattle, WA 98121 | Rubberized asphalt. No more than 5% slope. |
| Jiffy Seal | Protecto Wrap Company 2255 South Delaware Street Denver, Colorado 80223 303-777-3001 | Aromatic tars mixed with synthetic resins and reinforced with fibrous material. |
| Petrotac | Phillips Fibers Corporation 1900 Point West Way, Suite 261 Sacramento, CA 95815 800-437-6600 | Factory laminated sheet of rubberized asphalt reinforced with fabric. No more than 5% slope. No tack coat required. |
| Polyguard 665 | Polyguard Products, Inc. P.O. Box 755 Ennis, TX 75120-0755 | Tack coat required. |
| Protecto Wrap M-400A | Protecto Wrap Company 2255 South Delaware Street Denver, CO 50223 303-777-3001 | Pre-formed sheet. No more than 4% slope. No tack coat required. ½” maximum aggregate size. |
| Royston Bridge Deck Membrane 10A | Royston Laboratories, Inc. 128 First Street Pittsburgh, PA 15238 412-828-1500 or 800-245-3209 | Prefabricated laminate with fiberglass mesh layered between asphalt mastic. No more than 4% slope. No tack coat required. |
| Rub-R-Road | Rub-R-Road, Inc. Akron, OH 216-499-2901 | Rubberized asphalt concrete system. |
| SAMI Asphalt Rubber Chip Seal | International Surfacing, Inc. Rep: Jeffrey Smith or Dick Messick 800-528-4548 |  |
| Uniroyal Flexible Membrane 6125 | Uniroyal, Inc. Mishawak, IN 46544 | Hot applied rubberized asphalt compound. No more than 5% slope. |

559.08  Overlay Placement.  Limit traffic on the membrane to necessary construction equipment and emergency vehicles only.  Place a hot asphalt concrete overlay within 48 hours after placing the membrane.

Do not windrow AC on the membrane ahead of the paving machine.  Do not use an AC pickup machine.  Do not turn equipment on the membrane to avoid membrane movement and damage.  Avoid abrupt starts and stops.

Broom any excess blotter from the membrane surface before placing the overlay.  Repair all damaged areas on the membrane before commencing overlay placement.  Apply a light tack coat according to Section 412 before placing the overlay.

Limit the lay-down temperature of the mix to a maximum of 300(F.

559.09  Acceptance.  Construction will be accepted under Subsection 106.02.  Waterproof membrane material will be accepted under Subsection 106.03.

Measurement

559.10  Waterproofing will be measured by the square yard.  The area included will be the surface area of the bridge deck plus curb faces as specified or directed.  There will be no payment for overlaps or splices.

Payment

559.11  The accepted quantities, measured as provided above, will be paid for at the contract price per unit of measurement for the pay items listed below that are shown in the bid schedule.  Payment will be full compensation for the work prescribed in this section.

Payment will be made under:

Pay Item	Pay Unit

55901	Waterproof membrane, Class C	Square yard