The Lindhard critical angle for planar channeling for a charged particle in a straight single crystal is:

where  is the crystal atomic number,  the beam atomic number,  the momentum, N the atomic number density,  the planar spacing, ,  the T-F screening parameter, and  the Bohr radius. Below the TeV range,  is small compared to the typical beam divergence. At 1 TeV/c,  for the 110 plane in Si. Crystals must be aligned along planes or axes to see channeling. The critical angle is roughly equal to , the HWHM of a transmission or alignment distribution of , the particle angle relative to a crystal plane.

For a bent crystal (see below)

where  is the minimum radius of curvature  is the Tsyganov radius (see below).

Channeling dips and peaks in  are not Gaussian. Temperature variations may occur because of lattice vibrations. Higher crystals, e.g. W, have larger but large dislocation-free crystals are not available whereas they are for Si.