February 11, 2005

NASA Electronic Parts and Packaging Program

Performance of Vishay Siliconix U430 JFET Transistor at Extreme Temperatures

Richard Patterson, NASA Glenn Research Center

Ahmad Hammoud, QSS Group, Inc. / NASA GRC

Malik Elbuluk, University of Akron

Scope

Cryogenic temperatures are typically encountered in planetary exploration and deep space applications, such as Mars and Saturn environments.  Minimum temperature on the earth’s moon has been estimated to be as low as -235 °C.  Electronics on board of current spacecraft are maintained at about room temperature, through the use of various thermal control elements, for proper operation.  Great benefits would be gained if the electronics were made to function properly at the extreme temperatures without the use of these heating accessories.  These benefits include improved reliability, increased payload capacity, and decreased electronic system development and launched costs, to name a few.  Very little data exist on the performance of many electronic devices and circuits under cryogenic temperatures.  In this work, the performance of an N-channel JFET (Junction Field Effect) transistor was evaluated under low temperature and thermal cycling.  The investigations were carried out to establish a baseline on the functionality and to determine suitability of this device for use in space applications under cryogenic temperatures.  This device was chosen because it is being considered by the NASA Jet Propulsion Laboratory (JPL) for use in electronic circuits on future space missions.

Test Procedure

The device investigated in this work comprised of Vishay Siliconix U430 device. Each device had matched pair of N-channel JFET transistors.  This type of transistor is a depletion mode device with high slew rate, low noise and low offset/drift voltage, and can be used in wideband differential amplifiers, high speed comparators, and impedance converters [1].  The transistor pair was examined for operation between -195 °C and +100 °C.  Performance characterization was obtained in terms of their switching characteristics, using a Sony/Tektronix 370A programmable curve tracer, at specific test temperatures.  Cold-restart capability, i.e. power switched on while the devices were at a temperature of -195 °C, was also investigated.  Thermal cycling effects were also investigated over a wide temperature range.  The devices were exposed to a total of 10 cycles between -195 °C and +100 °C at a temperature rate of 10 °C/minute.  At each test temperature, the device was given a soak for 20 minutes before data were taken.  Following the thermal cycling, measurements were then performed at the test temperatures of +20, -195, +100, and again at +20 °C.  Some of the manufacturer’s specifications for this JFET transistor are shown in Table I [1].

Table I.  Specifications of Vishay Siliconix U430 JFET transistor [1].

| Parameter | Symbol | U430 |
| --- | --- | --- |
| Operating Temperature | T(oper) | -55 °C to +150 °C |
| Max Drain Current | ID | 30 mA |
| Max Gate-Source Voltage | VGS | -25 V |
| Total Power Dissipation | PD | 0.5 W |
| Drain-Source On-Resistance | RDS(on) | > 27 Ω |
| Package |  | TO-78 |

Test Results

Although two units of this transistor were evaluated, data pertaining to only one device is presented due to the similarity in their results.

Temperature Effects

The pre-cycling switching characteristics of the U430 device at +20 °C, -195 °C, and +100°C are shown in Figures 1, 2, and 3, respectively.  These output characteristics are defined as the drain current (ID) versus drain-to-source voltage (VDS) family curves at various gate voltages (VGS).  In this test gate voltages (VGS) ranged between 0 and -1.6 Volts.  Two deviations can be noted in the output characteristics with change in temperature.  The first is the downward shift of the switching curves, for a given gate voltage, as temperature moved away from room temperature.  This behavior, which is more profound at low temperatures, is an indicative of the increase in the gate threshold voltage with decreasing temperatures.  At the high test temperature, i.e. +100 °C, this change is insignificant as the temperature is still within the device’s operating temperature range.  The second deviation represents the variation, albeit minimum, in the slope of the switching curves in the linear region, for a given gate voltage, as the test temperature is changed.  This phenomenon is caused primarily by the dependence of the drain-source on-resistance (RDS(on)) on test temperature.

Cold Re-Start

Cold-restart capability of the Vishay Siliconix U430 matched N-channel JFET pair transistors was investigated by allowing the devices to soak at -195 °C for at least 20 minutes without the application of electrical bias.  Power was then applied to the device under test, and measurements were taken on the output switching characteristics.  Both transistors were able to cold-start successfully at -195 °C, and the results obtained were the same as those obtained earlier at that temperature.

Figure 1.  Pre-cycling output switching characteristics at 20 °C.

Figure 2.  Pre-cycling output switching characteristics at -195 °C.

Figure 3.  Pre-cycling output switching characteristics at +100 °C.

Effects of Thermal Cycling

The effects of thermal cycling were investigated by subjecting the devices to a total of 10 cycles between -195 °C and +100 °C at a temperature rate of 10 °C/minute.  Switching characteristics of the transistors were then taken at +20 °C, 
-195, and +100°C.  Figure 4 shows this post-cycling data at these selected temperatures.  It can be clearly seen that the post-cycling family of switching curves for these transistors were the same as those of pre-cycling for a given test temperature.  Also, little change occurred in the drain-source on-resistance (RDS(on)) of the transistors as depicted in Table II.  Therefore, the extreme temperature and the thermal cycling did not induce much change in the behavior of these transistors.  This limited thermal cycling also appeared to have no effect on the structural integrity of these devices as no structural deterioration or packaging damage was observed.

Table II.  Pre- and post-cycling on-state resistance RDS(on) versus temperature.

| Temperature (°C) | Pre-cycling RDS(on) (Ω) | Post-cycling RDS(on) (Ω) |
| --- | --- | --- |
| -195 | 58 | 55 |
| +20 | 48 | 48 |
| +100 | 67 | 68 |

Pre-cycling at 20 °C

Pre-cycling at -195 °C

Pre-cycling at +100 °C

Post-cycling at 20 °C

Post-cycling at -195 °C

Post-cycling at +100 °C

Conclusions

Two Vishay Siliconix U430 N-channel JFET devices were evaluated for operation between -195 °C and +100 °C.  Each device had a matched pair of transistors.  The effects of thermal cycling under a wide temperature range on the operation of these transistors and cold-restart capability were also investigated.  Both devices were able to maintain operation between -195 °C and +100 °C with minimal changes in their characteristics.  The temperature-induced changes included an increase in the gate voltage at cryogenic temperatures, and a slight increase in the on-resistance at 100 °C.  The limited thermal cycling performed on the transistors had no effect on their performance, and both devices were able to cold start at -195 °C.  Further testing under long-term cycling is required to fully establish the reliability of these devices and to determine their suitability for extended use in extreme temperature environments.

References

[1].	Vishay Siliconix, “U430 Matched N-Channel Transistor Pairs”, Data Sheet Document Number 70249, Rev. E, June 2001.

Acknowledgements

This work was performed under the NASA Glenn Research Center GESS Contract # NAS3-00145.  Funding was provided by the NASA Electronic Parts and Packaging (NEPP) Program.

# Text boxes

Figure 4.  Switching characteristics at selected test temperatures before and after cycling.