## MQXB06  Fabrication Report

#### TD-03-022

Kerby, Nobrega, Bossert, Rife

- Introduction

- Superconducting Cable

  - Cable mechanical parameters

  - Cable Electrical parameters

  - Cable test data

- Coil Fabrication

  - Cable and wedge insulation

  - Winding and Curing

  - Coil measurements (body, ends and longitudinal)

  - Coil shimming

  - Voltage taps

- Coil Assembly

  - Coil arrangement

  - Splices

  - Ground wrap system

- Collaring and Keying

  - Collaring

  - Keying

  - Mechanical measurements (longitudinal & collar deflection)

- End Clamps

  - Installation procedure

  - Measurements and shimming

- Yoke and Skinning

  - Assembly configuration

  - Welding

  - O.D. Measurements

  - Twist Measurements

  - Straightness Measurements

  - Axial loading

- Final Assembly

  - Final Electrical Measurements

  - Mechanical measurements

- Discrepancies and Comments

1.0 Introduction

MQXB06 is the sixth of eighteen production cold mass to be built in the LHCIR Quadrupole series.  Table 1.0.1 lists the previous cold masses in the MQXB series and the numbers assigned to the fabrication reports that describe them.

| Cold Mass number | Fabrication Report Number |
| --- | --- |
| MQXBP1 (prototype) | TD-02-009 |
| MQXB01 | TD-02-027 |
| MQXB02 | TD-02-038 |
| MQXB03 | TD-02-043 |
| MQXB04 | TD-03-004 |
| MQXB05 | TD-03-006 |

Table 1.0.1  MQXB Cold Mass Fabrication Report Numbers

All the production cold masses (MQXB01-MQXB018) are essentially the same in design.  They were preceded by one prototype, MQXBP1.  Like all production cold masses, MQXB06 does not include R & D related instrumentation, such as quench detection voltage taps, spot heaters, strain gauges to measure coil azimuthal preload, or instrumentation on the longitudinal preload screws (bullets).

The primary features of MQXB06 are listed below in Table 1.0.2.   Changes from the previous cold mass are highlighted in red and italicized.

| Inner Cable Strand No. |  | 37 |
| --- | --- | --- |
| Inner Strand Manufacturer |  | Alsthom |
| Inner Cable lay direction |  | Right Lay |
| Outer Cable Strand No. |  | 46 |
| Outer Strand Manufacturer |  | Alsthom |
| Outer Cable lay direction |  | Left Lay |
| Cable Pre-baking |  | None |
| Strand Coating |  | None |
| Cable Cleaning Fluid |  | ABZOL VG |
| Inner Cable Insulation |  | 25uM x 9.5mm w/ 58% overlap surrounded by 50uM x 9.5mm w/2mm gaps w/QIX |
| Outer Cable Insulation |  | 25uM x 9.5mm w/ 50% overlap surrounded by 25uM x 9.5mm w/48% overlap w/QIX |
| Coil Curing temperature |  | 190C/135C Two step cycle |
| Inner coil curing pressure |  | high at 135C/ low at 190C |
| Outer coil curing pressure |  | high at 135C/ low at 190C |
| Inner Coil target size |  | +300uM, (+.012) |
| Inner Coil target MOE |  | 9GPa |
| Outer Coil target size |  | +250uM, (+.010) |
| Outer Coil target MOE |  | 9GPa |
| Target Prestress |  | 75-80 MPa |
| Coil end azimuthal Shim System |  | Shim ends to be same as body, tapering off toward end of saddle. See Figure 3.4.1. |
| End Part Material |  | G-11CR |
| End Part Configuration |  | Iteration #2, 5 block design. |
| Splice Configuration |  | Internal |
| Voltage Tap Plan |  | No Quench characterization voltage taps. Taps on leads at ends (between quadrants) only. |
| Inter layer strip heaters |  | None |
| Outer layer strip heaters |  | CERN version #2, double element, dwg. No. MD-369619. |
| Key extension |  | None |
| Inner coil Bearing Strips |  | None |
| Outer coil Bearing Strips |  | None |
| Collar configuration |  | 38mm long solid welded packs, without bearing strips |
| Collar key configuration |  | 152.4 mm long, phosphor bronze. |
| Strain Gauges |  | No beam or capacitor gauges. |
| Spot Heaters |  | None. |
| End Radial Support |  | Collet end clamps on both ends. Aluminum exterior cans with G-11CR quadrant pieces. |
| Collar/Yoke Interface |  | Radial clearance between collar and yoke. |
| Quadrant Lead Configuration |  | Double lead with superconducting cable for stabilizer |
| End longitudinal loading |  | Bullets apply load directly to coils, 8.9 kN (2000 lbs.) force per bullet. End cans are bolted to end plates, preventing coils from contracting longitudinally (see Figure 7.6.1). |
| Yoke Key Width |  | 26.5mm |
| Strain Gauges on Skin |  | None. |
| End Plate Thickness |  | 35mm |
| Tuning Shims |  | None |
| Other |  | Non-lead end keys mold released and replaced. Thermometers on end plates. Axial preload bolts not instrumented. Inner coils shimmed azimuthally 25 um toward midplane from original design. See section 4.3. |
| Coil Fabrication Start Date |  | 6/1/02 |  |
| Cold Mass Completion Date |  | 9/28/02 |  |

Table 1.0.2  MQXB06 features.

2.0 Superconducting Cable

2.1 Cable Mechanical Parameters

Tables 2.1.1 and 2.1.2 summarize the cable dimensional parameters used in MQXB06.  Inner cable came from reel LHC-3-A-N0014, and was made by New England Electric Wire Corp. using Alsthom strand.  Outer cable came from reel LHC-4-A-N0011 and LHC-4-A-N0012, and was made by New England Electric Wire Corp. using Alsthom strand. All cable was cleaned ultrasonically, at an elevated temperature (160C), with ABZOL VG, in a degreaser made by Branson Inc (the same machine used for the Tevatron). The degreaser is inserted into the cable insulating line, just before the cable is insulated.

| Parameter | Unit | Inner cable | Outer cable |
| --- | --- | --- | --- |
| Radial width, bare | mm | 15.4 | 15.4 |
| Minor edge, bare | mm | 1.320 | 1.051 |
| Major edge, bare | mm | 1.610 | 1.241 |
| Midthickness, bare | mm | 1.465 | 1.146 |
| Keystone angle, | deg | 1.079 | 0.707 |
| Pitch Length | mm | 114 | 102 |
| Number of strands |  | 37 | 46 |
| Lay direction |  | Right | Left |

Table 2.1.1: Cable design parameters for MQXB Magnets.

| Parameter | Unit | Inner cable (N0014) | Outer cable (N0011/12) |
| --- | --- | --- | --- |
| Radial width, bare | mm | 15.3903 | 15.4064/15.4019 |
| Minor edge, bare | mm | 1.3222 | 1.0540/1.0552 |
| Major edge, bare | mm | 1.6080 | 1.2380/1.2372 |
| Midthickness, bare | mm | 1.4651 | 1.1460/1.1462 |
| Keystone angle, | deg | 1.064 | .684/.677 |
| Pitch Length | mm | 114.3 | 101.6/101.6 |
| Number of strands |  | 37 | 46/46 |
| Lay direction |  | Right | Left/Left |

Table 2.1.2: Cable actual parameters for MQXB06.

2.2 Cable Electrical Parameters

Electrical Data and cable test data in sections 2.2 and 2.3 were taken at BNL.  Two tests of inner cable N0014, four tests of outer cable N0011 and two tests of outer cable N0012 were done.  The ranges shown in the cable columns represent the range of values taken from the multiple tests.

| Parameter | Unit | Inner Cable (N0014) | Outer Cable (N0011) | Outer Cable (N0012) |
| --- | --- | --- | --- | --- |
| R(293 K) | ohms/cm | 16.282-16.314 | 17.867-17.913 | 18.056-18.123 |
| R(10 K) | ohms/cm | 0.182-0.204 | 0.376-0.376 | 0.434-0.447 |
| RRR |  | 80 - 90 | 48 - 48 | 41 - 42 |
| C/Sc |  | 1.29-1.31 | 2.06-2.07 | 1.87-1.89 |

Table 2.2.1: Cable electrical parameters as provided by BNL

2.3 Cable Test Data

|  | INNER CABLE N0014 | oUTER cABLE N0011 | Outer CAble N0012 |
| --- | --- | --- | --- |
| B, T | Ic, KA | Jc, A/mm2 | Ic, KA | Jc, A/mm2 | Ic, KA | Jc, A/mm2 |
| 6 | 21.094-21.097 | 2553-2565 | 11.822-12.191 | 2435-2519 | 12.173-12.376 | 2307-2359 |
| 7 | 15.458-15.510 | 1871-1886 | 8.625-8.924 | 1787-1849 | 9.002-9.030 | 1706-1721 |
| 8 | 9.821-9.923 | 1189-1206 | 5.333-5.685 | 1105-1178 | 5.684-5.831 | 1084-1105 |

Table 2.3.1: Cable test data at 4.2K as provided by BNL

3.0 Coil Fabrication

3.1 Cable and Wedge Insulation

Table 3.1.1 summarizes the cable insulation parameters used in MQXB06. Note that the adhesive on the outer wrap of both inner and outer cable is modified polymide (QIX) instead of QI.  QIX had been introduced late in the short magnet program.  The wedges were insulated identically to their respective coils.

| Parameter | Inner cable | Outer cable |
| --- | --- | --- |
| Number of wraps | 2 | 2 |
| Inner wrap: -material -adhesive -wrap structure | Kapton tape 25 m  9.5 mm None Spiral wrap with 58% overlap | Kapton tape 25 m  9.5 mm None Spiral wrap with 50 % overlap |
| Outer wrap: -material -adhesive -wrap structure | Kapton tape 50 m  9.5 mm Modified Polyimide (QIX) Spiral wrap with 2 mm gaps | Kapton tape 25 m  9.5 mm Modified polyimide (QIX) Spiral wrap with 48 % overlap |

Table 3.1.1: MQXB06 cable insulation parameters.

3.2 Winding and Curing

MQXB coils are cured using a two-step cycle (to control interstrand resistance) with low pressure/high temperature followed by a high pressure/low temperature step.  All coils have wedge breaks staggered such that the breaks are not coincident at any longitudinal location in the same coil.  Gaps between the wedges before curing are 2.2mm.

3.3 Coil Measurements

3.3.1 Coil Straight Section

Coil azimuthal size and modulus measurements were taken over a range of pressures, 55 to 100 MPa.  The design pressure for both the inner and outer coils at room temperature is about 75-80 MPa. Coils are measured with a 3 inch (76mm) gauge length along the straight section of the magnet, from lead end to non-lead end.  During this process, resistance measurements are taken to ensure that there are no turn-to-turn shorts.

The target sizes are +300 m for inner coils and +250 m for outer coils, at a pressure of 83 MPa.  These values represent a size “with respect to the design size inside the cross section when the magnet is operating”.  The larger sizes are necessary at room temperature to achieve the correct sizes when the magnet is cold and powered.  Table 3.3.1 lists the coils used in MQXB06 and their corresponding average (unshimmed) size and modulus of elasticity.

| Coil Numbers | SIDE A m | E(A) GPa | SIDE B m | E(B) GPa |
| --- | --- | --- | --- | --- |
| MQXBi-043 | 297 | 8.6 | 302 | 8.6 |
| MQXBi-044 | 318 | 8.8 | 323 | 8.8 |
| MQXBi-045 | 318 | 8.6 | 323 | 8.5 |
| MQXBi-046 | 295 | 8.9 | 295 | 9.0 |
| MQXBo-043 | 210 | 9.6 | 213 | 9.7 |
| MQXBo-044 | 221 | 9.7 | 224 | 9.6 |
| MQXBo-045 | 233 | 8.8 | 230 | 8.8 |
| MQXBo-046 | 234 | 9.4 | 237 | 9.5 |

Table 3.3.1: MQXB06 coil body size and modulus.

Variation of the size along the length of the coils is shown in Figs 3.3.1 and 3.3.2.  Side A is the “first wound” side of the coil and Side B is the side with the lead extending from the end of the saddle.  The full length of each coil is measured, encompassing 67 positions, each 76mm long.

Figure 3.3.1: Variation of size along the length of inner coils.

Figure 3.3.2: Variation of size along the length of outer coils.

3.3.2 Coil Length Measurements

MQXB coils are wound and cured using steel tooling which fixes the coil to a specific length.  When a coil is removed from the tooling after curing, it shrinks longitudinally, relieving the stresses incurred during the coil and cable manufacturing processes.  After curing, the straight section of each coil is measured longitudinally (back of key to back of key).  “Springback” is defined as the difference between the coil length before curing and after being removed from the curing tooling.    Measurements in mm are shown in Table 3.3.2..

| Coil Number | Springback |
| --- | --- |
| MQXBi-043 | 4.2 |
| MQXBi-044 | Not Available |
| MQXBi-045 | 4.1 |
| MQXBi-046 | 4.0 |
| MQXBo-043 | 8.8 |
| MQXBo-044 | 8.6 |
| MQXBo-045 | 8.6 |
| MQXBo-046 | 8.5 |

Table 3.3.2: “Springback”, or Coil Longitudinal Shrinkage.

3.4 Coil Shimming

3.4.1 Coil Straight Section

| I/O | Quadrant | Coil # | Coil Size m | Pole Shim m | Midplane shim m | Target m | Shimmed Coil Size m |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Inner | 1A | i-043 | 297 | 25 | -25 | 300 | 297 |
| Inner | 1B | i-043 | 302 | 25 | -25 | 300 | 302 |
| Inner | 2A | i-044 | 318 | 25 | -25 | 300 | 318 |
| Inner | 2B | i-044 | 323 | 25 | -25 | 300 | 323 |
| Inner | 3A | i-046 | 295 | 25 | -25 | 300 | 295 |
| Inner | 3B | i-046 | 295 | 25 | -25 | 300 | 295 |
| Inner | 4A | i-045 | 318 | 25 | -25 | 300 | 318 |
| Inner | 4B | i-045 | 323 | 25 | -25 | 300 | 323 |
| Outer | 1A | o-046 | 234 | 0 | 0 | 250 | 234 |
| Outer | 1B | o-046 | 237 | 0 | 0 | 250 | 237 |
| Outer | 2A | o-044 | 221 | 0 | 0 | 250 | 221 |
| Outer | 2B | o-044 | 224 | 0 | 0 | 250 | 224 |
| Outer | 3A | o-045 | 233 | 0 | 0 | 250 | 233 |
| Outer | 3B | o-045 | 230 | 0 | 0 | 250 | 230 |
| Outer | 4A | o-043 | 210 | 0 | 0 | 250 | 210 |
| Outer | 4B | o-043 | 213 | 0 | 0 | 250 | 213 |

Table 3.4.1: Kapton shimming used in the coil straight section.

If the magnet coil sizes do not meet the target, they may be azimuthally shimmed with kapton to reach the target levels.  The target pre-stress for MQXB06 is about 75-80 MPa. This corresponds to a nominal coil size of +300 m for inner coils and +250 m for outer coils. The inner coil sizes in MQXB06 varied from 295 to 323 m with an average of 309 m; whereas the outer coil size varied between 210 and 237 m with an average of 225 m.  Although no shimming was deemed necessary for preload adjustment, the inner coil pole and midplane were shimmed for harmonic purposes.  See section 4.3 for a detailed explanation.  Table 3.4.1 lists the coil and shim sizes used in MQXB06, and reflects the ground insulation changes shown in section 4.3.

3.4.2 Coil  Ends

Resistance readings were taken while compressing the ends of the MQXB06 coils to 83 MPa, both lead and non-lead end of both inner and outer coils.  Size measurements were not taken on the ends.  The ends of the MQXB06 coils were shimmed azimuthally with sheets of 125 um thick kapton, according to a formula that was established on the last short models (HGQ07-9), as are all long production coils.  Shimming is shown in Figure 3.4.1 and is recorded in FNAL drawings 5520-MD-369695 and 5520-MD-369696. Dimensions in Figure 3.4.1 are in mm.

Figure 3.4.1: End Shimming on MQXB06.

3.5 Voltage Taps

Quench characterization voltage taps and spot heaters were not used on MQXB06, and are not used on any MQXB production magnets.  As in all production magnets, MQXB06 includes ¼ coil taps, ½ coil taps, and taps on the leads as they exit the magnet.

4.0 Coil Assembly

4.1 Coil Arrangement

Coils in LHCIR Quadrupole magnets are arranged to obtain the most uniform possible preload distribution between quadrants, given the coils available.  The coil arrangement is shown in Figure 4.1.1.  The amount of shim placed at each pole and parting plane is shown in red (positive numbers indicate kapton added, negative numbers indicate kapton removed). Red numbers are in inches (.001 in. = 25 um).  Shims may be added to (or removed from) the midplane and/or pole area to achieve the “target” azimuthal coil size and hence the desired preload.  See also section 3.4 and 4.3 for discussions of coil shimming.  The numbers in light blue in Figure 4.1.1 shown near each midplane (e.g., 310i, 229o, for Q1/2) show the “after arrangement and shimming” sizes of the inner and outer “octant pairs”, respectively, in microns.

The shim sizes shown in Figure 4.1.1 are “with respect to the original design”, that is, the positive and negative .001 inch (25um) shims shown at the inner coil pole and midplane respectively, represent the shim change for adjustment of harmonics described in section 4.3.

# Figure 4.1.1  MQXB06 Coil Arrangement

4.2 Splices

The pole turns of each inner/outer coil pair need to be spliced together. Splices are 114 mm long, slightly greater than the cable transposition pitch.  Areas to be spliced are preformed, and filled with solder before the coil is wound.  The filled, or “tinned” sections are then spliced after the coils are assembled on the mandrel.  The MQXB06 splices were made at 225 degrees C with 96% tin 4% silver solder using a Kester 135 flux.

All pole splices were insulated with two layers of Kapton tape, one layer of 25um thick  9.5 mm wide surrounded by one layer of 50um thick  9.5 mm wide. Both layers are spiral wrapped with 2 mm gaps.   The second layer is wrapped directly on top of the first layer, leaving uncovered bare cable in the 2mm gaps. Axial and radial cooling channels were made in the G11CR spacers, which surround the splice as well.

4.3 Ground Wrap System

The original design configuration for the coil ground wrap and insulation (used on MQXB01-3) is shown in Figure 4.3.1.  A complete description of the original ground wrap system, including body and ends, is shown in assembly drawing #5520-MC-369659, Rev. B.    All layers of kapton are .005 inch (125um) thick unless otherwise specified in the figure.

To improve harmonics, a series of minor changes were made to the system, beginning with MQXB04.  An explanation of the purpose of the ground insulation revision follows:

The prototype (P1), along with the first three production magnets (MQXB01-MQXB03), showed a significant change in the normal dodecapole with respect to the model magnets, measured at the collared coil stage.  Taking into account the systematic warm-cold shift seen in the model magnets and prototype, the dodecapole in these magnets is expected to be about ½ unit more negative at operating temperature than the value implied by the model magnets.  As a result, the inner coils of magnet MQXB04 were shimmed toward the midplane by 38 um, reducing the normal dodecapole.  This modification is shown in Figure 4.3.2.  Dotted lines show where ground insulation pieces were cut away and removed.  Dimensions are in inches (.001 in = 25um).

Warm measurements of MQXB04 showed the 38um shift to be slightly more than necessary, so inner coils on later magnets, beginning with MQXB05, are shimmed only 25um toward the midplane with respect to the original design.  This was done on MQXB05 and MQXB06 by a method similar to that done on MQXB04, as shown in figure 4.3.3.  Then, beginning with MQXB07, the shift was incorporated permanently into the design by ordering new parts (as shown in figure 4.3.3), so that modification of existing parts on the assembly floor was no longer necessary. (See MQXB07 and subsequent Fabrication Reports).

Quench protection heaters are placed radially between the outer coil and collar laminations.  The heaters have stainless steel elements,  .001 inch (25um) thick, .630 inches (16mm) wide, copper plated on one side.  The copper is etched away intermittently over 4.00 inch ( 101.6mm) lengths, exposing the stainless, with 4.00 inch (101.6mm) lengths of copper plated areas between them.  The stainless/copper element is sandwiched between (and bonded to) two pieces of .004 in. (100 micron) thick kapton. They are described in detail in drawing #5520-MB-369369.

Figure 4.3.1  Original (MQXB01-3) Body Coil and Ground Insulation System

Figure 4.3.2  Ground Insulation Systems of MQXB01-3 and modifications of MQXB04.

Figure 4.3.3  Ground Insulation System Modifications made on MQXB05, MQXB06 and subsequent magnets.

5.0 Collaring and Keying

5.1  Collaring

To ensure that the splices are aligned properly, the coils are assembled so that the back surface of the lead end keys of all four quadrants in both layers are coplanar.  The back surfaces of the outer coil keys on the lead end are then “cut to fit” to allow the back of all four quadrant keys to be coplanar.  On the non-lead end, the outer coil keys are cured into the coils.  Their back surface defines the coil length after springback (springback is defined in section 3.3.2).   The inner coil keys are cut to fit at assembly to make them coplanar (quadrant-to-quadrant variations in length created by differences in outer coil springback are small enough to ignore).

Collars are welded into packs, each 38mm long, with “large” and “small” alternating laminations, and shown in Figure 5.1.1.  The collared coil assembly does not include bearing strips.  Each collar pack is 25 laminations long, (~39 mm total length).  Packs are made with a “large” lamination on each end, creating a gap between each collar pack in each quadrant, where a “small” lamination is missing.  These gaps allow passage for heat flow.

Figure 5.1.1: Collar pack.

5.2 Keying

MQXB06 was keyed according to procedure #TD-02-010.  Collaring keys are 6 inches long.  Cylinder pressures were increased slightly from the procedure to fully seat the keys.  Steps (including press pressures used on MQXB06) are shown below. Passes are done in 6 inch increments, aligned with the keys, unless otherwise noted.

- Massage at 900 pump psi main cylinder pressure

- Massage at 1800 pump psi main cylinder pressure

- Partial key insertion with main cylinder pressure 3000 pump psi/key cylinder pressure 700 pump psi

- Full key insertion pass with main cylinder pressure increased to 4400 pump psi and key cylinder pressure increased to 2700 pump psi

- 2nd full key insertion pass with main cylinder pressure increased to 4700 pump psi and key cylinder pressure increased to 3300 pump psi

- 3rd full key insertion pass with main cylinder pressure increased to 5000 pump psi and key cylinder pressure increased to 3600 pump psi, done in 3 inch increments.

- 4th full key insertion pass with main cylinder pressure maintained at 5000 pump psi and key cylinder pressure increased to 4000 pump psi, done in 3 inch increments.

- Final pass straddling keys at 5000 pump psi main cylinder pressure and 4000 pump psi key cylinder pressure.

5.3 Mechanical measurements

The outside collar diameter measurement data for the collared coil assembly is shown in Figures 5.3.2-5.3.3.  The measurements are taken from the non-lead end to the lead end of the collared area (back of key to back of key as shown in Figure 5.3.1), approximately every 8 cm (three inches).   Diameters are displayed in the figures in mm.

Figure 5.3.1: Collared coil assembly without end clamps installed.

Figure 5.3.2: Collared coil deflections at pole region after keying.

Figure 5.3.3: Collared coil deflections at midplane region after keying.

The measurements show a mean radial deflection of 189 um at the midplane and 202 um at the pole. When adjusted for actual collar lamination sizes (the plots in Figures 5.3.2 and 5.3.3, above, do not reflect these adjustments), these deflections are similar to that of the last two short models, HGQ08 and HGQ09 and previous long magnets, as shown in Table 5.3.1 and Figure 5.3.4, indicating a similar preload.  (Measurements for MQXB04 are unavailable).

Table 5.3.1: Collared coil deflections of HGQ08-MQXB06.

Figure 5.3.4: Collared coil deflections of HGQ08-MQXB06.

There is an inconsistency concerning the collar deflection measurements on MQXB06.  Figure 5.3.5 shows the relationship between the mean coil size (average of mean size of all inner and outer coils within the respective magnet) and mean collar deflection measurements (average of pole and midplane) for magnets MQXB01-MQXB06.  This relationship is routinely monitored to cross check the accuracy of the two measurements.  For all magnets except MQXB06, this data is consistent, i.e., larger coil sizes yield larger collar deflections.  Magnet MQXB06, however, while having the largest mean coil size, has the smallest collar deflections.  Although the preload inferred from either the coil sizes (highest of all production magnets) or the collar deflections (lowest of all production magnets), is within the “acceptable” range, the inconsistencies between the two measurements are a concern.

Some attempts have been made to resolve the issue.  Coils produced within the same time period as the MQXB06 coils, as well as a “standard” used to calibrate the measuring machine, have been re-measured.  These measurements support the accuracy of the coil measurements.  Assembly travelers have been checked to ensure that all coil insulation, ground wrap, and shims were placed into the magnet as specified.  Component size measurements have been verified.  Warm harmonic measurements have been checked and have not identified any inconsistencies related to conductor position within the body of MQXB06.  End clamp deflection measurements (see section 6.2) indicate a preload consistent with that derived from the coil measurements. Unfortunately, since the magnet has been yoked, collar deflection measurements cannot be retaken.

Therefore, at this writing, although the issue has not been completely resolved, it is assumed that the coil size measurements are correct and that the collar deflection measurements are erroneous.

Figure 5.3.5: Mean Coil Size vs. Radial Collar Deflection

After keying is complete, the magnet body is measured longitudinally, and the center of the magnetic length is marked on the collar surface.  This mark will be transferred to the skin surface during the yoking process.

# 6.0 End Clamps

# 6.1 Installation Procedure:

The lead end clamp on MQXB06 is 250mm (9.842 inches) long and the non-lead end clamp is 132mm (5.197 inches) long.  G-11 filler cones were used. Longitudinal force required to close the “collet’ end clamps was 460 kN (103500 lbs.) on the lead end and 227 kN (51100 lbs.) on the non-lead end.

# 6.2 Measurements and Shimming:

The production cold mass design allows for extra radial ground insulation to be added around the outer coil ends, if needed, to adjust the end preload.  Based on measurements of short models and P1 (the full size prototype), the thickness of radial ground insulation surrounding the outer coil ends was increased by 75 microns (on the radius) at both ends from the original design, beginning with MQXB01 (see the P1 Fabrication report, TD-02-009, for more details), and continuing through MQXB04.  Beginning with MQXB05, the shim was removed due to concerns about the shorts in the transition area between the body and ends, and because an acceptable deflection was achieved without it. As in MQXB05, no shim was used on MQXB06.  The deflection of the diameter of the aluminum end cans according to micrometer measurements are shown below in Figure 6.2.1 (target diameter change from FEA, was 250 - 300 microns at the LE and 200-250 microns at the non-LE).

Figure 6.2.1: Aluminum End Can Radial Deflection (Diameter)

# 7.0 Yoke and Skinning

# 7.1 Assembly Configuration:

All yoke lamination packs were fusion welded longitudinally in 7 places (5 welds on outer surface and 2 welds on inner surface). 9 stainless steel laminations were welded to the lead end side of the straight section yoke, and 21 on the non-lead end. Stainless steel modified yoke laminations were used for both lead and non-lead ends to cover the end cans.   Figure 7.1.1 shows the design length and the layout of the yoke laminations during assembly.  Actual length between end cans was 5226mm, 5mm shorter than the design, primarily due to coil shrinkage after curing.  The actual total coil length is therefore also shorter than the design by a similar amount.

Figure 7.1.1: Yoke Assembly Configuration Before Welding

# 7.2 Welding:

The skin alignment key was 26.5 mm wide for MQXB06, as are all the long magnets. The 26.5-mm wide skin alignment key leaves a gap of 3mm (.12 in.) between the upper yoke and the upper skin; also a 3mm (.12 in.) gap between the lower yoke pack and skin alignment key. The total gap allowed for weld shrinkage is 6mm (.24 in.).

The magnet was compressed in the contact tooling with a hydraulic press pump pressure of 4MPa (600 PSI) during welding, corresponding to a force of about 23700 kg/meter (16000 lbs./ft) of magnet length. A pressure above 3.3MPa (500 PSI) must be applied to completely collapse the springs in the wheel units of the bottom tooling. First a fusion pass, then, consecutively, four filler passes were applied. After welding, the skin was cut to length, and the end plates were welded.

7.3 Outside Diameter Measurements:

Skin outside diameter measurements were taken at different angles after welding the end plates, at the angles shown in Figure 7.3.1.  Data and plots are shown in Table 7.3.1 and Figure 7.3.2 (values in mm).

Figure 7.3.1: Yoke Outside Diameter Measurement Positions

Table 7.3.1: MQXB06 yoke outer diameter according to micrometer measurements taken at different angular positions between skin alignment keys

Figure 7.3.2: Yoke Outer Diameter Measurements Plotted

7.4 Twist Measurements:

The twist in the cold-mass assembly after welding the skin and the end plates was measured on a granite table with a level and is shown in Figure 7.4.1. The twist was measured to be 0.080 milli-radians per meter in the straight section of the magnet (rms). The allowed twist for the MQXB Cold Mass is less than 0.2 milli-radians per meter.

Fig 7.4.1: MQXB06 Cold Mass Assembly Twist Measurements

# 7.5 Straightness Measurements

Straightness of the yoke in both the vertical and horizontal axis is taken by measuring the distance between the skin surface and a stretched wire.  Measurement positions are described in Figure 7.5.1 and shown for MQXB06 below in Table 7.5.1.  The wire is stretched across the length of the skin, touching on each end.  Measurements are taken from the wire to the skin.  Positive numbers, therefore, in Table 7.5.1 represent concavity on the surface noted.  A straight or convex condition will result in zero readings.

###### Figure 7.5.1: Straightness Measurement Positions

###### Table 7.5.1: Straightness Measurements

# 7.6 Axial Loading (Bullets & Bolts):

The axial support system of the magnet is shown below in Figure 7.6.1:

# Figure 7.6.1: Axial Support of the Cold Mass Assembly

End load is applied by hand tightening the bullets to the bullet preload plate, then tightening the axial preload bolts to the specified amount. As on all production magnets, strain gauges to read longitudinal load were not used on MQXB06.  Torque applied to bullets was established from strain gauge readings of short models and the prototype.   The complete bullet tightening procedure is explained in FNAL document # 5520-ES-369708, Bullet Torque Specification for LHCIR Quad MQXB Prototypes.  Each of the four bolts are tightened with a torque wrench, to 1200 inch-lbs.  With that torque, each bolt applies 35.6 kN (8,000-lbs.) tension load to the magnet. As a result of the loading of the magnet with bolts, the bullets are subjected to a compressive load of 8.9 kN (2,000 lbs.) each. The total force applied to the magnet is therefore 107 kN (24,000-lbs.) tension.

8.0 Final Assembly

# 8.1 Final Electrical Measurements

MQXB06 was hipotted coil to ground, heaters to ground and heaters to coil at 5000 V.  Coils were hipotted across midplanes at 3000V.  Leakage in all cases is required to be less than 3 μA. All tests were successful. Hipot leakage values are shown in Table 8.1.1.  In Table 8.1.1, coil to ground and quench protection heater (strip heater) to ground measurements were taken after magnet was completed.  The quadrant-to-quadrant (midplane) measurements were taken slightly earlier, before the quadrant splices were made, because this hipot cannot be made after the quadrants are spliced together.

| Hipot | Result |
| --- | --- |
| Coil to Ground | 192nA at 5000V |
| Strip heaters to Coil & Ground | 140nA at 5000V |
| Coils Q1 to Coils Q2 across midplane | 412nA at 3000V |
| Coils Q2 to Coils Q3 across midplane | 73nA at 3000V |
| Coils Q3 to Coils Q4 across midplane | 179nA at 3000V |
| Coils Q4 to Coils Q1 across midplane | 355nA at 3000V |

# Table  8.1.1.   Cold Mass Hipotting Data

Final electrical data is shown in Table 8.1.2.

|  | Resistance ohms | Ls mH | Q |
| --- | --- | --- | --- |
| Q1 – Quadrant total | 0.5715 | 3.3713 | 4.90 |
| Q2 – Quadrant total | 0.5719 | 3.3552 | 5.03 |
| Q3 – Quadrant total | 0.5756 | 3.3563 | 4.73 |
| Q4 – Quadrant total | 0.5729 | 3.3115 | 5.07 |
|  | Resistance ohms | Ls mH | Q |
| Magnet Total | 2.293 | 13.2834 | 5.15 |

Table 8.1.2: Magnet Resistance, L and Q measurements.

Heater resistances are shown in Table 8.1.3:

| Strip Heater | Resistance ohm |
| --- | --- |
| Circuit A | 19.97 |
| Circuit B | 20.19 |

Table 8.1.3: Quench Protection (Strip) Heater resistance measurements

# 8.2 Mechanical Measurements

Design and actual finished longitudinal dimensions of the MQXB06 cold mass are shown in Figures 8.2.1 and 8.2.2.  Figure 8.2.2 shows the longitudinal position of the magnetic center, from the measurements described at the end of Section 5.3.

Figure 8.2.1:  Design Dimensions of MQXB06

Figure 8.2.2:  As-built Measured Dimensions of MQXB06

9.0 Discrepancies and Comments

Through MQXB05, a specific hipot failure (coil-to-ground, outer coil pole turn to collar laminations, where the collars end and the end clamps begin) occurred many times.  (See section 9 of the P1, MQXB01 and MQXB02, MQXB04 and MQXB05 Fabrication Reports).  The root cause of the problem, not discovered until the fabrication of MQXB05, was that solder had, during the cable splice perform tinning process, flowed or “wicked” into the area that is eventually covered by collar laminations, causing this area to short to the laminations.  A detailed explanation of the problem and solution can be found in section 9.0 of the MQXB05 Fabrication Report.

This solution (shortening the amount of tinned area), although acceptable for magnets beginning with MQXB07, did not work for MQXB05 or MQXB06, because the problem was not discovered after the coils for these magnets were already fabricated. An alternate solution was needed.  Therefore, for MQXB05 and MQXB06 only, the collar lamination pack in the area of failure was relieved on all four lead end quadrants.  The area at the end of the pack, where the lead enters, is relieved by about 1mm, tapering down to zero at about 1 cm into the pack. With the packs relieved, the magnets passed hipot.

An inconsistency exists between the collar deflection measurements and the coil size measurements of MQXB06.  A detailed explanation can be found in Section 5.3 of this report.

Whenever an anomalous situation occurs during the construction of a magnet, a discrepancy report is filed.  All discrepancy reports filed during the construction of the MQXB06 cold mass are listed in Table 9.0.1.  Complete reports, with their dispositions and corrective actions, can be obtained from the FNAL Technical Division Process Engineering Department.

| DRNo | Component SN | Discrepancy Description |
| --- | --- | --- |
| HGQ-0346 | MQXBi-044 | Coil measurement data unreadable after position 32 during the original sizing operation. Coil needs to be re-measured. |
| HGQ-0348 | MQXBC-006 | Non-Lead End of ground wrap layer #2 (MC-369624) on quadrant #2 was cut incorrectly during installation. Layer was cut to recess into non-lead end key, but the first flaps were not left to cover midplane area of coils. |
| HGQ-0350 | MQXB06 | The Collared Coil will not fit into the Bottom Yoke Packs. Yoke packs 363588 & 369828 are too long. 363588 is 3 lams larger than tolerance and 369828 is 2-3 lams larger than tolerance. |
| HGQ-0357 | MQXB06 | Lead End preload plate has to be modified so heater wires won't be pinched. |

Table 9.0.1  MQXB06 Discrepancy Reports