HF SiO2 Chemistry

Classically

4 HF + SiO2 ( SiF4 + H2O

This is stoichiometry not mechanism or kinetics.

With excess aqueous HF

6 HF + SiO2 ( H2SiF6

These are macroscopic descriptions suitable for defining endpoints.

To describe the kinetic rate behavior we need microscopic detail.

The detail level must include the mechanistic detail.

The order of the reaction will be dependant upon the rate limiting reaction and the number of reactants in this step.

The rate law will also include all of the side reactions, reverse reactions, and alternate reaction paths.

Known reaction properties.

- In the complete absence of water

HF + SiO2 ( No Reaction

- HF Oligomerizes

HF ( H2F2 ( H3F3 ( H4F4

- HF + SiC ( No Reaction

- Addition of strong acid (HCl, HNO3) accelerates HF + SiO2 reaction.

Equilibrium Review

- Equilibria are dynamic and activity based.

- Equilibria are based on population statistics, infinite time and Maxwell-Boltzman energy distribution assumptions, requiring large numbers of individual molecules.

- First year Chemistry assumes concentration (moles/L)= activity, reality is much more complex.

- Vapor pressure = ( * P0 (assuming equilibrium)

Pwater( 10-12 atm, Po ( 10-2 atm 				( (water = 10-10

This drastically affects the behavior of reactions involving water.

Known Steps in HF/ SiO2 Reaction

- The silica lattice must be severed by acid, neutral or base hydrolysis.

- Stepwise Substitution of F- for O-R- either concurrent with hydrolysis or subsequent of hydrolysis.

- Silica subtypes

Silicic Acid ( SiO2 I ( SiO2 II ( SiO2 III ( SiO2 IV

K1		     K2		K3

Assuming each type is in equilibrium ( a bad assumption due to dynamic time dependant system)

aSiO2 I  = ( K1K2K3*aSiO2 IV* aH2O3)1/2

aSiO2 II  = ( K2K3*aSiO2 IV* aH2O2)1/2

aSiO2 III  = (K3*aSiO2 IV* aH2O)1/2

Silica/ HF Reaction Kinetics

|  | Silicic Acid | SiO2 Type I | SiO2 Type II | SiO2 Type III | SiO2 Type IV |
| --- | --- | --- | --- | --- | --- |
| HF | Kr0 | Kr1 | Kr2 | Kr3 | Kr4 |
| HF2- | Kr5 | Kr6 | Kr6 | Kr7 | Kr8 |
| H2F2 | Kr8 | Kr9 | Kr10 | Kr11 | Kr12 |
| H2F3- | Kr13 | Kr14 | Kr15 | Kr16 | Kr17 |
| H3F3 | Kr18 | Kr19 | Kr20 | Kr21 | Kr22 |
| H3F3 (cyclic) | Kr23 | Kr24 | Kr25 | Kr26 | Kr27 |
| H3F4- | Kr28 | Kr29 | Kr30 | Kr31 | Kr32 |
| H4F4 | Kr33 | Kr34 | Kr36 | Kr37 | Kr38 |
| H2SiF6 | Kr39 | Kr40 | Kr41 | Kr42 | Kr43 |
| HsiF6- | Kr44 | KR45 | Kr46 | Kr47 | Kr48 |
| H2O | Kr49 | Kr50 | Kr51 | Kr52 | Kr53 |

These reaction rate constants only represent only the forward reactions, and assume only one reaction path.

To define the reaction rate, one must also consider the reverse reactions, and the alternate paths.

This requires knowledge of each species activity and the ability to discriminate between the reaction pathways.

Each pathway will have its own activation energy and kinetics.

Cable Insults:

Limited insult with Tesla coil, 0.27 femtomoles detected

Tesla coil assault generated active fluorine, assault at 0.5 m from instrument inlet.

Conclusions:

- HF chemistry is complex

- Silica and Germanium chemistry are not well defined.

- We are not at equilibrium.

- Many reaction pathways exist.

- All required reactants are present.

- The carbonaceous coating localizes the reactions.

- Mechanically generated ESD makes breaches in the coating and HF (assisted by C Coating).

- Uncoated Fiber is highly resistant to ESD.

- Ab initio rate modeling is not feasible.

- HF is the bad actor

- Pyrolytic carbon enhances the rate of reaction.

- The reaction is HF limited

- The absence of C coating will stabilize fiber life by spreading out the reaction.

- We are at or beyond the statistical predictive limits of chemistry.

- We can make measurements and observations and then make estimations ( with reservations.)