MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A17695 | In-Flight Anomaly Number -- | Contractor Report Number S-087 | JSC# -- | KSC# -- |  |
| --- | --- | --- | --- | --- | --- |
| Problem Title ET-117 LH2 TANK POST PROOF INSPECTION |  |  |  |  |  |
| EICN# -- | ELEMENT ET | Contractor LOCKHEED MARTIN | FSCM# -- | FCRIT 3 |  |
| HCRIT 1 | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |  |  |  |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |  |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |  |
| HARDWARE NCA | NOMENCLATURE LH2 TANK POST PROOF | PART# 80914004000-519 | SER/LOT# 1131190 | MANUFACTURER MAF |  |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode MS - STRUCT | Cause MW - MFG-WORK |  |
| System PRESSURE VES | Defect DC - BROKEN | Material S - STRUCT | Work Contact W.MATHEESSEN | Fail Date 06/08/2001 |  |
| Received at MSFC 06/11/2001 | Date Isolated 06/08/2001 | FMEA Reference -- | IFA: Mission Phase -- | Mission Elapsed Time -- |  |
| Location MAF |  | Symptom MS - STRUCT |  | Time Cycle -- |  |
| Effectivity Text -- |  |  |  |  |  |
| Vehicle Effectivity Codes |  |  |  |  |  |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |  |
| Mission Effectivity Codes |  |  |  |  |  |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |  |
| Estimated Completion Dates |  |  |  |  |  |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |  |  |
| Investigation / Resolution Summary |  |  |  |  |  |
| Last MSFC Update 02/01/2002 | CN RSLV SBMT -- | Defer Date -- | Add Date 06/12/2001 | R/C Codes 2 - MFG 4 - TEST -- |  |
| Assignee |  |  |  |  |  |
| Design M. BUTLER | Chief Engineer N. OTTE | S & MA K. LAYNE | Project -- | Project MGR J. SMELSER |  |
| Approval |  |  |  |  |  |
| Design M. BUTLER | Chief Engineer N. OTTE | S & MA K. LAYNE | Project -- | Project MGR J. SMELSER |  |
| PAC Assignee T. WHITE | PAC Review Complete TW | MSFC Closure Date 01/31/2002 | Status C - CLOSED | F/A Completion -- |  |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |  |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- |  | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |  |  |  |  |
| Related Document Type -- | Related Document ID N055015 |  |  |  |  |
| Related Document Title NCD |  |  |  |  |  |
| Related Document Type -- | Related Document ID -- |  |  |  |  |
| Related Document Title -- |  |  |  |  |  |
| Related Document Type -- | Related Document ID -- |  |  |  |  |
| Related Document Title -- |  |  |  |  |  |
| Contractor Status Summary |  |  |  |  |  |
| Reliability/Quality Assurance Concerns, Recommendations: |  |  |  |  |  |
| Problem Description DURING POST PROOF INSPECTION OF THE LH2 TANK FOR ET-117, TWO CRACKS WERE FOUND ON RIBS C-35 & C-37 (BARREL #3) NEXT TO THE S-12 STRINGER ON THE ISL. A HELIUM LEAK CHECK WAS PERFORMED ON JUNE 8, 2001, AND A LEAK CONDITION WAS IDENTIFIED. FURTHER EVALUATION OF THE HELIUM LEAK CHECK, DETERMINED THAT THE LEAK INDICATION FOR C35 WAS 0.3 X 10^-7 ATM-CC/SEC AND FOR C37 WAS 1.1 X 10^-6 ATM-CC/SEC. WHEN THE TANK WAS LEAK CHECKED WITH NITROGEN IN BLDG. 451 AT 6 PSI NO LEAK WAS DETECTED. |  |  |  |  |  |
| Contractor Investigation/Resolution 06/11/2001 - CONTRACTOR SUBMITTED PROBLEM REPORT OPENER AS FOLLOWS: GENERAL: DURING PERFORMANCE OF THE ET-117 LH2 TANK POST PROOF SHAKEDOWN INSPECTION, TWO CRACKS WERE VISUALLY IDENTIFIED ON RIBS C-35 & C-37 NEXT TO THE S-12 STRINGER ON THE ISL. THE CRACKS ARE LOCATED WHERE THE RIBS TRANSITION INTO THE WELD LAND AND THE THROUGH THE "DUTTON" GROOVE. THIS IS NEXT TO THE HB3-8 WELD AT STATION 1377, ON BARREL # 3. SUBSEQUENT INVESTIGATION HAS SHOWN THAT THE CRACK ON C-37 WAS VISIBLE ON THE OSL. HOWEVER, THERE WAS NO EVIDENCE ON THE OSL OF AN IMPACT THAT COULD HAVE CAUSED THE DAMAGE. C-35 (#1) C-37 (#2) --------- --------- X-RAY LENGTH 1.025" 1.225" UT REMAINING LIGAMENT 0.100" 0.0 -VISUAL THRU WALL VISUAL - NCD LENGTH 1.000" 1.100" VISUAL - NCD WIDTH 0.125" 0.125" THE CRACK ON C-37 APPEARS TO RUN FROM THE ISL TO THE OSL LEAVING A DIMPLE AND CRACK ON THE OSL. PANEL ID #'S ------------ DESCRIPTION/STATE PART # SERIAL # TRIM LOG 809114400940M509 OP1 1042590 DELIVERED PART (FORMED) 809114400930-502 0000024 MACHINED 809114400920-502 0000023 INITIAL INVESTIGATION HAS SHOWN THAT THE RIBS & STRINGERS ARE THE PROPER THICKNESS. IN ADDITION, THE WEB THICKNESS WAS MEASURED AND MEETS ENGINEERING REQUIREMENTS. TASK I FAILURE/PROBLEM INVESTIGATION A. DEVELOP AND CLOSE FAULT TREE. RESPONSIBILITY: MATERIALS TASK LEAD D. BOLSTAD / D4600 - P. HINKELDEY / D4600 DESIGN TASK LEAD J. PILET / D4130 - F. MANTO / D4100 OVERLOAD / FABRICATION TASK LEAD M. QUIGGLE / D3000 ECD: 6/25/01 B. PERFORM FAILURE ANALYSIS AT THE REQUEST OF FAULT TREE TEAM. RESPONSIBILITY: D. BOLSTAD/D4600 - P. HINKELDEY / D4600 W. MATTHEESSEN/D3741 - D. WESTPHAL/D3740 ECD: 6/25/01 C. DEVELOP FLEET CLEARANCE RATIONAL INDEPENDENT OF FAULT TREE INVESTIGATION. RESPONSIBILITY: T. MCKEOUGH/D3741 - D. WESTPHAL / D3740 ECD: 6/25/01 C.1 PERFORM AN INSPECTION OF RIBS AND STRINGERS TO DETERMINE IF ANY OTHER CRACKS OR DAMAGE EXISTS (ET-118 THRU 122). RESPONSIBILITY: J. SPRAY / D3724 - D. OWENS / D3720 ECD: 6/25/01 C.2 REVIEW NCDS & SAFETY INCIDENT REPORTS FOR ET-117 LH2 TANK TO DETERMINE IF ANY INCIDENT OCCURRED. RESPONSIBILITY: T. MCKEOUGH / D3741 - D. WESTPHAL/D3740 ECD: 6/18/01 C.3 REVIEW NCD HISTORY FOR PREVIOUS OCCURRENCES OF CRACKS. RESPONSIBILITY: J. VARRIELLO/D3741 - D. WESTPHAL/D3740 ECD: 6/18/01 C.4 DEVELOP AN INSPECTION METHOD FOR BUILT TANKS. RESPONSIBILITY: T. MCKEOUGH / D3741 & S. MCEVOY / 3742 D. WESTPHAL / D3740 ECD: 6/25/01 C.5 REVIEW BUILD PAPER AND INTERVIEW INSPECTORS AND PRACTITIONERS TO DETERMINE NUMBER AND TYPE OF INSPECTIONS. RESPONSIBILITY: T. MCKEOUGH / D3741 - D. WESTPHAL/D3740 ECD: 6/18/01 CAUSE ------ UNDER INVESTIGATION TASK II CORRECTIVE ACTION PENDING RESULTS OF INVESTIGATIONS. TASK III CLEARANCE OF EFFECTIVITIES IN WORK, SEE TASKS I.A & I.B. TASK IV CAPS CLOSURE SUMMARY PENDING COMPLETION OF ALL TASKS. 06/29/2001 - CONTRACTOR SUBMITTED UPDATE PLAN-OF-ACTION FOR CLOSURE REQUEST AS FOLLOWS: PROBLEM -------- *DURING POST PROOF INSPECTION OF THE LH2 TANK FOR ET-117, TWO CRACKS WERE FOUND ON RIBS C-35 & C-37 (BARREL #3) NEXT TO THE S-12 STRINGER ON THE ISL. A HELIUM LEAK CHECK WAS PERFORMED ON JUNE 8, 2001, AND A LEAK CONDITION WAS IDENTIFIED. FURTHER EVALUATION OF THE HELIUM LEAK CHECK, DETERMINED THAT THE INDICATION WAS BACKGROUND LEVEL. WHEN THE TANK WAS LEAK CHECKED WITH NITROGEN IN BLDG. 451 AT 6 PSI NO LEAK WAS DETECTED. CRITICALITY: ------------ *CRITICALITY 3 UPDATED PROBLEM, ALL TASKS IN TASK I & CLOSED TASK III. * - DENOTES CHANGES FROM LAST REVISION. GENERAL: -------- DURING PERFORMANCE OF THE ET-117 LH2 TANK POST PROOF SHAKEDOWN INSPECTION, TWO CRACKS WERE VISUALLY IDENTIFIED ON RIBS C-35 & C-37 NEXT TO THE S-12 STRINGER ON THE ISL. THE CRACKS ARE LOCATED WHERE THE RIBS TRANSITION INTO THE WELD LAND AND THROUGH THE "DUTTON" GROOVE. THIS IS NEXT TO THE HB3-8 WELD AT STATION 1377, ON BARREL # 3. SUBSEQUENT INVESTIGATION HAS SHOWN THAT THE CRACK ON C-37 HAS WITNESS MARKS ON THE OSL. CRACK ID -------- C-35 (#1) C-37 (#2) --------- --------- X-RAY LENGTH 1.025" 1.225" UT REMAINING LIGAMENT 0.100" 0.0 -VISUAL THRU WALL VISUAL - NCD LENGTH 1.000" 1.100" VISUAL - NCD WIDTH 0.125" 0.125" THE CRACK ON C-37 APPEARS TO RUN FROM THE ISL TO THE OSL LEAVING A DIMPLE AND CRACK ON THE OSL. PANEL ID #'S -------------- DESCRIPTION/STATE PART # SERIAL # TRIM LOG 809114400940M509 OP1 1042590 DELIVERED PART (FORMED) 809114400930-502 0000024 MACHINED 809114400920-502 0000023 INITIAL INVESTIGATION HAS SHOWN THAT THE RIBS & STRINGERS ARE THE PROPER THICKNESS. IN ADDITION, THE WEB THICKNESS WAS MEASURED AND MEETS ENGINEERING REQUIREMENTS. TASK I FAILURE/PROBLEM INVESTIGATION A. DEVELOP AND CLOSE FAULT TREE. RESPONSIBILITY: MATERIALS TASK LEAD D. BOLSTAD / D4600 - P. HINKELDEY / D4600 DESIGN TASK LEAD J. PILET / D4130 - F. MANTO / D4100 OVERLOAD / FABRICATION TASK LEAD M. QUIGGLE / D3000 ECD: 6/25/01 * EXTENSION: 7/20/01 - FORMAL CLOSURE OF ALL ITEMS * STATUS: ------- NO ISSUES WERE FOUND WITH THE MATERIAL OR DESIGN OF THE PANEL. HOWEVER, THE OVERLOAD - FABRICATION LEG OF THE FAULT TREE SHOWS DAMAGE OCCURRING AT MAF AS A POSSIBLE AREA OF CONCERN. CLOSURE OF ALL ITEMS IS IN WORK. B. PERFORM FAILURE ANALYSIS AT THE REQUEST OF FAULT TREE TEAM. RESPONSIBILITY: D. BOLSTAD / D4600 - P. HINKELDEY/ D4600 W. MATTHEESSEN / D3741 - D.WESTPHAL/D3740 ECD: 6/25/01 * EXTENSION: 7/20/01 - FORMAL CLOSURE OF ALL ITEMS * STATUS: ------- MATERIAL MEETS ENGINEERING REQUIREMENTS. FRACTURE SURFACES ARE CONSISTENT WITH A TENSILE OVER-LOAD SCENARIO. NO ANOMALIES WERE NOTED DURING THE ANALYSIS. C. DEVELOP FLEET CLEARANCE RATIONAL INDEPENDENT OF FAULT TREE INVESTIGATION. RESPONSIBILITY:T. MCKEOUGH / D3741 - D. WESTPHAL / D3740 ECD: 6/25/01 * COMPLETE: 6/25/01 * CLOSURE STATEMENT: ------------------- SEE TASK III. C.1 PERFORM AN INSPECTION OF RIBS AND STRINGERS TO DETERMINE IF ANY OTHER CRACKS OR DAMAGE EXISTS (ET-117 THRU 122). RESPONSIBILITY: J. SPRAY / D3724 - D. OWENS / D3720 ECD: 6/25/01 * EXTENSION: 8/14/01 - COMPLETION OF ET-122 BARREL #4 * STATUS: ------- NO DISCREPANCIES WERE NOTED. ET-117 THRU 120 COMPLETE. BARRELS 1, 2, AND 3 FOR ET-121 AND BARRELS 1 AND 2 FOR ET-122 ARE COMPLETE. C.2 REVIEW NCDS & SAFETY INCIDENT REPORTS FOR ET-117 LH2 TANK TO DETERMINE IF ANY INCIDENT OCCURRED. RESPONSIBILITY: T. MCKEOUGH / D3741 - D. WESTPHAL / D3740 ECD: 6/18/01 * EXTENSION: 7/20/01 - FORMAL CLOSURE OF ALL ITEMS * STATUS: ------ REVIEW SHOWED NO INCIDENCES IN THE AREA OF INTEREST ON ET-117 LH2 TANK. C.3 REVIEW NCD HISTORY FOR PREVIOUS OCCURRENCES OF CRACKS. RESPONSIBILITY: J. VARRIELLO / D3741 - D. WESTPHAL / D3740 ECD: 6/18/01 * COMPLETE: 6/18/01 * CLOSURE STATEMENT: ------------------ REVIEW WAS PERFORMED AND ALL PREVIOUS NON-CONFORMANCES WERE MAPPED AND PROVIDED TO THE FAULT TREE BLOCK LEADS C.4 DEVELOP AN INSPECTION METHOD FOR BUILT TANKS. RESPONSIBILITY: T. MCKEOUGH / D3741 & S. MCEVOY / 3742 D. WESTPHAL / D3740 ECD: 6/25/01 * COMPLETE: 7/27/01 FORMAL CLOSURE IN PROCESS * STATUS: ------- SEVERAL INSPECTION METHODS WERE EVALUATED. THE MOST EFFICIENT VISUAL METHOD WAS A HORIZONTAL INSPECTION WITH TANK ENTRY USING A SPOTTING SCOPE AS NECESSARY. A VERTICAL VISUAL INSPECTION FROM THE 2058 FRAME USING THE SAME SPOTTER SCOPE PRODUCED ACCEPTABLE RESULTS, HOWEVER ONE RIB ABOVE EACH "T" RING WAS BLOCKED FROM VIEW. AN INSPECTION PERFORMED FROM THE FWD END OF THE LH2 TANK WITH OUT MAKING A TANK ENTRY, PROVIDED VISUAL ACCESSIBILITY TO THE RIBS THAT COULD NOT BE INSPECTED FROM THE AFT END. THROUGH THE TANK, (DUAL WALL) X-RAY INSPECTION WAS DEVELOPED AND COULD DETECT A CRACK OF THE TYPE SEEN ON ET-117 LH2 TANK. C.5 REVIEW BUILD PAPER AND INTERVIEW INSPECTORS AND PRACTITIONERS TO DETERMINE NUMBER AND TYPE OF INSPECTIONS. RESPONSIBILITY: T. MCKEOUGH / D3741 - D. WESTPHAL / D3740 ECD: 6/18/01 * COMPLETE: 6/18/01 * CLOSURE STATEMENT: ----------------- NUMBER AND TYPE OF INSPECTIONS WERE IDENTIFIED AND ADDED TO THE ET-117 LH2 TANK PRODUCTION FAULT TREE FLOW CHART. INTERVIEWS WITH PRACTITIONERS WERE PERFORMED TO DETERMINE EFFECTIVENESS OF POST PROOF INSPECTIONS. IT WAS A CONSENSUS AMONG THE PRACTITIONERS THAT THE CLEANING/INSPECTION WOULD DETECT THIS TYPE OF DEFECT. THIS STEP IN THE PROCESS IS PERFORMED BY THREE DIFFERENT ORGANIZATIONS (PRODUCTION PRACTITIONER, QUALITY CONTROL INSPECTOR AND A MEMBER OF DCMA). CAUSE * INADVERTENT DAMAGE TO BARREL SECTION DURING MAF FABRICATION. TASK II CORRECTIVE ACTION ----------------- PENDING RESULTS OF INVESTIGATIONS. TASK III CLEARANCE OF EFFECTIVITIES -------------------------- * FLIGHT RATIONALE: O FAULT TREE TEAM AND SENIOR REVIEW BOARD CONCLUDED THAT THIS WAS AN ISOLATED EVENT AND NOT THE RESULT OF A SYSTEMIC PROBLEM. - ET DESIGN AND MATERIALS WERE EXONERATED AS CONTRIBUTORS TO THE ET-117 ANOMALY. - RIGOROUS REVIEW OF THE PROCESS INSTRUCTIONS FOR POST PROOF PROCESSING FOUND NO INADEQUACIES. - FAULT TREE AND FRACTURE FACE ANALYSIS CONCLUDED THAT THE ET-117 DAMAGE EVENT OCCURRED DURING PROCESSING, PRIOR TO PROOF TEST. - CRACKS COULD HAVE OCCURRED DURING THE DAMAGE EVENT OR DURING THE PROOF TEST DUE TO RESIDUAL STRESS FROM THE DAMAGE EVENT. - FIRST OF THREE PLANNED POST-PROOF CLEANING AND INSPECTION STEPS IDENTIFIED CRACKS. - INVESTIGATION VALIDATED PROOF TEST AND POST PROOF INSPECTIONS FOR CERTIFICATION OF TANKS. TASK IV CAPS CLOSURE SUMMARY -------------------- PENDING COMPLETION OF ALL TASKS. 11/27/2001 - CONTRACTOR SUBMITTED FULL CLOSURE AS FOLLOWS: PROBLEM -------- DURING POST PROOF INSPECTION OF THE LH2 TANK FOR ET-117, TWO CRACKS WERE FOUND ON RIBS C-35 & C-37 (BARREL #3) NEXT TO THE S-12 STRINGER ON THE ISL. A HELIUM LEAK CHECK WAS PERFORMED ON JUNE 8, 2001, AND A LEAK CONDITION WAS IDENTIFIED. FURTHER EVALUATION OF THE HELIUM LEAK CHECK, DETERMINED THAT THE INDICATION WAS BACKGROUND LEVEL. WHEN THE TANK WAS LEAK CHECKED WITH NITROGEN IN BLDG. 451 AT 6 PSI NO LEAK WAS DETECTED. GENERAL: -------- DURING PERFORMANCE OF THE ET-117 LH2 TANK POST PROOF SHAKEDOWN INSPECTION, TWO CRACKS WERE VISUALLY IDENTIFIED ON RIBS C-35 & C-37 NEXT TO THE S-12 STRINGER ON THE ISL. THE CRACKS ARE LOCATED WHERE THE RIBS TRANSITION INTO THE WELD LAND AND THROUGH THE "DUTTON" GROOVE. THIS IS NEXT TO THE HB3-8 WELD AT STATION 1377, ON BARREL # 3. SUBSEQUENT INVESTIGATION HAS SHOWN THAT THE CRACK ON C-37 HAS WITNESS MARKS ON THE OSL. CRACK ID -------- C-35 (#1) C-37 (#2) --------- --------- X-RAY LENGTH 1.025" 1.225" UT REMAINING LIGAMENT 0.100" 0.0 - VISUAL THRU WALL VISUAL - NCD LENGTH 1.000" 1.100" VISUAL - NCD WIDTH 0.125" 0.125" THE CRACK ON C-37 APPEARS TO RUN FROM THE ISL TO THE OSL LEAVING A DIMPLE AND CRACK ON THE OSL. PANEL ID #'S ------------- DESCRIPTION/STATE PART # SERIAL # ----------------- -------------------- --------- TRIM LOG 809114400940M509 OP1 1042590 DELIVERED PART (FORMED) 809114400930-502 0000024 MACHINED 809114400920-502 0000023 INITIAL INVESTIGATION HAS SHOWN THAT THE RIBS & STRINGERS ARE THE PROPER THICKNESS. IN ADDITION, THE WEB THICKNESS WAS MEASURED AND MEETS ENGINEERING REQUIREMENTS. TASK I FAILURE/PROBLEM INVESTIGATION ----------------------------- * A. DEVELOP AND CLOSE FAULT TREE. RESPONSIBILITY: MATERIALS TASK LEAD D. BOLSTAD/D4600 - P. HINKELDEY/D4600 DESIGN TASK LEAD J. PILET/D4130 - F. MANTO/D4100 OVERLOAD / FABRICATION TASK LEAD M. QUIGGLE / D3000 ECD: 6/25/01 EXTENSION: 7/20/01 - FORMAL CLOSURE OF ALL ITEMS EXTENSION: 11/2/01 - FORMAL CLOSURE OF ALL ITEMS COMPLETE: 10/31/01 * CLOSURE STATEMENT: ------------------ NO ISSUES WERE FOUND WITH THE MATERIAL OR DESIGN OF THE PANEL. HOWEVER, THE OVERLOAD - FABRICATION LEG OF THE FAULT TREE SHOWS DAMAGE OCCURRING AT MAF AS A POSSIBLE AREA OF CONCERN. THREE POSSIBLE ITEMS WERE NOTED: 1. IMPROPER CLAMPING OF PANEL IN LONGITUDINAL BARREL WELD FIXTURE (5016 TOOL) 2. INADVERTENT OBJECT OBSTRUCTION DURING TANK ROTATION IN MAJOR WELD TOOLS. 3. INADVERTENT, UNREPORTED IMPACT TESTING WAS CONDUCTED IN THE 5016 TOOL TO DETERMINE IF DEBRIS OR OTHER CONDITIONS COULD GENERATE CRACKS IN TAPERED RIBS AND IT WAS DETERMINED THAT THIS COULD OCCUR. IN ADDITION THE TESTING DETERMINED THAT THE FOLLOWING: 1. DESIGN HAS THE REQUIRED PROOF TEST CAPABILITY & TEMPERATURE CORRECTED FLIGHT CAPABILITY. 2. RESIDUAL STRESSES FROM FORMING WHEN COMBINED WITH PROOF TEST STRESSES WILL NOT CAUSE FAILURE. REF. FAULT TREE (CLOSED COPY) & THE PRESENTATION DATED 10/24/01 B. PERFORM FAILURE ANALYSIS AT THE REQUEST OF FAULT TREE TEAM. RESPONSIBILITY: D. BOLSTAD / D4600 - P. HINKELDEY / D4600 W. MATTHEESSEN / D3741 - D. WESTPHAL/D3740 ECD: 6/25/01 EXTENSION: 7/20/01 - FORMAL CLOSURE OF ALL ITEMS * EXTENSION: 11/31/01 - FORMAL CLOSURE OF ALL ITEMS * COMPLETE: 11/14/01 * CLOSURE STATEMENT: ----------------- MATERIAL MEETS ENGINEERING REQUIREMENTS. FRACTURE SURFACES ARE CONSISTENT WITH A TENSILE OVER-LOAD SCENARIO. NO ANOMALIES WERE NOTED DURING THE ANALYSIS. FAILURE MODE WAS DUPLICATED USING 3 & 4 POINT BENDING ON PANELS. BASED ON ANALYSIS OF FRACTURE SURFACES, FRACTURE OCCURRED AFTER ALL PROCESSING AT THE SUPPLIERS. REF: ETTR-MS-01-026 MATERIAL FAILURE ANALYSIS FOR ET-117 LH2 CRACK RIB FAULT TREE, NOVEMBER 9, 2001. C. DEVELOP FLEET CLEARANCE RATIONAL INDEPENDENT OF FAULT TREE INVESTIGATION. RESPONSIBILITY: T. MCKEOUGH / D3741 - D. WESTPHAL/D3740 ECD: 6/25/01 COMPLETE: 6/25/01 CLOSURE STATEMENT: ------------------ SEE TASK III. C.1 PERFORM AN INSPECTION OF RIBS AND STRINGERS TO DETERMINE IF ANY OTHER CRACKS OR DAMAGE EXISTS (ET-117 THRU 122). RESPONSIBILITY: J. SPRAY / D3724 D. OWENS / D3720 ECD: 6/25/01 EXTENSION: 8/14/01 - COMPLETION OF ET-122 BARREL #4 EXTENSION: 11/2/01 - FORMAL CLOSURE OF ALL ITEMS COMPLETE: 10/31/01 CLOSURE STATEMENT: ------------------ NO ADDITIONAL CRACKS ON ET-117 WERE NOTED. ET-118 THRU 122 WERE ALSO INSPECTED AND NO CRACKED STRINGERS WERE DOCUMENTED. REF.: J. SPRAY DATED 8/29/2001. * C.2 REVIEW NCDS & SAFETY INCIDENT REPORTS FOR ET-117 LH2 TANK TO DETERMINE IF ANY INCIDENT OCCURRED. RESPONSIBILITY: T. MCKEOUGH/D3741 - D. WESTPHAL/D3740 ECD: 6/18/01 EXTENSION: 7/20/01 - FORMAL CLOSURE OF ALL ITEMS EXTENSION: 11/2/01 - FORMAL CLOSURE OF ALL ITEMS COMPLETE: 10/31/01 CLOSURE STATEMENT: ------------------ REVIEW SHOWED NO INCIDENCES IN THE AREA OF INTEREST ON ET-117 LH2 TANK. DATA WAS INCORPORATED INTO THE FAULT TREE. * C.3 REVIEW NCD HISTORY FOR PREVIOUS OCCURRENCES OF CRACKS OR CRACK LIKE INDICATIONS. RESPONSIBILITY: J. VARRIELLO / D3741 - D. WESTPHAL/D3740 ECD: 6/18/01 COMPLETE: 6/18/01 CLOSURE STATEMENT: ------------------ REVIEW WAS PERFORMED AND ALL PREVIOUS NON-CONFORMANCES WERE MAPPED AND PROVIDED TO THE FAULT TREE BLOCK LEADS. * C.4 DEVELOP AN INSPECTION METHOD FOR BUILT TANKS. RESPONSIBILITY: T. MCKEOUGH / D3741 & S. MCEVOY / 3742 D. WESTPHAL / D3740 ECD: 6/25/01 COMPLETE: 7/27/01 FORMAL CLOSURE IN PROCESS EXTENSION: 11/2/01 - FORMAL CLOSURE OF ALL ITEMS COMPLETE: 10/31/01 CLOSURE STATEMENT: ------------------ SEVERAL INSPECTION METHODS WERE EVALUATED. THE MOST EFFICIENT VISUAL METHOD WAS A HORIZONTAL INSPECTION WITH TANK ENTRY USING A SPOTTING SCOPE AS NECESSARY. A VERTICAL VISUAL INSPECTION FROM THE 2058 FRAME USING THE SAME SPOTTER SCOPE PRODUCED ACCEPTABLE RESULTS, HOWEVER, ONE RIB ABOVE EACH "T" RING WAS BLOCKED FROM VIEW. AN INSPECTION PERFORMED FROM THE FWD END OF THE LH2 TANK WITHOUT MAKING A TANK ENTRY, PROVIDED VISUAL ACCESSIBILITY TO THE RIBS THAT COULD NOT BE INSPECTED FROM THE AFT END. THROUGH THE TANK, (DUAL WALL) X-RAY INSPECTION WAS DEVELOPED AND COULD DETECT A CRACK OF THE TYPE SEEN ON ET-117 LH2 TANK. C.5 REVIEW BUILD PAPER AND INTERVIEW INSPECTORS AND PRACTITIONERS TO DETERMINE NUMBER AND TYPE OF INSPECTIONS. RESPONSIBILITY: T. MCKEOUGH / D3741 - D. WESTPHAL/D3740 ECD: 6/18/01 COMPLETE: 6/18/01 CLOSURE STATEMENT: ------------------ NUMBER AND TYPE OF INSPECTIONS WERE IDENTIFIED AND ADDED TO THE ET-117 LH2 TANK PRODUCTION FAULT TREE FLOW CHART. INTERVIEWS WITH PRACTITIONERS WERE PERFORMED TO DETERMINE EFFECTIVENESS OF POST PROOF INSPECTIONS. IT WAS A CONSENSUS AMONG THE PRACTITIONERS THAT THE CLEANING/INSPECTION WOULD DETECT THIS TYPE OF DEFECT. THIS STEP IN THE PROCESS IS PERFORMED BY THREE DIFFERENT ORGANIZATIONS (PRODUCTION PRACTITIONER, QUALITY CONTROL INSPECTOR AND A MEMBER OF DCMA). CAUSE: --------- INADVERTENT DAMAGE TO BARREL SECTION DURING MAF FABRICATION. TASK II CORRECTIVE ACTION ----------------- NONE REQUIRED, THIS IS AN EXPLAINED CLOSURE CAPS. SEE CLEARANCE OF EFFECTIVITIES, TASK III. TASK III CLEARANCE OF EFFECTIVITIES -------------------------- * FLIGHT RATIONALE: 0 FAULT TREE TEAM AND SENIOR REVIEW BOARD CONCLUDED THAT THIS WAS AN ISOLATED EVENT AND NOT THE RESULT OF A SYSTEMIC PROBLEM. - ET DESIGN AND MATERIALS WERE EXONERATED AS CONTRIBUTORS TO THE ET-117 ANOMALY. - RIGOROUS REVIEW OF THE PROCESS INSTRUCTIONS FOR POST PROOF PROCESSING FOUND NO INADEQUACIES. - FAULT TREE AND FRACTURE FACE ANALYSIS CONCLUDED THAT THE ET- 117 DAMAGE EVENT OCCURRED DURING PROCESSING, PRIOR TO PROOF TEST. 0 THE FIRST OF THREE PLANNED POST-PROOF CLEANING AND INSPECTION STEPS IDENTIFIED CRACKS. 0 INVESTIGATION VALIDATED PROOF TEST AND POST PROOF INSPECTIONS FOR CERTIFICATION OF TANKS. * METHOD OF DETECTION IN FLIGHT: NONE, SEE FLIGHT RATIONALE * MISSION EFFECT: FRACTURE TESTING OF THE CRACKED RIBS DEMONSTRATED THAT A TANK WITH THESE CRACKS COULD COMPLETE MISSION. REF: ETTR-MS-01-026 - MATERIAL FAILURE ANALYSIS FOR ET-117 LH2 CRACK RIB FAULT TREE, NOVEMBER 9, 2001. * INSPECTION POINT TO FIND DEFECT: POST PROOF CLEAN & INSPECTION OF LH2 INTERIOR, IS A SERIES OF CLEANING & INSPECTION STEPS PERFORMED INDEPENDENTLY BY THREE ORGANIZATIONS, SEE TASK I.C.5. TASK IV CAPS CLOSURE SUMMARY -------------------- * DURING POST PROOF INSPECTION (SHAKEDOWN) OF THE LH2 TANK FOR ET-117, TWO CRACKS WERE FOUND ON RIBS C-35 & C-37 (BARREL #3) NEXT TO THE S-12 STRINGER ON THE ISL. THIS IS NEXT TO THE HB3-8 WELD AT STATION 1377, ON BARREL # 3. A THREE POINT APPROACH WAS USED TO INVESTIGATE THIS INCIDENT & PROVIDE FLEET CLEARANCE: 1. FORMAL FAULT TREE 2. INDEPENDENT FAILURE ANALYSIS 3. DETERMINE FLEET CLEARANCE / FLIGHT RATIONALE THE FAULT TREE WAS DIVIDED INTO THREE AREAS AND RESULTED IN THE FOLLOWING CONCLUSIONS: 1. MATERIALS - THE LH2 BARREL PANEL MET ALL SPECIFICATION REQUIREMENTS. 2. DESIGN - THE DESIGN OF THE PANEL IS ADEQUATE & MEETS ALL REQUIREMENTS. 3. OVERLOAD / FABRICATION - THE POSSIBILITY OF INADVERTENT & UNREPORTED DAMAGE EXISTS. ADDITIONAL TESTING CONFIRMED THAT SEVERAL DAMAGE SCENARIOS AT MAF WERE POSSIBLE. INDEPENDENT FAILURE ANALYSIS SHOWED THE FOLLOWING: 1. THE MATERIAL MEETS ALL SPECIFICATION REQUIREMENTS. 2. THE FRACTURE SURFACES ARE CONSISTENT WITH THE PROPOSED DAMAGE SCENARIOS AND COULD ONLY OCCURRED AT MAF PRIOR TO PROOF TEST. 3. NO ABNORMALITIES WERE NOTED. FLEET CLEARANCE/FLIGHT RATIONALE WITH INPUT FROM THE FAULT TREE GROUP & FAILURE ANALYSIS GROUP DETERMINED THAT: 1. THIS WAS AN ISOLATED EVENT AND NOT THE RESULT OF A SYSTEMIC PROBLEM. 2. THE FIRST OF THREE PLANNED POST-PROOF CLEANING AND INSPECTION STEPS IDENTIFIED CRACKS. 3. THE INVESTIGATION VALIDATED PROOF TEST AND POST PROOF INSPECTIONS FOR CERTIFICATION OF TANKS. IN ADDITION TWO METHODS WERE DEVELOPED TO INSPECT TANKS FOR DAMAGE POST PROOF. THIS WAS A SERIES OF ASSISTED VISUAL INSPECTIONS IN VARIOUS TANK ATTITUDES & A DOUBLE WALL X-RAY METHOD BASED ON THE FINDINGS IMPLEMENTATION WAS NOT NECESSARY. ************************************************************ THIS ADDENDUM WAS REQUESTED BY NASA S&MA. TO REDUCE THE RISK OF L02/LH2 TANK DAMAGE OCCURRING AFTER PROOF TEST BARREL CRACK THE FOLLOWING ENHANCEMENTS WERE IDENTIFIED DURING THE ET 117 INVESTIGATION. 1. ANGLE IRONS HAVE BEEN INSTALLED AT THE 7077 AND 7419 TOOLS TO PREVENT A VEHICLE OR DOLLY FROM COMING INTO CONTACT WITH THE TANK. 2. THE MPPS HAVE BEEN REVISED TO SPECIFY THE FOLLOWING AT THE 7077 (LH2) AND THE 7419(LO2) TOOL; A. VERIFY CLEARANCE PRIOR TO ROTATION B. LOCKOUT/TAGOUT ROTATION WHEN NOT IN USE C. INSTALL BARRICADE WITH POST AND CHAINS D. POST SIGNAGE 3. VIDEO SURVEILLANCE SCHEDULED TO BE IMPLEMENTED 4. THE FOLLOWING MAJOR TANK MOVES WILL BE WITNESSED BY QC: LO2 TANK MAJOR MOVES *7419 TO CELL "F" 2000-166 CELL "F" TO 7419 2000-289 7419 TO CELL "E" 2000-290 LH2 TANK MAJOR MOVES 5068 TO BUCKS 4000-503 BUCKS TO 7077 4000-119 7077 TO BUCKS 4000-517 *BUCKS TO 451 4000-502 451 TO BUCKS 4000-201 BUCKS TO CELL "P" 4000-014 CELL "P" TO CELL "N" 4000-531 CELL "N" TO CELL "E" 4000-534 *QC COVERED THIS PRIOR TO ET 117 |  |  |  |  |  |
| MSFC Response/Concurrence 07/09/2001 - BOARD ACCEPTED PLAN OF ACTION UNTIL 8/30/2001 - PER RATIONALE (B): THE PROBLEM CONDITION IS CLEARLY SCREENED DURING PREFLIGHT CHECKOUT OR SPECIAL TESTS. 08/30/2001 - PROBLEM REOPENED SINCE DEFERRAL DATE PASSED. 11/19/2001 - MSFC APPROVED INTERIM CLOSURE THRU 12/31/2001. 1/02/2002 - PROBLEM REOPENED SINCE DEFERRAL DATE PASSED. 1/31/2002 - BOARD ACCEPTED PROBLEM CLOSURE RATIONALE. SIGNATURES ARE ON FILE IN THE PAC. THIS PROBLEM IS OFFICIALLY CLOSED. |  |  |  |  |  |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A17695 | IFA# -- | Contractor RPT# S-087 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80914004000-519 | Asmnt Part Name LH2 TANK | Asmnt Serial/Lot# 1131190 |  |  |  |
| HCRIT CD 1 | FCRIT CD 3 | CAUSE CD MW - MFG-WORK | FAIL MODE MS - STRUCT |  |  |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |  |  |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |  |  |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |  |  |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |  |  |  |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |  |  |  |
| MAJOR DESIGN CHANGES |  |  |  |  |  |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |  |  |  |  |
| ASSESSMENT TEXT |  |  |  |  |  |