##### DEPARTMENT OF TRANSPORTATION

PERFORMANCE ORIENTED PACKAGE TESTING

CERTIFICATION

Performed by:

Good Results Testing

1 PHIMSA Ave

Nowhere, Maryland 20590

555-555-5555

Testing Performed for:

Big Guy Chemical Company

2 Old RSPA Way

Anyplace, Maryland 20590

555-555-1234

Design Qualification Testing of a

UN 4G Fiberboard Box

##### With Four 4-Liter Inner Bottles

###### 4G/X25.5/S/**

USA/+QQ2345

** Is to be replaced by the

year of manufacture

This package is NOT certified for shipment by air.

Signature of Certifying Individual

(Must be listed on the Laboratory’s Approval)

Section 2

Package Description

# Fiberboard Box: See Section 5 for drawing

| Manufacturer: | Big Box Company, Springfield, MD |
| --- | --- |
| Box Style: | Regular Slotted Container (RSC) International Box Code: 0201 Mullen Burst __X_ ECT ____ |
| Part Number: | BB12345 |
| Boxmaker’s Certification: | None |
| Outer dimensions cm (in): | 30.8 x 30.5 x 30.0 (12.0 x 12.0 x 12.0) |
| Inner Dimensions cm (in | 29.6 x 29.3 x 29.0 (11.5 x 11.5 x 11.5) |
| Manufacturers Joint: | Hot Melt Glued with a 4.4 cm (1.75) inside flap |
| Tare Weight | 525 grams |

| Partitions (if used) |  |
| --- | --- |
| Partition Style |  |
| Dimensions |  |
| Tare Weight |  |

Basis Weights of Box and Partitions:

| Item | Facing or Corrugation | Location | Basis Weight |
| --- | --- | --- | --- |
| Box | Facing | Inner | 42.1 |
|  | Facing | Middle | 26.2 |
|  | Facing | Outer | 36.5 |
|  | Corrugation | Inner- B Flute | 26.1 |
|  | Corrugation | Outer – B Flute | 26.2 |
| Partition | Facings |  |  |
|  | Facing |  |  |
|  | Corrugation |  |  |

Combined Board Caliper

| Box | 5.9 mm | 6.3 mm | 6.3 mm |
| --- | --- | --- | --- |
| Partition |  |  |  |

# Combined Facing Weights (average)

| Box |  |
| --- | --- |
| Partition |  |

# Inner Bottles: See Section 5 for drawing

| Manufacturer: | Joe’s Bottle Company Houston, TX |  |
| --- | --- | --- |
| Part Number: | JB11111-11 |  |
| Manufacturing Method | Blow molded |  |
| Material/Resin: | HDPE | Some Chemical Company Resin 12345 |
| Capacity | Nominal | 4.00 liters |
|  | Maximum* (avg.) | 4.15 liters |
| Dimensions: | Width | 146.6 mm (5.776 in) |
|  | Length | 147.7 mm (5.819 in) |
|  | Height: | 272.8 mm (10.740 in) |
| Min Thickness: | Bottom: | 2.0 mm (0.078 in) |
|  | Sides: | 1.0 mm (0.039 in) |
| Average Thickness: | Bottom: | 2.3 mm |
|  | Sides: | 1.2 mm |
| Tare Weight (avg.) |  | 145.0 grams |

# Closure: See Section 5 for drawing

| Manufacturer: | Sam’s Closures Houston, TX |  |
| --- | --- | --- |
| Part Number: | SC-38 |  |
| Material: | Polypropylene |  |
| Closure Weight: | 5.5 grams |  |
| Dimensions: | Diameter | 40.0.0 mm |
|  | Height | 11.46 mm |
|  | Thickness (min): | 2.0 mm |
| Lining – Glued in | Material | Foam |
|  | Diameter | 38.0mm |
|  | Thickness | 1.2 mm |

Closing Methods:

| Sealing Method for the fiberboard box | 3 strips of 2 inch fiber reinforced tape applied in an “H” pattern on the top and bottom of the box. Sides are taped approximately ½ inch from the corners of the box. The center tape extends approximately 2 inches over the end of the box. |
| --- | --- |
| Closing torque of caps for all testing: | 12.0 in-lbs +/- 2.5 in-lbs |

# Additional Test Information

| Overall Tare Weight of Package | 1.13 kg |
| --- | --- |
| Test Contents: | Water and antifreeze |
| Specific gravity | .98 |
| Minimum Weight of Package as Tested: | 17.41 kg |
| Authorized Package Gross Weight based on SG 1.5 | 25.5 |

Section 3 - TESTING

Test Descriptions and Results

Package Preparation – For All Testing

The packages were filled to a minimum of 98% full (see Section 4 for calculation).   The inner bottles were inserted as shown in Section 5.

Drop Test –

Test Method: 49 CFR 178.603

Number of Packages Tested – 5

Drop Height – 2.25 meters (Calculation for the drop height is provided in Section 4)

Testing was conducted to certify the package for PGI liquids with a specific gravity of up to 1.5.

Conditioning

The packages were conditioned to –18 degrees C in accordance with 49 CFR 178.603(c).  The packages were conditioned for 24 hours to ensure the package and contents were at the proper temperature prior to testing.  Drop testing was conducted approximately 2 minutes after removing the test package from the conditioning chamber.

# Results

| Box Number | Package Weight | Orientation | Result |
| --- | --- | --- | --- |
| 1 | 17.42 | Flat on Top | Pass – No damage |
| 2 | 17.43 | Flat on Short Side | Pass – No damage |
| 3 | 17.41 | Flat on Bottom | Pass – No damage |
| 4 | 17.45 | Flat on Long Side | Pass – No damage |
| 5 | 17.44 | Bottom Corner | Pass – Corner crushed approximately 2 inches, no release of the inner packages from the outer package or filling substance from the inner bottle. |

Pass/Fail Criteria -

A package is considered to successfully pass the drop tests if for each sample tested: There is no damage to the outer packaging likely to adversely affect safety during transport, there is no leakage of the filling substance from the inner packaging and any discharge from a closure is slight and ceases immediately after impact.

Stacking Test

Test Method: 49 CFR 178.606

Free standing:   X

Guided Load:   __

Packages Tested – 3

Test Duration: 24 hours

The packages were conditioned in accordance with 49 CFR 178.602(d) to 50% RH     +/- 2% at 23 C for 24 hours.

Stacking Test Weight – 250 kg (rounded up from 229.95)

See Section 4 for Calculation

The stacking test load was applied to the top of the packages by loading each package with 830 kg and the weight was maintained for 24 hours.

Results:

| Package 1 | No damage to the packaging |
| --- | --- |
| Package 2 | No damage to the packaging |
| Package 3 | No damage to the packaging |

Note: Stacking stability was not assessed since a guided load test was not performed.

Pass/Fail Criteria -

No test sample may leak.  There must be no leakage of the filling substance from the inner receptacle, or inner packaging. No test sample may show any deterioration which could adversely affect transportation safety or any distortion likely to reduce its strength, cause instability in stacks of packages, or cause damage to inner packagings likely to reduce safety in transportation.

# Vibration Standard

Packages Tested – 3

Test Method: 49 CFR 178.608 on a:	__ rotary vibration table

__ vertical linear vibration table

Duration: 1 Hour

Frequency: 3.6 Hz (216 rpm)

Results

| Package 1 | No damage |
| --- | --- |
| Package 2 | No damage |
| Package 3 | No damage |

Pass/Fail Criteria -

A packaging passes the vibration test if there is no rupture or leakage from any of the packages. No test sample should show any deterioration which could adversely affect transportation safety or any distortion liable to reduce packaging strength.

Cobb Test

# Test Method:  ISO International Standard 535 as required by 49 CFR 178.516(b)(1).

Samples were taken from the boxes and subjected to a water absorption test in accordance with ISO International Standard 535.

Samples tested - 5

Results

| Sample Number | Water Absorption | Pass/Fail |
| --- | --- | --- |
| Sample 1 | 97 g/m3 |  |
| Sample 2 | 94 g/m3 |  |
| Sample 3 | 96 g/m3 |  |
| Sample 4 | 92 g/m3 |  |
| Sample 5 | 91 g/m3 |  |
| Average | 94.0 | Pass |

Pass/Fail Criteria:

An increase in mass of greater than 155 g/m2 over the 30 minute duration of the test represents an unacceptable level of water resistance.

Section 4 - Calculations

- Weight of test package

Weight of Box			0.525 kg

Weight of Bottle + Cap		0.151 kg

Capacity of bottle			4.15 liter

Empty Package weight

Box + Partitions 			.525 kg

Empty Bottles (4 x.151)		.604 kg

Total				1.129 kg

Filled Package Weight

Weight of liquid fill .98 X 4.15= 	4.07 kg

# Weight of Filled Package

# 0.525 + 4(.151) + 4(4.07) =	17.41 kg

- Drop Test Height

# Specific Gravity of Certification	1.5

Packaging Group of Certification	I

For PG I 	SG x 1.5 meters

1.5 x 1.5 meters = 2.25 meters

- Marked Weight to Accommodate SG 1.5

Weight of Fill	 4(4.07 kg) x 1.5 =	24.42   kg

Weight of Box			  0.525 kg

Weight of Bottles			  0.604 kg

# Marked Weight (rounded down)	25.5     kg

- Stack Test Weight

Load = (n-1)[W+Q(L x S)]

Where:

N = number of containers to reach 3 meters

W= Tare weight of all packaging material

Q= Quantity of Inner Packages

L = Weight of Liquid Fill

S = Maximum Specific Gravity

Package Height = 30.0 cm

3.0 meters/.30 meters = 10.0

(10-1)[1.13+4(4.07 x 1.50)] = 229.95 kg

Section 5

Drawings of Packaging Components

Fiberboard Box

Closure

Inner Bottle

Appendix A

Test Equipment and Instrumentation

| Instrument or Equipment | Manufacturer | Model Number | Serial Number | Calibration Date |
| --- | --- | --- | --- | --- |
| Drop Tester |  |  |  |  |
| Gram Scale |  |  |  |  |
| Electronic Scale |  |  |  |  |
| Pressure Gauge |  |  |  |  |
| Vibration Table |  |  |  |  |

Appendix B

Additional boxes indicated below are certified through selective testing provisions:

| Part Number | Dimensions |  |
| --- | --- | --- |
| 23456 | 11.00 x 11.00 x 11.00 |  |
| 34567 | 12.00 x 11.00 x 9.00 |  |
| 45678 | 9.00 x 9.00 x 9.00 |  |
| 56789 | 6.00 x 6.00 x 6.00 |  |

# Text boxes

u

n