WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A10213 | In-Flight Anomaly Number -- | Contractor Report Number S-070-2 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title DARK LINE, X-RAY INDICATIONS AT INTERSECTION OF VPPA WELDS - LWT-42/ASSEMBLY INSPECTION |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (4) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE LH2 FWD DOME | PART# 80914100900-010 | SER/LOT# N/A | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE LH2 TANK COMPLETE | PART# 80904000000 | SER/LOT# N/A | MANUFACTURER MMC |
| HARDWARE NCA | NOMENCLATURE LH2 FWD DOME | PART# 80914100900-010 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation L - FLD | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode UC - UNSAT | Cause U - UNKNOWN |
| System STRUCTURAL | Defect DC - BROKEN | Material H - WELD | Work Contact MATTHEESSEN | Fail Date 05/08/1986 |
| Received at MSFC 07/22/1986 | Date Isolated -- | FMEA Reference 1.1.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text NONE |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 05/07/1992 | CN RSLV SBMT 02/23/1987 | Defer Date -- | Add Date -- | R/C Codes 4 - TEST -- -- |
| Assignee |
| Design J. WHITE | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| Approval |
| Design J. WHITE | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete -- | MSFC Closure Date 04/06/1987 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description REF MARS: T-94534, T-94535, T-94536, T-94537 AND T-94728. LWT-42 LH2 FORWARD DOME HAD TEN DARK LINE INDICATIONS AT INTERSECTIONS OF VARIABLE POLARITY PLASMA ARC (VPPA) WELDS OR AT TIG AND VPPA WELDS |
| Contractor Investigation/Resolution R/A - THE FAULTY AREAS WERE REPAIRED. FOR CORRECTIVE ACTION, ALL FUTURE OCCURRENCES WILL BE DOCUMENTED AND EVALUATED PER PAD 3740-054. 7/22/86 GENERAL - ON 80914100900-010 (LHW FORWARD DOME) TEN DARK LINE INDICATIONS WERE NOTED BY X-RAY. THESE WERE SHORT BLACK LINES (.200 INCH TO .300 INCH) LOCATED NEAR THE EDGE OF THE WELD IN THE INTERSECTION OF TWO WELDS. THIS CONDITION IS UNIQUE DUE TO THE FACT THAT INDICATIONS ARE AT VPPA INTERSECTIONS OR VPPA TO TIG INTERSECTIONS. THE AREAS WERE INSPECTED BY ULTRASONICS AND INDICATIONS WERE NOTED. THE AREAS WERE REPAIRED. IN SOME CASES, A SHALLOW REPAIR WAS ENOUGH TO REMOVE THE DEFECT. WHILE IN OTHERS, A LARGE GRIND FROM BOTH SIDES WERE REQUIRED. CAUSE OF FAULTY WELD AREAS IS UNDER INVESTIGATION. THIS PROBLEM IS A LAUNCH CONSTRAINT TO LWT-15, -20, -21, -22, -24 AND SUBS. 8/21/86 PRB STATUS - SOURCE OF THE SHORT BLACK LINES ON X-RAYS ARE UNKNOWN. UNDER INVESTIGATION. 9/18/86 PRB STATUS - MMC PREPARING TO RUN FULL SCALE TEST PANELS. ECD IS UNDETERMINED. 10/16/86 PRB STATUS - MMC HAS BEEN UNABLE TO DUPLICATE DARK LINE X-RAY INDICATIONS DURING TESTS; HOWEVER, THEY EXPECT TO OBTAIN A DEFECTIVE WELD SPECIMEN DURING REPAIR OF A DEFECTIVE WELD. FA WILL BE DONE ON THIS SPECIMEN TO TRY TO BETTER UNDERSTAND THE FAILURE MODE ADDITIONALLY, ALL X-RAYS OF PREVIOUSLY BUILT HARDWARE ARE TO BE REVIEWED FOR X-RAY INDICATIONS. ECD FOR COMPLETION OF X-RAY REVIEW IS 9-6-89. 1/29/87 PRB STATUS - CLOSURE IN WORK. CAPS ECD 2-6-87. 2-26-87 STATUS - AFTER EXTENSIVE INVESTIGATION, THE CAUSE COULD NOT BE DETERMINED. THE DEFECTED WELDS WERE REPAIRED AND X-RAYED WITHOUT RECURRENCE OF BLACKLINE INDICATIONS. CLEARANCE OF EFFECTIVITIES - ALL EFFECTIVITIES ARE BEING CLEARED USING THE FOLLOWING RATIONALE: IF AN INDICATION IS FOUND, ULTRASONICS WILL BE PERFORMED AND DISPOSITION WILL BE REQUESTED FROM ENGINEERING. THIS WILL BE ACCOMPLISHED BY THE RE-REVIEW OF X-RAYS PRIOR TO PROOF X-RAY REVIEW, AND DUAL X-RAY REVIEW |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A10213 | IFA# -- | Contractor RPT# S-070-2 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80914100900-010 | Asmnt Part Name LH2 FWD DOME | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD U - UNKNOWN | FAIL MODE UC - UNSAT |
| Asmnt FMEA 6.2.1.1 | Asmnt FM 1 | FMEA CSE D | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |