Homework Assignment ---B

Superpave PG Grading Systems

Name:___________________________

Date:____________________________

Use the Superpave software provided to determine the average 7 day high and 1-day minimum low pavement temperature and standard deviations for the following locations.

- San Antonio, Texas

- Denver, Colorado

- International Falls, Minnesota

- Chattanooga, Tennessee

- Washington, D.C.

Select a PG grade to use in each of the above locations.  Use the maximum and minimum temperatures plus 2 standard deviations.

What is the PG grade of the asphalt whose results are shown in Table 1?

TABLE 1.  Asphalt Cement Test Results.

| Properties | Asphalt No. 1 |
| --- | --- |
| Original Properties |
| Flash point temperature, oC | 278 |
| Viscosity at 135oC | 0.490 Pa.s |
| Dynamic shear G*/ sin  at 70oC G*/ sin  at 76oC G*/ sin  at 82oC | 0.88 1.25 2.10 |
| Rolling Thin Film Oven Aged Binder |
| Dynamic shear G*/ sin  at 70oC G*/ sin  at 76oC G*/ sin  at 82oC | 1.88 2.64 4.10 |
| Rolling Thin Film Oven and PAV Aged Binder |
| Dynamic shear G* sin  at 28oC G* sin  at 31oC G* sin  at 34oC | 2358 3107 4009 |
| Creep Stiffness Stiffness and m-value at -6oC Stiffness and m-value at -12oC Stiffness and m-value at -18oC | S m-value 255 0.329 290 0.305 318 0.277 |