SPECIAL SPECIFICATION

SECTION 07600

FLASHING AND SHEET METAL

Page

PART 1 - GENERAL

1.01  Summary	2

1.02  Submittals.	2

PART 2 - PRODUCTS

2.01  Sheet Metal Flashing and Trim Materials	3

2.02  Miscellaneous Materials and Accessories	3

2.03  Fabricated Units	4

PART 3 - EXECUTION

3.01  Installation Requirements.	5

3.02  Cleaning And Protection.	5

SPECIAL SPECIFICATION

SECTION 07600

FLASHING AND SHEET METAL

PART 1 - GENERAL

1.01  	 	SUMMARY

A.  This Section includes the following:

1.  Metal wall flashing and expansion joints.

2.  Gutters and downspouts.

3.  Miscellaneous sheet metal accessories.

4.  Splashblocks.

1.02   	SUBMITTALS

A.  	General:  Submit the following in accordance with Section 01300.

B.  	Product data, Flashing, Sheet Metal, and Accessories:  Manufacturer's technical product data, installation instructions and general recommendations for each specified sheet material and fabricated product.

PART 2 - PRODUCTS

2.01   	SHEET METAL FLASHING AND TRIM MATERIALS

A.  	Zinc-Coated Steel:  Commercial quality with 0.20 percent copper, ASTM A 526 except ASTM A 527 for lock-forming, G90 hot-dip galvanized, mill phosphatized where indicated for painting.

1.  Thickness as indicated on Drawings.

2.02  	 MISCELLANEOUS MATERIALS AND ACCESSORIES

A.  	Solder:  For use with steel, provide 50 - 50 tin/lead solder (ASTM B 32), with rosin flux.

B.  	Fasteners:  Same metal as flashing/sheet metal or other non- corrosive metal as recommended by sheet manufacturer.  Match finish of exposed heads with material being fastened.

C.  	Bituminous Coating:  SSPC - Paint 12, solvent-type bituminous mastic, nominally free of sulfur, compounded for 15-mil dry film thickness per coat.

D.  	Elastomeric Sealant:  Generic type recommended by manufacturer of metal and fabricator of components being sealed and complying with requirements for joint sealants as specified in Section 07900, Joint Sealers.

E.  Adhesives:  Type recommended by flashing sheet manufacturer for waterproof/weather-resistant seaming and adhesive application of flashing sheet.

F.  	Metal Accessories:  Provide sheet metal clips, straps, anchoring devices, and similar accessory units as required for installation of work, matching or compatible with material being installed, noncorrosive, size and gage required for performance.

G.  	Splashblock:  Provide preformed concrete splashblocks.

H.  	Gutter Guards:  20-gage bronze or nonmagnetic stainless steel mesh or fabricated units, with selvaged edges and noncorrosive fasteners.  Select materials for compatibility with gutters and downspouts.

I.  		Roofing Cement:  ASTM D 2822, asphaltic.

2.03   	FABRICATED UNITS

A.  	General Metal Fabrication:  Shop-fabricate work to greatest extent possible.  Comply with details shown and with applicable requirements of SMACNA "Architectural Sheet Metal Manual" and other recognized industry practices.  Fabricate for waterproof and weather-resistant performance, with expansion provisions for running work, sufficient to permanently prevent leakage, damage, or deterioration of the work.  Form work to fit substrates.  Comply with material manufacturer instructions and recommendations for forming material.  Form exposed sheet metal work without excessive oil-canning, buckling, and tool marks, true to line and levels indicated, with exposed edges folded back to form hems.

B.  	Seams:  Fabricate nonmoving seams in sheet metal with flat-lock seams.  For metal other than aluminum, tin edges to be seamed, form seams, and solder.  Form aluminum seams with epoxy seam sealer; rivet joints for additional strength where required.

C.  	Expansion Provisions:  Where lapped or bayonet-type expansion provisions in work cannot be used or would not be sufficiently water/weatherproof, form expansion joints of intermeshing hooked flanges, not less than 1 inch deep, filled with mastic sealant (concealed within joints).

D.  	Sealant Joints:  Where movable, nonexpansion type joints are indicated or required for proper performance of work, form metal to provide for proper installation of elastomeric sealant, in compliance with SMACNA standards.

E.  	Separations:  Provide for separation of metal from noncompatible metal or corrosive substrates by coating concealed surfaces at locations of contact, with bituminous coating or other permanent separation as recommended by manufacturer/fabricator.

F.  	Shop Finish:  Provide manufacturer's standard baked-on white acrylic shop finish on sheet metal (gutters and downspouts); 1.0-mil dry film thickness.

PART 3 - EXECUTION

3.01   	INSTALLATION REQUIREMENTS

A.  	General:  Except as otherwise indicated, comply with manufacturer's installation instructions and recommendations and with SMACNA "Architectural Sheet Metal Manual." Anchor units of work securely in place by methods indicated, providing for thermal expansion of metal units; conceal fasteners where possible, and set units true to line and level as indicated.  Install work with laps, joints, and seams that will be permanently watertight and weatherproof.

B.  	Bed flanges of work in a thick coat of bituminous roofing cement where required for waterproof performance.

C.  	Install continuous gutter guards on gutters, arranged as hinged units to swing open for cleaning gutters.  Install "beehive"-type strainer-guard at conductor heads, removable for cleaning downspouts.

D.  	Provide splashblocks at each downspout.

3.02   	CLEANING AND PROTECTION

A.  	Clean exposed metal surfaces, removing substances that might cause corrosion of metal or deterioration of finishes.

B.  	Protection:  Advise Contractor of required procedures for surveillance and protection of flashings and sheet metal work during construction to ensure that work will be without damage or deterioration other than natural weathering at time of Substantial Completion.

END OF SECTION