SECTION EIGHT

COPPER ROLLING AND DRAWING MILLS

8.1	PROFILE

Copper rolling, drawing, and extruding mills produce copper and copper-alloy rod, bar, sheet, strip, plate, piping, tube, and wire.  The metal forming processes used to produce beryllium-copper (Be-Cu) products are common to other metals and, depending on the product, may include rolling, extrusion, and hot or cold drawing.  Annealing, pickling or metal cleaning, and slitting or cutting operations may also be performed.

Table 8-1 shows the 2002 Economic Census statistics for this industry, NAICS 331421, Copper Rolling, Drawing, and Extruding (U.S. Census Bureau, 2004).  The Census reported 91 firms and 136 establishments, employing 13,004 production workers, engaged in copper rolling, drawing, and extruding.  The table also shows the industry breakdown by primary product specialization, with smaller numbers of establishments producing wire, bars, sheet, tube, and other copper and copper-alloy products.

Census data show, however, that considerably fewer companies in this industry manufacture products from alloyed copper (as opposed to unalloyed copper). Only 16 firms (with more than $100,000 in shipments) produced copper-alloy wire; 14 firms produced copper-alloy rod, bar, and shapes; 11 firms produced copper-alloy sheet, strip, and plate; and 8 firms produced copper-alloy pipe and tube (other than plumbing pipe).  Furthermore, beryllium-copper is only one of many copper alloys (e.g., brass and bronze) that such firms might produce. A list of beryllium-copper suppliers maintained by the Copper Development Association lists eight companies with 12 establishments producing rolled and drawn beryllium-copper products (CDA, 2002).  ERG identified three additional establishments engaged in redrawing or re-rolling copper alloy materials.  Based on this information, ERG estimates that 15 establishments are currently engaged in rolling, drawing, and extruding of beryllium-copper products. The 2002 Census shows an average of 96 production workers per establishment in this industry. Assuming that the 15 copper-beryllium establishments are of average size, there are 1,440 production employees in these establishments.

Additional establishments redraw purchased wire to customer specifications. These establishments are classified by in the NAICS industry 331422: Copper Wire (Except Mechanical) Drawing. The 2002 Economic Census shows 107 establishments in this industry, employing 11,480 employees and 8,195 production workers. No published data exist on the number of such establishments that handle copper-beryllium alloys, but estimates from Brush Wellman’s (BW) customer database show 59 such facilities (Kolanz, 2001). If these establishments were typical in size to the rest of the industry and employ about 77 production workers, their production employment would total 4,519. The statistics for NAICS 331422 are also shown in Table 8-1

Based on the distribution of establishments by employment size across each of the two industries, ERG estimated the number of copper-beryllium establishments in each size class. These are also shown in Table 8-1.

The technological feasibility analysis identified two occupations where median exposures exceed the lowest PEL option: wastewater treatment operators (0.11 μg/m3) and bulk pickling and annealing operators (0.12 μg/m3). ERG estimated there are typically one wastewater treatment operator and four pickling and annealing operators per affected facility. These estimates are consistent with results from the Bureau of Labor Statistics (BLS) 2002 Occupational Employment Survey (OES) which found 240 pickling operators and 30 waste treatment plant and system operators in the much broader four-digit NAICS industry, 3314 (BLS, 2004). The OES data, however, might undercount workers in some specific job classifications because it cannot identify all workers that might perform multiple tasks.

ERG also estimated the number of facilities that perform the pickling and annealing tasks in this sector. The BW customer survey database shows that among its strip and bulk customers (combined), approximately three times as many customers perform redrawing as perform pickling (Kolanz, 2001). ERG used this relationship to estimate the number of firms and affected workers with these processes. Some facilities, especially small firms, are believed to perform a smaller range of activities and might not perform bulk pickling and annealing. Based on the BW data, ERG estimates that 35 facilities among the beryllium-using firms in the affected industries perform pickling and annealing. These were allocated between the two NAICS codes as follows: 15 facilities in NAICS 331421 and 20 in 331422. ERG also estimated that each beryllium-using facility in this sector (74; see Table 8-1) also operates a wastewater treatment facility.

8.2	COST OF CONTROLS

Engineering Controls:  The technological feasibility discussion focuses on two job categories, bulk pickling and annealing operators and wastewater treatment operators.

Pickling and Annealing Operators: The largest engineering control costs will be incurred to reduce exposures to the pickling and annealing operator. As noted in the technological feasibility discussion, BW personnel expressed uncertainty about the exact source of these exposures, although many suspicions focus on beryllium releases from the bulk pickling tank. Further, based on discussions with project consultants and BW, the most cost-effective means of reducing exposures to these workers is not certain.

As a result, the applicability and likely effectiveness of possible engineering controls for the bulk pickling and annealing operations are uncertain. Nevertheless, ERG and its consultants used their own engineering judgments to develop a set of possible controls and to estimate the costs of installation. In applying the engineering control costs, ERG assumed that all affected facilities will require controls at the lowest PEL option level. No control costs are required at the higher PEL levels because the estimated median exposure level for pickling and annealing operators is below the all of the optional PELs.

The primary engineering control to limit beryllium release from the pickling bath is enclosure. Simply covering the bath would, however, present difficult operational issues, and ERG concluded that a ventilated tunnel enclosure within the manufacturing facility would work better. A crane system would be constructed inside the tunnel to move bulk products into and

| Table 8-1. Copper Rolling, Drawing, and Extruding (NAICS 331421) – 2002 |
| --- |
| NAICS | No. of Firms | No. of Establish-ments | Total Employees | Production Workers | Estabs. with < 20 Employees | Estabs. with 20-99 Employees | Estabs. with > 99 Employees |
| 331421 Copper Rolling, Drawing, and Extruding | 91 | 136 | 16,406 | 13,004 | 47 (35%) | 43 (32%) | 46 (34%) |
| By Primary Product Class Specialization (including both Cu and Cu-Be products) |
| 3314211 Copper wire, bare and tinned (non electrical), made in rolling mills | NA | 19 | 1,584 | 1,189 | NA | NA | NA |
| 3314213 Copper and copper-base alloy rod, bar, and shapes | NA | 24 | 3,334 | 2,468 | NA | NA | NA |
| 3314217 Copper and copper-base alloy sheet, strip, and plate | NA | 17 | 4,990 | 3,811 | NA | NA | NA |
| 3314219 Copper and copper-base alloy pipe and tube | NA | 26 | 6,063 | 5,201 | NA | NA | NA |
| 3314221 Copper Wire (Except Mechanical) Drawing | 79 | 107 | 11,480 | 8,195 | 31 (29.0%) | 38 (38.5%) | 38 (35.5%) |
| Estimates of Beryllium-Using Facilities |
| NAICS 331421(a) | NE | 15 | 1,809 | 1,440 | 5 | 5 | 5 |
| NAICS 331422(a) | NE | 59 | 6,330 | 4,519 | 17 | 23 | 21 |
| Source: US Census Bureau, 2004. (a) Estimated by ERG. NA = Not available. NE=Not estimated. |

through the pickling bath. The tunnel would also be equipped with a video system to allow outside operators to operate and observe the process. A second set of second engineering controls is needed which will enclose the coil handling operation as bulk materials are moved from the annealing furnace to the pickling operation. Finally, ERG estimates that reaching the 0.1 μg/m3 level will also require a ventilated material handling unit (Hawley Trav-L-Vent equipment) to move products from the annealing to the pre-treatment operation prior to pickling. Additional engineering controls were also considered but judged not to be necessary. These controls include the addition of a clean air island for the pickling operator station, a tunnel for the annealing operation, and a secondary hood over the annealing furnace to capture any leakage of beryllium-carrying emissions.

Wastewater Treatment Operators: For wastewater treatment operators, enhancements include the development and implementation of good work practices and effective housekeeping protocols to limit personal exposure and workplace contamination. ERG judged that because exposures are slightly over the lowest PEL option, only modest changes in housekeeping practices, such as incremental cleaning time, are needed. ERG estimated that 15 minutes per shift is adequate to address this issue.

Table 8-2 presents the list of controls and costs for the pickling and annealing task, while Table 8-3 summarizes the resultant costs by PEL option, affected job category, and industry. As shown in Table 8-3, the estimated engineering controls per establishment for the bulk pickling/annealing operators are estimated at $226,014 for 0.1 μg/m3 PEL level, with total costs of $7.9 million. The annual cost of additional housekeeping by affected wastewater treatment operators is estimated as $1,686 per worker, for a total of $124,773 at the 0.1 μg/m3 PEL level. No costs are associated with the higher PEL option levels.

Program Requirements: Table 8-4 shows the compliance costs for the program requirements for the two industries comprising rolling and drawing sector. A complete discussion of the methodology and underlying assumptions for estimating program costs is presented in Section 2. As noted there, rolling and drawing is assumed to be a low-exposure  sector for costing purposes under the 2.0 μg/m3 PEL option.

The majority of the program costs are associated with requirements for protective clothing and hygiene areas and include the costs associated with employee time for showering and vacuuming clothes at the end of each shift. Combined, these costs represent 74.2 percent of all program-related costs at the most stringent PEL level of 0.1 μg/m3.  Total annualized program costs range from $337,753 to $10.2 million over all the PEL option levels.

8.3	AGGREGATE COSTS

Table 8-5 presents the aggregate compliance costs arrayed by PEL option and by industry. Costs are significantly higher for the lowest PEL options due primarily to the additional engineering costs. As noted previously, there is also considerable uncertainty about eventual cost of engineering controls necessary for these facilities due to the limited experience with the effectiveness of engineering controls needed to control exposures at such low levels.

Program costs are also significant, although the major program-related costs are not sensitive to the PEL option level. At the highest PEL option, program costs represent about 54 percent of compliance costs. At the other option levels, all compliance costs are associated with the program requirements. Total annualized costs range from $357,753 million to $18.2 million per year, from the highest to lowest PEL, respectively.

REFERENCES

BLS. 2004. Bureau of  Labor Statistics, Occupational Employment Survey, 2002.

CDA. 2002. Copper Development Association Web site http://suppliers.copper.org/fab_frame.htm. Accessed February 18, 2002.

Kolanz, Mark. 2001. Brush Wellman Customer Data Summary. OSHA Presentation, July 2, 2001. Washington, DC.

U.S. Census Bureau. 2004. 2002 Economic Census: Copper Wire (Except Mechanical) Drawing, 2002; Copper Rolling, Drawing, and Extruding, 2002.