MSFC PRACA : 2003-02-12 07:54

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A01683 | In-Flight Anomaly Number -- | Contractor Report Number T-009 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title BARRY MOUNT HAD EPOXY PRIMER LIFT-OFF CRES SUBSTRATE |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (3) B C D E (X) F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE EXTERNAL TANK | PART# 82601000000 | SER/LOT# ET-1 | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE BARRY MOUNT | PART# 826710281088 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation L - FLD | Prevailing Condtion -- | F / U F | Fail Mode -- | Cause -- |
| System THERMAL | Defect -- | Material -- | Work Contact D. WESTPHAL | Fail Date 10/29/1979 |
| Received at MSFC 07/07/1980 | Date Isolated -- | FMEA Reference 1.2 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location KSC | Symptom -- | Time Cycle -- |
| Effectivity Text ET-1 AND SUBS |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 10/07/1987 | CN RSLV SBMT 11/30/1981 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design B. DAVIS | Chief Engineer -- | S & MA D. NEWMAN | Project G. CAVALARIS | Project MGR -- |
| Approval |
| Design B. DAVIS | Chief Engineer -- | S & MA D. NEWMAN | Project G. CAVALARIS | Project MGR -- |
| PAC Assignee M. GLASS | PAC Review Complete MG | MSFC Closure Date 12/10/1981 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description 1) REFERENCE: MAR T29609 2) EPOXY PRIMER ON THE TOP HALF OF BARRY MOUNT ON ET-1 WAS REJECTED ON MARS T29609. STRIPPING OF THE SLA OFF OF THE PART REVEALED EXTENSIVE PRIMER LIFT OFF FROM THE CRES SUBSTRATE WITH THE PRIMER REMAINING ADHERED TO THE SLA. LAUNCH CONSTRAINT: NONE |
| Contractor Investigation/Resolution 1) CAUSE: IMPROPER PREPARATION OF METAL SUBSTRATE PRIOR TO PRIMER APPLICATION AS REQUIRED BY PI 5013 METHOD 10. 2) RESOLUTION: A) GENERATED DC&R TO CHECK THE PRIMER ON FORTY-FIVE BARRY MOUNTS STAGED FOR ET-2. COMPLETE. B) R&QE DETERMINE SAMPLE SIZE TO BE USED FOR EVALUATING ET-1 BARRY MOUNT. COMPLETE. C) GENERATED DE&R 7-80-01A TO TEST THE PRIMER ADHERENCE ON THE SAMPLE OR BARRY MOUNT TOP HALVES ON ET-1. COMPLETE - FOURTEEN OUT OF EIGHTEEN BARRY MOUNTS HAD SIGNIFICANT PRIMER DEBOND. AS A RESULT, ALL 48 ET-1 BARRY MOUNTS WERE REMOVED & REPLACED. COMPLETE (REF PRA'S P-ET-1-ST- 0255 & P-ET-ST-254 & O.D ET/MGMT-172). D) MATERIALS ENGINEERING REVERIFY METHOD 10 OF PI 5013 WITH TEST PROGRAM. COMPLETE. REPORT ETTR-101 CONCLUDED THAT METHOD 10 WOULD PROVIDE SURFACE THAT WOULD PRODUCE GOOD PRIMER ADHERENCE. E) MATERIALS ENGINEERING PERFORM TEST PROGRAM TO DUPLICATE ET-1 BARRY MOUNT PRIMER FAILURES & TO DETERMINE CAUSE OF FAILURE. COMPLETE. TEST REVEALED THAT THE UNITS HAD NOT BEEN PROPERLY ABRADED - FAILURE MODE WAS DUPLICATED IN LABORATORY (REF MEMO 3516-80-068). F) REVIEW ET-1 & ET-2 BARRY MOUNT BUILD RECORDS (MAF) TO ISOLATE & IDENTIFY CAUSE OF PRIMER FAILURE. COMPLETE. DISCOVERY WAS THAT 38 OF THE ET-1 BARRY MOUNTS HAD BEEN CLEANED & PRIMED IN THE TPS AREA. G) TPS MATERIALS ENGINEERING INSPEC PRIMER ON THREE BARRY MOUNTS INSTALLED ON THERMAL CONDUCT- ANCE TEST TANK TO EVALUATE PRIMER ADHERENCE SUBSEQUENT TO CRYOGENIC EXPOSURE. COMPLETE. BARRY MOUNTS PASSED PRIMER TEST. H) REVIEW THE BUILD RECORDS FOR ALL CRES PARTS USED ON ET-1 THAT RECEIVED TPS & PREPARE MATRIX THAT DISPLAYS SPECIFIC PROCESSES USED FOR CLEANING & APPLICATION OF TPS. COMPLETE. NIFICANT INFO PROVIDED. I) KSC PERFORM PRIMER ADHESION TEST ON 25 PRIMED STAINLESS STEEL SUBSTRATES OTHER THAN BARRY MOUNTS & FIVE TITANIUM SUBSTRATES. COMPLETE. NO SIGNIFICANT FAILURES. J) RELIABILITY & MATERIALS ENGINEERING REVIEW BARRY MOUNT PROCESSING AT BARRY CONTROLS. COM- PLETE. NO SIGNIFICANT FINDING. K) PROPULSION ENGINEERING PERFORM SPRING RATE TEST OF BARRY MOUNTS TO DETERMINE NEED FOR MATCHED PAIR REQUIREMENT. COMPLETE. MATCHED PAIR NOT REQUIRED. L) GENERATE OPERATIONS DIRECTIVE TO REQUIRE THAT PARTS MUST NOT BE EPOXY PRIMED IN THE TPS AREAS & THAT CLEANED PARTS MUST BE ADEQUATELY PROTECTED. COMPLETE. (REF O.D. ET/MGNT-179 & STP 5013, ADMT 6). M) QUALITY ENGINEERING GENERATE A WORKMANSHIP STANDARD SHOWING PROPER SUBSTRATE PREPARATION PER PI 5013, METHOD 10. (IN-WORK). N) QUALITY ENGINEERING REVISED MPP'S FOR BARRY MOUNTS TO PROVIDE SPECIFIC INSTRUCTIONS FOR SUB- STRATE INSTRUCTRIONS FOR SUBSTRATE PREPARATION (IN-WORK). O) MATERIALS ENGINEERING REVISE STP 5013 METHOD 10 TO CLARIFY REWORK PROCEDURE IF TIME LIMIT IS EXCEEDED. COMPLETE. (REF STP 5013 AMENDMENT 6). 5/8/81 - MMC PRESENTED CAPS T009 AS "LIFTED" CONSTRAINT FOR STS-2 BECAUSE PRIMER ON ET-2 BARRY MOUNTS PASSED SCRAPE TEST PER DC&R T-80-02. MSFC ET PROJECT CONCURRED. 12/1/81 RESOLUTION - INVESTIGATION DETERMINED ET-1 BARRY MOUNTS WITH FAILED PRIMER RESULTED FROM OMISSION OF PROPER SUBSTRATE PREPARATION. STP 5013 METHOD 10 WAS REVISED TO CLARIFY CLEANING PREPARATION REQMNT. RECURRENCE CONTROL - PRIMER FAILURE WAS LIMITED TO ET-1 MOUNTS WHICH WERE NOT PROPERLY PREPARED PRIOR TO PRIMER APPLICATION, HOWEVER TO PRECLUDE RECURRENCE THE FOLLOWING DOCUMENTS WERE REVSIED/ ISSUED TO ASSURE PROPER PREPARATION: O.D. ET/MGMT-179, STP 5013 AMENDMENT 6, PI 5013 METHOD 10 12/1/81 - CLOSURE DISTRIBUTED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A01683 | IFA# -- | Contractor RPT# T-009 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# -- | Asmnt Part Name -- | Asmnt Serial/Lot# -- |
| HCRIT CD -- | FCRIT CD -- | CAUSE CD -- | FAIL MODE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |