Process Specification for Flame Retardant Treatment of Fabrics and Webbings

Engineering Directorate Structural Engineering Division July 2005 National Aeronautics and Space Administration Lyndon B. Johnson Space Center Houston, Texas

Process Specification for Flame Retardant Treatment of Fabrics and Webbings

| Prepared by: | Signature on File |  | 7/15/05 |
| --- | --- | --- | --- |
|  | Julie Henkener Materials and Processes Branch/ES4 |  | Date |
| Prepared by: | Signature on File |  | 7/21/05 |
|  | Rajib Dasgupta Materials and Processes Branch/ES4 |  | Date |
|  | Signature on File |  | 7/22/05 |
| Approved by: | Bradley Files, Acting Chief Materials and Processes Branch/ES4 |  | Date |

| REVISIONS |  |  |
| --- | --- | --- |
| VERSION | CHANGES | DATE |
| -- | Original version | 5/1/2003 |
| A | Added new Scotchgard product formulation. Scotchgard 4101W or Scotchgard 4101 may be used. | 7/25/2005 |

1.0  	SCOPE

This process specification establishes requirements for the application of flame retardant coatings to fabrics and webbings.

2.0  	APPLICABILITY

This process specification applies to flame retardant treatments for fabrics and webbings used in both flight and non-flight hardware.  Specifically it applies to the use of ammonium dihydrogen phosphate solution and Scotchgard 4101W or its replacement product, Scotchgard 4101.

3.0  	USAGE

This process specification shall be called out on the engineering drawing by using a drawing note that identifies the surface(s) to be coated.  One example of a standard callout is:

APPLY FLAME RETARDANT TREATMENT TO ALL SURFACES OF FABRIC PER NASA/JSC PRC-4005

The materials used for the flame retardant coating are not required to be listed in the drawing’s parts list.

## 3.1	WORK INSTRUCTIONS

Work instructions shall be generated for implementing this process specification.  The work instructions shall contain sufficient detail to ensure that the manufacturing process produces consistent, repeatable products that comply with this specification.

4.0  	REFERENCES

NASA-STD-6001	Flammability, Odor, Offgassing, and Compatibility Require-ments and Test Procedures for Materials in Environments that Support Combustion, February 1998.

5.0	MATERIAL REQUIREMENTS

The ammonium dihydrogen phosphate and Scotchgard 4101 or 4101W shall be used within the shelf life that is listed for each product.  The ammonium dihydrogen phosphate is GFS Chemicals P/N 13231 or P/N 13232.   Scotchgard 4101W is a 3M product that may no longer be available.  3M has indicated that the replacement product is Scotchgard 4101 and it has been screened at White Sands Test Facility for flammability and toxicity.

6.0  	PROCESS REQUIREMENTS

6.1 	PRE-TREATMENT PREPARATION

The surfaces of the fabric or webbing to be chemically treated shall be clean and dry prior to beginning the flame treatment process.

6.2	FLAME RETARDANT TREATMENT PROCESS SUMMARY

The fabric or webbing to be treated is immersed in an ammonium dihydrogen phosphate solution (6-7 oz by weight with 1 gallon deionized water) for 30 minutes.  Do not rinse.  Allow material to dry for a minimum of 24 hours.  Apply 2 coats of the Scotchgard 4101 or 4101W to each side of the fabric or webbing.

7.0	PROCESS QUALIFICATION

The flame retardant treatment process described in section 6.2 has already been qualified for flammability resistance.  Any new formulation must be qualified such that it will pass the NASA-STD-6001 Test 1 flammability test.

8.0	PROCESS VERIFICATION

When visually examined in its finished form, the appearance of the flame retardant coating shall be uniform and free of contamination, crystalline residue, streaking or other surface irregularities.

9.0	TRAINING AND CERTIFICATION OF PERSONNEL

All flame retardant treatment operations shall be performed by personnel who have received on-the-job training for this process.  No formal qualification or certification of employees is required.

10.0	DEFINITIONS

Flame retardant	The condition of a fabric or webbing that has been treated in order to reduce its flammability.