Process Specification for Electrodeposited Nickel Plating

Engineering Directorate Structural Engineering Division October 2004 National Aeronautics and Space Administration Lyndon B. Johnson Space Center Houston, Texas

Process Specification for Electrodeposited Nickel Plating

| Prepared by: |  |  |  |
| --- | --- | --- | --- |
|  | Julie A. Henkener, Materials and Processes Branch/ES4 |  | Date |

| Approved by: |  |  |  |
| --- | --- | --- | --- |
|  | Brad S. Files, Acting Chief Materials and Processes Branch /ES4 |  | Date |

| REVISIONS |
| --- |
| VERSION | CHANGES | DATE |
| Baseline | Original version | 5/14/96 |
| A | Typo on p. 3, formatting, and increased bakeout for steel alloys | 7/14/98 |
| B | Changed EM2 references to ES4, reviewed for accuracy | 6/2004 |
| C | Updated specification reference to AMS-QQ-N-290 | 10/2004 |

1.0  	SCOPE

This process specification establishes technical requirements for the application of electrodeposited nickel plating on steel, copper and copper alloys, and zinc and zinc alloys.

2.0  	APPLICABILITY

This process specification applies to the electrodeposition of nickel plating on substrates of steel, copper, zinc, and their alloys.

3.0 	USAGE

This process specification shall be called out on the engineering drawing by using a drawing note that identifies the process specification, the class, and the grade (if applicable).  For example:

NICKEL PLATE PER NASA/JSC PRC 5004, CLASS 1, GRADE D.

The two classes of electrodeposited nickel plating are:

Class 1		Corrosion protective nickel plating (0.0002-0.0016 in. thick)

Class 2		Engineering nickel plating (>0.002 in. thick)

Class 1 plating is used to protect iron, copper, or zinc alloys against corrosive attack in rural, industrial, or marine environments, which varies depending on the thickness of the nickel deposit.  It may also be used as an undercoat for a chromium plating or for aesthetic purposes.

Class 2 plating is used primarily for wear resistance, abrasion resistance, and incidental corrosion protection.  Heavy deposits of Class 2 plating, such as those produced by the Watts bath process, may be used for build-up of worn or undersized parts.

Class 1 nickel plating shall be one of the following grades, as-specified on the engineering drawing:

Grade A		0.0016 in. thick		Grade E	0.0006 in. thick

Grade B		0.0012 in. thick		Grade F	0.0004 in. thick

Grade C		0.0010 in. thick		Grade G	0.0002 in. thick

Grade D		0.0008 in. thick

The default thickness for a Class 2 nickel plating is 0.003 in.  If a different thickness is desired, it must be 0.002 in. or greater, and it must be specified on the engineering drawing.

- WORK INSTRUCTIONS

Work instructions shall be generated for implementing this process specification.  The work instructions shall contain sufficient detail to ensure that the manufacturing process produces consistent, repeatable products that comply with this specification.

4.0	REFERENCES

The following references were used in developing this process specification:

SOP-007.1		Preparation and Revision of Process Specifications

JSC 8500C		Engineering Drawing System Requirements

The following document is called out as an extension of the requirements given in this specification:

AMS-QQ-N-290	Aerospace Material Specification/Nickel Plating (Electrodeposited)

5.0		MATERIALS REQUIREMENTS

The materials used shall meet the requirements of AMS-QQ-N-290.

6.0  	PROCESS REQUIREMENTS

All electrodeposited nickel plating shall be applied according to the requirements of AMS-QQ-N-290 with the following exception:

All steel parts which have a hardness of Rockwell C40 and higher shall be subjected to a hydrogen bakeout procedure immediately following plating.  The parts shall be baked at 375 +/- 25(F for a minimum of 23 hours to provide hydrogen embrittlement relief.

7.0	PROCESS QUALIFICATION

Not required.

- PROCESS VERIFICATION

The process verification shall include visual examination, adhesion tests, and thickness measurements, as-specified by AMS-QQ-N-290A  In addition, steel parts shall be tested for hardness.  All steel parts having a hardness of Rockwell C40 or higher shall be baked out within 4 hours of the plating process at a minimum of 375 +/- 25(F for a duration of 23 hours or longer for hydrogen embrittlement relief.

9.0	TRAINING AND CERTIFICATION OF PERSONNEL

This nickel plating process shall be performed by personnel qualified to conduct the process through training or experience.  If this process is performed by an outside vendor, the development of an appropriate training program shall be the responsibility of the vendor.

10.0	DEFINITIONS

Electrodeposition	The electrodeposition process consists of putting a conductive material from a plating solution onto a substrate by the application of an electric current.

Substrate			The material, component, or workpiece to which the nickel plating is deposited.