Project Number:  AW-2271

Contract Number:  TW-0663

November 4, 1994

SPECIAL SPECIFICATION

SECTION 09200

STUCCO SYSTEM

Page

PART 1 - GENERAL

1.01	Description Of Work	2

1.02	Quality Assurance	2

1.03	Submittals	2

1.04	Delivery, Storage And Handling	3

1.05	Job Conditions	3

PART 2 - PRODUCTS

2.01	Materials	4

2.02	Metal Accessories	5

PART 3 - EXECUTION

3.01	Inspection	6

3.02	Mixing	7

3.03	Application	7

3.04	Scaffolding	9

3.05	Cutting And Patching	10

3.06	Cleaning And Protection	10

SPECIAL SPECIFICATION

SECTION 09200

STUCCO SYSTEM

PART 1 - GENERAL

1.01	DESCRIPTION OF WORK

The location and extent of stucco system on exterior wall surfaces is indicated on drawings.

A.	Work includes pre-mixed, fiber-reinforced portland cement plaster basecoat concentrate for job site mixing with sand to provide scratch and brown coats to receive exterior wall finish coat system.

B.	Pre-mixed, pre-sanded, colored acrylic polymer based finish coat system.

1.02	QUALITY ASSURANCE

A.	Single Resource Responsibility:  Obtain all lath and cement plaster finish coat system and all other materials for the stucco system from a single manufacturer.

B.	Requirements of Regulatory Agencies:  Install stucco basecoat system to comply with all applicable codes and standards and with requirements of local agencies having jurisdiction.

C.	Applicator Qualifications:  Application of similar stucco system for at least five years of experience and projects equal in scope to this work.

D.	Allowable Tolerances:  Maximum deviation from true plane 1/8" in 10 ft. as measured by straight edge placed at any location on surface.

E.	All materials used shall not contain asbestos fibers.

1.03	SUBMITTALS

A.	Product Data:  Submit manufacturer's product data for cementitious materials, colors, lath, metal support components, and accessories.

B.	Material Certificates:  Submit producer's certificate for each kind of plaster aggregate indicated evidencing that materials comply with requirements.

C.	Samples:  Two 2'-0" X 2'-0" minimum panels at job site, showing application workmanship, texture, techniques and colors.  Sample panel to be approved by the Sandia Designated Representative (SDR) and noted as to color and texture ranges.

D.	Do not proceed with work until sample stucco finish is reviewed and approved by SDR.  Maintain sample panel on project site for duration of project for comparison purposes.  Remove sample upon project completion or when directed by the SDR.

1.04	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original unopened packages, containers or bundles bearing brand name and identification of manufacturer.

B.	Store materials inside, under cover and in manner to keep them dry, protected from weather, direct sunlight, surface contamination, aging, corrosion, and damage from construction traffic and other causes.

C.	Environmental Requirements, General:  Comply with requirements of referenced stucco application standards and recommendations of stucco manufacturer for environmental conditions before, during, and after application of stucco.

D.	Remove wet or deteriorated materials from site.

1.05	JOB CONDITIONS

A.	Environmental requirements:

1.	Cold Weather Requirements:

a.	Do not use frozen materials in cement plaster mixes.

b.	Do not apply cement plaster to frozen surfaces or surfaces containing frost.

c.	Do not apply cement plaster when ambient temperature is less than 44 degrees F (4.4 degrees C) or expected to drop below 44 degrees F for 24 hours.

2.	Hot Weather Requirements:

a.	Protect cement plaster from uneven and excessive evaporation during hot, dry weather.  Wet cure basecoat a minimum twice daily for a minimum of 48 hours.

b.	Do not apply cement plaster when ambient temperature is above 100 deg. F.

B.	Protection:

1.	Protect finished surfaces installed prior to plastering.

2.	Maintain protection in place until completion of work.

PART 2 - PRODUCTS

2.01	MATERIALS

A.	Fiber-Reinforced Portland Cement Plaster Basecoat Concentrate:

Manufacturer's standard pre-mixed stucco basecoat consisting of portland cement and alkali resistant glass and acrylic fibers.

Product/Manufacturer:  FIBER-47 Concentrate as manufactured by El Rey Stucco Company, Inc., or approved equal.

B.	Exterior Wall Finish Coat System:

1.	Manufacturer's standard premixed exterior wall finish consisting of acrylic polymers, properly graded aggregates and colorant.

a.	Color:  As selected at time of submittals.

b.	Finish Texture:  Medium Brocade.

c.	Product/Manufacturer:  PERMA-FLEX as manufactured by El Rey Stucco Co., Inc., or approved equal.

C.	Sand:

1.	Comply with all requirements of ASTM C 897.

2.	Gradation:

US Standard Sieve	Weight Retained

No. 4	0%

No. 8	0-10%

No. 16	10-40%

No. 30	30-65%

No. 50	70-90%

No. 100	95-100%

D.	Water:  Potable

E.	Bonding Agent:

1.	Acrylic bonding agent as manufactured and as recommended by stucco basecoat system manufacturer.

2.	Product/Manufacturer:  PERMA-FLEX 400 as manufactured by El Rey Stucco Company, Inc., or approved equal.

F.	Metal Lath:  (ASTM C1063-86)

1.	Diamond Mesh:  Shall be US Gypsum Co.'s self-furring Diamond Mesh metal lath, weighing 3.4 lbs. per square yard , to be used on horizontal surfaces and as reinforcing around doors and windows.

2.	Stucco Lath:  Shall be Davis Walker 17 ga. self-furring stucco netting, or approved equal.  To be used on framing at 16" o.c. or less.

a.	Screw attach with minimum 1/2" penetration into steel stud attached every 6" at every stud.

b.	Masonry screw attach for application into CMU.

G.	Plywood Sheathing:  Waferboard, sheathing grade, Louisiana Pacific "Inner-Seal" or equal, by general contractor - see drawings for different requirements in rated and non-rated areas.  Gap all wood sheathing at least 1/8".

H.	Gypsum Sheathing:  Exterior grade, by general contractor - see drawings for different requirements in rated and non-rated areas.

I.	Weather Resistive Barrier:  Two layers of grade "D", 15 pound building paper over wood sheathing, one layer over gypsum sheathing attached per industry standards and Code requirements.

J.	Install lath in accordance with ASTM C1063, wire-tying control joints to mesh.  Do not attach to framing.

2.02	METAL ACCESSORIES

A.	General:  Utilize manufacturer's suggested construction details, and as shown on the drawings.

B.	Metal Accessories:  Manufacturer's suggested steel products unless otherwise indicated as Zinc Alloy.  Do not fill with plaster or cement.

1.	Exterior Components:  Hot dip galvanized finish, ASTM A525, G90 for 18 gauge and lighter, ASTM A123 for galvanized after fabrication for 16 gauge and heavier products.

2.	Corner Beads:  J-Metal or plaster stop, general purpose type with expanded or perforated flanges.  (Exterior Corners)

3.	Cornerite:  Manufacturer's standard preformed interior corner reinforcement made from 2.5 lbs./sq. yd. of diamond mesh lath.  (Interior Corners)

4.	Square-Edged Casing Beads:  Expanded or flanged to suit application.  (For Square Corners)

5.	No. 10x Bull Nose Corner Bead:  For rounded corner reinforcement. (Rounded Corners)

6.	Control Joints:  No. XJ15-3 control joint with 1/4" slot, and 1" grounds, or equal.  Control joints must be wire tied to the lath and not nailed or screwed to substrate.

7.	Expansion Joints:  No. 40 adjustable expansion joint, free floating with adjustments from 1/4" to 5/8".

8.	Weep Screeds:  No. 7 Foundation Sill Screed, with holes for drainage.

9.	Fasteners:  (CMU Applications) Galvanized steel of furring type and length suitable for at least 1/2" penetration of the brick or block substrate.

10.	Fasteners:  (Steel Stud Applications)  Furring nails and or screws, galvanized steel of type and length suitable for at least a 2/3" penetration of the steel stud system.

11.	Stucco which abuts windows, doors, or other terminations must be terminated with casing bead by El Rey Stucco Company, or approved equal.

C.	Apply plaster screeds at a maximum of 12'-0" o.c. to allow for rodding.

PART 3 - EXECUTION

3.01	INSPECTION

A.	Inspection for Base Coats:

1.	Verify that surfaces to be plastered are free of dust, loose particles, oil and other deleterious materials which would affect bond or proper hydration of cement plaster.

2.	Verify that lath is tight, properly secured and overlapped, and that all accessories are properly set and secured.

3.	Examine substrates, grounds and accessories to ensure that finished plaster work will be true to line, plane, level and plumb.

4.	Verify that masonry and concrete surfaces to receive direct bond applications of plaster base coats are rough or otherwise properly prepared to provide adequate bond.  All masonry surfaces are to be metal lathed with one layer of grade "D" building paper to provide adequate bond.

5.	Installer shall notify General Contractor and SDR in writing of any conditions detrimental to proper and successful installation of stucco base coats.  Do not proceed with installation until unsatisfactory conditions are corrected to satisfaction of SDR and Installer.

B.	Inspection for Finish Coat:

1.	Verify that surfaces to receive exterior wall finish coat are free of dust, loose particles, oil and other deleterious materials which would adversely affect bond of exterior wall finish.

2.	Examine base coats, grounds and accessories to ensure that finished work will be true to line, plane, level and plumb.

3.02	MIXING

A.	General:

1.	Accurately proportion materials for each plaster batch with measuring devices of known volume.

2.	Size batches for complete use within maximum of one hour after mixing.

3.	Retemper plaster stiffened from evaporation, but do not use or retemper partially hydrated cement plaster.

4.	Do not use frozen, caked or lumpy materials, and remove such materials from job site immediately.

5.	Mix factory prepared cement plaster in accordance with manufacturer's written instructions and recommendations.

6.	Use moist, loose sand in proportions recommended by basecoat concentrate manufacturer.

7.	Withhold 10% of mixing water until mixing is nearly complete, then add as needed to produce desired working consistency.

B.	Polymer Based Tinted Wall Finish:

1.	Add very small amounts of water as needed at job site to adjust consistency of finish coat material for application method required.

2.	Mix finish in accordance with manufacturer's written instructions and recommendations.

C.	Mechanical Mixing:

1.	Mix materials with machine driven paddle.

2.	Clean mixer of set or hardened materials before loading new batch.

3.	Maintain mixer in continuous operation while adding materials.

4.	Conform to mixing sequence, cycle of operations, and time recommended by the manufacturer of the basecoat mix materials.

D.	Hand Mixing:

1.	Do not hand mix stucco basecoat system materials unless authorized by SDR.

2.	Use waterproof mixing boxes and water barrels when mixing within building.

3.03	APPLICATION

A.	General:

1.	Apply cement plaster by hand and in accordance with manufacturer's instructions and recommendations, and in compliance with requirements of applicable codes, regulations and agencies having jurisdiction.

2.	Interrupt cement plaster only at junctions of plaster planes, at openings, or at control joints.

3.	Tool through second and finish coats to produce "V" joint at intersection of frames or other items of metal or wood which act as plaster grounds.

4.	Apply second coat to first coat, bringing out to grounds, flat to true surface, and free of imperfections which would reflect in finish coat.

5.	Reconsolidate and even plane of second coat.  Trowel to smooth and uniform surface to receive acrylic polymer based finish.

6.	Nominal plaster thicknesses = 1":

a.	First coat:  3/8"+ (10 mm)

b.	Second coat:  3/8"+ (10 mm)

c.	Third coat:  1/8" (3 mm)

B.	Base Coats:

1.	Over Metal Lath Base:

a.	Apply with sufficient material to form keys through metal lath.

b.	Embed and fill all spaces of lath and scratch vertical surfaces horizontally.

c.	Scratch horizontal surfaces in one direction only, prior to initial set, using sufficient trowel pressure to key plaster into lath or to create bond to substrate as applicable.

2.	Over Solid Bases:

a.	Apply first coat with sufficient pressure to insure tight contact with complete coverage of solid bases, immediately scratching to provide mechanical key for second coat.

3.	Second Coat:

a.	Apply second coat with sufficient pressure to insure tight contact with first coat.

b.	Bring surface to true and even plane.

c.	Float to uniformly rough surface to provide bond for acrylic polymer finish coat.

d.	Tool brown coat to provide a v-joint at intersection of plaster with frames or other item of wood, or metal.

C.	Primer:  Apply primer with brush, roller or spray for complete coverage of area to receive polymer based finish.

D.	Finish Coats:

1.	Apply plaster in number of coats and consistency to achieve required texture, to minimal thickness specified, using sufficient trowel pressure to bond finish coat to basecoat.

2.	Texture finish coat to match acceptable samples.

E.	Workmanship shall be neat and in accordance with the best standards of workmanship.  Entire coated surfaces must appear to be evenly applied, without excess lumping or surface irregularities.  Cut, patch, and repair stucco system as necessary to accommodate other work and to restore dents and imperfections. Repair or replace work to eliminate blisters, buckles, similar defects, and where bond to the substrate has failed.  No patch work shall be evident.

F.	Curing:

COAT	FIRST	SECOND	THIRD

Minimum Period

Moist Curing	48 Hours	 72 Hours	48 Hours

Minimum 			Protect from

Interval			dust and water

Between Coats	48 Hours	7 Days	for a minimum of

12 hrs. following					application

1.	Maintain moist conditions by fogging mist.  Do not saturate.

2.	Moist cure each coat of stucco base coat system sufficiently frequently to maintain uniform moisture continuously for a minimum of 48 hours after application.

3.	Moist cure brown coat continuously for a minimum of 72 hours.

4.	Air cure polymer based finish cot.  Do not wet coat.

5.	In freezing weather, do not apply stucco unless special precautions are taken to keep materials above 50o F. during mixing and 48 hours thereafter.

3.04	SCAFFOLDING

The stucco contractor shall provide all necessary planks and scaffolding required for his work.

3.05	CUTTING AND PATCHING

Cut, patch, point-up and repair stucco as necessary to accommodate other work and to repair cracks, dents and imperfections.  Repair or replace work to eliminate blisters, buckles, excessive crazing and check cracking, dry-outs, efflorescence, sweat-outs and similar defects, and where bond to the substrate has failed.  Point-up plaster around trim and other locations where plaster meets dissimilar material.  Cut out and patch stained or discolored finished plaster not scheduled to be painted.  Match patch of defective or damaged plaster to existing work in form, texture and color.

3.06	CLEANING AND PROTECTION

Remove temporary protection and enclosure of other work.  Promptly remove stucco from door frames, windows, and other surfaces which are not to be stuccoed.  Repair floors, walls and other surfaces which have been stained, marred or otherwise damaged during the stuccoing work.  When stucco work is completed, remove unused materials, containers and equipment and clean grounds of stucco debris.

END OF SECTION