MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A16519 | In-Flight Anomaly Number -- | Contractor Report Number P-077A | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LH2 SIPHON COVER JOINT LEAK |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE ET COMPLETE | PART# 80901006000-059 | SER/LOT# ET-80 | MANUFACTURER LMMSS |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE NAFLEX SEAL | PART# 55L11-7T | SER/LOT# 8354900855 | MANUFACTURER LANGLEY |
| Test/Operation LF - FDF | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode MV - EXT LEAK | Cause MAT - MFG-ASY-EQUP |
| System PROPULSION | Defect DA - ROUGH | Material P - SEAL | Work Contact DAVE O`NEAL | Fail Date 05/05/1995 |
| Received at MSFC 06/09/1995 | Date Isolated 05/09/1995 | FMEA Reference 2.10.6.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location -- | Symptom MV - EXT LEAK | Time Cycle -- |
| Effectivity Text ET-80 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/15/2001 | CN RSLV SBMT -- | Defer Date -- | Add Date 06/09/1995 | R/C Codes 0 - EXPL -- -- |
| Assignee |
| Design -- | Chief Engineer -- | S & MA -- | Project -- | Project MGR -- |
| Approval |
| Design -- | Chief Engineer -- | S & MA -- | Project -- | Project MGR -- |
| PAC Assignee J. NELSON | PAC Review Complete JN | MSFC Closure Date 06/09/1995 | Status E - CLOSED-E | F/A Completion 05/09/1995 |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N005973 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description THE LH2 SIPHON COVER JOINT LEAKED AT 472 SCCM WHICH EXCEEDED THE ALLOWABLE LEAK RATE OF 20 SCCM PER TP-8C101-FA CRITICALITY: THE NAFLEX SEAL IS CRIT.1 FMEA ITEM CODE 2.10.6.1; "LEAKAGE" REV "A": CLOSES TASKS I.A, I.B, I.C AND ADDS I.D (SEE ASTERISKS) |
| Contractor Investigation/Resolution GENERAL: DURING THE DUAL SEAL CAVITY LEAK CHECK OF THE LH2 SIPHON COVER IN FINAL ASSEMBLY, A 472 SCCM LEAK WAS DETECTED. THE ALLOWABLE LEAKAGE IS 20 SCCM, MAXIMUM, AT 6.0+/-0.5 PSIG GHE AS TESTED PER TP-8C101-FA THIS FLANGE USES A TEFLON COATED NAFLEX SEAL (55L11-7T), INSTALLED IN THE VAB CELL "A" WITH THE ET IN A VERTICAL ATTITUDE TROUBLE SHOOTING STEPS DETECTED NO TEST EQUIPMENT MALFUNCTION. AN INSPECTION WITH GHE MASS SPEC DETECTED INDICATIONS OF SECONDARY SEAL LEAKAGE AT APPROXIMATELY THE 2:00 - 2:30, 6:00 - 7:30 AND 11:30 POSITIONS, HOWEVER, THESE INDICATIONS COULD NOT BE QUANTIFIED. UPON JOINT DISASSEMBLY A PIECE OF TEFLON/PLASTIC SHAVING WAS FOUND ALONG THE -Z LIP OF THE COVER. A DETAILED INSPECTION PERFORMED ON THE SEAL FOUND AN AREA ON THE PRIMARY SEAL LIP, RUNNING CIRCUMFERENTIALLY FOR APPROXIMATELY 0.5 INCHES WHERE NO EVIDENCE OF SEAL TO FLANGE CONTACT WAS PRESENT, I.E. NO CONTACT WITNESS MARK. FURTHER INSPECTION FOUND A DISHED AREA AT THESE LOCATION WITH NO DISRUPTION OR DAMAGE TO THE TEFLON COATING PRESENT THIS SEAL WAS MANUFACTURED BY LANGLEY CORPORATION. THE SEAL SERIAL NUMBER IS 835490085517 TASK I. FAILURE /PROBLEM INVESTIGATION * A. INSPECT THE SEAL AND TANK COVER FOR CONFORMANCE TO ENGINEERING REQUIREMENTS RESPONSIBILITY: D. O'NEAL/3741 - D. WESTPHAL/3740 V. PHELPS/3724 - D. OWENS/3720 J. SPRAY/3725 - D. OWENS/3720 COMPLETE 5/17/95 CLOSURE STATEMENT VISUAL AND DIMENSIONAL INSPECTIONS WERE PERFORMED ON THE SEAL THE VISUAL INSPECTION FOUND ONE AREA ON THE PRIMARY SEAL LIP WITH NO EVIDENCE OF TEFLON COMPRESSION (WITNESS MARK) EXTENDING FOR APPROXIMATELY 0.5 INCHES CIRCUMFERENTIALLY ALONG THE LIP, INDICATING NO SEAL TO FLANGE CONTACT. A SUBTLE LOW AREA WAS DETECTED BY "FEEL" (UNGLOVED FINGER) AND VISUALLY ONCE THE AREA WAS KNOWN. NO DISRUPTION OR DAMAGE TO THE TEFLON WAS NOTED. UPON STRIPPING THE COATING FROM THE DEFECT AREA, THE SUBSTRATE WAS FOUND TO HAVE A UNIFORM, ETCHED OR SANDBLASTED APPEARANCE WITH NO SURFACE DISRUPTIONS THE DIMENSIONAL INSPECTION OF THE DEFECT AREA WITH THE TEFLON INTACT FOUND THE TRANSITION OF THE DEPRESSION TO BE GRADUAL OVER APPROXIMATELY A ONE INCH AREA WITH THE LOW POINT 0.004 INCHES LOWER THAN ADJACENT AREAS. WITH THE TEFLON REMOVED, THE LOW POINT MEASURED 0.005 INCHES LOWER THAN ADJACENT AREAS, A VIOLATION OF THE 0.0003 INCH/INCH REQUIREMENT FOR WAVINESS. THE PRIMARY SEAL HEIGHT WAS 0.0027 INCHES BELOW THE MINIMUM ALLOWABLE. THE REQUIREMENT PRIOR TO COATING IS 0.006 + 0.000/-0.002; THE LOWEST SEAL HEIGHT WAS MEASURED AT 0.0013 INCHES. THE SEAL THICKNESS RELATIVE TO THE OUTER SEAL DIAMETER AND SECONDARY SEALING SURFACE MET REQUIREMENTS, SHOWING NO NEGATIVE TAPER. REFERENCE NCD N005992 THE TANK FLANGE AND SIPHON COVER WERE INSPECTED WITH NO ANOMALIES FOUND. A SUCCESSFUL REINSTALLATION OF THE COVER WAS PERFORMED USING A NEW SEAL, THE LEAK RATE TESTING AT 0.1 SCCM * B. REVIEW SEAL BUILD HISTORY AND INSPECTION REQUIREMENTS FOR ACCEPTANCE RESPONSIBILITY: D. O'NEAL/3741 - D. WESTPHAL/3740 S. THOMPSON/3761 - S. PARIKH/3760 COMPLETED 5/18/95 CLOSURE STATEMENT A REVIEW OF RECEIVING INSPECTION RECORDS SHOW THE SEAL WAS ACCEPTED AT MAF 11/15/93 AS AN INITIAL RECEIPT. ACCEPTANCE REQUIREMENTS CONSISTED OF VERIFYING PACKAGING, IDENTIFICATION AND MARKINGS, AND VENDOR CERTIFICATIONS AND PERFORMING A VISUAL INSPECTION ON THE SEAL THROUGH THE PRIMARY ACLAR BAG AFTER REMOVAL FROM THE OUTER POLYETHYLENE BAG. THIS INSPECTION ASSURES NO TEFLON DEFECTS EXIST ON THE PRIMARY AND SECONDARY SEALING SURFACES AND THAT THE PARTS ARE FREE FROM BURRS AND SLIVERS. PRIOR TO INSTALLATION, THE SEALS ARE AGAIN VISUALLY INSPECTED THE SUPPLIER REPORTED INSPECTIONS CONSISTING OF DIMENSIONAL INSPECTIONS PERFORMED AFTER MACHINING/DRILLING AND SANDBLASTING FOR TEFLON APPLICATION, INCLUDING INSPECTION OF THE PRIMARY SEAL HEIGHT ON AN INCH PER INCH BASIS, DIMENSIONAL INSPECTIONS FOR TEFLON THICKNESS DURING AND AFTER APPLICATION, AND VISUAL INSPECTIONS PERFORMED AFTER TEFLON APPLICATION, AFTER CLEANING AND PRIOR TO PACKAGING FOR SHIPMENT. LANGLEY HAS REPORTED THAT THIS PARTICULAR SEAL WAS REWORKED DUE TO CONTAMINATION. REFERENCE LANGLEY COMMUNICATION, DATED 5/5/95, AND CCMAIL FROM PROCUREMENT QUALITY, DATED 5/16/95 * C. ISSUE A SCAR TO SUPPLIER FOR CAUSE AND CORRECTIVE ACTION RESPONSIBILITY: M. MCANDREW/3742 - D. WESTPHAL/3740 COMPLETE 5/5/95 CLOSURE STATEMENT SCAR 95-064 ISSUED 5/5/95 * D. SUPPLIER (LANGLEY CORPORATION) TO EVALUATE THE SEAL DEFECT AND REVIEW THEIR MANUFACTURING PROCESSES FOR CAUSE DETERMINATION AND IMPLEMENT CORRECTIVE ACTIONS TO PREVENT RECURRENCE RESPONSIBILITY: R. TORTORICH/3760 - S. PARIKH/3760 ECD: 6/15/95 CLOSURE STATEMENT PENDING TASK COMPLETION CAUSE PENDING INVESTIGATION RESULTS TASK II. CORRECTIVE ACTION PENDING CAUSE IDENTIFICATION TASK III. CLEARANCE OF EFFECTIVITIES ET-80 JOINT REWORKED. INSTALLATION ACCEPTABLE ALL OTHERS, NO ISSUE. PROBLEMS OF THIS NATURE ARE DETECTED DURING ACCEPTANCE TEST NOTE: THIS IS ALSO THE DEFERRAL RATIONALE TASK IV. CAPS CLOSURE SUMMARY PENDING THE COMPLETION OF ALL TASKS THIS CAPS IS OPEN |
| MSFC Response/Concurrence 6/9/95 - THIS PROBLEM REPORT WAS OPENED IN ERROR. IT IS A DUPLICATE PROBLEM REPORT NUMBER A16486. TRACKING OF THIS NONCONFORMANCE SHALL BE REPORTED ON PR #A16486. JESSE M. NELSON - ET AE |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A16519 | IFA# -- | Contractor RPT# P-077A | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 55L11-7T | Asmnt Part Name NAFLEX SEAL | Asmnt Serial/Lot# 835490085517 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MAT - MFG-ASY-EQUP | FAIL MODE MV - EXT LEAK |
| Asmnt FMEA 2.10.6.1 | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |