MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A16486 | In-Flight Anomaly Number -- | Contractor Report Number P-077 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LH2 SIPHON COVER JOINT LEAK |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE ET COMPLETE | PART# 80901006000-059 | SER/LOT# ET-80 | MANUFACTURER LMMSS |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE NAFLEX SEAL | PART# 55L11-7T | SER/LOT# 8354900855 | MANUFACTURER LANGLEY |
| Test/Operation LF - FDF | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode MV - EXT LEAK | Cause MAT - MFG-ASY-EQUP |
| System PROPULSION | Defect DA - ROUGH | Material P - SEAL | Work Contact DAVE O`NEAL | Fail Date 05/05/1995 |
| Received at MSFC 05/11/1995 | Date Isolated 05/09/1995 | FMEA Reference 2.10.6.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location AF | Symptom MV - EXT LEAK | Time Cycle -- |
| Effectivity Text ET-80 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date 11/18/1995 | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/15/2001 | CN RSLV SBMT -- | Defer Date -- | Add Date -- | R/C Codes 0 - EXPL -- -- |
| Assignee |
| Design M. MOOREY | Chief Engineer M. PESSIN | S & MA M. SMILES | Project -- | Project MGR P. COUNTS |
| Approval |
| Design M. MOORE | Chief Engineer M. PESSIN | S & MA M.D. SMITH | Project -- | Project MGR P. V. COUNTS |
| PAC Assignee J. NELSON | PAC Review Complete JMN | MSFC Closure Date 07/07/1995 | Status C - CLOSED | F/A Completion 05/09/1995 |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N005973 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description THE LH2 SIPHON COVER JOINT LEAKED AT 472 SCCM WHICH EXCEEDED THE ALLOWABLE LEAK RATE OF 20 SCCM PER TP-8C101-FA CRITICALITY: THE NAFLEX SEAL IS CRIT.1 FMEA ITEM CODE 2.10.6.1; "LEAKAGE" REV "B": CLOSES TASKS I.D., II AND IV AND CLOSES CAPS.(SEE ASTERISKS) |
| Contractor Investigation/Resolution GENERAL: DURING THE DUAL SEAL CAVITY LEAK CHECK OF THE LH2 SIPHON COVER IN FINAL ASSEMBLY, A 472 SCCM LEAK WAS DETECTED. THE ALLOWABLE LEAKAGE IS 20 SCCM, MAXIMUM, AT 6.0+/-0.5 PSIG GHE AS TESTED PER TP-8C101-FA THIS FLANGE USES A TEFLON COATED NAFLEX SEAL (55L11-7T), INSTALLED IN THE VAB CELL "A" WITH THE ET IN A VERTICAL ATTITUDE TROUBLE SHOOTING STEPS DETECTED NO TEST EQUIPMENT MALFUNCTION. AN INSPECTION WITH GHE MASS SPEC DETECTED INDICATIONS OF SECONDARY SEAL LEAKAGE AT APPROXIMATELY THE 2:00 - 2:30, 6:00 - 7:30 AND 11:30 POSITIONS, HOWEVER, THESE INDICATIONS COULD NOT BE QUANTIFIED. UPON JOINT DISASSEMBLY A PIECE OF TEFLON/PLASTIC SHAVING WAS FOUND ALONG THE -Z LIP OF THE COVER. A DETAILED INSPECTION PERFORMED ON THE SEAL FOUND AN AREA ON THE PRIMARY SEAL LIP, RUNNING CIRCUMFERENTIALLY FOR APPROXIMATELY 0.5 INCHES WHERE NO EVIDENCE OF SEAL TO FLANGE CONTACT WAS PRESENT, I.E. NO CONTACT WITNESS MARK. FURTHER INSPECTION FOUND A DISHED AREA AT THESE LOCATION WITH NO DISRUPTION OR DAMAGE TO THE TEFLON COATING PRESENT THIS SEAL WAS MANUFACTURED BY LANGLEY CORPORATION. THE SEAL SERIAL NUMBER IS 835490085517 TASK I. FAILURE /PROBLEM INVESTIGATION A. INSPECT THE SEAL AND TANK COVER FOR CONFORMANCE TO ENGINEERING REQUIREMENTS RESPONSIBILITY: D. O'NEAL/3741 - D. WESTPHAL/3740 F. HARRIS/3726 - D. OWENS/3720 J. SPRAY/3725 - D. OWENS/3720 COMPLETE 5/17/95 CLOSURE STATEMENT VISUAL AND DIMENSIONAL INSPECTIONS WERE PERFORMED ON THE SEAL THE VISUAL INSPECTION FOUND ONE AREA ON THE PRIMARY SEAL LIP WITH NO EVIDENCE OF TEFLON COMPRESSION (WITNESS MARK) EXTENDING FOR APPROXIMATELY 0.5 INCH CIRCUMFERENTIALLY ALONG THE LIP, INDICATING NO SEAL TO FLANGE CONTACT. A SUBTLE LOW AREA WAS DETECTED BY "FEEL" (UNGLOVED FINGER) AND VISUALLY ONCE THE AREA WAS KNOWN. NO DISRUPTION OR DAMAGE TO THE TEFLON WAS NOTED. UPON STRIPPING THE COATING FROM THE DEFECT AREA, THE SUBSTRATE WAS FOUND TO HAVE A UNIFORM, ETCHED OR SANDBLASTED APPEARANCE WITH NO SURFACE DISRUPTIONS THE DIMENSIONAL INSPECTION OF THE DEFECT AREA WITH THE TEFLON INTACT FOUND THE TRANSITION OF THE DEPRESSION TO BE GRADUAL OVER APPROXIMATELY A ONE INCH AREA WITH THE LOW POINT 0.004 INCHES LOWER THAN ADJACENT AREAS. WITH THE TEFLON REMOVED, THE LOW POINT MEASURED 0.005 INCHES LOWER THAN ADJACENT AREAS, A VIOLATION OF THE 0.0003 INCH/INCH REQUIREMENT FOR WAVINESS. THE PRIMARY SEAL HEIGHT WAS 0.0027 INCHES BELOW THE MINIMUM ALLOWABLE. THE REQUIREMENT PRIOR TO COATING IS 0.006 + 0.000/-0.002; THE LOWEST SEAL HEIGHT WAS MEASURED AT 0.0013 INCHES. THE SEAL THICKNESS RELATIVE TO THE OUTER SEAL DIAMETER AND SECONDARY SEALING SURFACE MET REQUIREMENTS, SHOWING NO NEGATIVE TAPER. REFERENCE NCD N005992 THE TANK FLANGE AND SIPHON COVER WERE INSPECTED WITH NO ANOMALIES FOUND. A SUCCESSFUL REINSTALLATION OF THE COVER WAS PERFORMED USING A NEW SEAL, THE LEAK RATE TESTING AT 0.1 SCCM B. REVIEW SEAL BUILD HISTORY AND INSPECTION REQUIREMENTS FOR ACCEPTANCE RESPONSIBILITY: D. O'NEAL/3741 - D. WESTPHAL/3740 S. THOMPSON/3761 - S. PARIKH/3760 COMPLETE 5/18/95 CLOSURE STATEMENT A REVIEW OF RECEIVING INSPECTION RECORDS SHOW THE SEAL WAS ACCEPTED AT MAF 11/15/93 AS AN INITIAL RECEIPT. ACCEPTANCE REQUIREMENTS CONSISTED OF VERIFYING PACKAGING, IDENTIFICATION AND MARKINGS, AND VENDOR CERTIFICATIONS AND PERFORMING A VISUAL INSPECTION ON THE SEAL THROUGH THE PRIMARY ACLAR BAG AFTER REMOVAL FROM THE OUTER POLYETHYLENE BAG. THIS INSPECTION ASSURES NO TEFLON DEFECTS EXIST ON THE PRIMARY AND SECONDARY SEALING SURFACES AND THAT THE PARTS ARE FREE FROM BURRS AND SLIVERS. PRIOR TO INSTALLATION, THE SEALS ARE AGAIN VISUALLY INSPECTED THE SUPPLIER REPORTED INSPECTIONS CONSISTING OF DIMENSIONAL INSPECTIONS PERFORMED AFTER MACHINING/DRILLING AND SANDBLASTING FOR TEFLON APPLICATION, INCLUDING INSPECTION OF THE PRIMARY SEAL HEIGHT ON AN INCH PER INCH BASIS, DIMENSIONAL INSPECTIONS FOR TEFLON THICKNESS DURING AND AFTER APPLICATION, AND VISUAL INSPECTIONS PERFORMED AFTER TEFLON APPLICATION, AFTER CLEANING AND PRIOR TO PACKAGING FOR SHIPMENT. LANGLEY HAS REPORTED THAT THIS PARTICULAR SEAL WAS REWORKED DUE TO CONTAMINATION. REFERENCE LANGLEY COMMUNICATION, DATED 5/5/95, AND CCMAIL FROM PROCUREMENT QUALITY, DATED 5/16/95 C. ISSUE A SCAR TO SUPPLIER FOR CAUSE AND CORRECTIVE ACTION RESPONSIBILITY: M. MCANDREW/3742 - D. WESTPHAL/3740 COMPLETE 5/5/95 CLOSURE STATEMENT SCAR 95-064 ISSUED 5/5/95 D. SUPPLIER (LANGLEY CORPORATION) TO EVALUATE THE SEAL DEFECT AND REVIEW THEIR MANUFACTURING PROCESSES FOR CAUSE DETERMINATION AND IMPLEMENT CORRECTIVE ACTIONS TO PREVENT RECURRENCE RESPONSIBILITY: R. TORTORICH/3760 - S. PARIKH/3760 LANGLEY CORPORATION COMPLETE 6/9/95 * CLOSURE STATEMENT LANGLEY'S ANALYSIS OF THE SEAL DEFECT ELIMINATED DAMAGE BY IMPACT OR THEIR SANDBLASTING PROCEDURE USED PRIOR TO TEFLON COATING AS BEING THE CAUSE OF THE DEPRESSED AREA. CAUSE HAS BEEN ATTRIBUTED TO AN INCONEL CHIP BEING LODGED BETWEEN THE SEAL AND LATHE CHUCK DURING THE MACHINING OPERATIONS. DURING THE TIME THIS SEAL WAS MANUFACTURED, IT WAS RESTRAINED ON THE LATHE CHUCK BY FINGER CLAMPS. THE SEAL BODY WAS MACHINED COMPLETE, THEN THE SEAL WAS FLIPPED WHILE MACHINING THE RECESS AND PRIMARY SEAL LIP. A CHIP WOULD HAVE RAISED THE PLANE OF THE PRIMARY SEAL LIP, CREATING THE LOW SPOT ONCE THE SEAL WAS REMOVED AND RELAXED. THIS CAUSE IS SUPPORTED BY THE FACT THAT THE PRIMARY SEAL LIP PROFILE (ANGLES AND WIDTH) WAS NOT AFFECTED. IN DECEMBER 1993 THE RESTRAINING METHOD WAS CHANGED TO HOLD THE SEAL BY THE OUTSIDE DIAMETER AND EACH SIDE IS MACHINED COMPLETE BEFORE FLIPPING THE SEAL. BY LESSENING THE NUMBER OF SEAL FLIPS, THE CHANCES OF ENTRAPPING A MATERIAL CHIP IS REDUCED. EFFECTIVE 6/5/95, AN ADDITIONAL INSPECTION STEP WAS ADDED FOR INSPECTION TO WITNESS FLATNESS CHECKS PERFORMED WITH THE SEAL STILL RESTRAINED ON THE MACHINING LATHE. LANGLEY REPORTED INSPECTING A LOT OF 55L11-7T SEALS CURRENTLY IN PRODUCTION AND FINDING NO SIMILAR DEFECT REFERENCE SCAR 95-064 RESPONSE CAUSE DURING MACHINING OPERATIONS AN INCONEL CHIP BECAME LODGED BETWEEN THE SEAL AND LATHE CHUCK, DEFORMING THE SEAL BY TEMPORARILY RAISING THE PRIMARY SEAL HEIGHT. UPON RELEASE, THE SEAL HEIGHT BECAME UNDERSIZED. THIS IS AN ISOLATED INCIDENT * TASK II. CORRECTIVE ACTION - THE MACHINING TECHNIQUE WAS CHANGED IN DECEMBER 1993 TO RESTRAIN THE SEAL IN THE LATHE BY AN IMPROVED METHOD AND CHANGING THE MACHINING SEQUENCE, LESSENING THE CHANCES OF ENTRAPPING A MATERIAL CHIP - EFFECTIVE 6/5/95, ADDITIONAL INSPECTION STEP WAS ADDED TO WITNESS THE SEAL FLATNESS CHECK PRIOR TO REMOVING THE SEAL FROM THE MACHINING LATHE TASK III. CLEARANCE OF EFFECTIVITIES - ET-80 JOINT REWORKED. INSTALLATION ACCEPTABLE - ALL OTHERS, NO ISSUE. PROBLEMS OF THIS NATURE ARE DETECTED DURING ACCEPTANCE TEST NOTE: THIS IS ALSO THE DEFERRAL RATIONALE * TASK IV. CAPS CLOSURE SUMMARY THE LH2 SIPHON COVER LEAK WAS FOUND TO BE CAUSED BY A MANUFACTURING DEFECT ON THE NAFLEX SEAL PRIMARY SEAL LIP. THE CAUSE OF THE DEFECT WAS DETERMINED BY THE SUPPLIER TO HAVE BEEN A MATERIAL CHIP LODGED BETWEEN THE SEAL AND MACHINING LATHE WHICH TEMPORARILY RAISED THE LIP PLANE DURING MACHINING. AFTER REMOVAL FROM THE LATHE THE SEAL RETURNED TO ITS FREE STATE CREATING A DEPRESSED AREA ON THE LIP. CORRECTIVE ACTIONS HAVE INCLUDED PREVIOUSLY IMPLEMENTED CHANGES TO THE WAY THE SEAL IS MACHINED, BOTH IN THE WAY THE SEAL IS RESTRAINED IN THE LATHE AND THE SEQUENCE OF MACHINING, AND BY ADDING AN ADDITIONAL INSPECTION STEP TO WITNESS THE FLATNESS CHECK ON THE SEAL WHILE THE SEAL IS STILL RESTRAINED THESE CORRECTIVE ACTIONS WILL PREVENT A RECURRENCE OF THIS TYPE DEFECT. DEFECTS OF THIS TYPE ARE DETECTABLE THROUGH LEAK TEST, THEREFORE, NO CONCERN EXIST RELATIVE TO ALREADY INSTALLED AND TESTED SEALS. NO FLEET CONCERN EXISTS. THIS DEFECT IS ISOLATED BASED ON A HISTORY REVIEW OF SEAL DEFECTS SHOWING NO PAST DEFECTS OF THIS NATURE AND THE SUPPLIER REINSPECTION OF AN IN-PROCESS LOT OF THE SAME SEAL FINDING NO DEFECTS THIS CAPS IS CLOSED. NO FURTHER ACTION REQUIRED |
| MSFC Response/Concurrence 05/11/95 - DEFERRAL CONCURRENCE THIS REPORT HAS BEEN DEFERRED FOR THE NEXT SIX MONTHS PER NSTS 07700, VOLUME XI, PARAGRAPH 3.4.1, ITEM C AND NSTS 08126 REV. F PARAGRAPH 3.3.10.1, ITEM D WHICH STATES "THE PROBLEM CONDITION IS CLEARLY SCREENED BY PREFLIGHT CHECKOUT OR SPECIAL TESTS." THE DEFERRAL STATUS HAS BEEN APPROVED BY THE EXTERNAL TANK PROJECT MANAGER, MR. PARKER COUNTS CRAIG E. SUMNER (SIGNED 05/18/95) ------------------------------------------------------------------- |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A16486 | IFA# -- | Contractor RPT# P-077 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 55L11-7T | Asmnt Part Name NAFLEX SEAL | Asmnt Serial/Lot# 835490085517 |
| HCRIT CD -- | FCRIT CD -- | CAUSE CD -- | FAIL MODE -- |
| Asmnt FMEA 2.10.6.1 | Asmnt FM 1 | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |