WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A12135 | In-Flight Anomaly Number -- | Contractor Report Number P-063 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title CONTAMINATION WAS DETECTED INSIDE AFT FEEDLINE LO2 ELBOW OF ET 29 & 31 |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT 1 | Sys_Lvl N | Misc Codes A (X) B C D E (X) F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE LO2 PROP LINES | PART# 80921011009-019 | SER/LOT# 71 | MANUFACTURER MMC |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE LO2 PROP LINES | PART# 80921011009-019 | SER/LOT# 71 | MANUFACTURER MMC |
| Test/Operation L - FLD | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode MS - STRUCT | Cause MAP - MFG-ASY-INST |
| System PROPULSION | Defect CN - CONTAM | Material M - LINK-G | Work Contact J. FINCHER | Fail Date 03/22/1989 |
| Received at MSFC 04/03/1989 | Date Isolated -- | FMEA Reference 2.1.21.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location KSC | Symptom UC - UNSAT | Time Cycle N/A |
| Effectivity Text DEFERRED FOR STS-28, STS-34, STS-33 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary CAUSE: TAPE RESIDUE TRANSFER AS A RESULT OF USING FREON AS A PARTICLE BARRIER WIPE |
| Last MSFC Update 02/10/1995 | CN RSLV SBMT 07/24/1989 | Defer Date -- | Add Date 04/03/1989 | R/C Codes 5 - TRNG -- -- |
| Assignee |
| Design P. MULLER | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR P. BRIDWELL |
| Approval |
| Design P. MULLER | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR P. BRIDWELL |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete CM | MSFC Closure Date 08/16/1989 | Status C - CLOSED | F/A Completion 04/03/1989 |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description DURING BLACK LIGHT INSPECTION OF THE L02 AFT FEEDLINE ELBOW, INDICATIONS WERE PRESENT WHICH CREATED A SUSPECT CONDITION RELATIVE TO NON-VOLATILE RESIDUE. A VISUAL INDICATION WAS PRESENT IN THE VICINITY WHICH WOULD NORMALLY BE USED TO BUILD A PARTICAL BARRIER WHEN FLANGE LAPPING IS REQUIRED TO PROVIDE A GOOD SEALING SURFACE. A WIPE TEST WAS PERFORMED AND THE NVR EXCEEDED THE REQUIREMENT OF ONE MILLIGRAM PER SQUARE FOOT CRITICALITY: FAILURE TO MEET LO2 CLEANLINESS REQUIREMENTS IS CRITICALITY 1 PER THE CIL. REF. FMEA ITEM CODE 2.1.21.1 |
| Contractor Investigation/Resolution 4/18/89 - THIS PROBLEM REPORT HAS BEEN DEFERRED FOR STS-30 BASED ON THE FOLLOWING RATIONALE: 1 - CONTAMINATION INSIDE THE ELBOW AND THE DISCONNECT OF ET-29 WERE ACCEPTED BASED ON BLACK LIGHT INSPECTION AFTER CLEANING 2 - CONTAMINATION LEVELS IN ET-31 AND TRANSFER TESTS WERE BELOW L02 IMPACT THRESHOLDS 3 - NO IMPACT SOURCES 4 - NO ALUMINUM IGNITION POSSIBLE 5 - IF CONTAMINANT IGNITION OCCURRED, IT WOULD NOT DEGRADE THE PROPERTIES OF THE ALUMINUM 6 - CONTAMINANT STRONGLY ADHERES TO THE SIDE WALL THE ABOVE DEFERRAL MEETS THE DEFERRAL REQUIREMENTS OF NSTS 07700 VOLUME X1 ITEM C, WHICH STATES "THE PROBLEM CONDITION DOES NOT EXIST IN THE FLIGHT HARDWARE AND IS CLEARLY SCREENED BY ACCEPTANCE TEST, PREFLIGHT CHECKOUT, OR SPECIAL TEST". THE SPECIAL TESTS PERFORMED WERE LOX COMPATIBILITY OF THE SAME CONTAMINATE LEVEL AS ET 31 AND SUBSEQUENT RESIDUE TRANSFER TESTS AS WELL AS WORST CASE LOX IMPACT TESTING WITH ALUMINUM SAMPLES. REF FRR CHARTS THE ABOVE DEFERRAL RATIONALE HAS BEEN APPROVED BY THE ET PROJECT MANAGER, MR. J. SMELSER ________________J. SMELSER (SIGNED 4/24/89)_____________________ THIS PROBLEM REPORT HAS BEEN DEFERRED FOR STS-28, STS-34 AND STS-33 BASED ON THE ABOVE RATIONALE THE ABOVE DEFERRAL RATIONALE HAS BEEN APPROVED BY THE ET ACTING PROJECT MANAGER, MR. G.P. BRIDWELL ________________G.P. BRIDWELL (SIGNED)__________________________ GENERAL REFERENCE CAPS P-063A DATED 7/24/89 - DURING NORMAL (OMRSD) BLACKLIGHT INSPECTION OF THE ET-29 LO2 ET/ORBITOR DISCONNECT, THE FLAPPER VALVE OF THE DISCONNECT FLUORESCED. THE SUBSEQUENT INVESTIGATION DISCOVERED THE AFT LO2 FEEDLINE ELBOW ALSO FLUORESCED ADJACENT TO THE INTERFACE WITH THE DISCONNECT. THE FLUORESCING MATERIAL IN BOTH AREAS WAS REMOVED WITH SOLVENTS, BUT THE NVR OF THE ELBOW WAS NOT VERIFIED. THE ELBOW AS WELL AS THE DISCONNECT WERE ACCEPTED BASED ON BLACKLIGHT INSPECTION AFTER CLEANING IN FOLLOW-UP TO THE ET-29 BLACK LIGHT INSPECTION, THE ET-31 LO2 ELBOW WAS INSPECTED WITH A BLACK LIGHT AT KSC. THE ELBOW FLUORESCED ADJACENT TO THE INTERFACE WITH THE DISCONNECT AND CONTAMINATION/RESIDUE WAS VISUALLY APPARENT IN THE SAME AREA OF THE OBSERVED ON ET-29. THE SUBSEQUENT NVR TEST FAILED WITH A VALUE OF 3.4 MILLIGRAMS PER SQUARE FOOT (REF. WAD PR ET-31 - FP-0035) WITH THE REQUIREMENT BEING 1 MILLIGRAM PER SQUARE FOOT MAXIMUM. THE PURPOSE OF THIS CAPS IS TO PERFORM THE INVESTIGATION NECESSARY TO DETERMINE THE CAUSE OF THE CONTAMINATION, TO DETERMINE THE FLEET CLEARANCE TASKS AND TO OBTAIN CORRECTIVE ACTION TASK I -FAILURE/PROBLEM INVESTIGATION A WIPE TEST WAS PERFORMED TO DETERMINE THE NON-VOLATILE RESIDUE CONTENT ON ET-31 AT KSC. THIS FOLLOWED BLACK LIGHT AND VISUAL INDICATION ON THE INTERIOR OF THE QUICK DISCONNECT END OF THE LO2 AFT ELBOW CASTING. AS A RESULT OF THIS FINDING, THE FOLLOWING ACTIONS ARE REQUIRED TO DETERMINE THE CAUSE FOR THE ANOMALOUS CONDITIONS AND TO DETERMINE THE REQUIRED CORRECTIVE ACTION 1. CONTACT THE VENDOR WHO PROVIDES G02 PRESSURIZATION LINES AND L02 FEEDLINES TO DETERMINE IF PARTICLE BARRIERS ARE INSTALLED INSIDE OF CLEAN LINES WHEN WORK IS PERFORMED ON CLEANED HARDWARE CLOSURE STATEMENT NO PARTICULATE BARRIERS ARE INSTALLED IN LINES RETURNED TO THE SUPPLIER COMPLETE RECLEANING AND REPACKAGING IS ACCOMPLISHED. REF. MEMO 3761-89-037, DATED 5 APRIL 1989, FAULKNER TO FINCHER 2. REVIEW ALL G02 AND L02 LINE MAF BUILD RECORDS TO DETERMINE WHICH LINES HAD PARTICLE BARRIERS INSTALLED CLOSURE STATEMENT A REVIEW OF RECORDS IDENTIFIED ALL L02 FEEDLINES WHICH HAVE UTILIZED PARTICLE BARRIERS DURING REWORK ACTIVITIES. BY MANAGEMENT DECISION, ALL PRESSURIZATION LINES WERE NOT RESEARCHED. REF. MEMO 3741-89-048 3. PERFORM TESTS ON AN INDIVIDUAL L02 ELBOW (ET-55) TO DETERMINE THE ADEQUACY OF TAPE RESIDUE REMOVAL AND PERFORM NVR TEST CLOSURE STATEMENT INSPECTIONS WERE PERFORMED ON TWO UNINSTALLED L02 ELBOWS (ET-54 AND 55) THIS CONSISTED OF A VISUAL, BLACK LIGHT (ULTRA VIOLET) AND NON-VOLATILE RESIDUE WIPE. NO VISUAL INDICATIONS WERE OBSERVED IN EITHER ELBOW HOWEVER, ON ET-55, FOUR AREAS FLUORESCED BUT NO TRANSFER WAS OBTAINED WHEN WIPED WITH A PCA FREON SOAKED SWAB. ET-54 HAD NO FLUORESCENT AREAS. BOTH LINES WERE NVR WIPED AND WERE WITHIN THE ACCEPTABLE LIMITS OF LESS THAN ONE MILLOGRAM PER SQUARE FOOT. REF. LAB REPORTS 89A094 AND 89A095 4. DETERMINE IF VENDOR OF ET-29 AND ET-31 ELBOW CASTINGS UTILIZE ANY PROCESSES WHICH WOULD CONTRIBUTE TO BLACK LIGHT INDICATIONS INSIDE OF THE ASSEMBLY CLOSURE STATEMENT NO UNUSUAL CIRCUMSTANCES INVOLVING ET-29 OR 31 ELBOWS WERE REPORTED BY THE SUPPLIER (STADCO) WHICH WOULD CONTRIBUTE TO FLUORESCENT AREAS IN THE L02 ELBOW CASTING. REF. MEMO 3761-89-037, W. FAULKNER TO J FINCHER 5. INTERVIEW SHOP AND INSPECTION PERSONNEL TO DETERMINE IF CONSISTENCIES EXIST RELATIVE TO PARTICLE BARRIER INSTALLATION/REMOVAL AND SAMPLING FOR NVR PER THE STANDARD REPAIR INSTRUCTIONS M-004 CLOSURE STATEMENT INTERVIEWS WITH SHOP, Q.C. AND LABORATORY PERSONNEL REVEALED THAT A GENERAL CONSISTENCY IN TECHNIQUE WAS UTILIZED IN CONJUNCTION WITH CLEANING, INSPECTION AND SAMPLING FOR NVR AFTER LAPPING FLANGES USING STANDARD REPAIR INSTRUCTION M-004 6. OBTAIN DATA FROM KSC RELATIVE TO PROCESSING DIFFERENCES IN THE AREAS OF THE L02 ELBOW AND QUICK DISCONNECT, IF ANY, ON ET-29 VS. ET-31 CLOSURE STATEMENT NO DIFFERENCES ARE EVIDENT WHICH WOULD CONTRIBUTE THE THE ANOMALOUS CONDITIONS AFTER THE ET WAS DELIVERED TO KSC. REF. AR MK9061-MK1 7. COMPARE PROCESSING OF L02 AFT ELBOW CASTING AT MAF FOR ET-29 AND 31 WITH EMPHASIS ON ANY DIFFERENCES WHICH WOULD PRODUCE ANOMALOUS CONDITIONS INSIDE OF THE ELBOW CLOSURE STATEMENT NO DIFFERENCES WERE EVIDENT IN REVIEWING THE ELBOW PROCESSING WHICH WOULD CONTRIBUTE TO THE ANOMALOUS CONDITION. REF. TO MATRIX P-63-7 8. PERFORM LOX IMPACT TESTING TO DETERMINE SENSITIVITY OF TAPE/CLOTH RESIDUE CLOSURE STATEMENT LOX IMPACT TESTING WAS PERFORMED ON MATERIALS WHICH ARE USED IN CONJUNCTION WITH REWORK OF FLANGES. IT WAS DETERMINED THAT 155 MG/FT-SQUARED PASSED IMPACT TESTING. IT WAS ALSO DETERMINED THAT ANY CONCENTRATION OF ANTI-STATIC COMPOUND IS LOX COMPATIBLE. REF MATERIALS ENGINEERING TEST REPORT - ETTR-349 9. DETERMINE EFFECT (IF ANY) OF AGING OF TAPE/CLOTH RESIDUE CLOSURE STATEMENT TESTS INDICATE THAT WHEN J414 TAPE IS IN CONTACT WITH PCA FREON, THE AMOUNT OF ADHESIVE TRANSFER IS PROPORTIONAL TO THE CONTACT TIME WITH THE SOLVENT AND LENGTH OF TIME LEFT ON THE SURFACE OF THE METAL SUBSTRATE REF. TO MATERIALS ENGINEERING TEST REPORT ETTR-349 10. TEST SAMPLES OF TAPE/CLOTH RESIDUE ON MACHINED/CAST SURFACES WITH OSEE CLOSURE STATEMENT RESULTS OF THE OSEE WERE INCONCLUSIVE BECAUSE OF ELBOW CONFIGURATION AND DUE TO THE FACT THAT NO DATA WERE OBTAINABLE ON A357-T6 CASTINGS. REF MEMO 3573-89-062 11. KSC PROVIDE RESULTS OF TESTING ON ET HARDWARE AT KSC AS IT RELATES TO RESIDUE FOUND ON ET-31 CLOSURE STATEMENT VISUAL AND BLACK LIGHT INDICATIONS WERE PRESENT. IN ONE AREA OF THE ELBOW A ONE SQUARE FOOT AREA WAS WIPED BY MAF PERSONNEL USING THE SAME METHOD THAT IS USED IN ET PRODUCTION. THE NVR WIPE REVEALED 3.4 MG/FT- SQUARED WHICH IS IN VIOLATION OF THE REQUIRED 1 MG/FT-SQUARED. REF WAD-PR-ET-31-FP-0035 TASK II - CORRECTIVE ACTIONS 1. IMPLEMENT TOOLING TO REPLACE ACLAR BARRIERS TO PRECLUDE USE OF TAPE INSIDE OF FEEDLINES AND PRESSURIZATION LINES CLOSURE STATEMENT TOOLING HAS BEEN PROVIDED TO PRECLUDE THE REQUIREMENT FOR TAPED IN PARTICLE BARRIERS ON PROPULSION LINES AND THE APPLICABLE IMPLEMENTING PLANS AND SRIS HAVE BEEN REVISED. THIS IS EFFECTIVE FOR ET-55. REF SRI-M004 REV. 5 AND MEMO 3743-89-178 2. REVISE STPS 5008, 5009, 5011 AND 5017 TO INCLUDE CLARIFICATION OF VISUALLY CLEAN SURFACES TO AVOID MISINTERPRETATIONS. SUBSTITUE DEMINERALIZED WATER FOR PCA FREON AS A BARRIER WIPE TO PRECLUDE FREON CONTACT WITH J414 TAPE CLOSURE STATEMENT ALL STPS HAVE BEEN REVISED TO CLARIFY VISUAL INSPECTION REQUIREMENTS THIS REVISION ALSO INCLUDES DELETION OF PCA FREON WIPE ON ACLAR BARRIERS FOR TANK PENETRATION; I.E. MANHOLES, ELECTRICAL FEED THROUGHS, ETC. REF. JOB SHEET DCN-34809-305 3. IMPLEMENT ADHESIVE RESIDUE ACCEPTANCE TEST AND REVISE RECEIVAL ACCEPTANCE PLANS TO IMPOSE THE REQUIREMENT CLOSURE STATEMENT ADHESIVE ACCEPTANCE TEST REQUIREMENTS HAVE BEEN RELEASED AND THE RECEIVING ACCEPTANCE PLAN HAS BEEN REVISED TO IMPOSE THIS REQUIREMENT REF. RAP-J414 4. SCHEDULE AND INSPECT FIVE (5) ETS DURING THE MODIFICATION AND PRODUCTION PERIOD BY VISUAL, BLACKLIGHT AND NVR BY PERFORMING A DISCREPANCY CHECK AND REPORT (DC&R P89-001A & P-89-002) NOTE: ET-27, 32, 33, 34 AND 53 CLOSURE STATEMENT FIVE ETS WERE INSPECTED WITH BLACK LIGHT, VISUAL AND NVR (ETS 27, 32, 33, 34 & 53). VISUAL INDICATIONS ON ET-27 WOULD INDICATE SMALL AMOUNTS OF TAPE RESIDUE WAS PRESENT. THE TWO LARGEST OF SIX INDICATIONS WERE LESS THAN .3" INCH. ALL NVR SAMPLES PASSED THE 1 MG/FT-SQUARED REQUIREMENTS. REF. ATTACHEMENT 6 5. REVISE SRI M-004 TO PRECLUDE USE OF FREON OVER BARRIER TAPE CLOSURE STETEMENT SRI-M004 WAS REVISED TO DELETE THE USE OF FREON TO WIPE PARTICULATE FROM THE PARTICLE BARRIER. D.M. WATER IS USED TO PRECLUDE THE FREON FROM CONTACTING THE J414 TAPE. REF. SRI-M004 6. REVISE BARRIER MPP'S TO PRECLUDE USE OF FREON OVER TAPE CLOSURE STATEMENT MPPS FOR ETS 47 AND UP HAVE BEEN REVISED TO DELETE THE USE OF FREON ON PARTICLE BARRIERS AND USE D.M. WATER. REF. MEMO DATED 5-10/89 TO D WESTPHAL FOR R. CAMPBELL 7. ISSUE PRODUCTION TIPS FOR PRECLUDING SOLVENT OVER BARRIER TAPE CLOSURE STATEMENT A PRODUCTION TIP (NUMBER 102) WAS ISSUED TO MAKE ALL PERSONNEL AWARE OF THE REQUIREMENT TO NOT USE FREON WHICH WOULD CONTACT J-414 TAPE TASK III CLEARANCE OF EFFECTIVITIES ALL ET'S CLEARED: THE L02 FEEDLINE ELBOWS ARE INSPECTED AT KSC IN CONJUNCTION WITH AN INSPECTION OF THE ET TO ORBITER QUICK DISCONNECT. THIS CAST ELBOW IS THE ONLY VISUALLY ACCESSIBLE SECTION OF THE L02 LINE DURING THIS INSPECITON. HOWEVER, ALL OTHER LINES IN THE L02 PROPELLANT FEED SYSTEM AND PRESSURIZATION SYSTEM ARE SMOOTH SURFACES WHICH LEND THEMSELVES TO VERIFICATION OF A CLEAN SURFACE. THE RESIDUE LEVELS ON ET-31 AND ALL OTHER TANKS INSPECTED TO DATE ARE BELOW L02 IMPACT THRESHOLDS. NO IMPACT SOURCES HAVE BEEN IDENTIFIED NOR IS THERE A POTENTIAL OF ALUMINUM IGNITION OR PROPERTY DEGRADATION DUE TO RESIDUE IGNITION. ADHERENCE PROPERTIES OF THE RESIDUE IS SUCH THAT VERY AGRESSIVE SOLVENTS AND PERSISTENT SCRUBBING IS REQUIRED TO REMOVE THE RESIDUE WHICH MINIMIZES THE POTENTIAL OF INTRUSION OF THIS MATTER INTO THE PROPELLANT FLOW. IN ADDITION, THE FLUORESCING AREAS ON THE ET-27, ET-29, AND ET-31 ELBOWS WERE CLEANED TASK IV CAPS CLOSURE SUMMARY LOX IMPACTS TESTS DETERMINED THAT THE VISUAL INDICATIONS ARE BELOW L02 IMPACT THRESHOLDS NOR HAVE ANY IMPACT SOURCES BEEN IDENTIFIED. ADHERENT PROPERTIES OF RESIDUE ARE SUCH THAT THE POTENTIAL OF THIS MATERIAL INTRUSION INTO THE PROPELLANT LOW IS MINIMIZED. CORRECTIVE ACTIONS HAVE BEEN IMPLEMENTED TO ELIMINATE SOLVENT CONTACT WITH TAPE AND SPECIAL TOOLING FOR THE PROPELLANT LINES WILL ELIMINATE TAPE IN THESE APPLICATIONS |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A12135 | IFA# -- | Contractor RPT# P-063 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80921011009-019 | Asmnt Part Name L02 PROP LINES | Asmnt Serial/Lot# 71 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MAP - MFG-ASY-INST | FAIL MODE UC - UNSAT |
| Asmnt FMEA 2.1.21.1 | Asmnt FM 1 | FMEA CSE A | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |