MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A16207 | In-Flight Anomaly Number -- | Contractor Report Number P-076 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title BELLOWS CONVOLUTE HAS "BLISTERED" |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE GH2 PRESSURIZATION L | PART# PD4800205-009 | SER/LOT# 0000468 | MANUFACTURER ARROWHEAD |
| Test/Operation A - ATP | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode MV - EXT LEAK | Cause MP - MFG-PRC |
| System PROPULSION | Defect DB - BENT | Material N - HOLE | Work Contact D. O'NEAL | Fail Date 09/09/1994 |
| Received at MSFC 09/12/1994 | Date Isolated 09/01/1994 | FMEA Reference 2.7.1.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location ARROWHEAD | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text -- |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date 10/04/1994 | LVL 3 Close -- | Remark / Action 10/04/1994 |
| Investigation / Resolution Summary |
| Last MSFC Update 11/07/1994 | CN RSLV SBMT 10/05/1994 | Defer Date 09/27/1994 | Add Date 09/12/1994 | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design W. PATTERSON | Chief Engineer M. PESSIN | S & MA M. SMILES | Project N/A | Project MGR P. COUNTS |
| Approval |
| Design W. PATTERSON | Chief Engineer M. PESSIN | S & MA M. SMILES | Project -- | Project MGR P. COUNTS |
| PAC Assignee B. HURST | PAC Review Complete BH | MSFC Closure Date 11/03/1994 | Status C - CLOSED | F/A Completion 09/06/1994 |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID NCD N004352 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description A. WHILE UNDERGOING DEFLECTION TESTING AS PART OF ATP 14205-309, A BELLOWS CONVOLUTE OF THE BSTRA ASSEMBLY ADJACENT TO THE OUTLET FLANGE WAS VISUALLY DETECTED TO BE DISTORTED (BULGED) B. FIFTEEN PARTS PREVIOUSLY RECOGNIZED AS SUSPECT OF HAVING INTERPLY WATER INTRUSION WERE ALLOWED TO ENTER THE MANUFACTURING FLOW WITHOUT A CORRECTIVE BAKEOUT OF THE INTERPLY AREA CRITICALITY: FMEA PARA. 2.7.1.1 REFLECTS "LEAKAGE: AS A FAILURE MODE WHICH MAY RESULT IN LOSS OF MISSION REVISION "A": REVISED PROBLEM, GENERAL, TASKS I, II, III AND IV AND CLOSES THIS CAPS. SEE ASTERISKS |
| Contractor Investigation/Resolution GENERAL: AFTER SUCCESSFULLY PASSING A HYDROSTATIC PROOF TEST (1530 +/- 10 PSIG, 60 SECONDS MAXIMUM), THE GH2 LINE WAS UNDERGOING DEFLECTION TESTING WHILE HYDROSTATICALLY PRESSURIZED TO 600 +10/-0 PSIG, WHEN A DISTORTION (BULGE) OF THE FIRST BELLOWS CONVOLUTE OF THE FIRST BELLOWS FROM THE OUTLET FLANGE WAS NOTED. THE DISTORTION EXTENDED IN EXCESS OF TWO-THIRDS THE CIRCUMFERENCE OF THE BELLOWS REFERENCE AHP PART NUMBER 14205-309, SERIAL NUMBER 08-94-017 THE BSTRA ASSEMBLY IS A FLEXIBLE JOINT CONTAINING A PRESSURE CARRIER BELLOWS AND A BALL-STRUT TIE ROD ASSEMBLY (BSTRA). IT IS THE BELLOWS THAT IS OF CONCERN. THE BELLOWS IS MANUFACTURED OF THREE PLIES OF CRES 21-6-9, EACH PLY .008 INCHES THICK MANUFACTURE OF THE FLEXIBLE JOINT IS PERFORMED IN THREE PHASES: 1) BELLOWS - FORM INDIVIDUAL TUBES, TELESCOPE TUBES (JOIN BY SLIDING TOGETHER), FORM CONVOLUTES, TEST, TRIM. WET RESISTANCE WELDING IS USED DURING THIS PHASE 2) BELLOWS ASSEMBLY - ASSEMBLE AND WET RESISTANCE WELD TOGETHER THE BELLOWS COLLAR, SHIELD AND SUPPORT; TRIM AND TEST 3) BSTRA ASSEMBLY - ASSEMBLE AND FILLET WELD TOGETHER THE BELLOWS ASSEMBLY, FLOW LINER AND BSTRA IN SEPTEMBER 1992, DURING GO2/GH2 PRESSLINE COMPONENT PROCESSING AT AHP A SIMILAR ANOMALY WAS FOUND ON SEVERAL IN-PROCESS BSTRA ASSEMBLIES. THE ENSUING INVESTIGATION DETERMINED THAT WATER INTRUSION BETWEEN THE BELLOWS PLIES DURING THE BELLOWS OR BELLOWS ASSEMBLY STAGE OF MANUFACTURE (WET RESISTANCE WELDING) WAS THE CAUSE, THE WATER VAPORIZING AND CAUSING A HIGH PRESSURE BUILDUP BETWEEN THE PLIES DURING SUBSEQUENT HIGH HEAT WELDING OPERATIONS TO AN EXTENT THAT THE BELLOWS PLIES SEPERATED. THE DISCREPANT BELLOWS WERE DETERMINED TO HAVE BEEN MANUFACTURED TO A THEN RECENTLY REVISED PROCESS THAT HAD DELETED A BAKEOUT OF THE BELLOWS PLIES DURING RESISTANCE WELDING BY LEAVING A GAP IN THE WELD, BAKING THE PART TO ENSURE INTERPLY DRYNESS, THEN CLOSING THE WELD DRY. THIS PROCESS AFFECTED SEVENTEEN PRESSLINES (50 BSTRA ASSEMBLIES) HAVING BEEN RECEIVED BY MAF AT THE TIME AND 189 BSTRA ASSEMBLIES IN VARIOUS STAGES OF ASSEMBLY OR INSTALLED IN HIGHER ASSEMBLIES AT AHP INCLUDED IN THIS 189 AT AHP WERE 82 THAT WERE AT A RECOVERABLE STAGE WHERE A BAKEOUT COULD STILL BE PERFORMED TO DRY THE INTERPLY AREA ALL SUSPECT BSTRAS WERE INSPECTED AT MAF OR AHP FOR ACCEPTABILITY BY X-RAY OR SCRAPPED. REFERENCE SPECIAL INVESTIGATION SI-93-P003 TASK I. PROBLEM/FAILURE INVESTIGATION * A. THE FAILURE AND THE ASSOCIATED CAUSES ARE BEING INVESTIGATED RESPONSIBILITY: D. O'NEAL/3741 - D.P. WESTPHAL/3740 COMPLETED 9/21/94 CLOSURE STATEMENT AN X-RAY INSPECTION CONDUCTED OF THE BULGED BELLOWS SHOWED THE DEFORMATION TO RESULT FROM THE MIDDLE AND OUTER PLIES INVERTED ACROSS A TWO CONVOLUTE SPAN WITH SOME DEGREE OF DEFORMATION EXTENDING CIRCUMFERENTIALLY FOR MORE THAN 270 DEGREES. THE INNER PLY WAS COLLAPSED. PENETRATION OF THE CAVITY FORMED BY THE INVERSION FOUND WATER TO BE PRESENT WITH A SUBSEQUENT GHE MASS SPECTROMETER LEAK TEST FINDING A LEAK PATH THROUGH THE INNER PLY TO LINE INTERIOR. IN THE AREA OF THE GREATEST DEFORMATION THE BELLOWS WAS DISCOLORED FROM EXCESSIVE HEAT, THE DISCOLORATION ALIGNING DIRECTLY WITH AN INTERNAL STRUT-TO-HOUSING WELD ENGINEERING ANALYSIS AT AHP SHOWED THE TWO BALLOONED PLIES WOULD NOT HAVE YIELDED AT THE PROOF PRESSURE OF 1500 PSIG A SECTIONING OF THE BELLOWS WAS PERFORMED AT MAF TO GAIN VISUAL ACCESS TO THE BELLOWS INTERIOR. OPTICAL MICROSCOPY EXAMINATION OF THE INTERNAL DAMAGE SHOWED THAT THE INNER PLY CONVOLUTES APPEARED TO HAVE EXPANDED INTERNALLY INITIALLY THEN COLLAPSED BACK ON THEMSELVES, POSSIBLY AS A RESULT OF THE HYDROSTATIC TESTING THIS COLLAPSE CAUSED SEVERE DEFORMATION OF THE INNER PLY WITH KINKED, BENT AND FOLDED-OVER REGIONS. IT WAS IN THIS COLLAPSED AREA THAT THE MOST PROBABLE LEAK PATH WAS FOUND, A TIGHT CRACK APPROXIMATELY 0.012 INCHES LONG RUSTED SHUT PRESUMABLY BY WATER INTRUSION DURING HYDROSTATIC TESTING, SURROUNDED BY A LARGE NUMBER OF SMALL STRESS CRACKS. THE CRACKING WAS STRESS RELATED, NO CORROSION-ASSISTED FRACTURE WAS INDICATED. REFERENCE TECHNOLOGY LABORATORY TEST REPORT 94A223 A PROCESSING/HISTORICAL REVIEW HAS SHOWN THAT THIS BSTRA ASSEMBLY WAS ONE OF 15 OF THE 82 DESCRIBED IN SI-93-P003 AS AT A RECOVERABLE STAGE, TO BE BAKED OUT TO DRY THE BELLOWS INTERPLY AREAS AT THE BELLOWS ASSEMBLY LEVEL. THESE FIFTEEN WERE AT A COMPLETED BELLOWS LEVEL. AS THE PROCESS CHANGE EVOLVED TO CORRECT THE PROCESSING DEFICIENCIES THAT CREATED THE INTERPLY MOISTURE PROBLEM, THE BAKE- OUT TO ASSURE INTERPLY DRYNESS MOVED FROM THE BELLOWS ASSEMBLY LEVEL TO THE LOWER BELLOWS LEVEL. THE SUBJECT 15 PARTS WERE ALREADY COMPLETED AT THIS LEVEL AND AS THEY ENTERED THE MANUFACTURING FLOW NO BAKEOUT WAS PERFORMED. ALL 15 PARTS HAVE BEEN ACCOUNTED FOR WITH NONE INSTALLED ON ANY ET THE CONCLUSION DRAWN RELATIVE TO THIS ANOMALY IS THAT THIS PROBLEM IS A CONTINUATION OF THE SI-93-P003 ISSUE AND THE DEFORMED BELLOWS CONVOLUTE WAS A PRE-EXISTING CONDITION CREATED AT A LOWER MANUFAC- TURING LEVEL AND NOT DETECTED UNTIL ATP DURING VISUAL INSPECTION * B. ARROWHEAD PRODUCTS AND MAF TO ADDRESS THE INSPECTION OF ALL SUSPECT BSTRAS FOR ACCEPTANCE RESPONSIBILITY: D. O'NEAL/3741 - D. WESTPHAL/3740 ARROWHEAD PRODUCTS COMPLETED 9/20/94 CLOSURE STATEMENT MAF TO INSPECT TWO BSTRAS INSTALLED ON TWO DELIVERED GH2 PRESSLINES (PD4800205-029) BY X-RAY. REFERENCE NCDS N007615 AND N002196 AHP TO INSPECT ELEVEN BSTRAS AT AHP, THOSE DEDICATED TO THE GO2 SYSTEM BY BAKEOUT AT 625 DEGREES F (TO SIMULATE MAXIMUM FLIGHT TEMPERATURES, APPROXIMATELY 619 DEGREES F) FOLLOWED BY X-RAY AND THOSE DEDICATED TO THE GH2 SYSTEM BY X-RAY ONLY. THE GH2 SYSTEM BSTRAS HAVE ALREADY BEEN EXPOSED TO IN-PROCESS TEMPERATURES GREATER THAN THEY SEE IN FLIGHT (APPROXIMATELY 129 DEGREES F). ONE BSTRA OF THE FIFTEEN IS AT THE BELLOWS LEVEL AND WILL BE SCRAPPED REFERENCE AHP LETTER CT-GKF-33-94 AND MMMSS LETTER AP-0994-RDR-029 * C. PROCUREMENT QUALITY TO ADDRESS THE SYSTEM FAILURE THAT ALLOWED THE PREVIOUSLY IDENTIFIED 15 PARTS TO ENTER THE MANUFACTURING FLOW WITHOUT A CORRECTIVE BAKEOUT RESPONSIBILITY: J. MAJOR/3760 COMPLETE 10/4/94 CLOSURE STATEMENT THE SYSTEM FAILURE THAT OCCURRED AND ALLOWED THE 15 PARTS TO ENTER THE MANUFACTURING FLOW WITHOUT A CORRECTIVE BAKEOUT RESULTED FROM AN AHP MANAGEMENT DECISION AT THE TIME NOT TO TAG THE PARTS AS SUSPECT. IT WAS REASONED AT THAT TIME THAT NO MRB WAS REQUIRED BECAUSE IT WAS ASSUMED THE NEXT MANUFACTURING PROCESS WOULD CORRECT THE PROBLEM IN THE SAME MANNER AS THE OTHER 67 PARTS IDENTIFIED AS BEING AT A RECOVERABLE STAGE WERE CORRECTED - BY REVISED PLANNING THAT PROVIDED A BAKEOUT AT THE BELLOWS ASSEMBLY LEVEL. THIS ASSUMPTION BY MANAGEMENT AT AHP WAS EVENTUALLY OVERRIDDEN MONTHS LATER BY ENGINEERING (MAF) CONTRACT DIRECTION WHEN THE FINAL PROCESSING CHANGES WERE APPROVED THAT REQUIRED THE BAKEOUT TO BE PERFORMED AT THE EARLIER MANUFACTURING LEVEL. CONSEQUENTLY, THE BELLOWS WERE NOT INVENTORIED AND WERE ALLOWED TO PROCEED THROUGH THE MANUFACTURING PROCESS WITHOUT THE REQUIRED WORK THAT WOULD HAVE CONVERTED THEM TO AN ACCEPTABLE CONFIGURATION ARROWHEAD PRODUCT'S MANAGEMENT HAS RECOGNIZED THEIR FAILURE TO PROVIDE ENOUGH PROCEDURAL CONTROL OF SUSPECT HARDWARE AND HAS ADDED A WRITTEN PROCEDURE WITH SPECIFIC CONTROLS AND CHECKS TO ENSURE THAT FUTURE STOCK CHECKS AND INVENTORIES OF DISCREPANT HARDWARE WILL BE ADEQUATELY DOCUMENTED AND CONTROLLED REFERENCE MMMSS LETTER 3760-94-131 AND AHP LETTER AMQ4-082.MMC * CAUSE A. WATER ENTRAPMENT BETWEEN THE BELLOWS PLIES DURING RESISTANCE WELDING WHICH VAPORIZED AND PRESSURIZED THE INTERPLY AREA DURING SUBSEQUENT HIGH HEAT WELDING OPERATION NOTE: THIS ANOMALY WAS NOT AN ATP FAILURE BUT RATHER A PRE-EXISTING CONDITION RECOGNIZED DURING ATP B. LACK OF PROCEDURAL CONTROL TO FORCE PROPER DOCUMENTATION AND CONTROL OF SUSPECT HARDWARE * TASK II. CORRECTIVE ACTION A. NO PROCESSING CHANGES REQUIRED. THIS ANOMALY IS ISOLATED TO 15 PARTS MANUFACTURED TO AN OBSOLETE PROCESS B. ARROWHEAD PRODUCTS HAS DEVELOPED AND RELEASED A WRITTEN PROCEDURE TO ASSURE POSITIVE IDENTIFICATION, TIMELY SEGREGATION AND FEEDBACK ON THE INSPECTION STATUS OF SUSPECT HARDWARE THIS PROCEDURE HAS BEEN RELEASED AS QS-226, "SUSPECT PARTS - WIP AND STOCK PURGE PROCEDURE". REFERENCE AHP LETTER AMQ4-082.MMC * TASK III. CLEARANCE OF EFFECTIVITIES THIS DISCREPANCY IS ISOLATED TO 15 PARTS (BSTRA ASSEMBLIES) FOUND TO HAVE NOT BEEN BAKED OUT DURING PROCESSING TO ENSURE INTERPLY DRYNESS. ALL 15 PARTS HAVE BEEN ACCOUNTED FOR, NONE HAVING BEEN INSTALLED ON ANY PRESSURIZATION LINE INSTALLED ON ANY ET. NO ET IS AFFECTED. ALL 15 SUSPECT PARTS ARE BEING INSPECTED FOR PLY SEPARATION BY X-RAY OR WILL BE SCRAPPED THE REMAINDER OF PRESSURIZATION LINE BELLOWS ON ETS OR IN MAF OR AHP INVENTORY ARE NOT SUSCEPTIBLE TO THIS CONCERN OR WERE INSPECTED BY X-RAY PER SPECIAL INVESTIGATION SI-93-P003 DIRECTION THIS IS ALSO DEFERRAL RATIONALE * TASK IV. CAPS CLOSURE SUMMARY THE DEFORMED BELLOWS NOTED DURING ATP RESULTED FROM WATER ENTRAPMENT BETWEEN THE BELLOWS PLIES OCCURRING DURING RESISTANCE WELDING WHICH VAPORIZED AND PRESSURIZED THE INTERPLY AREA DURING SUBSEQUENT HIGH HEAT WELDING OPERATIONS. THE CAUSE OF THIS ANOMALY WAS FIRST RECOGNIZED IN 1992 AND ADDRESSED BY INSPECTING ALL PARTS WHICH HAD THIS POTENTIAL CONDITION AND BY CHANGES TO THE MANUFACTURING PROCESS THAT REQUIRE A BAKEOUT OF THE INTERPLY AREAS DURING RESISTANCE WELDING TO ENSURE THE PLIES WERE DRY. THE SUBJECT PART IS ONE OF FIFTEEN PARTS THAT WERE AT A LEVEL OF MANUFACTURE KNOWN TO BE CORRECTABLE BUT DUE TO A PROCESS REVISION THAT CHANGED THE POINT OF INTERPLY BAKEOUT TO AN ALREADY COMPLETED STEP, WERE ALLOWED TO BYPASS THE INTERPLY DRYING OPERATION. THIS ANOMALY IS ISOLATED TO THESE FIFTEEN PARTS AND ALL HAVE BEEN ACCOUNTED FOR WITH NONE INSTALLED ON ANY ET. ALL ARE BEING INSPECTED FOR ACCEPTANCE OR SCRAPPED. THIS ANOMALY WAS NOT A FAILURE THAT OCCURRED DURING ATP BUT RATHER A PRE-EXISTING CONDITION OF THE BELLOWS THAT WAS NOT SEEN UNTIL ATP VISUAL INSPECTIONS THIS CAPS IS CLOSED. NO FURTHER ACTION IS REQUIRED |
| MSFC Response/Concurrence 09/27/94 - DEFERRAL RATIONALE: THE CLOSURE RATIONALE SUBMITTED BY MAF ON 09/23/94 WAS CONSIDERED INCOMPLETE AND WAS REJECTED BY MIKE SMILES/CR70. IN LIEU OF CLOSURE, THIS PROBLEM REPORT HAS BEEN DEFERRED FOR THE NEXT (6) MONTHS PER NSTS 07700, VOLUME XI, PARAGRAPH 3.4.1, ITEM C AND NSTS 08126 REV. E PARAGRAPH 3.3.10.1, ITEM D WHICH STATES "THE PROBLEM CONDITION IS CLEARLY SCREEND BY PREFLIGHT CHECKOUT OR SPECIAL TESTS (I.E., FAILURE MODE SHOULD NOT OCCUR FOLLOWING THE TEST)." _____________________PARKER V. COUNTS (SIGNED) 09/27/94_____________ ET PROJECT MANAGER |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A16207 | IFA# -- | Contractor RPT# P-076 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD4800205-009 | Asmnt Part Name PROPULSION LINE | Asmnt Serial/Lot# 0000468 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MP - MFG-PRC | FAIL MODE MV - EXT LEAK |
| Asmnt FMEA 2.7.1.1 | Asmnt FM 1 | FMEA CSE A | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |