WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A10384 | In-Flight Anomaly Number -- | Contractor Report Number S-072 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title FORWARD SRB FITTINGS AND VERTICAL STRUTS HEAT TREATMENT PROCESS IS SUSPECT |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT 1 | Sys_Lvl Y | Misc Codes A (0) B (X) C D E F (X) G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE FWD SRB FITTING | PART# 80913000637-001/-002 | SER/LOT# VARIOUS | MANUFACTURER BENNET |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE FWD SRB FITTING | PART# 80913000637-001/-002 | SER/LOT# VARIOUS | MANUFACTURER BENNET |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U F | Fail Mode UC - UNSAT | Cause MAW - MFG-ASY-WORK |
| System AERODYNAMIC | Defect HS - TEMSEN | Material S - STRUCT | Work Contact MATTHEESSEN | Fail Date 10/28/1986 |
| Received at MSFC 11/10/1986 | Date Isolated -- | FMEA Reference 4.5.50.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location BENNET | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text LWTS 16, 20, 21, 22, 24 AND UP |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 01/10/1992 | CN RSLV SBMT 05/11/1988 | Defer Date -- | Add Date -- | R/C Codes 1 - DES -- -- |
| Assignee |
| Design F. HUNEIDI | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR P. BRIDWELL |
| Approval |
| Design A. JACKMAN | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR P. BRIDWELL |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete JE | MSFC Closure Date 06/03/1988 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description THE 80913000637-001 AND -002 FORWARD SRB FITTINGS MAY NOT HAVE BEEN PROPERLY PROCESSED BY THE HEAT TREATING VENDOR. CERTAIN CRITERIA SPECIFIED IN STP 8002 IS IN QUESTION, SUCH AS ELECTRICAL CONDUCTIVITY REQUIREMENTS, TENSILE PROPERTY VERIFICATION, PLACEMENT OF THERMOCOUPLES, AND OTHER HEAT TREAT IRREGULARITIES |
| Contractor Investigation/Resolution CAUSE - SUPPLIER ERROR. AVCO DID NOT PROPERLY INTERPRET THE SPECIFICATIONS, MONITOR THE PRODUCTION AND TESTING OF THE FITTINGS, AND REVIEW ACCEPTANCE DOCUMENTATION. MMMA ALSO FAILED TO DETECT THE UNACCEPTABLE TEST VALUES 12/4/86 GENERAL - A. THE SRB ATTACH FITTINGS ARE ALLOY 7050 DIE FORGINGS THAT ARE HEAT TREATED TO T736. THE FORGINGS ARE FORGED FROM INGOT BY ALCOA TO STM 5168. THE ELLANEF COMPANY THEN ROUGH MACHINES THE PARTS TO SIZE SO BENNET HEAT TREAT COMPANY CAN HEAT TREAT TO STP 8002A AND MIL-H-6088 THE HERCULES COMPANY PERFORMS MECHANICAL PROPERTIES TESTING. UPON ACCEPTANCE BY BENNETT HEAT TREAT COMPANY, THE PARTS ARE SHIPPED TO ELLANEF COMPANY FOR FINAL MACHINING. THE FINISHED PARTS ARE THEN SHIPPED TO AVCO FOR FINAL ACCEPTANCE AND ASSEMBLY INTO THE SRB BEAM B. THE ORIGINAL PROBLEM WAS THAT BENNETT HEAT TREATING EXCEEDED THE TIME DELAY REQUIREMENT FOR QUENCHING. THIS WOULD NOT ALLOW OPTIMUM PROPERTIES TO BE DEVELOPED. IN ORDER TO CLARIFY THE DATA, AN AUDIT TEAM MADE UP OF QUALITY AND ENGINEERING VISITED BENNETT ON OCTOBER 28 AND 29, 1986 SEVERAL ADDITIONAL, AND MORE SERIOUS, ISSUES WERE DISCOVERED. THE ISSUES ADDRESSED WERE: 1. THE QUENCH DELAY TIME FROM SOLUTION ANNEAL TO QUENCH VARIED FROM 10 TO 30 SECONDS. A MAXIMUM OF 15 SECOND DELAY IS ALLOWED BY SPECIFICATION. THIS IMPLIES POSSIBLE LOSS OF OPTIMUM MECHANICAL PROPERTIES 2. THE PART, AS HEAT TREATED BY BENNETT, HAS NEVER BEEN PROPERLY TESTED TO SEE IF IT CONFORMS TO ACCEPTABLE MECHANICAL PROPERTIES 3. LOAD THERMOCOUPLES WERE NOT ATTACHED TO THE PART. THE ACTUAL TIME AT TEMPERATURE DURING SOLUTION ANNEAL AND AGING IS IN DOUBT 4. THE TREPANNED TEST SPECIMEN WAS NOT WIRED TO THE PART. THEREFORE, IT IS UNCERTAIN IF THE SPECIMENS REPRESENT THE PART 5. ELECTRICAL CONDUCTIVITY WAS NOT MEASURED ON ALL OF THE TREPANNED TEST SPECIMENS, AND WHERE PERFORMED, IT WAS NOT RECORDED 6. BENNETT AND AVCO HAVE ACCEPTED PARTS THAT DO NOT MEET REQUIREMENTS SOME OF THESE PARTS ARE LOCATED AT MAF A. SEVERAL FITTINGS HAVE UNKNOWN STRESS CORROSION CRACKING RESITANCE (LWT'S 32, 35, AND 44) B. GRAIN FLOW ORIENTATION IS QUESTIONABLE RELATIVE TO IN-HOUSE ANALYSIS AND ALCOA'S REPORTS RELATING TO THE SUBJECT 1/7/87 - CRITICALITY 3 ASSIGNMENT CHANGED TO CRITICALITY 1 PER REVISION B TO CAPS S-072. THIS PROBLEM CONSTRAINS USE OF LWT-26, -32, -33, -35, AND -44. MISSION ASSIGNMENT OF THESE TANKS HAS NOT BEEN MADE TO DATE, THEREFORE A FICTICIOUS MISSION ASSIGNMENT (STS-00X) HAS BEEN USED TO ASSURE TRACKING OF THESE CONSTRAINTS. THE FICTICIOUS MISSION ASSIGNMENT (STS-00X) WILL BE REPLACED WITH A LEGITIMATE ASSIGNMENT NUMBER AS THE TANKS ARE ALLOCATED TO MISSIONS. THIS ACTION HAS BEEN COORDINATED WITH ET PROJECT MANAGER, G. P. BRIDWELL - G.P. BRIDWELL 1/29/87 1/29/87 PRB STATUS - MMC VENDOR INVESTIGATION OF SHOT PEENING IS BEING DONE FOR IMPROVING THE STRESS CORROSION RESISTANCE OF THE FITTING 2/19/87 PRB STATUS - MMC IS STILL COLLECTING BULK MATERIAL PROPERTIES OF THE FITTINGS. ECD 3/21/87. MMC TO REVIEW THE DATA AND TO RECOMMEND RATIONALE FOR CLOSURE BY 4/1/87. IT WAS AGREED ON FOR J. WHITE AND P HINKELEY TO MEET WITH MSFC MATERIAL ENGINEERS FOR STATUS UPDATE AFTER 2/27/87 3/26/87 PRB STATUS - A MEETING HAS BEEN SCHEDULED IN THE WEEK OF 3/30/87 FOR MSFC'S UPDATE. NO CHANGE 4/28/87 UPDATE STATUS (REF. MMC CAPS OPEN ITEMS SUMMARY DATED 4/21/87) ET CLEARANCE: - LWTS 24, 30, AND 40 ARE CLEARED OF ALL CONSTRAINTS. THIS IS BASED ON MARS T-62347 (ENGINEERING STRESS ANALYSIS. - LWTS 26, 32, 33, 35, AND 44 HAVE CONSTRAINTS TO LAUNCH. THESE WILL BE CLEARED BY ENGINEERING TEST AND/OR REPAIR. - ALL OTHER ETS CLEARED BY ACCEPTABLE TEST RESULTS IN ACCEPTANCE DATA 5/28/87 - PRB STATUS - NO CHANGE 9/14/87 - THE FOLLOWING IS A VERBATIM OF MCC CAPS S-072G DATED 5/3/88: TASK I PROBLEM INVESTIGATION A. DOCUMENTATION AND SYSTEMS REVIEW ITEM 1: REVIEW MARTIN MARIETTA MICHOUD AEROSPACE APPROVAL OF BENNETT MANUFACTURING PROCEDURES WITH RESPECT TO THE LISTED PROBLEMS. THIS SHALL INCLUDE THE DOCUMENTS APPROVED ON DAS CLOSURE STATEMENT RECOMMENDS REJECTING THE BENNETT PROCEDURES AS NOT COMPLYING WITH THE REQUIREMENTS. BENNETT IS NO LONGER A HEAT TREATING SUPPLIER AND NO ADDITIONAL FORGINGS WERE HEAT TREATED BY THAT VENDOR. (INTEROFFICE MEMORANDUM 3743-86-196 FROM B. GOUFMAN) ITEM 2: REVIEW ALL OTHER CRITICAL PROCESS DEPENDENT CRITICAL HARDWARE DOCUMENTATION FOR PROBLEMS SIMILAR TO BENNETT. THE REVIEW WILL CONSIST OF CRITICAL INTERFACE HARDWARE ONLY AND 7050 ALLOY PARTS. IT WILL BE FOR LWTS 16, 20, 21, 22, 24 THROUGH 53, AND 20 SETS OF LONG LEAD FORGINGS AND CASTINGS A. DETERMINE HARDWARE AND PARAMETERS FOR REVIEW, INCLUDING PART NUMBERS. COMPLETE B. REVIEW CRITICAL HARDWARE DOCUMENTATION (REFERENCE ATTACHED SUM- MARY REPORT). STATUS: 7050 REVIEW IS COMPLETE CLOSURE STATEMENT ALL ITEMS WERE FOUND TO BE IN COMPLIANCE WITH SPECIFICATION REQUIREMENT EXCEPT FOR CERTAIN 7050 ALUMINUM ALLOY PARTS. ALL DISCREPANT HARDWARE WAS DOCUMENTED ON MARS AND SUBMITTED FOR MRB ACTION (IOM 3761-87-193) ITEM 3: REVIEW BENNETT'S PROCESSING TO DETERMINE WHY THE PROBLEMS LISTED IN PARAGRAPH B OF THE GENERAL SECTION OCCURRED CLOSURE STATEMENT AVCO AND BENNETT DID NOT PROPERLY MONITOR THE PRODUCTION AND TESTING OF THE FORGINGS. (INTEROFFICE MEMORANDUM 3761-86-151 FROM J. KING) ITEM 4: REVIEW OF AVCO ACCEPTANCE, QUALITY CONTROL, AND VENDOR SURVEILLANCE SYSTEMS TO DETERMINE HOW NONCONFORMING MATERIAL COULD BE DELIVERED AS ACCEPTABLE HARDWARE CLOSURE STATEMENT AVCO QUALITY PERSONNEL DID NOT PROPERLY INTERPRET AND ENFORCE THE SPECIFICATIONS. (INTEROFFICE MEMORANDUM 3761-86-151) B. FORGING REVIEW/EVALUATION ITEM 1: REVIEW OF EACH PART INDIVIDUALLY FOR TENSILE, HARDNESS, AND CONDUCTIVITY DATA USING THE SUPPLIER DATA PACKAGES CLOSURE STATEMENT THE DATA HAS BEEN EXTRACTED AND ADDITIONAL DATA REQUESTED AND RECEIVED SEVERAL FORGINGS ARE SUSPECT OF HAVING EITHER LOW MECHANICAL PROPERTIES OR STRESS CORROSION RESISTANCE (LWTS 24, 26, 30, 32, 33, 35, 40 AND 44 - 1 FITTING EACH). (FORWARD SRB ATTACH FITTINGS DATA SHEETS 11/10/86) (NOTE: SEE TASK I, ITEM B.8 FOR DATA APPLICABLE TO LWTS 24, 30, AND 40) ITEM 2: PERFORM ADDITIONAL TESTING ON AVAILABLE RETAINED TEST BARS THIS SHALL CONSIST OF MECHANICAL PROPERTY TESTING, HARDNESS, CONDUCTIVITY, AND TENSILE BAR GRAIN FLOW ORIENTATION CLOSURE STATEMENT THE BARS HAVE BEEN TESTED. THE DATA IS IN ENGINEERING FOR REVIEW (M&P LAB REPORTS MTL-1462-86, MTL-1421-86, QC LAB REPORT 86A337) ITEM 3: PERFORM HARDNESS AND CONDUCTIVITY READING ON ALL MAF FITTINGS ON ETS AND INVENTORY STORES CLOSURE STATEMENT ALL FITTINGS AT MAF HAS BEEN INSPECTED. THE RESULTS HAVE BEEN SUBMITTED TO ENGINEERING FOR ANALYSIS. (QC LAB REPORTS 86A333, A, B, C, AND 86A334, A, B, C) ITEM 4: AN AS "HEAT TREATED FORGING" SHALL BE TESTED TO DETERMINE MECHANICAL PROPERTIES AND CONDUCTIVITY CLOSURE STATEMENT TEST RESULTS SHOWED SEVERAL AREAS WITH LOWER THAN EXPECTED TENSILE RESULTS. ALSO, THE GRAIN FLOW DIRECTION WAS UNCLEAR. (INTEROFFICE MEMORANDUM 3573-86-289, W. BAXTER) ITEM 5: A SECOND FORGING SHALL BE REHEATED USING PROPER PROCEDURES AND INSTRUMENTATION. AFTER HEAT TREATMENT, THE PARTS SHALL BE TESTED FOR MECHANICAL PROPERTIES AND CONDUCTIVITIES CANCELLED BENNETT: HEAT TREAT DISAPPROVED BY QUALITY. BENNETT WAS DROPPED FROM THE APPROVED SUPPLIER LIST AND NOT USED FOR ANY OTHER HEAT TREATING (REFERENCE INTEROFFICE MEMORANDUM 3573-87-106) ITEM 6: ENGINEERING ESTABLISHED ACCEPTANCE CRITERIA FOR DISCREPANT FITTINGS WITH CONCURRENCE OF RELIABILITY ASSURANCE CLOSURE STATEMENT ENGINEERING EVALUATED THE FOLLOWING DATA THAT WAS GENERATED TO DETERMINE THE ACCEPTABILITY OF THE FORWARD SRB FITTINGS: A. SUPPLIER DATA PACKAGE (TASK I.B. ITEM 1) B. RETAINED TEST BAR MECHANICAL PROPERTY TESTING (TASK I.B. ITEM 2) C. HARDNESS AND CONDUCTIVITY READINGS THAT WERE TAKEN ON THE PRODUCTION FITTINGS (TASK I.B. ITEM 3) D. FORGING ORIENTATION (TASK I.B. ITEM 10) LWTS 26, 32, 33, 35, AND 44 ARE UNACCEPTABLE FOR FLIGHT. THEY WILL BE REMOVED AND REPLACED BY B01795 AND MRB DISPOSITION (REFERENCE INTEROFFICE MEMORANDUM 3540-87-030, R HOKANSON) ITEM 7: PERFORM ADDITIONAL THERMO ANALYSIS AND TESTING TO DETERMINE: A. TREPAN SLUG IS REPRESENTATIVE OF FORGING B. COMPONENT SAW CORRECT TIME AND TEMPERATURES CLOSURE STATEMENT THE BENNETT PROCEDURE FOR HEAT TREATING THE FORWARD SRB THRUST FITTING MEETS ALL SPECIFICATION REQUIREMENTS. HOWEVER, PROCEDURAL VARIABLES, ESPECIALLY FURNACE LAG TIME DURING SECONDARY AGING, ALLOW FOR A WIDE RANGE OF FINAL PROPERTIES (REFERENCE STRUCTURAL MATERIALS TEST REPORT ETTR-271) ITEM 8: EVALUATE LOW MECHANICAL PROPERTIES OF DISCREPANT FORGINGS AND PERFORM ADDITIONAL STRESS ANALYSIS TO DETERMINE THE ACCEPTABILITY OF THE FORGINGS CLOSURE STATEMENT LOW MECHANICAL PROPERTIES ACCEPTABLE TO STRESS ANALYSIS. (REFERENCE INTEROFFICE MEMORANDUM 3521-87-004, C. BALASABRAMANIAN AND MARS T-62347) ITEM 9: PERFORM TESTING TO DETERMINE THE RESIDUAL STRESS LEVELS AT SELECTED LOCATIONS ON THE PART. THESE WILL BE BASED ON PROBABLE HIGH STRESS AREAS AND GRAIN FLOW DIRECTION CLOSURE STATEMENT RESIDUAL STRESS LEVELS ARE HIGH AND POSITIVE IN THE 7.5" BORE (REFERENCE RESIDUAL STRESS REPORT FOR S/NS 132 AND 175, AND C. O. RUAD, "RESIDUAL STRESS MEASUREMENT ON ALUMINUM FORWARD SRB THRUST FITTINGS", MARCH 1987) ITEM 10: EVALUATE AND RECONCILE THE VARIOUS REPORTS OF THE FORGING ORIENTATION. DETERMINE THE MAXIMUM PART THICKNESS CLOSURE STATEMENT FORGING ORIENTATION IS DEPENDENT ON EXACT LOCATION (REFERENCE REPORT ON S/N 142, INTEROFFICE MEMORANDUM 3573-87-100) ITEM 11: FAILURE ANALYSIS OF FITTING, S/N #94. THIS FITTING CRACKED BEFORE HEAT TREATMENT COMPLETION AT BENNETT HEAT TREAT CLOSURE STATEMENT THE FAILURE ANALYSIS SHOWED THE FOLLOWING (REFERENCE FAR CAPS S-072): A. THE INITIAL PORTION OF THE CRACK (0.3 INCHES) WAS LIKELY DUE TO ENVIRONMENTALLY ASSISTED STRESS CORROSION CRACKING, WHILE THE REMAINING PORTION OF THE CRACK WAS BY STRESS OVERLOAD B. THE FORWARD SOLID ROCKET BOOSTER BEAM FITTING, S/N 94, WAS FABRICATED FROM 7050 ALUMINUM ALLOY AND HEAT TREATED TO THE T736 CONDITION C. MECHANICAL PROPERTIES MET STM 5168 REQUIREMENTS, HOWEVER, THE SHORT TRANSVERSE YIELD STRENGTH EXCEEDED STP 8002 ACCEPTANCE CRITERIA D. EXTENSIVE SEM AND SURFACE ANALYSIS CHARACTERIZED AND OXIDE LAYERS AND DETECTED CONTAMINATES ON THE PART AND FRACTURE SURFACE. THEY ALSO SHOWED THAT THE USE OF CHEMICALS IN THE INSPECTION OF THE CRACK PRECLUDED A MORE DEFINITIVE EVALUATION. PROOF OF WHEN THE FRACTURE OCCURRED COULD HAVE BEEN GAINED HAD CHEMICALS NOT BEEN USED NO CORRECTIVE ACTIONS NEED BE ADDRESSED BEYOND THOSE COVERED BY THIS CAPS FOR THE FOLLOWING REASONS: 1. THIS IS AN ISOLATED CASE OF CRACKING SINCE THE INITIAL STARTUP PROBLEMS (2 FORGINGS WITH CRACKS) 2. THE PROCESS DEFICIENCIES THAT COULD HAVE CONTRIBUTED TO THIS PROBLEM (POOR CONTROL OF AGING TIME AND TEMPERATURES) HAVE BEEN ADDRESSED BY THIS CAPS 3. ALL FUTURE SUPPLIERS PROCESSING DOCUMENTATION WILL BE REVIWED TO ASSURE COMPLIANCE TO STP 8002 4. ALL PRESENT SUPPLIERS' PROCESSING DOCUMENTATION HAVE BEEN REVIEWED TO ASSURE COMPLIANCE TO STP 8002 ITEM 12: SECTIONING OF SEVERAL FITTINGS TO DETERMINE THE VARIATIONS IN MECHANICAL PROPERTIES AND CONDUCTIVITY. SEVERAL NODIAL POINTS SHALL BE EXAMINED WITH SPECIAL ATTENTION TO C5, D2, D8, AND D11 CLOSURE STATEMENT NODE ANALYSIS FOR C5 SHOWS SEVERAL ADDITIONAL QUESTIONABLE FITTINGS: LWTS 25-002, 27-001, 29-002, 31-002, 47-001, 48-001, AND 48-002. FURTHER INVESTIGATIONS WERE PERFORMED AND THESE FITTINGS WERE CLEARED OF ALL CONCERNS. (REFERENCE INTEROFFICE MEMORANDUM 3573-87-100 AND TASK I, ITEM 13) ITEM 13: PRODUCE ADDITIONAL STRESS CORROSION CRACKING DATA (SCC) TO CLARIFY YIELD CONDUCTIVITY ACCEPTANCE BOX AND CLARIFY NODE ANALYSIS CLOSURE STATEMENT TESTING HAS SHOWN THE FWD SRB FITTING TO BE IMMUNE TO SCC THROUGHOUT THE FITTING AT STRESSES 45 KSI OR LESS. THE WORST CASE RESIDUAL STRESS LEVEL IS 32 KSI SO THE FITTINGS WITH QUESTIONABLE C5 READINGS ARE ACCEPTABLE FOR USE. (IOM 3573-87-198) C. REPAIR INVESTIGATION ITEM 1: SHOT-PEENING IS A CANDIDATE FOR IMPROVING THE STRESS CORROSION RESISTANCE OF THE FITTING. TO DETERMINE THE ACCEPTABILITY OF THIS FIX, ADDITIONAL WORK NEEDS TO BE PERFORMED A. DETERMINE THE AREAS THAT SHOULD BE SHOT-PEENED B. DETERMINE THE CRITICAL DIMENSIONS AND SURFACE FINISHES THAT MUST BE MAINTAINED AFTER SHOT-PEENING C. DETERMINE THE ABILITY TO: 1. SUPPORT THE TANK SO ALL OSL SURFACES CAN BE SHOT-PEENED 2. GAIN PHYSICAL ACCESS TO PERFORM SHOT-PEENING ON THE ISL OF THE FITTING. THIS INCLUDES THE REMOVAL OF SRB BEAM WEB 5 INSTALLED AT MAF CLOSURE STATEMENT ADDITIONAL WORK WAS NOT NEEDED AS REHEAT TREATMENT IS THE METHOD OF REPAIR IN LIEU OF SHOT PEENING. (INTEROFFICE MEMORANDUM 3511-86-054, W. VANBEEK AND 3573-86-317, B. SYMS) ITEM 2: DETERMINE THE USEFULNESS AND PRACTICALITY OF AN INSITU HEAT TREATMENT OF THE FITTINGS. CLOSURE STATEMENT INSITU HEAT TREATMENT OF THE FORGING WAS NOT PRACTICAL (REFERENCE INTEROFFICE MEMORANDUM 3540-87- 030, R. HOKANSON AND 3522/T-87-016, L. HARTLEY) ITEM 3: DETERMINE BEST METHOD TO NONDESTRUCTIVELY INSPECT FORWARD SRB FITTINGS CLOSURE STATEMENT THERE IS NO BEST METHOD. EACH AREA HAS ITS OWN BEST METHOD. ADDITIONAL WORK IS NEEDED TO GET A FINAL SRB FITTING TEST PLAN (INTEROFFICE MEMORANDUM 3770-87-002, M. MCANDREW) ITEM 4: DETERMINE THE BEST METHOD OUT OF THE PROPOSED METHODS OF REPAIR: A. INSITU HEAT TREATMENT B. REPLACING THE SRB BEAM C. REPLACING THE FITTING BY A INSITU REPAIR D. SHOT PEENING OF FITTING AND PAINTING CLOSURE STATEMENT LWTS 26, 32, 33, 35, AND 44 WILL BE REPAIRED BY REMOVING AND REPLACING FITTING BY OPENING UP THE INTERTANK CROSS BEAM. THE SAME FITTING WILL BE REINSTALLED AFTER IT HAS BEEN AGED 350 DEGREES-F FOR FOUR HOURS (REFERENCE INTEROFFICE MEMORANDUM 3540-87-030, R. HOKANSON) TASK II CORRECTIVE ACTION A. CORRECTION OF AFFECTED ETS FOR SRB FITTINGS ITEM 1: REMOVE, REWORK (AGE) AND REINSTALL FORWARD SRB FITTING PER BO 1795. (CANCELLED. THIS BO WHEN APPROVED WILL BE TRACKED AND PERFORMED BY A MARS DISPOSITION) B. SYSTEM CORRECTIVE ACTION ITEM 1: SUPPLIERS, PROCESSORS, AND MMA PROCUREMENT QUALITY REPRESENTATIVES WILL BE MADE AWARE OF THE REQUIREMENTS OF STP 8002. TEST DATA VERIFICATION OF MAXIMUM PROPERTIES WILL BE ESTABLISHED AS A MANDATORY INSPECTION POINT A. MMMA PERSONNEL CLOSURE STATEMENT "TIPS" ISSUED TO CLARIFY AND EMPHASIZE 7050 REQUIREMENTS (TIPS #2) B. SUPPLIERS AND PROCESSORS NOTIFICATIONS ALONG WITH THE VERIFICATION OF MAXIMUM PROPERTIES MADE MANDATORY INSPECTION POINT CLOSURE STATEMENT ALL SUPPLIERS HAVE BEEN NOTIFIED. FUTURE SUPPLIERS WILL BE SENSITIZED DURING 5TH BUY START UP. (IOM 3761-87-064 AND 134) ITEM 2: DEVELOP MATERIAL FLOW DIAGRAMS FOR PROCESS SENSITIVE HARDWARE CLOSURE STATEMENT THESE DIAGRAMS HAVE BEEN GENERATED AND ARE AVAILABLE TO CLARIFY THE PROCESSING ITEM 3: MAF RECEIVING ACCEPTANCE PLANS (RAPS) WILL BE REVIEWED TO DETERMINE IF ANY CHANGES ARE NECESSARY CLOSURE STATEMENT ALL RAPS HAVE BEEN REVIEWED AND NEED CHANGES TO PREVENT FURTHER OCCURRENCES. THIS WILL BE CONDUCTED AS PART OF THE TD 813 STAND ALONE FORMAT CONVERSION. THIS HAS A TARGET DATE OF JUNE 1988 FOR COMPLETION UNTIL THEN, PAD 3740-061 HAS BEEN ISSUED TO COVER THE REQUIREMENTS (IOM 3743-87-135) ITEM 4: REVIEW ALL PROCESS INSTRUCTIONS CLOSURE STATEMENT THE RE-REVIEW OF ALL SUPPLIER PROCESS INSTRUCTIONS IS NOW COMPLETE. 43% OF THE PI'S REQUIRE REVISION. THESE CHANGES HAVE BEEN FORWARDED TO THE SUPPLIERS AND THE PI'S WILL BE TRACKED BY PROCUREMENT QUALITY THROUGH RE-APPROVAL. (IOM 3761-87-233) ITEM 5: REVIEW AND REVISE, AS NECESSARY, STM AND CRITICAL STANDARD DRAWINGS ASSOCIATED WITH METALS CLOSURE STATEMENT STM S168 AND Q250 WILL BE REVISED. OTHER SPECIFICATIONS WERE CHANGED TO INCORPORATE CLARIFICATIONS ON AN ON-GOING BASIS ITEM 6: REVIEW PURCHASE DOCUMENTATION TO SEE IF ALL REQUIREMENTS ARE MET A. REVIEW EACH CONTRACT VS. THE PURCHASE REQUISITION B. REVIEW CONTRACTS TO SEE IF ALL ENGINEERING REQUIREMENTS ARE MET (LETTER ISSUED STATING THAT ENGINEERING REQUIREMENTS TAKE PRECEDENCE OVER EXHIBIT A OF CONTRACT) CLOSURE STATEMENT REVIEW HAS BEEN ACCOMPLISHED AND AN ADMINISTRATIVE STATEMENT ISSUED CLARIFYING THE REQUIREMENTS (REFERENCE INTEROFFICE MEMORANDUM AP-0587-WRB-015, W. BOWEN) ITEM 7: REVALIDATE ALL APPROVED SUPPLIER PROCESS INSTRUCTIONS CLOSURE STATEMENT THE SUPPLIERS PROCESS INSTRUCTIONS WILL BE REVALIDATED AS THE SUPPLIERS ARE RESTARTED FOR 5TH BUY ITEM 8: EXAMINE THE FEASIBILITY OF CHANGING THE 7050 ALLOY PARTS TO REQUIRE SHOT PEENING AFTER FINAL MACHINING AS A PRODUCT ENHANCEMENT CLOSURE STATEMENT SHOT PEENING UNINSTALLED PARTS IS A WAY TO REDUCE SUSCEPTIBILITY TO SSC HOWEVER, IF THE PARTS ARE PROPERLY PROCESS, THIS STEP IS NOT NECESSARY (IOM 3573-87-159) ITEM 9: PROVIDE SCHEDULE AND PLAN FOR IMPLEMENTATION OF SUPPLIER SENSITIZATION TO 7050 CRITERIA. SUBMIT THE PLAN TO RELIABILITY ASSURANCE. THIS SHALL COVER THE IMPLEMENTATION OF TASK I.D., ITEMS 2.B AND 8 CLOSURE STATEMENT ALL SUPPLIERS AND MAF PERSONNEL WERE INDOCTRINATED ON 7050 PROBLEMS (INTEROFFICE MEMORANDUM 3761- 87-064) ITEM 10: ISSUE PRELIMINARY ALERT ON 7050 HEAT TREATING PROBLEMS CLOSURE STATEMENT ALERT WRITTEN AND SENT TO L. HERKES ON 6/16/87 C. CLEARANCE OF DISCREPANT HARDWARE DISCOVERED BY HARDWARE REVIEW (TASK I.A, ITEM 2) ITEM 1: 7050 HARDWARE A. REVIEW OF WEBER METALS PROCESSING AND DATA CLOSURE STATEMENT INVESTIGATION SHOWS THIS TO BE A NO ITEM. RETESTING IS ALLOWED BY SPECIFICATION (REFERENCE MARS T-91414) B. GENERATE MARS AND FIND EFFECTIVITIES CLOSURE STATEMENT MARS GENERATED FOR THE DISCREPANT PARTS (7050 PROBLEM SUMMARY, REVISED 6/10/87) ITEM 2: DETERMINE IF ANY ALLOY 7075 PARTS ARE SUSCEPTIBLE TO STRESS CORROSION CRACKING CLOSURE STATEMENT THERE ARE 500 + PARTS ON THE TANK, OF THOSE ONLY 23 ARE FRACTURE CRITICAL. THESE 23 WILL BE REVIEWED IN TASK II C.4. (IOM 3511- 87-039) ITEM 3: THE VERTICAL STRUT SHALL BE INVESTIGATED TO DETERMINE THE PROPER ENGINEERING DISPOSITION OF THE STRUTS. THIS SHALL INCLUDE TENSILE TESTING, RESIDUAL STRESS MEASUREMENTS, AND GRAIN FLOW ANALYSIS CLOSURE STATEMENT THESE STRUTS HAVE BEEN DISPOSITIONED USE-AS-IS. (MARS T-91442 AND OTHERS. SEE 7050 PROBLEM SUMMARY) ITEM 4: REVIEW THE 23 FRACTURE CRITICAL 7050 PARTS PER TANK. THIS WILL BE PERFORMED ON LWTS 16, 20, 21, 22, 24 THRU 53 CLOSURE STATEMENT THIS WAS COMPLETED AND ALL EXCEPT 3 PARTS WERE FOUND TO BE ACCEPTABLE THE 3 UNACCEPTABLE PARTS WERE PLACED ON A MARS. (INTEROFFICE MEMO 3761-88-049) TASK III. CAPS, CAUSE AND CORRECTIVE ACTION SUMMARY THE BASIC CAUSE WAS THE SUPPLIERS' FAILURE TO PROPERLY INTERPRET THE SPECIFICATIONS, MONITOR THE PRODUCTION AND TESTING OF THE PARTS AND REVIEW ACCEPTANCE DOCUMENTATION. MMMA ALSO FAILED TO DETECT THE UNACCEPTABLE TEST VALUES THE MAJOR CORRECTIVE ACTIONS TAKEN TO PRECLUDE REOCCURANCE WERE MAKING VENDOR AND MAF PERSONNEL AWARE OF THE 7050 REQUIREMENTS ANOTHER SIGNIFICANT CORRECTIVE ACTION WAS THE RE-REVIEW AND REVISION IF NEEDED OF RAPS, STMS, CRITICAL STANDARD DRAWINGS, SUPPLIER PROCESS INSTRUCTIONS AND SUPPLIER CONTRACTUAL REQUIREMENTS. IN ADDITION, ALL SUPPLIER PROCESS INSTRUCTIONS WILL BE REVALIDATED AS 5TH BUY IS STARTED THE GENERIC CONCERN WAS RESOLVED THROUGH A REVIEW OF THE CRITICAL 7075, 7050 AND INTERFACE HARDWARE ACCEPTANCE TEST RESULTS. AS A RESULT MANY MARS WERE WRITTEN TO IDENTIFY DISCREPANT HARDWARE (REFERENCE ATTACHED MATRIX) AND OBTAIN HARDWARE DISPOSITION. THE DISCREPANT SRB FITTINGS WILL BE REMOVED AND REHEAT TREATED IN ACCORDANCE WITH BO 1795 TASK IV CLEARANCE OF EFFECTIVITIES A. FORWARD SRB FITTINGS: 1. LWTS 24, 30, AND 40 ARE CLEARED OF ALL CONSTRAINTS. THIS IS BASED ON MARS T-62347 (ENGINEERING STRESS ANALYSIS) 2. LWTS 26, 32, 33, 35, AND 44 ARE CLEARED OF ALL CONSTRAINTS TO LAUNCH. THESE WILL BE REPAIRED BY DISPOSITIONED MARS (TASK II.A.1) 3. ALL OTHER EFFECTIVITIES CLEARED BASED ON ACCEPTABLE VALUES ON TEST REPORTS B. VERTICAL STRUTS: 1. LWTS 26, 28, 30, 31, 32, 33, 34, 37, AND 39 ARE CLEARED OF ALL CONSTRAINTS TO LAUNCH. THESE HAVE BEEN ACCEPTED UAI ON MARS 2. ALL OTHER EFFECTIVITIES CLEARED BASED ON ACCEPTABLE VALUES ON TEST REPORTS CAUSE AND CORRECTIVE ACTION SUMMARY: 1/26/88 UPDATE - SEE ATTACHMENT A OF MMC CAPS FOR 7050 PROBLEM SUMMARY 5/3/88 - THIS REPORT HAS BEEN DEFERRED FOR STS-26, PER NSTS 07700, VOLUME XI AND NSTS 08126 PARAGRAPH 3.4.1, ITEM C WHICH STATES "PROBLEM CONDITION DOES NOT EXIST IN THE FLIGHT HARDWARE AND IS CLEARLY SCREENED BY ACCEPTANCE TEST, PREFLIGHT CHECKOUT, OR SPECIAL TEST." THE DEFERRAL STATUS HAS BEEN APPROVED BY THE ET PROJECT MANAGER, MR. G.P. BRIDWELL ___________________ THIS CLOSURE IS SUBMITTED TO MSFC FOR REVIEW AND APPROVAL |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A10384 | IFA# -- | Contractor RPT# S-072 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80913000637-001/-002 | Asmnt Part Name FWD SRB FITTING | Asmnt Serial/Lot# VARIOUS |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MAW - MFG-ASY-WORK | FAIL MODE UC - UNSAT |
| Asmnt FMEA 4.5.50.1 | Asmnt FM 1 | FMEA CSE A | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |