Natural resources conservation service
conservation construction sPECIFICATION

904 - gabions

1. Scope

This work shall consist of furnishing and installing rock filled wire mesh baskets for an installation as shown on the drawings or as staked in the field.

II.  Materials

Gabions

Gabions shall be fabricated, assembled and installed in accordance with the nominal wire sizes and dimensions found in Tables 1 and 2, using the following materials.

Wire for fabrication and assembly shall be hot-dipped galvanized.  The wire shall have a minimum tensile strength of 60,000 psi.  Galvanized steel wire shall conform to ASTM A 641, class 3, soft temper.

When Epoxy or Polyvinyl Chloride (PVC) coated wire is specified in the Practice Requirements, the galvanized wire shall be coated by fusion bonded epoxy; or fusion bonded, extruded, or extruded and bonded PVC material.  The wire coating shall be colored black, gray, green or silvery; and the initial properties of the PVC coating shall meet the following requirements:

(a)	Specific Gravity.  In the range of 1.30 to 1.40, ASTM D 792.

(b)	Abrasion Resistance.  The percentage of weight loss shall be less than 12%, when tested according to ASTM D 1242, Method B at 200 cycles, CSI-A Abrader Tape, 80 Grit.

(c)	Brittleness Temperature.  Not higher than 15o F, ASTM D 746.

(d)	Tensile Strength.  Extruded Coating (not less than 2,980 psi. ASTM D 412).  Fusion Bonded Coating (not less than 2,275 psi. ASTM D 638).

(e)	Modulus of Elasticity.  Extruded Coating (not less than 2,700 psi. at 100 percent strain, ASTM D 412). Fusion Bonded Coating (not less than 1980 psi. at 100 percent strain, ASTM D 638).

(f)	Ultraviolet Light Exposure.  A test period of not less than 3000 hours, using apparatus type E at 63 C, ASTM G 23.

(g)	Salt Spray Test.  A test period of not less than 3000 hours, ASTM B 117.

After the exposure to ultraviolet light and the salt spray test as specified above, the PVC coating shall not show cracks, blisters, splits, nor noticeable change of coloring (surface chalk).  In addition, the specific gravity shall not change more than six (6) percent, resistance to abrasion shall not change more than ten (10) percent, tensile strength shall not change more than 25 percent, and modulus of elasticity shall not change more 25 percent from their initial values.

The wire sizes shown in Tables 1 and 2 are the size of the wire after galvanizing and before coating with PVC.

Spiral binders are the standard fastener for welded-mesh gabion baskets and mattresses, and shall be formed from wire meeting the same quality and coating thickness requirements as specified for the gabion baskets and mattresses.

Alternate fasteners for use with wire mesh gabions, such as ring fasteners, shall be formed from wire meeting the same quality and coating thickness requirements as specified for the gabions.  Hog rings are not acceptable

Standard fasteners and alternate fasteners must provide a minimum strength of 1,400 lb. per lineal foot for gabion baskets and 900 lb. per lineal foot for gabion mattresses.  When used to interconnect gabion baskets or mattresses with PVC coating, ring fasteners shall be made of stainless steel and spiral fasteners will be PVC coated.  All fasteners shall meet all of the closing requirements of the gabion manufacturer in addition to any requirements specified in Section 8.

TABLE 1 (Minimum Requirements)*

GABION BASKETS--Height 12, 18, or 36 Inches; Length as Specified

Type	Mesh	Wire	PVC	Total	Galvanized

of Wire	Size	Diameter	Coating	Diameter	Coating

# Inches	Inches	Inches 	Inches	oz./SF

### Woven	3-1/4 x 4-1/2	0.118	None	0.118	0.80

##### Mesh	3-1/4 x 4-1/2	0.105	 0.02 	0.145	0.80

## Selvage 		0.153	None	 0.153	0.80

0.132	0.02	 0.172	0.80

## Lacing and Internal		0.086	0.02	0.126	0.70

##### Connecting Wire

### Welded	3 x 3	0.118	None	0.118	0.80

Mesh	3 x 3	0 105	0.02	0.145	0.80

## Spiral		0.105	0.02 	0.145	0.80

##### Binder

TABLE 2 (Minimum Requirements)*

###### GABION MATTRESSES--Height 6, 9, or 12 Inches; Length as Specified

Type	Mesh	Wire	PVC	Total	Galvanized

of Wire	Size	Diameter	Coating	Diameter	Coating

Inches	Inches	Inches	Inches	oz./SF

Woven	2-1/2 x 3-1/4	 0.086	 0.02 	 0.126	0.70

Mesh

Selvage		0.105	0.02	0.145	0.80

Lacing and Internal	0.086	0.02	0.126	0.70

Connecting Wire

Welded	1-1/2 x 3	0.080	0.02	0.120	 0.70

Mesh

Spiral		0.105	0.02	0.145	0.80

Binder

NOTE:	The wire sizes and PVC coating thickness shown are nominal sizes.

The wire sizes include the galvanizing coating thickness.

Rock

Rock shall be sound, dense and durable with a bulk specific gravity of not less than 2.5.  Rock gradation shall conform to that specified below:

Gabion Basket	Predomi-	Min. Rock	 Max. Rock or Mattress 	nant Rock	Dimension	Dimension

Height		Size Inches	Inches		Inches

12, 18, or 36	4 to 8	4	9

Inch Basket

6, 9, or 12	3 to 6	3	7

Inch Mattress

The greatest dimension of the rock shall not be greater than 2 times the least dimension.  The engineer will inspect the rock gradation after it has been placed in the gabion baskets.

III.  Foundation Preparation

The foundation on which the gabions are to be placed shall be cut or filled and graded to the lines and grades shown on the drawings.  Surface irregularities, loose material, vegetation, and all foreign matter shall be removed from foundations.  When fill is required, it shall consist of materials conforming to the specified requirements.  Gabions and bedding or specified geotextiles shall not be placed until the foundation preparation is completed, and the subgrade surfaces have been inspected and approved by the Engineer.

IV.  Filter Layer or Bedding

When filter layers or bedding are specified, the filter or bedding material shall be spread uniformly on the prepared subgrade surfaces to the depth specified.  Compaction of filter layers or bedding will not be required, but the surface of such layers shall be finished free of mounds, dips or windrows.

V.  ASSEMBLY AND PLACEMENT

The assembly and placement of gabions shall be in accordance with the following procedures:

Assembly.  Rotate the gabion panels into position and join the vertical edges with fasteners for gabion assembly.  Where lacing wire is used, wrap the wire with alternating single and double half-hitches at intervals between four (4) to (5) inches.  Where spiral fasteners are used for welded-wire mesh, crimp the ends to secure the spirals in place.  Where ring type

alternate fasteners are used for basket assembly, install the fasteners at a maximum spacing of 6 inches.  Use the same fastening procedures to install interior diaphragms where they are required.

Interior diaphragms will be required where any inside dimension exceeds three (3) feet.  Diaphragms will be installed to assure that no open intervals are present that exceeds three (3) feet.

Placement.  Place the empty gabions on the foundation and interconnect the adjacent gabions along the top, bottom, and vertical edges using lacing wire.  Wrap the wire with alternating single and double half-hitches at intervals between four (4) to six (6) inches.  Unless otherwise specified in Section 8, lacing wire will be the only fastener allowed for interconnecting woven mesh gabions.  Spiral fasteners are commonly used for the assembly and interconnection of welded mesh gabions.  Spirals are screwed down at the connecting edges then each end of the spiral is securely tied down to prevent unraveling.  Lacing may be used as needed to supplement the interconnection of welded mesh gabions, and the closing of lids.

Interconnect each layer of gabions to the underlying layer of gabions along the front, back, and sides.

Stagger the vertical joints between the gabions of adjacent rows and layers by at least one-half of a cell length.

VI.  FILLING OPERATION

After adjacent empty woven wire gabion units are set to line and grade and common sides properly connected, they shall be placed in straight-line tension and stretched to remove any kinks from the mesh and to gain a uniform alignment.  Welded-mesh gabions do not require stretching.  Staking of the gabions may be done to maintain the established proper alignment prior to the placement of rock.  No stakes shall be placed through geotextile material.  Connecting lacing wire and other fasteners (as allowed) shall be attached during the filling operation to preserve the strength and shape of the structure.

Internal connecting cross-tie wires shall be placed in each unrestrained gabion cell greater than 18 inches in height, including gabion cells left temporarily unrestrained.  Two internal connecting wires shall be

placed concurrently with rock placement, at each 12-inch interval of depth.  In woven mesh gabions these cross-ties will be placed evenly spaced along the front face and connecting to the back face.  All cross-tie wires shall be looped around two mesh openings and each wire end shall be secured by a minimum of five 180-degree twists around itself after looping.

In welded mesh gabions these cross-ties or stiffeners will be placed across the corners of the gabions (at 12 inches from the corners) providing diagonal bracing.  Lacing wire or preformed hooked wire stiffeners may be used.

The gabions shall be carefully filled with rock, either by machine or hand methods, ensuring alignment, avoiding bulges, and providing a compact mass that minimizes voids.  Machine placement will require supplementing with handwork to ensure the desired

The last layer of rock shall be uniformly leveled to the top edges of the gabions.  Lids shall be stretched tight over the rock filling using only approved lid closing tools as necessary.  The use of crowbars or other single point leverage bars for lid closing is prohibited as they may damage the baskets.  The lid shall be stretched until it meets the perimeter edges of the front and end panels.  The gabion lid shall then be secured to the sides, ends, and diaphragms with spiral binders, approved alternate fasteners, or lacing wire wrapped with alternating single and double half-hitches in the mesh openings.

Any damage to the wire or coatings during assembly, placement and filling shall be repaired promptly in accordance with the manufacturer's recommendations or replaced with undamaged gabion baskets.

VII.  Vegetative Cover

Unless otherwise specified, a protective cover of vegetation shall be established on the disturbed area.  The planting of vegetative materials shall conform to the requirements of Practice Specification 342, Critical Area Planting.

VIII.  Special Measures

Measures and construction methods shall be incorporated as needed and practical that enhances fish and wildlife values.  Special attention shall be given to protecting visual and maintaining key shade food and den trees.

IX.  Construction Operations

Construction operations shall be done in such a manner that erosion and air and water pollution are minimized and held within legal limits.  The owner, operator, Contractor or other persons will conduct all work and operations in accordance with proper safety codes for the type of construction being performed with due regards to the safety of all persons and property.

The completed job shall be workmanlike and present a good appearance.

OPERATION AND MAINTENANCE ITEMS

A properly maintained gabion structure is an asset to your farm.  The life of this installation can be assured and usually increased by developing and carrying out a good maintenance program.

This will require you to perform periodic maintenance inspections.  Here are some recommendations to help you develop a checklist of items to observe and to perform necessary maintenance:

Re-tie any breaks in baskets.

Replace any rocks that may have been removed.

Repair any locations due to settlement as differential settlement.

Removal any debris that may accumulate.

Repair any damage due to vandalism, vehicular, or livestock.

Other items specific to your project are listed on the "Practice Requirement" sheet.