QENS STUDIES OF THE HYDROGEN STORAGE CAPACITY OF NOVEL SEPIOLITE-DERIVED CARBONACEOUS MATERIALS

Giselle Sandí1, Chang Keun Back2, Humberto Joachin2, Nicolas de Souza3, and Jai Prakash2

1Chemistry Division and 3Intense Pulsed Neutron Source, Argonne National Laboratory, 9700 South Cass Ave., Argonne, IL  60439-4803; 2Department of Chemical and Environmental Engineering, Illinois Institute of Technology, 10 W. 33rd Street, Chicago, IL  60616

INTRODUCTION

Gas-on-solid adsorption is an inherently safe and potentially high energy density hydrogen storage method that could be extremely energy efficient.  Consequently, the hydrogen storage properties of high surface area activated carbons have been extensively studied (1-3).  However, activated carbons are ineffective in storing hydrogen because only a small fraction of the pores in the typically wide pore size distribution are small enough to interact strongly with hydrogen molecules at room temperatures and moderate pressures. Many new carbon nanostructured adsorbents have been produced, including graphite nanofibers, carbon multi-wall, and single-wall nanotubes (1-3).  However, most of these materials are synthesized using very long and costly procedures.  In our laboratories we have recently used a particular clay called sepiolite as an inorganic template to load organic precursors and obtain carbonaceous materials. Sepiolite has fibers of 0.2 to 2 µm in length, 100 x 300 Å in width and a thickness of 50 to 100 Å (4).  Channels are present and oriented in the longitudinal direction of the fibers.  The channels are suitable for controlling the structure of organic compounds.

EXPERIMENTAL

Details about the synthesis of the carbon derived from sepiolite can be found in (4).  In brief, ethylene or propylene were loaded and pyrolyzed in the gas phase in one step using a three-zone furnace.  Quartz boats containing sepiolite were placed within a quartz tube.  The temperature of the oven was gradually increased from room temperature to 700 °C.  The oven was then held at that target temperature for 4 hours. The clay from the loaded/pyrolyzed sepiolite sample was removed using HF, rinsed to neutral pH and refluxed with concentrated HCl for 2 hours. The sample was washed with distilled water until the pH was > 5 to ensure that there was no acid left.  The resultant carbon was oven dried overnight at 120 °C. The hydrogen storage set up has been described in details in (5).

Hydrogen absorption in the carbon nanofiber material was studied in situ, by inelastic neutron scattering, on the Quasi-Elastic Neutron Spectrometer at the Intense Pulsed Neutron Source, Argonne National Laboratory. Two nanofiber carbon samples were investigated, as synthesized from raw sepiolite (A), and from the second fraction of the sepiolite (B) (See Figure 1). Both samples were loaded by applying a hydrogen pressure of 100 bar, to the sample at 77 K for 18 h, and then further cooling in stages to 20-25 K, before isolating the hydrogen cylinder. The inelastic neutron spectra were recorded at 12 K; to determine the scattering from the loaded hydrogen alone, the signal from the samples before loading was subtracted from the signal of the loaded samples.

RESULTS

The hydrogen storage capacity of carbons derived from sepiolite is summarized in (5). From those results, it is inferred that the samples derived from fraction two are considered the best candidates for practical applications. Quasi-elastic neutron spectroscopy spectra of the carbons derived from raw material and fraction two are shown in Figure 1A (blue curve) and 1B (red curve). The peaks around 14.5 meV evidence that the hydrogen absorbed in both samples stayed in molecular form. Apart from this, the significant differences are indicative of hydrogen being in its liquid state in sample A (blue curve), whereas the feature around 5 meV in sample B (red curve) indicates that hydrogen is in its solid state in sample B. To address the possibility that a significant amount of hydrogen condensed in the sample by the loading procedure outlined above, the hydrogen pressure in sample A was released at 25 K, before re-measuring at 12 K. The result (black curve) shows that there is some hydrogen left in the sample, in the form of adsorbed layer(s).

REFERENCES

1. Lee, S. M.;.Park, K S.; Choi, Y. C.; Park, Y. S.; Bok, J. M.; Bae, D. J.; Nahm, K. S.; Choi, Y. G.;Yu, S.C.; Kim, N. G.; Frauenheim, T.; Lee, Y. H. Synthetic Metals 113, 3, 209 (2000).

2. Wu, X. B.; Chen, P.; Lin, J.; Tan, K. L. International Journal of Hydrogen Energy 25, 3, 261 (2000).

3. Lee, S. M.; Lee, Y. H. Applied Physics Letters 76, 20, 2877 (2000).

4. G. Sandí, R. E. Winans, K. Carrado-Gregar. USA Patent 6,110,621.

5. G. Sandí, H. Yang, H. Joachin, K. A. Carrado, R. E. Winans, and J. Prakash. J. New Materials for Electrochemical Systems 6, 169-173 (2003).

ACKNOWLEDGMENTS

This work was performed under the auspices of the Office of Basic Energy Sciences, Division of Chemical Sciences, Geosciences, and Biosciences, U.S. Department of Energy, under contract number W-31-109-ENG-38.