Homework Assignment ---A

Viscosity Grading Systems

Name:___________________________

Date:____________________________

Use each of the three viscosity specifications shown in ASTM D3381 to grade (if possible) each of the three asphalts shown in Table 1.  If an asphalt can not be graded, explain why.

Determine the appropriate mixing and compaction temperatures for each of the three asphalts.

Explain the differences between the three specifications in ASTM D3381.

TABLE 1.  Asphalt Cement Test Results.

| Properties | Asphalt No. 1 | Asphalt No. 2 | Asphalt No. 3 |
| --- | --- | --- | --- |
| Original Properties |  |  |  |
| Viscosity at 60oC, Poise | 299 | 4205 | 2005 |
| Viscosity at 135oC, centistoke | 92 | 425 | 165 |
| Penetration, 25oC, 100 g, 5 sec | 223 | 50 | 88 |
| Flash point, oC | 171 | 275 | 265 |
| Solubility in trichloroethylene, % | 99.8 | 99.9 | 99.8 |
| After Thin Film Oven Aging |  |  |  |
| Viscosity at 60oC, Poise | 689 | 9852 | 4021 |
| Ductility at 25oC, 5 cm/min, cm | 100+ | 33 | 88 |
| After Rolling Thin Film Oven Aging |  |  |  |
| Viscosity at 60oC, Poise | 1255 | 9768 | 4002 |
| Viscosity at 135oC, centistoke | 588 | 952 | 299 |
| Penetration, 25oC, 100 g, 5 sec | 180 | 31 | 50 |
| Ductility at 25oC, 5 cm/min, cm | 100+ | 35 | 85 |