03M05/01/08

S702-03M.doc

Use on projects as appropriate.

Section 702. - ASPHALT MATERIAL

702.01  Asphalt Binder.  Delete the Subsection and add the following:

702.01  Asphalt Binder.  Conform to M 320, Table 1.  Conform to Subsection 702.04.

In AASHTO M 320, Table 1 replace footnote g with the following:

g  If the creep stiffness is below 300MPa, the direct tension test is not required.  If the creep stiffness is between 301 and 600 MPa, the direct tension failure strain requirement shall be used in lieu of the creep stiffness requirement.  The m-value requirement must be satisfied in both cases.

When an Open Graded Friction Course is specified, use the following:

702.01  Asphalt Cement.  Add the following:

Asphalt cement for the open-graded asphalt friction course will be viscosity Grade AC-20 (P or R) conforming to Table 702-2 and Subsection 702.04.  Add the rubber additive at the refinery.

Table 702-2

Open-Graded Friction Course Asphalt Cement

| Property | AASHTO Test No. | Minimum | Maximum |
| --- | --- | --- | --- |
| Tests on Original Material |
| Penetration, 25ºC, 100 g, 5 sec | T 49 | 50 | --- |
| Viscosity @ 60ºC, Poises | T 202 (1) | 1600 | 2400 |
| Viscosity @ 135ºC, cSt | T 201 | 325 | --- |
| Flash Point, ºC, COC | T 48 | 230 | --- |
| Ductility @ 4ºC (5 cm/min.) cm | T 51 (2) | 50 | --- |
| Synthetic Rubber, residual wt. |  | 2.0 % | --- |
| Toughness, Newton-meters | ASTM D 5801 | 12.43 | --- |
| Tenacity, Newton-meters | ASTM D 5801 | 8.47 | --- |
| Test on Residue |
| Viscosity @ 60ºC, Poises | T 202 (1) | --- | 8000 |
| Ductility @ 4ºC (5 cm/min.) cm | T 51 (2) | 25 | --- |

(1) Use an Asphalt Institute viscometer to determine viscosity @ 60ºC.  Heat the asphalt up to 163ºC prior to pouring if desired.

(2) Trimming the ductility specimen prior to testing is waived.

When a PBA grade asphalt binder is specified with Section 401 or 402, use the following:

702.01  Asphalt Cement.  Delete the text and substitute the following:

Conform to Table 702-3 and Subsection 702.04.

Table 702-3

Performance Based Asphalt Binder

| Property | AASHTO Test No. | Performance Based Asphalt Grade |
| --- | --- | --- |
|  |  | PBA-1 | PBA-4 | PBA-6a | PBA-6b | PBA-7 |
| Tests On Original Asphalt Binder Material |
| Flash point, COC, min. (1) (°C) | T 48 | 232 |
| Absolute viscosity at 60°C, min. (Pa·s x 10-1) | T 202 | 800 | 2800 | 2000 (2) | 2000 (2) | 2000 (2) |
| Kinematic viscosity at 135°C, max. (m2/s x 10-6) | T 201 | --- | --- | 2000 | 2000 | 2000 |
| Solubility in Trichloroethylene, min. (%) | T 44 | 99.0 | 99.0 | Report (3) | Report (3) | Report (3) |
| Tests On Aged Residue Asphalt Binder Material (4) |
| Mass loss after RTFO, max (%) | T 240 | Report (3) | Report (3) | 0.60 (5) | 0.60 (5) | 0.60 (5) |
| Penetration at 25°C (dmm) | T 49 | 25 | 20 | --- | --- | --- |
| Ductility at 25°C, 5cm., min. (cm) | T 51 | 75 | 50 | 60 | 60 | 75 |
| Absolute viscosity at 60°C (Pa·s x 10-1) | T 202 | 2500-5000 (6) | 14000 max. | 5000 min. (2) | 5000 min. (2) | 3000 min. (2) |
| Kinematic viscosity at 135°C, min. (m2/s x 10-6) | T 201 | 275 | 350 | 275 | 275 | 275 |
| Absolute viscosity ratio at 60°C RTFO vis/Orig vis , max. |  | 4.0 | 4.0 | 4.0 | 4.0 | 4.0 |
| Tests On Pressure Aging Vessel Residue Asphalt Binder Material (7) |
| PAV test temperature | R 28 | 90°C | 100°C | 100°C | 100°C | 110°C |
| Stiffness, 300.0 Mpa, max.And M-value, 0.30 min. at test temp | T 313 | -6°C | -6°C | -24°C | -30°C | -6°C |

(1) Actual results of the test shall be part of the certified copy of test results and when PBA-6a, 6b, or 7 is used an additional statement verifying an acceptable flash point shall be included with the Certificate of Compliance.

(2) The Absolute Viscosity at 60ºC of PBA-6a, 6b, and 7 will be determined a 1 sec-1 using ASTM Designation D 4957 with Asphalt Institute Vacuum Capillary Viscometers.  Sample preparation and viscometer charging temperature shall be 150 ± 5°C.

(3) Where “Report” is indicated, there is no requirement.  However the actual test result shall be part of the certified copy of test results, or shall be furnished with the Certificate of Compliance.

(4) “Aged Residue Asphalt Binder Material” means the asphaltic residue obtained using the Rolling Thin Film Oven Test (RTFO Test), AASHTO Test Method T 240.

(5) Actual results of the test shall be part of the certified copy of test results and when PBA-6a, 6b, or 7 is used an additional statement verifying an acceptable mass loss shall be included with the Certificate of Compliance.

(6) Where actual limits (2500-5000) are indicated, the actual test results shall be part of the certified copy of test results, or shall be furnished with the Certificated of Compliance.

(7) “Pressure Aging Vessel Residue Asphalt Binder Material” means the asphaltic residue obtained using the Accelerated Aging of Asphalt Binder Using a Pressure Aging Vessel Test (PAV Test), AASHTO Test Method R-28.

Use on all projects when a Prime coat is specified.

702.03  Emulsified Asphalt.  Add the following:

(e) Other emulsified asphalts.  Other emulsified asphalts not covered by item (a) through (d) will conform to the following:

(1) Saybolt furol viscosity at 50(C, AASHTO T 59	15 - 150 sec

(2) Settlement, AASHTO T 59	1% max.

(3) Residue by distillation, AASHTO T 59	65% min.

(4) Oil Distillate by volume, AASHTO T 59	25% max.

(5) Solubility in trichloroethylene, AASHTO T 44	97.5 % min.