WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A14467 | In-Flight Anomaly Number STS-42-T-001 | Contractor Report Number T-062 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title MISSING FOAM (TPS DIVOTS) IN INTERTANK ON STS-42/ET-52 |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl N | Misc Codes A B C D E F G (X) H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE ET COMPLETE | PART# 80901006000-059 | SER/LOT# ET-52 | MANUFACTURER MMMSS |
| Test/Operation F - FLT | Prevailing Condtion F - FUNCTIONAL | F / U UC | Fail Mode MSI - INSULATION | Cause U - UNKNOWN |
| System TPS | Defect DD - DETACH | Material F - INSUL | Work Contact K. KILLIAN | Fail Date 01/22/1992 |
| Received at MSFC 02/18/1992 | Date Isolated 02/17/1992 | FMEA Reference 5.6.2.1 | IFA: Mission Phase ASCENT | Mission Elapsed Time -- |
| Location KSC | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text 2/27/92 - DEFERRED FOR ET'S 43-45 AND ET'S 48-50 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 12/16/1992 | CN RSLV SBMT 08/27/1992 | Defer Date 02/27/1992 | Add Date 02/21/1992 | R/C Codes 0 - EXPL -- -- |
| Assignee |
| Design C. BRAMON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR P. COUNTS |
| Approval |
| Design C. BRAMON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR C. SUMNER |
| PAC Assignee B. HURST | PAC Review Complete BH | MSFC Closure Date 09/01/1992 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description POST-SEPARATION ET PHOTOGRAPHS TAKEN BY THE CREW SHOW POSSIBLE MISSING FOAM IN THE INTERTANK FOAM ACREAGE ON STS-42/ET-52 AS DOCUMENTED ON IFA STS-42-T-001 HIGHER THAN AVERAGE TILE DAMAGE MAY BE RELATED |
| Contractor Investigation/Resolution |
| MSFC Response/Concurrence THE EXTERNAL TANK'S INTERTANK TPS APPLICATION, THROUGH ET-50, INVOLVES TWO DIFFERENT SOFI CONFIGURATIONS. THE +/- Y THRUST PANELS AND AN AREA OF THE + Z PANELS HAVE BX-250 FILLING THE VALLEY BETWEEN THE STRINGERS WITH ISOCHEM APPLIED OVER THE BX-250. CPR IS APPLIED OVER THE BX-250 AND ISOCHEM DURING THE SPRAY OF THE INTERTANK. THE FINAL TPS CONFIGURATION INCLUDES TWO-TONE AREAS (CPR OVER BX) AND CPR-488 OVER THE PRIMED SUBSTRATE. VENT HOLES ARE DRILLED IN THE TWO-TONE AREAS AT KSC THESE EIGHTH-OF-AN-INCH DIAMETER HOLES ARE LOCATED IN THE VALLEYS BETWEEN THE STRINGERS AND PENETRATE THROUGH THE CPR-488/ISOCHEM INTERFACE TO ALLOW VENTING OF ANY LOCALIZED VOIDS THAT MAY EXIST EFFECTIVE ET-51 AND SUBSEQUENT, THE FOAM CONFIGURATION WAS REVISED FROM FILLING OF THE VALLEYS WITH BX-250 TO THE USE OF THE TWO (2) SPRAY GUNS WHICH FILL THE VALLEYS BETWEEN THE STRUCTURAL STRINGERS AND COVER THE STRINGERS IN A SINGLE CPR FOAM SPRAY TASK I. FAILURE INVESTIGATION A. MATERIAL SCIENCES (TPS ENGINEERING) 1. REVIEW AVAILABLE PHOTOGRAPHS AND FILM OF ET-52 FOR MISSING INTERTANK FOAM AND DETERMINE APPROXIMATE SIZE AND DEPTH OF AREAS COMPLETE: 2/25/92 CLOSURE STATEMENT: REVIEW OF ALL AVAILABLE PHOTOGRAPHS HAS BEEN COMPLETED AT MAF, JSC, MSFC, AND KSC. THE PHOTOGRAPHS SHOW TWO LIGHT SPOTS ON THE INTERTANK ACREAGE AT XT=1062, 55.1 DEGREES FROM +Z TOWARDS -Y AND AT XT=1081, 45.4 DEGREES FROM +Z TOWARDS -Y. THE SPOTS HAVE BEEN ESTIMATED TO BE APPROXIMATELY 14 INCHES IN DIAMETER. NONE OF THE PHOTOGRAPHS HAVE SUFFICIENT RESOLUTION TO DETERMINE THE DEPTH OF THESE FEATURES. PRE-LAUNCH PHOTOGRAPHS TAKEN APPROXIMATELY 3 HOURS BEFORE LAUNCH SHOW NO VISIBLE EXISTING DAMAGE OR REPAIRS IN THESE AREAS. NO OTHER ANOMALIES ARE CLEARLY VISIBLE IN ANY OF THE POST-SEPARATION VIEWS HOWEVER, JSC WILL REPORT ADDITIONAL SUSPECT ANOMALIES NEAR THE +Y ET/SRB FITTING. PHOTOGRAPHS OF THIS AREA ARE VERY POOR AND DO NOT HAVE SUFFICIENT DETAIL TO DETERMINE IF A PROBLEM ACTUALLY EXISTS IN THIS AREA. (REFERENCE STS-42 ORBITER DAMAGE REVIEW, ACTION ITEM NUMBER 1 AND 6) 2. REVIEW SRB DAMAGE REPORTS FOR LOSS OR DAMAGE TO TPS. REVIEW USBI'S SRB NOSE CONE FABRICATION PROCESS FOR POTENTIAL CHANGES COMPLETE: 2/25/92 CLOSURE STATEMENT: THE DAMAGE REPORT OF THE LEFT HAND SRB FRUSTUM AND FORWARD SKIRT WAS REVIEWED. THERE WAS NO MISSING ABLATOR. SOME SMALL "UNBONDS" WERE PRESENT AND THE BOND STRENGTH VALUES ON NOSE CONE AND BEANIE CAP WERE WITHIN SPECIFICATION REQUIREMENTS. ALSO, THERE WERE NO REPAIR OR SUSPECT AREAS NOTED. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 11) 3. DETERMINE HOW SAFETY MATS ARE INSTALLED ON THE INTERTANK FOR HORIZONTAL ACCESS COMPLETE: 2/25/92 CLOSURE STATEMENT: STYROFOAM WEDGES IN THE VALLEYS BETWEEN THE STRINGERS AND MATS ARE REQUIRED PER FINAL ASSEMBLY SET-UP LOG 80911001000 OP105. THE LOCATION AND NUMBER OF MATS USED ARE DETERMINED BY THE LOCAL SUPERVISOR. THE LOCATION OF THE SUSPECT DIVOTS ON THE INTERTANK DO NOT FALL WITHIN THE REQUIRED WORK AREAS, THUS ARE LOCATED OUTSIDE THE AREA USUALLY COVERED BY THE MATS. ATTACHED PHOTOGRAPHS ARE OF ET-52 DURING ASSEMBLY WORK IN FINAL ASSEMBLY AND SHOW THE NORMAL PLACEMENT OF WEDGES AND MATS. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 16) 4. MSFC LABORATORIES IS ANALYZING DAMAGED ORBITER TILES FOR TRACES OF IMPACTING MATERIAL. VERIFY THE RESULT OF THE ANALYSIS. (NOTE: MSFC ANALYSIS IS COMPLETE. EXECUTIVE SUMMARY IS DUE 6/23/92) 1ST ECD: 2/28/92 2ND ECD: 4/6/92 3RD ECD: 6/30/92 COMPLETE: 8/27/92 CLOSURE STATEMENT: LABORATORY ANALYSIS OF ORBITER TILE WAS INCONCLUSIVE, A DETERMINATION OF THE CAUSE OF THE TILE DAMAGE COULD NOT BE ASCERTAINED. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 18) 5. CONSTRUCT FAULT TREES FOR INTERTANK LOSS OF TPS AND FOR OVERALL ET DEBRIS SOURCES COMPLETE: 2/25/92 CLOSURE STATEMENT: WORKING FAULT TREES HAVE BEEN PROVIDED (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 19) 6. REVIEW/EVALUATE THE EFFECTS OF MOMENTARY GUN ANOMALIES ON FOAM INTEGRITY COMPLETE: 3/20/92 CLOSURE STATEMENT: AVAILABLE DATA INDICATE THAT FOAM RATIOS FROM 1.25 TO 1 THROUGH 2.75 TO 1 (NORMAL RATIO IS 2 TO 1) DO NOT DRAMATICALLY AFFECT FOAM STRENGTH (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 27) B. PRODUCT ASSURANCE 1. DETERMINE CPR LOT USED IN FABRICATION OF ET-52 INTERTANK DETERMINE OTHER USES OF THIS LOT AND ANY ASSOCIATED ANOMALIES COMPLETE: 2/25/92 CLOSURE STATEMENT: CPR MATERIAL LOT #87G265 WAS USED ON ET-52 INTERTANK (EXPIRATION DATE 4/88). OTHER USES OF LOT #87G265 ARE ET-51 L02 TANK, ET-52 L02 AND LH2 TANKS, ETS 53 AND 54 INTERTANKS NO ANOMALOUS CONDITIONS WERE ASSOCIATED WITH THE USE OF CPR LOT #87G265 (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 8) 2. EXTRACT ETS -51 THROUGH 55 INTERTANK ACCEPTANCE PLUG PULL DATA AND REQUIREMENT FROM THE FABRICATION RECORDS. INDICATE ANY OUT OF SPECIFICATION DATA COMPLETE: 2/25/92 CLOSURE STATEMENT: PLUG PULL ACCEPTANCE OF TWO GUN SPRAY WAS REVIEWED FOR ETS 51-55 - NO ANOMALOUS CONDITIONS WERE ASSOCIATED WITH FOAM APPLIED PER TWO GUN SPRAY PROCESS FOR ETS 52, 54, AND 55 - ONE (1) LOW PLUG PULL VALUE WAS DETECTED ON ET 51 - ONE (1) LOW PLUG PULL VALUE WAS DETECTED ON ET 53 - THESE AREAS WERE CLEARED BY ACCEPTANCE ADJACENT RETESTS - A REVIEW OF THE CODE 3 RISK DEFECT LOG DISCLOSED THAT NO PLUG PULLERS, FOR THIS TIME FRAME, WOULD HAVE ACCEPTED UNACCEPTABLE FOAM. (REFERENCE STS-42 - ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 9) 3. REVIEW TPS MRB MARS FOR ETS 51-53. REPORT ANY ANOMALIES THAT MAY BE POTENTIALLY RELATED TO LOSS OF FOAM FORWARD OF STATION 1129 COMPLETE: 2/25/92 CLOSURE STATEMENT: EIGHT TPS MRB MARS WERE DETECTED AS POTENTIALLY RELATED. (3 ON ET-51, 2 ON ET-52 AND 3 ON ET-53) (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 10) 4. REVIEW VENDOR'S (AVCO, NOW TEXTRON AEROSTRUCTURES) FABRICATION PAPERWORK FOR PRIMING OR CLEANING ANOMALIES OF THE +Z INTERTANK PANELS COMPLETE: 2/25/92 CLOSURE STATEMENT: ALL OF VENDOR'S FABRICATION PAPERWORK CONCERNING THESE PANELS WAS LOST IN A RECENT FIRE. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 17) 5. EXTRACT FROM THE MPP'S OF ET'S 51-53 INTERTANK CPR FOAM SPRAY ENVIRONMENTS OF CELLS, FLOW RATES, SUBSTRATES TEMPERATURES, ETC COMPLETE: 2/25/92 CLOSURE STATEMENT: A REVIEW OF THE MPP'S FOR ETS 51-53 INTERTANK CPR FOAM APPLICATION WAS CONDUCTED AND DISCLOSED NO OUT OF SPECIFICATION PROCESSING CONDITIONS. THERE WERE NO SIGNIFICANT DIFFERENCES IN THE FOAM APPLICATION CONDITIONS OF THE THREE (3) INTERTANKS. MATRICES FOR EACH INTERTANK FOAM APPLICATION CONSOLIDATING THE EXTRACTED DATA HAVE BEEN CONTRUCTED AND COPIES OF THE WEATHER SUMMARIES (RECORDED AT NEW ORLEANS INTERNATIONAL AIRPORT AND PUBLISHED BY NOAA) FOR THE MONTHS THE APPLICABLE ET'S WERE SPRAYED HAVE BEEN REVIEWED. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 21) 6. IDENTIFY THE LOCATION AND LOT NUMBERS OF THE TYPE OF TIE-COAT USED DURING FABRICATION OF ET'S 51-53 AT THE L02 AND LH2 INTERTANK FLANGE CLOSEOUTS, THE L02 PAL RAMP, L02/INTERTANK ICE FROST RAMPS, THE +/- Y BIPOD RAMP, THE +Z AERO VENT INSTALLATION AND THE +/- Y BATH TUB AREAS COMPLETE: 2/25/92 CLOSURE STATEMENT: A MATRIX OF THE TIE-COAT TYPES AND LOT NUMBERS UTILIZED IN THE FABRICATION OF THE APPLICABLE ET'S AT THE REQUESTED LOCATIONS HAS BEEN CONSTRUCTED. LAB REPORTS AND TWO (2) MRBS, THAT ACCEPTED LOTS AT RECEIVING WERE ALSO REVIEWED FOR POTENTIAL IMPACTS NONE WERE FOUND. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 24) C. DESIGN ENGINEERING 1. OVERLAY A CAD STRUCTURAL DRAWING OF THE ET ONTO THE SCANNED SEPARATION PHOTO. DETERMINE THE ORIENTATION AND LOCATION OF THE AREAS OF POSSIBLE LOSS. REVIEW OF THE STRUCTURAL SUBSTRATE FOR ANY POTENTIAL CONTRIBUTORS TO THE LOSS OF FOAM. OVERLAY THE ORBITER TO THE ET SHOWING THE RELATIONSHIP OF THE TILE DAMAGE AND THE SUSPECTED INTERTANK AREAS COMPLETE: 2/25/92 CLOSURE STATEMENT: THE OVERLAYS WERE CONSTRUCTED AND ANALYZED. NO CONTRIBUTING INFORMATION WAS DISCOVERED. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 2) 2. PROVIDE A PLUG PULL ACCEPTANCE TEST LAYOUT FOR THE INTERTANK FOAM AND THE INTERTANK FLANGE CLOSEOUT COMPLETE: 2/25/92 CLOSURE STATEMENT: THE REQUESTED LAYOUT HAS BEEN PROVIDED (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 3 & 4) 3. PROVIDE A SKETCH DENOTING THE TWO TONE CONFIGURATION (IF IT WERE APPLICABLE) WITH THE TWO SUSPECT AREAS IDENTIFIED COMPLETE: 2/25/92 CLOSURE STATEMENT: THE COMPOSITE SKETCH HAS BEEN FURNISHED AND PROVIDES AN OVERVIEW OF THE FOLLOWING ITEMS, 2 SUSPECT DIVOTS, +Z TWO TONE ENVELOPE, 8 PLUG PULL LOCATIONS, BIPOD RAMPS, SAFETY MAT USAGE AND MARS T093234 REPAIR. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 20) 4. PERFORM A DETAIL REVIEW OF MARS T93234 BATH TUB CREASES AND T 100865 L02 PAL RAMP LOW PLUGPULL VALUE COMPLETE: 2/25/92 CLOSURE STATEMENT: A DETAILED REVIEW OF THE MARS DISCLOSED NO DEBRIS CONCERNS. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 23) D. SYSTEM ENGINEERING 1. REVIEW THE FLIGHT TRAJECTORY OF ET-52 FOR ANY UNUSUAL PERTURBATION COMPLETE: 2/25/92 CLOSURE STATEMENT: POST FLIGHT RECONSTRUCTED TRAJECTORY PARAMETER COMPARISONS FOR STS-42 (28.5 DEGREES) AND STS-44 (57 DEGREES) REVEALED NO UNUSUAL OR UNEXPECTED CONDITIONS OR ANOMALIES. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 7) 2. DETERMINE ALL TRAJECTORIES OF FOAM COMING FROM SUSPECT LOCATION AND DEFINE THEIR KINETIC ENERGIES COMPLETE: 2/25/92 CLOSURE STATEMENT: DEBRIS THAT DAMAGED THE ORBITER NOSE TILE DID NOT ORIGINATE FROM THE SUSPECTED TPS ANOMALY LOCATION. ALTHOUGH THERE IS NO OBVIOUS FLOW MECHANISM AT THE SUSPECT TPS ANOMALY LOCATION TO TRANSPORT DEBRIS TO THE ORBITER, THERE IS A LOW PROBABILITY THAT SMALL SIZE DEBRIS AT HIGH DYNAMIC PRESSURE AND LARGER SIZE DEBRIS EARLY/LATE IN FLIGHT FROM THE SUSPECT TPS ANOMALY LOCATION COULD DAMAGE ORBITER TILE AFT OF THE ORBITER NOSE. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 14) 3. DETERMINE THE MOST PROBABLE DEBRIS SOURCE DEBOND IMPACT SCENARIO COMPLETE: 2/25/92 CLOSURE STATEMENT: AN INVESTIGATION BY MAF'S SYSTEMS ANALYSIS GROUP DISCLOSED THE MOST PROBABLE DEBRIS SOURCE FOR ORBITER TILE DAMAGE MAY BE ATTRIBUTED TO SMALL SIZE (1" CUBE OR SMALLER) DEBRIS PARTICLES ORIGINATING AT THE FORWARD END OF INTERTANK AND PROBABLY OCCURRING EITHER EARLY IN FLIGHT OR AT SRB SEPARATION. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 15) 4. DETERMINE IF SRB NOSE CONE DEBRIS OR ET DEBRIS COULD CAUSE THE SURFACE DIVOTS IN THE INTERTANK FOAM ACREAGE COMPLETE: 3/20/92 CLOSURE STATEMENT: ANALYSIS DISCLOSED THAT DEBRIS FROM THE SRB COULD IMPACT THE SUSPECT TPS ANOMALY LOCATION BUT WITH INSUFFICIENT KINETIC ENERGY TO RESULT IN TPS DIVOTS. DEBRIS FROM THE ET NOSE AREA WILL NOT IMPACT THE INTERTANK. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 25) E. AMT 1. CONSTRUCT A HISTORY OF THE TWO GUN SPRAY DEVELOPMENT AND VALIDATION. DOCUMENT ANY ANOMALIES DURING BUILD/CHECKOUT AND THEIR POTENTIAL IMPLICATION TO THE ORBITER COMPLETE: 2/25/92 CLOSURE STATEMENT: THE HISTORY HAS BEEN DOCUMENTED WITH NO ADVERSE EFFECT TO THE ORBITER DISCOVERED (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 5) 2. PROVIDE A CELL HISTORY FOR THE ETS 51-53 INTERTANK CPR FOAM APPLICATION COMPLETE: 2/25/92 CLOSURE STATEMENT: ET'S 51, 52, 53, AND 55 WERE SPRAYED WITH THE TWO GUN SPRAY PROCESS IN CELL "G". ET'S 54 AND 56 WERE SPRAYED WITH THE TWO GUN SPRAY PROCESS IN CELL "H". (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 12) 3. REVIEW AND SUMMARIZE THE FLOW METER DATA FOR ET-52 INTERTANK FOAM SPRAY COMPLETE: 3/20/92 CLOSURE STATEMENT: THE FLOW METER DATA WAS SUMMARIZED AND REVIEWED NO DETRIMENTAL CONDITIONS WERE DETECTED. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 28) F. STRESS ENGINEERING 1. DETERMINE IF STRUCTURAL FLEXURE FROM THERMALLY INDUCED HOOP COMPRESSION AND STRUCTURAL DISCONTINUITIES MAY RESULT IN DIVOTS COMPLETE: 2/25/92 CLOSURE STATEMENT: STRESS ENGINEERING HAS REVIEWED THE STRUCTURAL FLEXURE IN THE AREA OF THE SUSPECTED DIVOTS ON STS-42 (STATIONS 1062 AND 1081 AT 55.1 DEGREES AND 45.4 DEGREES OFF +Z TOWARDS -Y RESPECTIVELY). ANALYSIS DISCLOSED THAT THERE IS NO SIGNIFICANT THERMAL INDUCED HOOP COMPRESSION IN THE AREA OF SUSPECT DIVOTS. MECHANICAL DISCONTINUITIES IN THE STRUCTURAL CONFIGURATION TYPICALLY OCCUR ONLY IN END BAYS, AROUND INTERTANK PENETRATION AND ACROSS PANEL SPLICES, NONE OF WHICH EXIST IN THE AREA OF SUSPECT DIVOT. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 13) G. MSFC OPERATIONS 1. INSPECT THE SRB "BEANIE CAP" FOR ANY UNUSUAL CONDITIONS COMPLETE: 3/20/92 CLOSURE STATEMENT: INSPECTION REVEALED NO UNUSUAL CONDITIONS (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 22) H. KSC OPERATIONS 1. REVIEW KSC PROCESSING OF ET-52 INTERTANK AND DOCUMENT ANY CONDITIONS THAT COULD CONTRIBUTE TO THE INTERTANK ANOMALY COMPLETE: 3/20/92 CLOSURE STATEMENT: NO ANOMALOUS CONDITIONS WERE DETECTED. (REFERENCE STS-42 ORBITER DAMAGE REVIEW ACTION ITEM NUMBER 26) TASK II. CORRECTIVE ACTION THERE IS NO IMMEDIATE OR PLANNED CORRECTIVE ACTION. THIS IS AN EXPLAINED CLOSURE CAPS, DOCUMENTING AN UNEXPLAINED ANOMALY THAT IS CLASSIFIED AS AN ISOLATED INCIDENT TASK III. CLEARANCE OF EFFECTIVITIES ET 43 THROUGH 45 AND 48 THROUGH 50 ARE CLEARED FOR FLIGHT SINCE THESE ET'S WERE MANUFACTURED UTILIZING THE TWO-TONE SOFI APPLICATION WITH EIGHT-OF-AN-INCH DIAMETER VENT HOLES ET-51, ET-54 AND SUBSEQUENT ARE CLEARED FOR FLIGHT. THE CAUSE OF THE ANOMALY COULD NOT BE ASCERTAINED BY EXTENSIVE TESTING AND ANALYSIS LOSS OF THIS TYPE OF FOAM (IF IT OCCURS) IS NOT A SAFETY OF FLIGHT CONCERN BUT ONE OF ORBITER TILE MAINTENANCE TASK IV. CAUSE AND CORRECTIVE ACTION SUMMARY THIS IS AN EXPLAINED CLOSURE CAPS FAULT TREE ANALYSIS WAS USED TO IDENTIFY POSSIBLE CAUSES OF DIVOTS. THE MAJOR AREAS INCLUDED IN THE FAULT TREE WERE: - EXCESSIVE FLIGHT ENVIRONMENTS - MECHANICAL DAMAGE - PROCESSING OR ASSEMBLY ANOMALY - OTHER CAUSES - MATERIAL AGE, BSM IMPINGEMENT, FLUID SPILL NO CREDIBLE EVIDENCE FOR A POSSIBLE CAUSE WAS FOUND IN ANY OF THE ABOVE NINE FLIGHT TILES AND ONE CONTROL TILE WERE ANALYZED AT MSFC MATERIALS & PROCESSES LABORATORY. NO ET OR SRB TPS MATERIALS WERE IDENTIFIED IN THE TILES THE CAUSE OF THE ANOMALY WAS NOT DETERMINED AND IS CLASSIFIED AS AN ISOLATED INCIDENT THERE IS NO IMMEDIATE OR PLANNED CORRECTIVE ACTION ********************************************************************* 2/24/92 - PAC NOTE: DEFERRAL RATIONALE ********************************************************************* DEFERRAL RATIONALE: THIS PROBLEM HAS BEEN DEFERRED FOR ET'S 43-45 AND ET'S 48-50 PER NSTS 08126, REVISION D, PARAGRAPH 3.3.10.1, ITEM A WHICH STATES "THE PROBLEM IS NOT APPLICABLE TO THE FLIGHT(S) (SYSTEM NOT INSTALLED OR USED ON THE FLIGHT)." APPROVAL: _____GERALD C. LADNER (SIGNED)____________ DATE: __2/27/92__ GERALD C. LADNER ET PROJECT MANAGER |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A14467 | IFA# STS-42-T-001 | Contractor RPT# T-062 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80901006000-059 | Asmnt Part Name ET COMPLETE | Asmnt Serial/Lot# ET-52 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD U - UNKNOWN | FAIL MODE MSI - INSULATION |
| Asmnt FMEA 5.6.2.1 | Asmnt FM 1 | FMEA CSE AA | FMEA SCSE N/A |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |