MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A09603 | In-Flight Anomaly Number -- | Contractor Report Number S-068 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title QUARTER PANEL-TO-CHORD WELD MISMATCH |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A (1) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE LRU | NOMENCLATURE LO2 DOME BODY WELD | PART# 80912620000 | SER/LOT# N/A | MANUFACTURER MMC |
| HARDWARE NCA | NOMENCLATURE LO2 QTR PANEL CHORD | PART# 80912640000-020 | SER/LOT# N/A | MANUFACTURER MMC |
| Test/Operation L - FLD | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode UC - UNSAT | Cause MAT - MFG-ASY-EQUP |
| System STRUCTURAL | Defect MD - M SIZE | Material S - STRUCT | Work Contact C. VOGEL | Fail Date 09/18/1985 |
| Received at MSFC 10/22/1985 | Date Isolated -- | FMEA Reference 1.1.3 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text LWT-42 AND SUBS |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 10/07/1987 | CN RSLV SBMT 05/20/1986 | Defer Date -- | Add Date -- | R/C Codes 3 - F/TE -- -- |
| Assignee |
| Design J. WHITE | Chief Engineer -- | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| Approval |
| Design J. NICHOLS | Chief Engineer -- | S & MA R. JACKSON | Project M. PESSIN | Project MGR -- |
| PAC Assignee G. MILLER | PAC Review Complete GM | MSFC Closure Date 06/17/1986 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description NOTE: THIS CAPS PERTAINS TO BOTH THE LO2 AND THE LH2 QTR PANEL CHORD WELDS. THIS IS A PRODUCTION PROBLEM. THE QUARTER PANEL-TO-CHORD WELD HAS HAD LOCALIZED AREAS OF MISMATCH. THIS IS A SIX INCH LONG AREA ADJACENT TO THE INTERSECTION OF THE PANEL WELD. THE MISMATCH VIOLATIONS HAVE TYPICALLY BEEN IN A RANGE OF .040 TO .070 INCHES WHERE THE REQUIREMENT IS LESS THAN .035 |
| Contractor Investigation/Resolution 10/23/85 BACKGROUND - MISMATCH ON THE LO2 1/4 DOME OCCURS ON THE OAF WELD WHERE THE ODG INTERSECTS IT. ON THE LH2 1/4 DOMES THE MISMATCH OCCURS ON THE HFF AND HAF WELDS WHERE THE HFG AND HAG RESPECTIVELY, INTERSECT. THE MAGNITUDE OF THE MISMATCH HAS NOT BEEN SEVERE. REPAIR HAS NOT BEEN WARRANTED. THE OUT-OF-TOLERANCE CONDITION, HOWEVER, HAS OCCURRED CONSISTENTLY ON EVERY UNIT AND NEEDS TO BE CORRECTED. THE 1/4 DOME CONSISTS OF THREE GORE PANELS WELDED TOGETHER TO FORM THE 1/4 PANEL ASSEMBLY (ODG, HFG OR HAG WELDS, DEPENDING ON DOME). THIS ASSEMBLY, ALONG WITH A CHORD SEGMENT, ARE INSTALLED INTO THE T01A5002 FIXTURE TO TRIM AND WELD THE 1/4 DOME (OAF, HFF OR HAF WELD). THE MISMATCH HAS OCCURRED AT ONLY THE LOWER PANEL WELD INTERSECTION AS ORIENTED ON THE 5002. THIS DRAWS SUSPICION TO THE TOOLING ON THE 5002 USED TO POSITION AND HOLD THE PARTS. THE MISMATCH ALSO APPEARS TO BE LOCALIZED AND SHORT DURATION IN THE IMMEDIATE VICINITY OF THE PANEL WELD. THUS, PEAKING ON THE PANEL WELD AND ITS SUBSEQUENT DEPEAKING PROCESS ARE ALSO SUSPECT. 4/17/86 PRB STATUS - THE 5002 TOOL WAS MODIFIED BY SHIMMING THE CHILL BAR AND ADDING SCREW TYPE CLAMPS. ALSO, ADJUSTED THE TORCH HEAD ANGLE. CAPS IS IN MMC SIGNATURE LOOP. ECD IS 5-9-86. 5/21/86 RESOLUTION - MISMATCH WAS CAUSED BY THE INADEQUACY OF THE TO1A5002 WELD FIXTURE TO HOLD THE PANEL IN PROPER CONTACT WITH THE CHILL BAR. THE TRIM HEAD ANGLE WAS NOT OPTIMIZED TO THE ANGLE OF THE TORCH HEAD. THUS, HEAT DISTRIBUTION TO THE PANEL AND CHORD WAS NOT UNIFORM. MISMATCH PROBLEMS, ALONG THE QUARTER PANEL-TO-CHORD WELD MADE ON THE T01A5002 FIXTURE, WERE RESOLVEDBY INCORPORATING SHIMS TO THE CHILL BAR TO PROVIDE BETTER CONTACT WITH THE PANELS. THE FRAME WAS ALSO MODIFIED TO REDUCE DEFLECTION, AND SCREW TYPE CLAMPING FINGERS WERE ADDED. IN ADDITION TO THIS, THE ANGLE OF THE TRIM HEAD WAS CHANGED TO OPTIMIZE ITS RELATIONSHIP TO THE TORCH ANGLE TO PROVIDE OPTIMUM HEAT DISTRIBUTION BETWEEN THE CHORD AND PANELS. CHANGES WERE INCORPORATED AS OF MARCH 7, 1986. THIS WAS A PRODUCTION PROBLEM HAVING NO AFFECT ON FLIGHT. MISMATCH IS CHECKED ON EACH QUARTER DOME AND ANY NONCONFORMANCES ARE RESOLVED BEFORE ACCEPTANCE OF THE QUARTER DOME RECOMMEND THIS PROBLEM REPORT BE CLOSED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A09603 | IFA# -- | Contractor RPT# S-068 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80902000000-020 | Asmnt Part Name L02 TANK COMPLETE | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 3 | CAUSE CD MAT - MFG-ASY-EQUP | FAIL MODE UC - UNSAT |
| Asmnt FMEA N/A | Asmnt FM N/A | FMEA CSE N/A | FMEA SCSE N/A |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |