# Petascale Electronic Structure Calculations for Nanostructures

Lin-Wang Wang, Zhengji Zhao and Juan Meza

## OVERVIEW

Density functional theory (DFT) is the most widely used ab initio method in material simulations accounting for 75% of the NERSC allocation time in the materials science category. DFT can be used to calculate the electronic structure, the charge density, the total energy and the atomic forces of a material system, and with the advance of new algorithms, DFT can now be used to study thousand-atom systems.  But there are many problems that either require much larger systems (more than 100,000 atoms), or many total energy calculation steps (molecular dynamics or atomic relaxations). Examples include: grain boundary, dislocation energies and atomic structures, impurity transport and clustering in semiconductors, nanostructure growth, electronic structures of nanostructures and their internal electric fields. However due to the O(N3) scaling of conventional DFT algorithms (as implemented in codes like Qbox, Paratec, Petot) these problems are even beyond the reach of planned petascale computers.  In addition, as proposed petascale computers might have millions of processors, new computational paradigms and algorithms are needed to solve these problems.  For a large materials science problem, a natural approach to achieve this goal is by a divide-and-conquer approach: spatially divide the system into many small pieces and solve each piece by a small local group of processors. This solves the O(N) scaling and the parallelization problem at the same time.  However, the challenge of this approach is in decomposing the system into small pieces and patching them up again.  We present a linear scaling 3 dimensional fragment (LS3DF) method that uses a novel decomposition/patching scheme that cancels out the artificial boundary effects of the spatial division. As a result, the LS3DF results are essentially the same as the original full system DFT results with errors smaller than chemical accuracy, and the resulting computational times are thousands of times smaller than conventional DFT methods, making calculations with 100,000 atom systems feasible.  The LS3DF method is applicable to insulator and semiconductor systems, which covers a current gap in DOE’s material science code portfolio for ab initio ultrascale simulations. We will use it here to solve the internal electric field problems for composite nanostructures.

## SCIENTIFIC PROBLEM

Nanostructures such as quantum dots and wires, composite quantum rods and core/shell structures have been proposed for electronic devices or optical devices like solar cells. Understanding the electronic structures of such systems and the corresponding carrier dynamics is essential to the successful design and deployment of such devices. Despite more than a decade of research, some critical issues of the electronic structure of moderately complex nanostructures are still poorly understood. One issue is the internal electric field in a composite colloidal nanostructure and its consequences on the electron wavefunctions. It is well known that there are strong internal electric fields in some of the bulk semiconductor heterostructures, like the InN/GaN superlattice. These electric fields could be caused by surface and interface dipoles, total dipole of the nanostructure, piezoelectric effects, surface trapped charges and charged dopants. They induce strong spatial localizations of the wavefunctions, thus cause different electron-hole recombination rates, charge transports, and nonlinear optical properties, all important to the performance of the nanostructure electro-optical devices. Unfortunately, the continuous model used in conventional device simulations can no longer be used for these nanostructures due to the atomic natures of the charge, dopant and geometry, the high order effects of different phenomenon, and the change of dielectric functions, etc.  Thus, what is needed here is a direct atomistic ab initio selfconsistent calculation for the charge density and the electric field, and the corresponding atomic relaxation for the nanosystem. Since the atomic number N of such composite nanostructures easily exceeds 10,000 or even 100,000 atoms, the traditional O(N3) scaling DFT method cannot be used. Partly because of this, the internal electric field problem remains one of the most outstanding unsolved problems in colloidal nanoscience. For example, we don’t even know whether there is a large internal electric field in a simple quantum dot consisted with dipolar semiconductors, and if there is one, what is the cause of such internal electric field.

Here, we propose to use our newly developed LS3DF method to calculate 10,000–100,000 atom composite nanosystems using the local density approximation (LDA) of the DFT.  We will investigate nanostructures with different geometries and heterostructure composites: A/B nanorod, A/B core/shell nanowire, A/B/A dumbbell structures. We will also study 1) the effect of different surface passivation and surface termination layers; 2) the effect of a charge trapped in a surface dangling bond, and 3) the effect of a single dopant in a nanostructure, and test the bulk concepts of p-type and n-type semiconductors, and p-n conjunctions in colloidal nanosystems.  Our theoretical calculations could help experimentalists design better solar cells using nanostructures, which has been identified as one of the possible interruptive technologies that can revolutionize the solar cell field.

## ALGORITHM

While planewave LDA codes, like Qbox, have demonstrated the capability of using hundreds of thousands of processors on the BlueGene/L computer [1], the O(N3) scaling for its floating point operation (and O(N2) communication) may not necessarily be the most efficient way to solve a given science problem.  To reduce the time to solution, one would ideally like to use a linear scaling method ab initio method [2].  Most of these methods use localized orbitals, and minimize the total energy as a function of these orbitals.    Unfortunately the use of localized orbitals can introduce extraneous local minima in the total energy functional, which makes the total energy minimization more difficult.  On the computational side, it is difficult to effectively use thousands of processors because localized orbitals can have strong overlaps that make parallelization a nontrivial task.  As a result of these challenges and in spite of a decade of intense research, the application of these types of linear scaling methods is still quite limited. Another O(N) approach, the LSMS method [3], has been shown to scale to thousands of processors.   However this method can only be applied to metals and has been mainly used to study metallic alloys and magnetic systems.    The LSMS method could not be used to study, for example, the class of semiconductor nanostructures that we propose here.

Our LS3DF is based on the observation that the total energy of a system can be decomposed into the quantum mechanical part (the wavefunction kinetic energy and the exchange correlation energy), and the classical electrostatic part. While the electrostatic energy (Coulomb energy) is long range, the quantum mechanical energy is local in nature (short sighted). While the long range Coulomb interaction can be solved efficiently by the Poisson equation even for million-atom systems, the quantum mechanical part is the most difficult one to be solved. For this, we will take advantage of its locality by using the aforementioned spatial decomposition divide-and-conquer method. While there are previous methods [4,5] based on this divide-and-conquer concept, they all rely on positive spatial partition functions to divide and patch the spaces. There are intrinsic difficulties to use this positive partition function technique, especially for dividing the kinetic energies. In contrast, our novel division-patching method avoids these problems, thus result in a much more accurate algorithm (with the accuracy essential the same as the original full system LDA method).

Our LS3DF spatial division-patching technique is inspired by the fragment molecular orbital (FMO) method proposed by Kitaura et al [6,7] and combined with the ideas from our own charge patching techniques [8].  FMO is used for organic chain like molecules. In FMO, the long chain molecule is chopped into fragment pieces. Then each piece and pairs of nearby pieces are calculated. The electron charge density is then added up from all the pieces and their pairs, with positive sign for the pair and negative sign for the pieces itself. The usage of pairs and negative signs are innovative as this allows the calculation of the energy of the artificial boundaries, which can subsequently be subtracted from the total energy and charge density summation. Our LS3DF method extends this technique to arbitrary 3 dimensional systems. Instead of using pairs of pieces, we divide the system using overlapping regions (pieces, fragments). More specifically, our division scheme is illustrated in Fig.1 for a 2 dimensional system for clarity. Here, a supercell is divided into m1x m2 grid points. From each grid point corner (i1,i2), we can defined four pieces with dimension: 1x1, 1x2, 2x1, 2x2.  Note that, they are overlapping pieces. Now, after all the pieces at all the (i1,i2) corners are calculated, the total charge density of the whole system can be patched together as:, here D denotes the dimension 1x1, 1x2, 2x1, 2x2, and the signD is + for 1x1 and 2x2, and – for 1x2, 2x1. The total energy (especially the kinetic energy part) can be expressed in similar fashion using the wavefunctions of each piece, although the electron-electron Coulomb interaction is expressed based on the total charge density ρtot(r).  To make sense out of the above formula, we can check each point inside a piece (A point in Fig.1). Note that, each spatial point will be included in 32 pieces: 4 “2x2” pieces, 2 “2x1” pieces, 2 “1x2” pieces, and 1 “1x1” piece. After the above +/- cancellations, it will be covered by only one piece, that is what we need. We can also check for each boundary point. A boundary can be defined with a direction (i.e, boundary from A to B is different than boundary from B to A, we has used an arrow in Fig.1 to represent a directional boundary). A given directional boundary is covered by 6 pieces, with equal numbers of positive and negative signs.  Since all these pieces have the same (directional) boundary at that point, and given the near-sightedness, their charge density will be the same near that point. As a result, the boundary effect will be cancelled out. The same is true for the corner effects. This division scheme can be extended to 3 dimension, where at each corner point (i1,i2,i3), there will be eight pieces: 1x1x1, 1x1x2, 1x2x1, 2x1x1, 1x2x2, 2x1x2, 2x2x1, 2x2x2. In this case, each spatial point will be covered by 33 pieces. The sign in the formula is positive for 2x2x2, 1x1x2, 1x2x1, 2x1x1, while negative for 2x2x1, 2x1x2, 1x2x2, 1x1x1.

The near-sightedness comes from an energy gap between the occupied states and the unoccupied states in the semiconductor system. In order to keep this near-sigthedness in each piece, we need to maintain an energy gap in each piece. This is achieved by a proper surface passivation (usually with the H atoms) for the dangling bonds in the artificially created boundaries. Each small piece with a small vacuum margin is solved using a conventional planewave code (PEtot [9]) with a small number of processors.   When the wavefunctions are solved for each piece, there is no communication need between the pieces. Since the accuracy of this method depends only on the size of the pieces, for larger systems, more pieces will be generated. This makes the total floating point operation scale as O(N) and also makes it easily parallelized to a large number of processors (as each processor group calculates its own pieces independently). Thus we believe the LS3DF method is a good candidate for petascale calculations.

The LS3DF result is extremely accurate when compared to the full-system direct LDA calculation.  For example, using a cubic 8 atom cell in a diamond Si structure as our smallest 1×1×1 piece to calculate a Si box passivated with H atoms, we found that the relative energy error is 8.E-6, which is smaller than the error introduced by other sources of numerical approximations.  The absolute energy error is less than 4 meV/atom = 0.1Kcal/mol and thus better than chemical accuracy, and the total electron charge density has a relative error of 0.03%, which is essentially the same as the directly calculated results.  Finally, the atomic force error is 6.4E-5 a.u, which is an order of magnitude smaller than the typical stopping criterion used in ab initio atomic relaxation.  Thus, for all practical purposes, the result of the LS3DF method can be considered the same as the LDA calculation.   Also, note that the final accuracy depends on the size of the small pieces, so that for the same accuracy, a large system can be divided into similar sized fragments, at the cost of a larger number of fragments.  This ensures the linear algorithmic scaling of the problem, good parallelization, and acceptable accuracy.

## CODE AND SCALING

The LS3DF code is based on the planewave DFT PEtot code.  The flow chart of the LS3DF code is shown in Fig. 2 (right side), in comparison to the original LDA code (left side).  The LS3DF code consists of several components: PEtot_F, which divides the number of processors into processor groups, and the calculation of the fragment wavefunctions ψF,I by each group for a given fragment potential VF(r).  It also calculates the fragment charge density ρF(r) from the wavefunction ψF,I; Gen_dens patches together the fragment charge densities ρF(r) to generate the total charge density ρtot(r) of the whole system.  The Poisson step generates the LDA total potential Vtot(r) from the total charge density ρtot(r).  This step solves the Poisson equation for the whole system using a global FFT.  It also uses the Pulay scheme to mix the resulting LDA potential that is used in the next iteration.  Finally, Gen_VF generates the fragment potential VF(r) from the input total potential Vtot(r).

Fig. 2.  Program flow chart for a conventional LDA method and the LS3DF method

All the codes in Fig. 2 are parallelized.  As a demonstration, we have used this approach to calculate a ~3000 atom Si2253H652 quantum dot.  The calculated total charge density of this quantum dot is shown in Fig. 3a.  The calculation took approximately 2 hours on 1024 processors of the NERSC Seaborg computer.

In Fig. 2, the PEtot_F step is the most time consuming part.  The scaling of this part for the 3000 quantum dot (QD) test case on Seaborg computer is shown in Fig. 3b.  As can be seen, this step scales well up to 1024 processors.   We believe it should scale effectively to tens of thousands of processors since each small processor group solves the fragments independently.

Fig. 3. a) the charge density isosurface (green) plot of a ~3000 atom Si quantum dot passivated by H atoms.  The pink color indicates the bonds. b) the speedup (blue line) as a function of the number of processors used in PEtot_F.

Note that there are about 4605 fragments in this test case.  Thus, the number of fragments is slightly larger than the total number of atoms.  The number of atoms in each fragment ranges from 2 to 150 atoms. By using 1024 processors, we have 64 groups (assuming 16 processors/group).  Thus each group will solve on average 72 fragments.   We estimate that, in order to keep a proper load balance, each processor group at least will need to solve two fragments in average. As a result, the maximum number of processors that we can efficiently use will be in the order of 10 times the number of atoms in the system. Thus for a 100,000 atom system, we should be able to efficiently use a million processors.  For our 3,000 Si atom QD, when we used 1024 processors, the PEtot_F part of each self-consistent iteration took about 10 minutes.  The Poisson solver we used in this calculation was based on FFTs.   For the 3,000 atom Si QD case, the real space numerical grid employed was 240×240×240 and it took about 1 minute to solve the Poisson equation using 128 processors.  It took about half a minute each to finish the Gen_dens and Gen_VF program using 128 processors. Thus, in total, for the 1024 processors calculation above, it took approximately 12 minutes to finish one self-consistent field (SCF) step. For such a large QD, it typically takes 10 to 20 SCF steps (the outer loop in Fig. 2) to converge the self-consistent iteration.  As a result, it will take about 2 to 4 hours to finish one self-consistent calculation (for a fixed atomic position) for this type of QD system using 1024 processors.

The comparison between the O(N) LS3DF with the conventional O(N3) LDA method is shown in Fig.4 for the total number of floating point counts for one SCF step. As we can see, the cross over based on this floating point operation count is at about 500 atoms, which is similar to the reported cross over for the localized orbital method [10].

# Text boxes

REFERENCES:

[1] F.  Gygi, et al., Proceedings of Supercomputing, 2005 (ACM,2005)

[2] G. Goedecker, Rev. Mod. Phys., 71, 1085 (1999).

[3] http://www.psc.edu/general/software/packages/lsms/

[4] W. Yang, Phys. Rev. Lett. 66, 1438 (1991).

[4] [5] F. Shimojo, R.K. Kalia, A. Nakano, P. Vashishta, Comp. Phys. Commun. 167, 151 (2005).

[6] K. Kitaura, E. Ikeo, T. Asada, T. Nakano, and M. Uebayasi, Chem. Phys. Lett., 313, 701(1999).

[7] K. Kitaura, S.-I. Sugiki, T. Nakano, Y. Komeiji, and M. Uebayasi, Chem. Phy. Lett, 336, 163 (2001).

[8] L.W. Wang, J. Li, Phys. Rev. B 69, 153302 (2004).

[8] [9] http://hpcrd.lbl.gov/~linwang/PEtot/PEtot.html

[[9 [10] J.-L. Fattebert, F. Gygi, Phys. Rev. B 73, 115124 (2006).

[

Fig.4 total floating point operation per scf iteration

Fig. 1, The division of space and fragment pieces from corner (i1,i2).