Magnetic Field Sensors

Roadmap

November 2003

TABLE OF CONTENTS

List of Figures………………..3

List of Tables………………...3

List of Acronyms………….....3

List of Attendees ……………4

Section 1 – Introduction……..5

Section 2 – Devices………...7

Section 3 – Applications…..18

Section 4- Materials……….28

Section 5 – Outlook..…….. .38

Section 6 -References……..40

LIST OF FIGURES

| Figure 1. Detectivity of various magnetic field sensors as a function of frequency (see text for a list of references). | …….7 |
| --- | --- |
| Figure 2. Detectivity at 10 Hz as a function of sensor size. | …….9 |
| Figure 3. Field ranges for battlefield magnetic anomaly detection. Courtesy of A. Edelstein, Army Research Laboratory. | ……20 |
| Figure 4. Medical applications for sensors. From “Biomagnetism,” by Malvivuo. | ……22 |
| Figure 5. Magnetic bead array counter (BARC) as implemented by NVE and NRL. The left panel shows the concept of tagging both sensors and beads which target specific proteins. When either the A or B target is present, the field from the bead will be sensed magnetically at the corresponding site. The right panel shows a picture of the actual device. An individual sensor is shown in the zoom, and illustrates the serpentine design of the spin valve GMR sensors. Images courtesy of NVE and NRL. | ……24 |
| Figure 6. Non-destructive testing of VLSI chips. Left panel: Magnetic field above entire 20x20 cm RAM chip, showing the fields from the current supply lines. Right panel: Current vector calculated by inverting the fields. Images courtesy of NIST, samples courtesy of Intel Corp. | ……24 |
| Figure 7. Rendering of magnetic field above a cassette tape. Courtesy of NIST and the FBI Audio Forensics Laboratory. | ……29 |
| Figure 8. Comparison of a variety of different magnetic materials. Modified from Ref [1]. | ……29 |
| Figure 9. TEM image showing two nanocrystals in an amorphous matrix. [2] | ……33 |
| Figue 10. Schematic of self-powered sensor concept Ref [3] | ……34 |

LIST OF TABLES

| Table 1. Magnetic sensors matix | ……………16 |
| --- | --- |
| Table 2. Applications requirements matrix | ……………26 |
| Table 3 Materials requirements matrix | ……………36 |

LIST OF ACRONYMS

| AMR | Anisotropic magnetoresistance |
| --- | --- |
| BARC | Bead array counter |
| G | Gauss |
| GMI | Giant magnetoimpedance |
| GMR | Giant magnetoresistance |
| HDD | Hard disk drive |
| MCG | Magnetocardiography |
| MEG | Magnetoencepholography |
| MO | Magneto-optic |
| MR | Magnetoresistive |
| MRAM | Magnetic random access memory |
| Oe | Oersted |
| NDE | Nondestructive evaluation |
| Oe | Oersted |
| SFA | Strategic Focus Areas |
| T | Tesla |
| TMR | Tunneling magnetoresistance |

List of Workshop Participants and Contributors

| Group | Name | Organization |
| --- | --- | --- |
| Planning Committee | David P. Pappas | NIST, EEEL |
|  | Fabio da Silva | NIST, EEEL |
| Devices | Chair - Mark Tondra | NVE |
|  | Secretary – Stephen Russek | NIST, EEEL |
|  | Tony Arrott | NIST, MSEL |
|  | Jack Rife | NRL |
|  | Purabi Mazumdar | NIST, ATP |
|  | X. Liu | Micromagnetics |
|  | Barry Megdal | SHB |
|  | Casey Uhlig | NIST, PL |
|  | Don Porter | NIST, ITL |
|  | Solomon Woods | Neocera |
|  | Hong Wan | Honeywell |
|  | Alan Edelstein | Army Research Labs |
|  | Roger Koch | IBM |
| Applications | Chair - Yacine Dalichaouch | Quantum Magnetics |
|  | Secretary - John Unguris | NIST, PL |
|  | Konrad Bussman | NRL |
|  | Jim Daughton | NVE |
|  | Alan Edlestein | ARL |
|  | Charles Krafft | University of Maryland |
|  | John Matthews | Neocera |
|  | Ken Neimiller | NSA |
|  | Lloyd Whitman | NRL |
| Materials | Chair - Michael McHenry | CMU |
|  | Secretary - William | NIST |
|  | Thomas Ambrose | Seagate |
|  | Harsh Harshavardhan | Neocera |
|  | Frank Johnson | CMU |
|  | Chester Lo | Iowa State |
|  | Bob O’Handley | MIT |
|  | Martha Pardavi-Horvath | GWU |
|  | Robert McMichael | NIST, MSEL |
|  | Mark Stiles | NIST, PL |
|  | William Egelhoff, Jr. | NIST, MSEL |
| Other workshop attendees | William Anderson | NIST, EEEL (Director) |
|  | Lawrence H. Bennett | George Washington University |
|  | Bob Celotta | NIST, Physics Lab |
|  | Edward Della Torre | George Washington University |
|  | Vince Fratello | Integrated Photonics |
|  | Barbara Goldstein | NIST, EEEL |
|  | Can Korman | George Washington University |
|  | Dave Krefft | NSA |
|  | Steve Licht | Integrated Photonics |
|  | Lin, XY | Brown University |
|  | Bob Shull | NIST, MSEL |
|  | Cy Tamanaha | Naval Research Library |
|  | Venky Venkatessan | Neocera |
|  | Han Wen | National Institutes of Health |
|  | Dave Wollman | NIST, EEEL |
|  | Lloyd Whitman | NRL |

Section 1 - Introduction

Magnetic field sensors have had a significant impact over the past fifty years in many different technological areas, ranging from data storage to geomagnetic exploration. In 2003, the NIST leadership recognized that this technology has important applications in its four strategic focus areas (SFAs). These SFAs include homeland security, health care, information technology, and nanotechnology. Therefore, a five-year program was established to develop competence in the general area of metrology for magnetic field sensors. In particular, low noise; high sensitivity devices were identified as a key technology. In addition, a significant thrust of the program was to cultivate interaction with national industry and academia to support and transfer technology in this area. Therefore, in the first year of the program a workshop was held to gather information relevant to this field and develop a roadmap that outlines where this field is going and where significant progress can be made.

At the workshop, presentations were given that outlined many economic benefits, types of devices, applications, and materials research related to magnetic field sensors. These were discussed in separate breakout sessions. In the course of the discussion, several specific driver applications were identified. These applications were defined as those that would have a large impact in areas such as homeland security, health care, and industrial applications. Once these applications were identified, it was then possible to start evaluating the specific criteria that they need to comply with. This will then allow us to match various sensors with the specific applications.

A number of issues must be considered in choosing the materials for use in each of the various sensors.  For instance one must consider the targeted range of fields to be measured, the required field sensitivity, the sensitivity to both environmental and internal noise sources, the type of environment in which the sensor is used, the power requirements of the devices, and the read out mechanism for the device structures employed, to name a few.  The performance of a material generally must be stated with reference to a particular geometry, with the magnetic domain configuration for the material in that geometry being of paramount importance to the ultimate sensitivity and noise spectrum.

For low noise sensors, the sources of increased noise with respect to standard thin-film resistors need to be understood and decreased in magnetic systems.  This can potentially be accomplished with improved device fabrication but will likely need improved materials performance as well.  Nanoscale anisotropy variations in materials will need to be decreased while controlling the materials’ susceptibility.  Improved AMR, GMR, and TMR materials would simplify incorporation of these new materials into functioning devices.  Magnetostrictive and composite materials hold great promise for low power applications by making self-powered sensors that require no external sources of power to function.  These materials also allow the manufacture of multifunctional sensors capable of responding to more than one type of stimulus.  For low field applications the sensitivity of all of these materials will need to be improved over the next several years.

The data obtained from the workshop and the various breakout sessions was organized into a single document. This document is comprised of three sections, Devices, Applications, and Materials, representing the three breakout session. The sections are organized into a common hierarchy, including the participants, strategy, a matrix showing the relevant considerations, and a vision for the future.

Section 2 - Devices

# I. Participants

| Mark Tondra (chair) | NVE |
| --- | --- |
| Stephen Russek (secretary) | NIST, EEEL |
| Tony Arrott | NIST, MSEL |
| Jack Rife | NRL |
| Purabi Mazumdar | NIST, ATP |
| X. Liu | Micromagnetics |
| Barry Megdal | SHB |
| Fabio da Silva | NIST, EEEL |
| Casey Uhlig | NIST, PL |
| Don Porter | NIST, ITL |
| Solomon Woods | Neocera |
| Hong Wan | Honeywell |
| Alan Edelstein | Army Research Labs |
| Roger Koch | IBM |

# II. Strategy for Development of Magnetic Sensors

# Magnetic sensor technologies are extremely diverse with many different types of existing and proposed field sensors, each with its own set of advantages and disadvantages.1-8 Fig. 1 shows a plot of the magnetic field detectivity for some of the commercially available magnetic sensor technologies versus frequency. While field detectivity is an important parameter in optimizing field sensors, it is not the only and often not the most important metric in optimizing field sensors.  Several general considerations were identified as underlying elements in advancing magnetic sensor technology.  The first step in planning the advancement of magnetic sensor technology is to determine which areas of magnetic sensor applications will have the greatest impact.  This step is critical since the numbers of existing and proposed magnetic sensor technologies are so large that is imperative to target critical applications, understand the application requirements, and target sensor development towards these applications.  To pursue this targeted development it is important to clearly identify the current state-of-the-art in different sensor technologies and determine what advancements are theoretically and reasonably possible.

In parallel with targeted sensor development, it is necessary to continue to build understanding through basic research.  Particularly, it is essential to understand and control sources of noise and to understand the fundamental limitations due to both noise and signal. Research must provide clear pathways for applications developers to improve signal and reduce noise.  Continued work on materials will be required for improved sensors.  In particular, there is considerable room for improvement in ferromagnetic materials.

Magnetic sensor development must be cognizant of market considerations. The market drives the acceptable cost of a sensor as well as the total allowable funds that are available to develop new sensor technologies. The cost of making sensors includes much more than the cost of fabricating the transducer.  The costs include research and development, testing, characterization, calibration, etc.  For many of the applications the market will not support the cost of research and development, therefore, it may be necessary to leverage off of other technologies, such as magnetic recording sensor technology.

Magnetic sensors can be distinguished by several criteria that determine their range of applications.  The important criteria include:

Operation temperature: room temperature or cryogenic.  The best field sensors (SQUIDs) require cryogenic (< 77 K) operating conditions.  The required cryogenic system and thermal isolation prohibit use of such sensors in many applications.

Integrability:  Many applications can be enabled and made less costly if the sensor can be integrated with conventional semiconductor technology and into large arrays.  Conversely, if this is not the case, then the system costs are increased and applications are limited to only a few input channels.  The requirement of integrability favors the development of thin film or semiconductor sensors.

Type of field sensing: vector or scalar, field or flux.  Most sensors sense the magnetic field in a certain direction (vector sensitivity).  In many applications this is desired, however, there are cases, such as geologic imaging, when high sensitivity total field measurements are required and scalar sensors perform much better than multi-axis vector sensors.  Magnetic field sensors can also be divided into field or flux sensors.  Search coils and SQUIDs are flux sensors, hence the field sensitivity is proportional to size.  This is advantageous for large systems since the sensitivity can be greatly increased going to larger input structures.  For small scale sensing, field sensors are advantageous since their sensitivity is, in general, constant as the sensor size is scaled down.

Frequency range: low frequency 0.1 Hz – 100 Hz or high frequency (up to 10 GHz).  Each application has a particular frequency range of operation and each type of sensor has a particular frequency range of operation. Magnetocardiography, for instance requires low frequency sensors (0.1 to 10 Hz), while characterization of high-speed circuits and data storage applications requires operation in the GHz range.

Sensor size: Different applications require different sensor sizes.  The smallest sensor size (<1 (m) is required for data storage applications and imaging fields above integrated circuits.  Many applications, such as magneto cardiogram and battlefield sensors the size requirements are lenient (1 (m to 1 mm).  In general, there is a trade off between selectivity and sensor size with the detectivity scaling as d-2 to    d-0.5 for many types of sensors (see Fig. 2).

These general criteria listed above are used in the next section to assess present and future magnetic sensor technologies.

III. Magnetic Sensor and Properties Matrix

1. Search coil

Search coils are a mature, inexpensive technology that have great sensitivity.  They are based on Faraday’s law of induction and provide a voltage signal proportional to the time rate of change of flux through the coil.  Search coils can have either an air core or a soft magnetic core.  As a flux sensor, search coils can achieve high sensitivity only for large coils and their utility decreases on small size scales.   Further, as a dynamic sensor (with a signal proportional to the rate of change of flux) stationary search coils cannot operate at DC and their frequency of operation is limited to > 1 Hz.  While rotating coils can be used for DC measurements, it involves additional mechanical complications.

2. Hall probes

Hall probes rely on voltages induced by Lorentz forces on charge carriers in semiconductor structures. Hall probes are a mature technology, and have good sensitivity over a wide range of device sizes (<1 (m to 1 mm).9  The frequency range of operation is generally limited to < 1 kHz due to signal-to-noise problems.  Hall probes can be implemented in many semiconductor technologies from InAs to Si with a general trade-off between performance and material complexity.  Hall probes have several advantages, including a large dynamic range, linear response, and scalability over a wide range of dimensions. Disadvantages include temperature dependence of the Hall coefficient and relatively small signal. Given the maturity of semiconductor technology there appears little room for improving the performance of traditional Hall sensors.

3. Fluxgate

Fluxgate magnetometers, originally developed in 1928, are based on the nonlinear response of a soft magnetic core.  Typically, a soft magnetic core is driven by an AC signal at a frequency between 100 Hz and 10 kHz and the magnetic field is determined by monitoring the second harmonic signal. Fluxgates provide extremely high sensitivity with the convenience of room temperature operation and relatively simple system requirements.10 Recent advances in understanding and eliminating noise in bulk flux gate sensors have improved the sensitivity to ~ 1 pT/Hz0.5 .11 Bulk fluxgates, however, are hard to integrate into arrays or integrate on-chip with standard semiconductor electronics.  The complete system tends to be bulky and require considerable power.  Several attempts have been made to fabricate thin-film versions of fluxgates with limited success.  Several theoretical models indicate that low noise thin-film fluxgates may not be possible.

4. Superconducting Quantum Interference Device (SQUID)

SQUIDs are, at present, the most sensitive magnetic field sensors.12, 13 The advent of high-temperature superconductors have pushed their operation temperatures up to ~77K and has greatly simplified cryogenic requirements.14 SQUIDs, as flux sensors, lose sensitivity when scaled down.  However, given their high sensitivity, they can still perform well at dimensions down to a few micrometers.  When coupled with flux guides, their effective spatial resolution can be sub-micrometer.  SQUID technology is relatively mature with systems approaching their theoretical limits.  Further improvements in SQUID technology can come from materials development that increases the operation temperature.

5. Anisotropic Magnetoresistance (AMR)

AMR refers to the change in the resistance of a magnetic material that is dependent on the relative orientation of the magnetization and the applied current.15 AMR is a mature technology that has seen wide applications for industrial sensors as well as in recording heads.16, 17 The devices are scalable with device sizes ranging from < 1 (m to 100 (m.  The systems can be integrated with semiconductor electronics and can be integrated into arrays.  The sensitivity is limited to the sized of the anisotropic magnetoresistance (< 5%). No theoretical limitations have been determined for this effect and it may be possible to find materials with larger AMR.  AMR systems, which rely on single layer, single material systems, in general, have lower 1/f noise than the more complicated GMR and TMR systems. They can, therefore, in many instances, provide good signal to noise even though the intrinsic output is lower.

6. Giant Magnetoresistance (GMR)

The GMR effect, discovered in 1988,18,19 arises from the change in resistance due to the change in relative orientations of adjacent magnetic thin-film layers.  GMR provides considerably higher resistance changes (up to 70%) than obtainable by AMR.  The similarity to AMR in device configuration and system implementation has led to rapid incorporation of GMR sensors for applications in data storage, industrial sensors, and magneto-electronic devices such as magneto-isolators.20-24 One major limitation of GMR sensors is that high magnetoresistance has been obtained only in systems that require a high saturation field.  Hence, devices with high GMR often have the same sensitivity as devices with lower GMR and lower saturation fields. The major challenge for GMR sensors is to understand and eliminate noise sources and bring the 1/f noise down to the same levels found in AMR sensors.25 Most GMR sensors have detectivity greater than 0.1 nT/Hz0.5.  However, with a flux concentrator, detectivities of 10 fT/Hz0.5 at 1 Hz and 4.2 K have been reported.26

7. Tunneling Magnetoresistance (TMR)

TMR utilizes the change in tunneling resistance between two adjacent ferromagnetic electrodes.27 TMR provides high signal levels (up to 220%) and has the same scalability and integrability advantages that AMR and GMR devices have.7, 8 The advantage of TMR devices is that the larger change in resistance can be obtained in smaller fields and the resistance can be engineered over a large range while maintaining constant device geometry.  Obtaining high-impedance sensors allows for low power operation, although these high-impedance devices will be Johnson noise limited and may not have as good signal to noise as lower impedance lower magnetoresistance devices.  One major limitation of TMR devices is that the (R/R falls off with applied voltage so that the maximum signal from a single TMR device is limited to about 50 mV.  A key issue in improving the performance of TMR devices is understanding and eliminating low frequency noise.28-32

8.  Extraordinary Magnetoresistance (EMR)

A new class of magnetic sensors, extraordinary magnetoresistance (EMR), has been recently introduced that has many similarities with Hall sensors.33-35 These types of probes use careful design of electron trajectories in high-mobility semiconductors and close proximity of high conductivity shunts to manipulate the device resistance.  This sensor has been scaled down to sub-micrometer dimensions and shown to have detectivities of ~ 1nT/Hz0.5.

9. Giant Magneto-Impedance (GMI)

Giant magneto-impedance is a new technology that, at present, is restricted to bulk applications using amorphous wires.  GMI relies on the inductance change of a soft magnetic sample due to changes in the permeability in an applied magnetic field. GMI has many of the same advantages and disadvantages as flux-gate sensors.  At present this technology is similar to fluxgate technology in that the sensor systems are large, hard to integrate into arrays and require considerable power.

10. Magneto-optic

Magneto-optic (MO) sensing is a relatively mature technology.  For most implementations, MO sensors rely on the same type of magnetization rotation that occurs in AMR, GMR and most other sensors.  The difference is that the detection mechanism is optical.  This provides several advantages in applications in which electrical connection is undesirable, such as sensing magnetic fields from high-voltage transmission lines.

11. Nuclear and electron magnetic resonance

Nuclear resonance magnetometers are, at present, the most accurate magnetometers available.  The combination of narrow NMR line widths, the ability to precisely measure frequencies and the absolute calibration make this sensor useful for metrology.  The small bandwidth, restricted field range, large size, power consumption, and high cost make this type of sensor, at present, not practical in many applications.

12. Optical pumping

Recent advances in optical pumping have demonstrated field sensitivities down to 1 fT.  The high resolution is due to the ability to precisely measure atomic transitions optically.  The optical pumped magnetometers are scalar magnetometers suitable for geophysical imaging and biomedical applications such as magnetocardiograms. At present the optical cells and control hardware are large and bulky and emphasis is on developing compact low power systems.

13.  Magnetostrictive / Magnetoelectric

Magnetoelectric sensors are a new sensor concept in which a magnetostrictive sensor is coupled with piezoelectric sensor.  The applied field rotates the magnetic elements’ magnetization and the associated strain is detected as a piezoelectric voltage.  This technology has the advantage of being self-powered and has the potential of large output voltages (up 10 V/mT).  The noise performance for magneto-electric sensors is still under investigation.  Fabricating magnetoelectric sensors in an integrated format, on a silicon wafer with conditioning electronics, remains a challenge and requires a micromachined structure to allow magnetostrictive stress to be applied to the piezoresistive element.

The information from Section II and Section III is combined in order to compare the properties directly. This matrix is shown in Table 1. It shows the identified magnetic sensor technologies and their properties.  The magnetic sensor technologies are listed roughly in order of their maturity, with the most mature technologies listed first.

Table 1 – Magnetic sensors matrix

| Sensor type | Sensitivity/ Field range | Frequency Range | Operation Temperature | Minimum sensor size/ Scalability | Vectorial/ scalar | Cost | Advantages | Disadvantages | Status |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Search coil | 30 fT | >1 Hz | RT | 1 mm | vector | Moderate | Low cost for the sensitivity | Limited to > 1Hz, sensitive to angular vibrations, Loose sensitivity as decrease size | Mature |
| Hall probe/EMR | 100 nT/ 1nT | < 1kHz | RT | < 1(m | Vector | Moderate | Large range, linear | Temperature dependent | Mature |
| Fluxgate | 1 pT/Hz)0.5 @ 1Hz | < 1kHz | RT | Loose S/N scaling down | Vector | Moderate | High sensitivity | Cost, size, energy consumption | Bulk filmv versions possible |
| SQUID | 1 fT | <1kHz | <77K | < 1(m (system large) | Vector | Expensive | Sensitivity | Need for low temperature | mature |
| AMR | 50 – 100 pT | 0-5 GHz | RT | < 1(m | Vector | Moderate | Lower 1/f noise |  |  |
| GMR | 20 nT | 0- 5 GHz | RT | < 1(m | Vector | Cheap | Low cost in large quantities |  |  |
| TMR | 1 nT | 0-1 GHz | RT | < 1(m | Vector | Cheap | Large MR, low cost in large quantities | High 1/f noise, hysteretic |  |
| GMI | 100 pT | <500 kHz | RT | 1 mm | Vector | Moderate |  | Cost, size, high power |  |
| Magneto-optic | 100 pT | 0-5GHz | RT | . 1 mm | Vector | Moderate | No electrical connection |  |  |
| Resonance |  | DC | RT |  | Scalar | Expensive |  |  |  |
| Optical pumping | 10-1000 fT | < 100 Hz | RT | 10 mm | Scalar or vector | Expensive | Insensitive to angular vibrations | Cost, power consumption, loss of sensitivity at higher frequencies |  |
| Magnetostrictive/ Magneto-electric | 1 nT |  | RT | 10 (m | Vector | Moderate | Low power Large output voltage | Sensitive to vibrations |  |

IV. Improvement of magnetic sensors: vision for the future

There are several clear directions for improvement of magnetic sensor technology to enable new applications.  While SQUID sensors provide adequate low field sensitivity for most applications it is difficult and expensive to implement SQUID systems due to the cryogenic requirements.  Several approaches exist to make SQUID systems more useable including implementation of high Tc materials and developing smaller integrated cooling systems.

Fluxgate sensors have shown continual improvement in performance with the use of new types of magnetic materials and geometries.  Continued improvement is required on miniaturizing flux gate sensors and making them more integrable with signal processing and control circuits.  It remains a challenge to fabricate a thin film flux gate that has comparable performance with bulk versions. GMI sensors have similar requirements to fluxgates requiring improved materials, miniaturization, and integrability.

While magnetic resonance and optical pumping magnetometers are extremely accurate, measuring deviations in magnetic fields of less than 1 pT, there is considerable room for improving these sensors to allow a greater range of applications.  More effort is required to reduce the low field performance of these sensors, make the systems smaller and more integrable in multi-sensor systems.

Magnetoresistive sensors (GMR, TMR, CMR) are already operating in the 0.1 nT regime, show great promise in  that they can easily be integrated with silicon processing, can be miniaturized, and can be fabricated cheaply in large quantities.  The challenge remains in increasing the signal size and understanding and eliminating the low frequency noise sources.  There are good reasons to believe that this type of sensor technology can be pushed into the 1 pT regime.

New sensor concepts, such as integrated magnetostrictive/piezoelectric or EMR sensors, must continue to be explored.  There is however, a need for consistent testing and benchmarking of magnetic sensors so that the relevant merits and weakness of each technology are quantified and readily accessible.

Section 3 - Applications

I. Participants

| Yacine Dalichaouch – chair | Quantum Magnetics |
| --- | --- |
| John Unguris – secretary | NIST, PL |
| David Pappas | NIST, EEEL |
| Konrad Bussman | NRL |
| Jim Daughton | NVE |
| Alan Edlestein | ARL |
| Charles Krafft | University of Maryland |
| John Matthews | Neocera |
| Ken Neimiller | NSA |
| Lloyd Whitman | NRL |

II. Strategy for Identification of sensor applications

Presentations were given that outlined many applications that are based on magnetic field sensors. In the course of the workshop, several specific “driver applications” were identified. These applications were defined as those that would have a large impact in areas such as homeland security, health care, and industrial applications. Once these applications were identified, it was then possible to start evaluating the specific criteria that they need to comply with. This will then allow us to match up various sensors with the specific applications.

- Sensitivity – For the various applications, this parameter varies significantly. The units are typically reported in tesla, T, or gauss,G (1 G = 10-4 T). In free space, the conversion from gauss to oersted (Oe) is unity. In SI units, the corresponding units are ampere/meter, and can be found using the relation 1 Oe =1000/4( A/m. Intrinsic to this parameter is the dynamic range that is required in order to achieve acceptable performance. This may imply the necessity of using shielded rooms or dynamic feedback. The main problem here is that ultra-high sensitivity devices will tend to saturate under ambient conditions.

- Frequency range – Again, there are many different frequency ranges that are needed for the various applications. Fortunately, however, most applications need a relatively small bandwidth. This leads to a natural separation of applications into low and high frequency. In general, active feedback can be used in the low frequency range (as is done for SQUID magnetometers), while band pass filters can be used for high frequency applications (e.g., magneto-resistive sensors for hard disk drives).

- Operation temperature – Nearly all of the applications involved measurement of magnetic fields in a room temperature environment. However, the sensors themselves may require cooling. In this case, it is necessary for the cooling apparatus (typically a dewar) to be non-magnetic and allow the sensor to be close enough to the source of the magnetic field.

- Sensor size – This specification refers to the volume that the package or individual sensor can be allowed to encompass. While there is a wide range of package sizes, it must also be noted that cooling apparatus can significantly increase the required volume.

- State-of-the-art sensors – There has been significant development in most of these application areas. One of the main goals of this work is to identify areas where new, innovative technologies can have a significant impact. This may be either by supplanting the existing technology or enhancing the current methods, sensors, and associated materials.

- Arrays vs. single element and scanning techniques – Many applications require arrays of sensors for field mapping or parallel detection methods. The actual spatial dimensions that the field needs to be mapped over also help define what sensor will be optimal. For example, very large arrays of sensors can be fabricated on wafers, thereby allowing for small-scale magnetic field mapping. However, for mapping magnetic fields in a battlefield or border situation may require arrays of individual sensors that are linked with telemetry.

- Nano-scale vs. macro-scale – This parameter is similar to that of (4), however, it refers to the relevant dimensions of the actual sensor, independent of the packaging.

- Cost – In general, low cost is important when transferring technology. However, some applications may be important enough that cost is no object. Examples might be in specific homeland security and health care applications.

- Power consumption – This is most important in situations where either individual sensors are distributed with limited local sources of power, or where there is a very high density of magnetic sensors in a small area.

- Environment – In contrast to (3), this item includes other aspects such as corrosion and high temperature environments. These must be considered when comparing various technologies.

# III. Magnetic Sensor Applications Worksheet

Driver applications were identified in the general discussion leading up to the breakout sessions. These included:

- Battlefield/unattended ground sensors – This is an application with possibly the most stringent requirements. These include operation with high field sensitivity in relatively high ambient fields, low frequency, low power consumption, and low cost. In addition, the environment that these sensors operate in is highly variable (see Fig. 2). All possible types of terrain, weather conditions, and deployment methods must be accommodated. In general, distributed arrays of sensors with telemetry to a central station would have the most impact. Finally, the reliability of these devices is critical because lives and homeland security are at stake. Therefore, this is a high-risk, high-payoff application.

- Magneto-cardiography – It is well known that bio-magnetic signals from both the heart (MCG) and the brain (MEG) can be detected with ultra-high sensitivity magnetometers. Related applications include early detection fetal MCG. Again, these signals require very low frequency operation. Fig. 4 illustrates this, and also compares various sensor response curves with the background magnetic noise. At present, these signals are typically measured using superconducting quantum interference devices (SQUIDs). These devices require cryogens, and are therefore limited in how close to the subject they can get and how many can be deployed effectively in an array. This is not such a critical concern, however, due to the fact that the magnetic fields vary relatively slowly over the regions to be measured. In general, the cost of these systems is not as critical as identifying the specific impact and mode of operation.  However, it can be seen that relatively modest improvements room temperature sensors such as fluxgates or induction coils could allow for these techniques to be applied to MCG. In addition, if magneto-resistive (MR) sensors are integrated with flux guides, they may also have a significant impact. The goal would be to develop a real-time system with at least 1 cm source localization capability. The advantages of these devices would be low cost screening systems for routine checkups, arrhythmia diagnosis, and advance myocardial electrical diagnosis.  This is a relatively high payoff, medium risk application.

- Bead Array counters (BARC) – These devices represent direct competition for the fluorescence tag technique that is used in health care assay applications. The sensors needed for these must be packed into a very high density array, and single bead detection is desirable. An example of this technology is shown in Fig. 5. The field sensitivity is modest, and medium frequency operation (~1 kHz) is acceptable. Existing devices are currently limited by the micro-fluidics and the chemistry of tagging, however, as these issues are worked out, the opportunity for magnetic sensors to make a high impact is there. This is a high payoff, relatively low risk application.

Other identified applications

- Sensors for measuring currents on high tension wires – Reliability of the power grid are dependent on adequate distributed diagnostics. Magneto-optic sensors for this application would allow reduced costs significantly reduced size (3% of current technologies). These are installable without breaking the circuit (as opposed to technologies currently in use) and can be safely queried by fiber optic means. There are no conductors and the fiber cables can be permanently installed to the ground. Such pervasive sensors are an enabling technology of an autonomously reconfigurable power grid. The challenges of this are the harsh environment, with a linear response up to 100 kV/m over a temperature range from subzero to 160 C. The sensor material (typically ferromagnetic garnets) and readout system must be able to deal with this. Improvements in sensitivity at low currents enable opportunities in “smart” buildings, optical power metering, and shipboard sensors. Coordination with voltage sensors can yield a complete power sensor. Moderate field sensors are inherently required. The timeline for development will depend on when mil-spec qualified prototypes could be available. This typically takes 1 – 2 years. Temperature independent and high sensitivity materials can be developed another 1 – 2 years down the line. Qualification by power companies will depend on their own agendas, but will be accelerated by military applications.

- Bead tracking in-vivo - This application has been identified by researchers at NIH as being a very promising avenue of studying blood flow in capillaries and organs. This can be used, for example, in conjunction with other imaging techniques to understand the impact of stroke on cardiac function and the electrical circuits in the heart. Pneumomagnetometry is a unique method of evaluating an iron overload in organs such as the liver and lungs. It is non-invasive and real-time, showing the integrated signal from the area under evaluation.

- Non-destructive evaluation (NDE) for micro-electronics – NDE using magnetic field mapping to obtain source current distribution can be conducted at two scales – either at the macro-scale, to evaluate the current vectors in a circuit, or at the nanoscale, to evaluate the current distribution in individual traces on a die. In an example of the first case, Fig. 6 shows the magnetic field map above a RAM chip. The perpendicular component of the field is measured. This allows for de-convolution of the currents in the two in-plane directions, as shown in the right hand panel. In this application, arrays of relatively large (tens of micrometers) scale sensors can be used. This is because the sensors are typically scanned at distances at least the same distance from the source, i.e. from the back-side of a flip-chip package, circuit board, or other electronics package. In the second case, where the current distribution in individual traces is of interest, nano-scale sensors that come in direct contact are needed. These sensors can be highly shielded, and good results have been obtained using off-the-shelf components designed for hard disk drive readers.

- Magnetic media scanning and characterization – This application includes testing for advanced magnetic data storage media in hard disk drives as well as forensic analysis of conventional media from cassettes and other ubiquitous magnetic data storage media. In the first case, both of-the-shelf and custom read/write assemblies have been used to study the efficacy of nano-scale, fine-grained and patterned media. In general, this application requires scanning of a single, nano-scale sensor. In the second case, arrays of sensors that can map out wide swaths of data from audio and video storage media are needed. This is demonstrated in the image from a cassette tape, shown in Fig. 7. The image is approximately 4 mm long and 4 mm wide, representing 0.1 seconds of sound. The ridge along the left side is a ½ width (mono) erase head stop event, and the washboard on the top right is a test pattern written with a dual ¼ width (stereo) head. The magnetic texture of the tape and the details of the write stop even are significant in a forensic evaluation, and this image represents details that are orders of magnitude better than can be obtained by traditional magnetic powder/fluid techniques. The main obstacle is the need to screen many hours of tape in real time with high resolution.

After the breakout session, the applications and various requirements discussed in sections II and III were compiled. This data is presented in Table 2. From this table, it can be seen that there is a wide disparity in the requirements for the various driver applications

Table 2 – Applications requirements matrix

| Application | Sensitivity /field range | Freq. Range | Oper. temp | Sensor size | Current sensor | Array vs. scan | Nano vs. macro-scale | Cost | Power Issues | Envir-onment |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BARC | 0.01 mT | DC-1 kHz | 20 – 80 C | 100x100 (m “area” | GMR, Hall, coils | Array |  | $1/ chip |  |  |
| Magneto-Cardiogram | 5 – 100 pT | 0.1 – 40 Hz | 4 – 77 K | 10s μm2 | SQUID | Single and arrays |  |  |  |  |
| Magneto-Encephalogram | 10’s fT | 10 mHz- 1 kHz | 4K | 10 μm2 | SQUID | Array |  |  |  |  |
| Forensic | 0.1 mT | Dc- 60 kHz | RT | 1x1 cm | Garnets | Imag-ing |  |  |  |  |
| VLSI NDE Package vs die | PT | DC – 100 MHz | 77K- RT | 1- 10 μm | SQUID/MR | Both | 1- 10 μm, package 10 nm, device |  |  |  |
| Geophysical | PT – 10 nT | 0 – 300 kHz | RT | 1x1 cm | Induction coils, MR | Both | Nano |  |  | RT-250C (bore hole) |
| MRAM | 10 mT | 10 – 500 mHz | -25 – 100C | 100 nm | TMR | Array | Nano | <DRAM |  |
| Data sensors (read heads) | 1 mT | 500 mHz | 60 C | 500nm | GMR | Scan-ning | Nano | <$2 |  |  |
| Filtration monitors |  |  |  |  |  |  |  |  |  |  |
| Battlefield | 1pT – 1nT | 0.01 – 1 kHz | -20 – 40 C | 3x3x3 | AMR, FG, coils, OPM | Both |  | <$1 | <50 mW |  |
| Naval situations | 1pT – 1nT | 1 Hz- 5 kHz | 5 – 40 C | 3x3x3 | Fluxgate, AMR | Both | Macro | <$10 | <10 mW | Water |
| Field sensing communications |  | GHz |  |  |  |  |  |  |  |  |

IV. Development of applications: vision for the future

Many uses for advanced sensors were put forward at the meeting. However, the point was made that only a few specific applications may drive a given technology to its ultimate potential. Given that consideration, the three main driver applications were identified: battlefield, magneto cardiography, and bead arrays. These applications fit in the general areas of homeland security and health care, and are therefore good matches with NIST Strategic Focus Areas (SFA’s). Other identified applications also fit well with the Information Technology SFA, and are compatible with existing funded programs at NIST.

The general approach to this work will therefore be to focus on these areas of research. We will do this by identifying specific sensor technologies and materials systems that will enable the driver technologies.

Materials for magnetic field sensors

I. Participants

| Michael McHenry (chair) | CMU |
| --- | --- |
| William Rippard (secretary) | NIST |
| Thomas Ambrose | Seagate |
| Harsh Harshavardhan | Neocera |
| Frank Johnson | CMU |
| Chester Lo | Iowa State |
| Bob O’Handley | MIT |
| Martha Pardavi-Horvath | GWU |
| Robert McMichael | NIST, MSEL |
| Mark Stiles | NIST, PL |
| William Egelhoff, Jr. | NIST, MSEL |

II. Materials identification strategy

As discussed above there are a great number of potential uses for new magnetic field sensing devices.  The applications for these devices are widespread, with the specific requirements of each device being particular to its application.  A number of issues must be considered in choosing the materials for use in each of the various sensors.  For instance one must consider the targeted range of fields to be measured, the required field sensitivity, the sensitivity to both environmental and internal noise sources, the type of environment in which the sensor is used, the power requirements of the devices, and the read out mechanism for the device structures employed, to name a few.  The performance of a material generally must be stated with reference to a particular geometry with the magnetic domain configuration for the material in that geometry being of paramount importance to the ultimate sensitivity and noise spectrum.

Potential soft magnetic materials include traditional crystalline and amorphous ferromagnetic transition metals and alloys, high resistivity oxides (ferrites) as well as more recently developed materials such as nanocrystalline alloys, nanocomposities, and magnetic oxides, each of which can be incorporated into a multilayered structure.  A number of different materials properties may be exploited in sensor application including magnetoresistance, giant magnetoimpedence, magnetocaloric, magneto-optical, and magnetostrictive effects. Each of these effects will also have its own advantages and disadvantages for a particular field sensing application and device structure, and each presently has its own obstacles to be overcome for full integration into new field sensing technologies.  Below we will give a general overview of the various materials systems with regards to both device structures and their present limitations.

The materials will be distinguished by two broad features that determine their potential integration into the different types of sensors and applications discussed above.  These features include:

Magnetic Properties:  The magnetic properties of materials can be partitioned into intrinsic and extrinsic properties.  The intrinsic properties include saturation induction, Curie temperature, magnetocrystalline anisotropy, and are derived from the composition of a particular phase.  Some extrinsic magnetic properties, like coercivity, induced anisotropy, permeability, depend on microstructure, while others, such as shape and thickness, are engineered.  Many materials systems are innately well suited for measuring magnetic fields over a specific range of applied fields. This depends on the anisotropies of the material system, coercivities, and permeabilities that can be engineered.  Further limitations on integration into devices include the functional temperature range, operating environment, susceptibility, and tunability of these properties. Figure 8 shows a comparison of two figures of merit, permeability and saturation induction, of a number of the different magnetic materials discussed below.  For many applications the frequency dependent magnetic loss and the temperature dependence of properties are also a consideration.

Field Response Mechanisms:  Different materials systems can respond to the application of a magnetic field in a number of different ways that determine the read out mechanism appropriate for each system.  These include electrical responses, caloric response, optical responses, and magnetostrictive responses.  Together the combined magnetic response mechanisms, read out schemes, and field sensitivity will determine the applicability of individual materials systems to the different field sensing devices.  Perhaps the most difficult task in realizing the materials required for new sensors is that efficacy of a particular material system in meeting the requirements for a specific set of devices can not be determined from simple magnetometry measurements alone.  Instead each must be characterized and optimized in order to meet the specific requirements of active devices, which not only measure magnetic fields but also magnetic noise and noise associated with the device readout.  A systems based approach to sensor development is thus preferred.

III Specific Materials for Sensors

- Semiconductors

Conventional semiconductor materials have long been used to make Hall sensors.  The materials range from simple to compound semiconductors, with the latter typically giving improved performance.  These materials are fairly mature and seemingly unlikely to provide dramatically improved magnetic sensors.  More recently, magnetic semiconductors have been used to produce novel field sensors.  These materials are relatively unexplored and may provide promise in new sensor technologies.  Presently most of these materials are limited to low temperature operation.

- Superconductors

SQUIDs are presently the most sensitive field sensors. Both conventional and high Tc materials have been demonstrated.  This is a mature technology with the clear path towards increasing the utility of these sensors based on increased critical temperatures.  As the sensitivity of the superconductor based sensors are close to their theoretical limits, it seems unlikely that other materials improvements are needed.

- Transition Metals and Alloys (Bulk)

Transition metals and alloys have been used as field sensors since the advent of the compass.  Modern devices typically rely on the anisotropic magnetoresistance, AMR, effect as the field sensing mechanism and are still being used as the sensing mechanism in tape read heads.  The drawback of these systems is that the AMR, typically a few percent, is a relatively small effect.  Presently the theoretical limit on the size of the AMR effect in materials is not understood.  Hence while being a relatively mature technology there may be a great potential for improvement for these materials.  However, since there has already been a great deal work done in investigating the AMR effect in both simple and complex transition metal alloys, it seems unlikely that great improvements will be made without the study of novel alloyed materials.  These materials are also presently used as flux concentrators.  Improvements in both susceptibility and saturation magnetization would increase the functionality of these materials as flux concentrators.

- Single Crystal Metals

Single crystal metals have number of properties that make them attractive for use in magnetic sensors.  They can have very high susceptibilities, theoretically they can have very high spin polarization at the Fermi level, and they should lack both the electronic and magnetic noise associated with defect states.  Their major drawback is the difficulty associated with growing single crystal materials.  A small density of defects or slight material contamination can remove the advantages of single crystal materials.  Without a large technology need to drive mass production, they are likely to remain prohibitively expensive for incorporation into sensor devices.

- Oxides

The most commonly studied materials are ferromagnetic garnets, ferrites, and perovskite structures which can be both conducting and insulating.  Depending on the particular class of materials under consideration, these types of materials may be queried by either optical or electrical methods.  They are comparatively less sensitive than other materials or have high sensitivity over a small range of temperatures. However, they have great potential for incorporation into field sensors for niche markets in which these are not limitations.  Because of their high resistivities, these are the materials of choice for high frequency applications.  At lower frequencies their relatively small inductions are a drawback.

- Multilayers

In practice most electronic based sensors will incorporate multilayered structures for improving the sensitivity of the device readout.  Layered materials can also be used to create multifunctional sensors and manipulate the readout mechanism of the device.  Multilayered materials can also result in new interactions between magnetic layers such as interlayer exchange coupling.  However, undesired magnetostatic interactions between the layers can also be problematic.  Multilayered structures can also be used to effectively magnetically bias a material without the need for an externally applied field.  Novel laminating schemes can potentially enable the engineering of an array of magnetic sensing devices. Lamination also provides the means for taking advantage of the high moments of metals and the high resistivity of intervening oxide layers.

7.  Nanocrystalline (Nanocomposite) Alloys

These alloys consist of small grains embedded in a host material (often an amorphous metal) system (see Fig. 9).   They have a number of appealing aspects for their incorporation into ultra-low field sensors.  These materials can be made to have large inductions and very large susceptibilities as well as tunable anisotropies while retaining very low losses.  This makes them particularly attractive as the core material in flux gate sensors and as flux concentrators. The choice of materials, their magnetorestriction coefficients and geometries to promote favorable domain configurations is essential to many of these applications where a giant magnetoimpedance (GMI) effect is of interest. These materials can also potentially be incorporated into electrical sensors through the GMR or TMR effects, although electrical resistance noise associated with the relatively high resistivity of these materials may be problematic.  These materials are relatively new and have a large phase space of materials combinations that remains to be explored.  Development of novel nanocrystalline alloys has the potential to greatly impact magnetic sensors over the next several years.

8.   Multifunctional Nanocomposites

Another class of materials is that of multifunctional nanocomposites.  These materials typically consist of a magnetically sensitive material embedded in a host material matrix.  Because the material composition is controlled on a length scale similar to magnetic length scales the resulting materials can have properties more complicated than just the average properties of the constituent components.  Composite materials can have a wide array of response mechanisms to magnetic fields including magnetoelectrical, magnetooptical, magnetocaloric, and magnetorestrictive responses.  Furthermore, these composite materials hold great promise in creating dual function sensors.  By appropriate choice of the materials used in creating a composite the sensors can be made to be sensitive to multiple types of stimuli, creating hybrid sensors.  Each of these materials has advantages and drawbacks.  In general, the largest present impediment to their use in widespread applications is that they presently lack sensitivity or ability to be used in a wide range of environments.

9.   Rare-earth alloys

Rare earth alloyed materials is a less mature class of materials but one with novel material attributes.  These are typically magneto-restrictive and magneto-optical materials with some showing shape memory attributes.  These materials can be engineered to have either high or low anisotropies making them making them attractive as both magnets as well as sensors.  By combining them in multilayered structures with, for instance, piezoelectric materials, self-powered sensors can be made (Fig.10).  These materials would benefit from increased sensitivity and increased operational temperature range.  They can also be used in GMI device structures.  Comparatively little is known about the noise output in these materials.

- Nanofabricated Materials

In principle, all of the discussed materials systems are nanofabricated in that their compositions and thicknesses are typically controlled at the nanoscale.  However, in order to create both single devices and arrays, their physical geometries must also be controlled at the nanoscale as well.  With fine enough control, structured materials can be induced to behave as single-domain particles, likely improving control and repeatability of device performance.  Nanopatterning of materials also allows some control over the coercivity of the materials and can lead to the observation of new effects such as spin-transfer effects.  Manufacturing technology presently allows device geometries to be controlled at this level for transition metal alloys, semiconductors, oxides, and some other materials.  Fabrication techniques for newer materials such as amorphous and rare-earth alloys are less developed.

- Amorphous alloys

The materials properties of amorphous alloys such as anisotropies, magnetization, and coercivity can be tuned over a wide range, similar to transition metal alloys.  They also offer the advantage of being able to create very smooth magnetic films and the absence of grain boundaries that can act as nucleation and pinning sites for magnetic domain walls.  Hence they are a potential avenue to pursue for use in ultra-low noise sensors and the realization of nanostructured elements that behave as single-domain structures.  They can also provide interesting electronic properties. For instance, B doped materials are presently in use in prototype MRAM configurations not only exhibit better switching behavior but also larger TMR signals.  Novel materials and doping structures may prove very useful in future sensor devices.  In addition to being incorporated into GMR and TMR devices they are also used in GMI sensors.

The data from sections II and III are compiled in Table 3 to show the considerations needed for the various materials. This table shows a matrix of materials that can be used in magnetic fields sensors along with descriptions of their properties, potential applications and drawbacks of the materials.

Table 3 – Materials requirements matrix

IV) Improvements and Goals

To reach the goals outlined in the previous sections new materials will need to be engineered and integrated into device structures.  For low noise sensors, the sources of increased noise with respect to standard thin-film resistors need to be understood and decreased in magnetic systems.  This can potentially be accomplished with improved device fabrication but will likely need improved materials performance as well.  Nanoscale anisotropy variations in materials will need to be decreased while controlling the materials susceptibility.  Improved AMR, GMR, and TMR materials would simplify incorporation of these new materials into functioning devices.  Magnetostrictive and composite materials hold great promise for low power applications by making so called self-powered sensors that require no external sources of power to function.  These materials also allow the manufacture of multifunctional sensors capable of responding to more than one type of stimulus.  For low field applications the sensitivity of all of these materials will need to be improved over the next several years.

Section 5 – Outlook

It was found that there are many different devices, applications, and materials relevant to the general field of magnetic field sensors. In fact, there is often a wide disparity in the characteristics, requirements, and properties of the sensors, applications, and materials, respectively. This presents significant difficulty in defining one unique direction to pursue at NIST.

However, this problem is mitigated to some extent by specifically considering NIST’s four strategic focus areas, Homeland Security, Health Care, Information Technology, and Nanotechnology. In the case of the first area, Homeland Security, low power, high sensitivity, room temperature specifications are called for in the applications matrix shown in Table 2. Comparing this to the sensor matrix on Table 1, it can be seen there is not yet a specific sensor that meets all of these specifications. Therefore, this is one direction that can immediately be identified as important to pursue. Some of the low power sensors from Table 1 include the magnetoresistive sensors. From Section 4, and  refering to the materials matrix, Table 3, it is clear that  this technology would require very high susceptibility materials coupled with high MR ratio, pointing to the TMR devices. However, it is clear that significant technical problems must be overcome in order for this technology to be viable in these applications. These include, ost significantly, the noise and dynamic range issues.

Similarly the Health Care SFA also calls out for high sensitivity; however, the requirements for power and room temperature operation are relaxed. Therefore, a less aggressive approach using mature technologies, i.e., SQUID and fluxgate sensors, may be called for.

When considering the Information Technology SFA, the first application that comes to mind is data storage, specifically the area of hard disk drive (HDD) read heads. At present, work by industry in this area probably represents the most intensive, coordinated research ever conducted in the area of magnetic field sensors. In the HDD area, the requirements for sensors are intricately coupled to the specific product. While general characteristics, such as are listed in Table 1, can be given, the exact specifications for a given device must be determined by the industry. In addition, with data densities pushing past 100 Gbit/in2, and still increasing, it is extremely hard to compete with the rapid progress made by teams at large private labs. That being said, however, it still remains incumbent on NIST to keep up to date in this technology because it is likely that many of the developments there can be transferred over to other areas. This holds particularly true in the area of magneto-resistive sensors, where significant advances are being reported on a monthly basis. In order to keep up with this rapid pace, it is critical that NIST researchers maintain a high profile at international conferences and workshops.

Nanotechology, the fourth NIST SFA, appears as an underlying theme throughout the magnetic sensor development. This is illustrated in the materials matrix, Table 3, where nearly every entry can be correlated with nanoscale properties. This is true not only for the nanocrystalline, nanocomposite, and nanofabricated materials, but also for nanometer scale grains in amorphous alloys, spacers in multilayers, clusters in magnetic semiconductors, and defects in single crystal materials.

In addition, however, nanoengineering is particularly important when designing sensors. For example, the dimensions for read heads in Hdds are pushing the limits of optical lithography, and it can be expected that the actual magnetic elements may soon be defined using e-beam lithography. Because the magnetic properties are intricately linked to the shape of the sample through the magnetic dipole energy, it is very important that defects at the nanometer level are removed. In fact, due to the long range nature of the dipole interaction, this consideration of nm control holds for sensors over a wide range of size scales.

In summary, we have identified research into high sensitivity, low power, room temperature magnetic field sensors as having impact in all four SFA’s. However, the Roadmap clearly shows that there are many combinations of devices, applications and materials research that need be investigated in order to meet all industrial demands. This is truly a rich field of research.

Section 6. References

1. J.E. Lenz., "A Review of Magnetic Sensors," Proceedings of the IEEE, 78, No. 6:973-989 (1990).

2. Ciureanu and S. Middelhoek, Thin Film Resistive Sensors, New York: Institute of Physics Publishing, (1992).

3. J.M. Janicke, The Magnetic Measurement Handbook, New Jersey: Magnetic Research Press., (1994).

4. Magnetic Sensors International Data Book. Siemens Aktiengesellschaft, München, Germany, (1995).

5. Pavel Ripka, Magnetic Sensors and Magnetometers (Artech House Remote Sensing Library) (2001).

6. Sensors, Volume 5, Magnetic Sensors, Richard Boll (Editor), Kenneth J. Overshott (Editor), ISBN: 3-527-26771-9, December (1996).

7. J.M. Daughton, “GMR and SDT sensor applications,” IEEE Trans. Magn. 36 , 2773 - 2778,  (2000).

8. J. M. Daughton,  “Spin-dependent sensors,” Proceedings of the IEEE  91, 681 - 686, (2003 ).

9.R. S. Popovic : Hall Effect Devices, Adam Hilger (Bristol, New York, now IOP Institute of Physics Publishing) (1991).

10. P. Ripka. "Review of Fluxgate Sensors," Sensors and Actuators A, 33:129-141 (1996).

11. R. H. Koch and J. R. Rozen “Low-noise flux-gate magnetic-field sensors using ring- and rod-core geometries,” Appl. Phys. Lett. 78, 1897 (2001).

12. H. Weinstock, SQUID Sensors: Fundamentals, Fabrication and Applications (Kluwer Academic, Dordrecht, Netherlands, (1996).

13.  J. Gallop, “SQUIDs: some limits to measurement,” Supercond. Sci. Technol. 16, 1575 (2003).

14. H. J. Barthelmess et al., “Low-noise biomagnetic measurements with a multichannel dc-SQUID system at 77 K,” IEEE Trans. Appl. Superconduct.11, 657 (2001).

15. T. I. McGuire and R. I. Potter, “Anisotropic Magnetoresistance in Ferromagnetic 3d Alloys,” IEEE Trans. Magn. 11, 1010-1038, (1975).

16. D. A. Thompson, L. T. Romankiw, and A. F. Mayadas, “Thin Film Magnetoresistors in Memory, Storage, and Related Applications,”  IEEE Trans. Magn. 11, 1039-1050, (1975).

17. B.B. Pant,  "Magnetoresistive Sensors," Scientific Honeyweller,  8, No. 1:29-34. (1987).

18.M. N. Baibich, J. M. Broto, A. Fert, F. Nguyen Van Dau, F. Petroff, P. Etienne, G. Cruezet, A. Friederich, and J. Chazelas, Phys. Rev. Lett. 61, 2472 (1988).

19.G. Binasch, P. Grünberg, F. Saurenbach, and W. Zinn, Phys. Rev. B 39, 4828 (1989).

20. J. Daughton and Y. Chen "GMR Materials for Low Field Applications," IEEE Trans Magn,  29:2705-2710 (1993).

21. J. Daughton et al. 1994. "Magnetic Field Sensors Using GMR Multilayer," IEEE Trans Magn, Vol. 30:4608-4610

22. J.K. Spong et al., "Giant Magnetoresistive Spin Valve Bridge Sensor," IEEE Trans Magn, Vol. 32:366-371 (1996).

23. Neil Smith, Alexander M. Zeltser, Danny L. Yang, and Peter Koeppe, „Very High Sensitivity GMR Spin-Valve Magnetometer, IEEE Trans. Magn. 33, 3385 (1997).
24. M. J. Sablik, R. S. Beech, and M. Tondra, “Designing a giant magnetoresistance field sensor via inferences from a giant magnetoresistance hysteresis model”,J. Appl. Phys. 87, 5347 (2000).

25. H. T. Hardner, S. S. P. Parkin, M. B. Weissman, M. B. Salamon, and E. Kita , “1/f noise in giant magnetoresistive materials,” J. Appl. Phys. 75, 6531 (1994).

26. Myriam Pannetier, Claude Fermon, Gerald Le Goff,, Juha Simola, Emma Kerr, “Femtotesla Magnetic Field Measurement with Magnetoresistive Sensors,” Science 304,1648  (2004).

27. J. Moodera and L. Kinder. "Ferromagnetic-insulator-ferromagnetic tunneling: Spin-dependent tunneling and large magnetoresistance in trilayer junctions," J Appl Phys 79, No. 8:4724-4729 (1996).

28.Reed, D.S.; Nordman, C.; Daughton, J.M.,  “Low frequency noise in magnetic tunnel junctions,” IEEE Trans. Magn 37 , 2028 – 2030, (2001).

29.Wan Kyu Park, Jagadeesh S. Moodera, John Taylor, Mark Tondra, James M. Daughton, Andy Thomas, and Hubert Brückl, “Noise properties of magnetic and nonmagnetic tunnel junctions,” J. Appl. Phys. 93, 7020 (2003).

30.Peter K. George, Y. Wu, R. M. White, Ed Murdock, and Mark Tondra, “Shot noise in low-resistance magnetic tunnel junctions,” Appl. Phys. Lett. 80, 682 (2002).

31.Xiaoyong Liu and Gang Xiao, “Thermal annealing effects on low-frequency noise and transfer behavior in magnetic tunnel junction sensors,” J. Appl. Phys. 94, 6218 (2003).

32.L. Jiang, E. R. Nowak, P. E. Scott, J. Johnson, J. M. Slaughter, J. J. Sun, and R. W. Dave, “Low-frequency magnetic and resistance noise in magnetic tunnel junctions,” Phys. Rev. B 69, 054407 (2004).

33. S. A. Solin, Tineke Thio, D. R. Hines, and J. J. Heremans Enhanced Room-Temperature Geometric Magnetoresistance in Inhomogeneous Narrow-Gap Semiconductors,” Science , 1530-1532, (2000).

34. S. A. Solin, D. R. Hines, A. C. H. Rowe, J. S. Tsai, and Yu A. Pashkin, “Nanoscopic magnetic field sensor based on extraordinary magnetoresistance,” J. Vac. Sci. Technol. B 21, 3002 (2003).

35. C. H. Möller, O. Kronenwerth, Ch. Heyn, and D. Grundler  ”Low-noise magnetic-flux sensors based on the extraordinary magnetoresistance effect”  Appl. Phys. Lett. 84, 3343 (2004).

36 A. Makino et al., T. Mat. Trans. JIM, 32 551 (1995).

37 M. E. McHenry and M. A. Willard, Prog. Mat. Sci., 44 291 (1999).

38  Y.-Q. Li and R. C. O’Handley, J. Appl. Sens. Tech. 17, 10 (2000).

# Text boxes

Figure 7. Rendering of magnetic field above a cassette tape. Courtesy of NIST and the FBI Audio Forensics Laboratory.

Figure 6. Non-destructive testing of VLSI chips. Left panel: Magnetic field above entire 20x20 cm RAM chip, showing the fields from the current supply lines. Right panel: Current vector calculated by inverting the fields. Images courtesy of NIST, samples courtesy of Intel Corp.

Figure 5. Magnetic bead array counter (BARC) as implemented by NVE and NRL. The left panel shows the concept of tagging both sensors and beads which target specific proteins. When either the A or B target is present, the field from the bead will be sensed magnetically at the corresponding site. The right panel shows a picture of the actual device. An individual sensor is shown in the zoom, and illustrates the serpentine design of the spin valve GMR sensors. Images courtesy of NVE and NRL.

Figure 4. Medical applications for sensors. From “Biomagnetism,” by Malvivuo.

Figure 3. Field ranges for battlefield magnetic anomaly detection. Courtesy of A. Edelstein, Army Research Laboratory.

Figure 8. Comparison of a variety of different magnetic materials. Modified from Ref [36]

Figure 9. TEM image showing two nanocrystals in an amorphous matrix. [37]

Figue 10. Schematic of self-powered sensor concept Ref [38].

Figure 1. Detectivity of various magnetic field sensors as a function of frequency (see text for a list of references)

Figure 2  Detectivity at 10 Hz as a function of sensor size.