Title:	Reliability Assessment of Microvias for Spaceborne Electronics

(Check one):	    New Proposal		    Continuing NEPP Work

##### Total $ Requested for FY02:	$120,000

Technology Type:	    Newly Available (COTS)	    Emerging/Advanced

(check one)

Project Area:	     Parts	    	Packaging 	     Radiation

(check one)

Proposing Centers: 	JPL

(Estimated Center 	       % GSFC               %  GRC               % LaRC        100 % JPL

Participation, %$):		% MSFC      	% JSC       	Other

Collaborators (include %$, if any, to collaborators): 50% JHU/APL

Point of Contact:	Mr. David Mih, (818-354-9218), david.t.mih@jpl.nasa.gov

Investigator(s):	Mr. David Mih (NASA/JPL), (818-354-9218), david.t.mih@jpl.nasa.gov

Mr. Binh Le (JHU/APL), (240-228-4711), binh.le@jhuapl.edu

Dr. Sharon Ling (JHU/APL), (240-228-8139), sharon.ling@jhuapl.edu

Objective(s):

- Design and fabricate test boards with microvias (buried and blind vias), leveraged from commercial technologies.

- Perform microsection evaluation on printed wiring board test coupons to form a referenced basis for the reliability study.

- Perform temperature cycling test (MIL standard temperatures and extended temperature range to support missions to Mars).

- Implement non-destructive evaluation (NDE) methods to evaluate the integrity of the microvias before and after thermal cycling tests.

- Perform finite element analyses to correlate test results and NDE for reliability prediction.

- Establish guidelines for reliable, cost-effective microvias design and fabrication procedures that can be verified through standard test coupon verification.

Task Description:

The team of NASA/JPL and the Johns Hopkins University Applied Physics Laboratory (JHU/APL) proposes to evaluate the reliability of microvia technology (buried and blind vias) in high density printed wiring board (PWB) design.  We will also define criterion for reliable microvia PWB design standards and reliability testing procedures.  This project leverages from previous NASA ATD project conducted at JHU/APL.  To be more focused and effective, we will evaluate microvias in the conventional PWBs with etch-back process only, since this process has been typically applied in space electronics.  The task will also employ novel NDE techniques to inspect microvia PWB, and analytical approaches to acquire in-depth understanding of microvia behavior in temperature cycling environment as well as to predict the reliability of microvias.

### Task Approach to meeting NEPP Objectives:

### The work proposed in this project meet the NEPP program objectives in many areas:

### Assessing Reliability:	As PWB hole sizes are getting smaller, maintaining the minimum copper wall thickness of 0.001 inch (as required by the MIL standards) becomes very difficult, especially for high-aspect-ratio vias.  The question of whether the integrity of the vias relies on the copper plating thickness or the interface between the plated vias and the inner layer annular rings, is still the subject for many research projects.  To understand the characteristics and performances of the microvias developed by different manufacturing processes, a fundamental test plan is developed in this project on specific PWB technology for the reliability assessment of microvia for future space application.  This project will also assess the reliability of PWB technology with microvias for temperature ranges beyond the typical MIL standard requirements, where no data are available from commercial companies, yet a situation that will be encountered for future space missions to Mars.

### Expediting Infusion Paths:	Microvia technology has been used in commercial products to support miniaturized consumer electronics.  However, the reliability of the microvia technology needs to be thoroughly and carefully studied before implementation for space electronics.  Once the behavior of the microvias is quantified, and reliability qualified, we will then work with future NASA programs to leverage from this existing technology and to ensure that it is available for infusion into space programs.

### Provide Validation Guidelines:	One of the goals of this project is to establish criterion for validation PWB with microvias.  Existing MIL standards do not address the microvia issues, and the commercial IPC standards do not have definitive requirements and convincing test data to support microvias for high reliability application.  Upon completion of this project, we will provide guidelines on the minimum plating thickness and minimum via size requirements, as well as tools to predict life expectancy for microvias in space application.

Disseminating Information to

the NASA Community:	The results from this study will be disseminated to the NASA community via NEPP publications, the NASA Tech-Digest, and publications in technical journals. We will actively participate and inform the two on-going programs: X2000 and MESSENGER on the status of this technology for potential technology insertion.

Technical Background:

Miniaturization in consumer electronics has resulted in implementation of small electronic components in the form of flip chip, micro-ball-grid array, and chip-scale surface-mount packages.  To support the miniaturized electronic systems, innovative PWB technologies with microvias and very fine feature were developed.  The typical microvia-hole diameters range from 0.002 inch to 0.008 inch.  These vias are divided into three categories: blind, buried and through-hole.  Blind vias provide interconnections from the external signal layer to an internal one; whereas buried vias interconnect only among internal signal layers.  Both the blind and buried vias can effectively divert signals from high I/O density ICs for routing without compromising significant board surface area.  In conventional PWB fabrication process, mechanical drilling is used when via size is greater than 0.010 inch.  For smaller holes, laser-drilling processes are required.

Two laser-drilling processes: conformal-mask drilling and full-via formation drilling will be evaluated in this project.  In the conformal-mask drilling method, the external copper is chemically pre-etched using a photolithographic process to expose the dielectric layer.  A CO2 laser beam is then focused onto the surface of the PWB to ablate the dielectric material thus, form the via.  A post drill clean with plasma or chemical etching prior to electroless copper plating is required for conformal-mask drilling, to ensure a clean surface for subsequent plating steps.  Full-via formation drilling process uses dual laser sources, the UV laser and the CO2 laser.  The UV laser source is used for ablating the copper layer, and the CO2 laser is used subsequently to ablate the dielectric material to form the vias.  A post-drill clean prior to the electroless copper plating is also required.  The potential advantage of the full-via formation drilling process is the elimination of the tedious inspection step that is needed in conformal-mask drilling process, to ensure proper removal of copper before the laser drilling step.  A critical step in high quality microvia fabrication is the electroless copper deposition after the drilling and cleaning of via holes.  Two plating processes will be evaluated in this study: the conventional DC plating process and the pulsed plating process.  In the pulsed plating process, the supplied electrical input is turned on and off repetitively with adjustable duty cycle and frequency.  The agitated/regulated current induces more evenly ion distribution, which leads to better Cu ion deposition and plating quality, especially for blind holes with high aspect ratios.

Defining systematic design procedures and inspection guidelines for reliable printed wiring boards with microvias will provide important building blocks for satellite electronics miniaturization.  Understanding the performance of microvias and limitation of manufacturing processes will avoid problems in making design decisions (Figs. 1).  The trend in PWB fabrication is more towards manufacturability than qualification, especially when MIL standards are in the process of being replaced by commercial IPC standards [1,2].  Problems could occur when the PWB coupon does not represent the board features, and successful inspection of the coupon does not necessarily guarantee the quality of the board.  	A good example of the non-representative coupon inspection failing to reveal PWB process problem is the CHANDRA spacecraft [3].  The PWB failure was discovered in a late stage of spacecraft integration, resulting in extra cost and schedule delay to replace the defect PWB from the flight hardware.  Although there are studies supported by ITRI [4] in the area of microvia technologies, the studies are mainly focused on statistical results rather than establishing criterion and procedures to qualify PWB.  Furthermore, there is no existence of test data to support the reliability assessments of microvias for temperature ranges that are beyond the typical MIL standard requirements, such as the extremely low temperatures that will be encountered for missions to Mars [5].

Therefore, our approach for this project is to fabricate microvia PWBs with controlled processes to facilitate the verification steps with NDE and analytical techniques.  Our tests will cover not only the typical MIL standard ranges, but also at lower temperatures to support future missions to Mars.  With NDE and analytical techniques we will provide a fundamental study for reliability assessments of microvias.  Our goal is to define criterion for reliable microvia PWB designs, and to ensure that once the test coupons associated with each PWB panel pass the acceptance tests, the PWB will be reliable for flight.

Figure 1: Micro-sections of (left) defect microvia (poor plating, over etching), and (right) buried-filled via (voids, plating fold, and misalignment).

Technical Approach:

| Task | Approach | Comment |
| --- | --- | --- |
| Design and fabrication of test boards with microvias (blind, buried vias) | PWBs with CO2 laser drilled vias. PWBs with UV/CO2 laser drilled vias PWBs with pulsed plating PWBs with DC plating PWBs with unfilled buried vias PWBs with filled buried vias | JHU/APL and two Commercial PWB Vendors: To build the test boards. Independent processes from different vendors will be evaluated. JHU/APL test samples will serve as referenced test samples. |
| Environmental Testing | Perform thermal shock, and thermal cycling tests | JHU/APL: Perform the environmental tests Leverage from test fixtures and software developed from the previous NASA ATD project. |
| Destructive Inspection | Perform microsection inspection of test coupons to form a basis reliability reference for the test boards | JHU/APL: Perform the microsection evaluation using its existing facility. |
| Non-destructive Evaluation | Inspect microvias with real time Microfocus X-ray technique. | NASA/JPL: Apply the NDE process. Applying reliable NDE is crucial to ensure reliability of microvia technology insertion for future space missions. |

NASA Customers:

Since the work developed in this project is at the basic electronic packaging level, the results from this study will supports all future NASA programs.  The near-term potential applications are for the X2000, the MESSENGER, and future Mars programs where miniaturization of electronics is critical for mission success.

Clearly Stated Deliverables:

- Test boards with microvias (blind and buried) with size variation and built-in test structure.

- Test plan for qualification of microvia PWBs to simulate flight environments.

- Procedures for NDE for reliability evaluation of microvias.

- Reliability assessment procedures using finite element analysis that correlates test results for reliability prediction

- NASA Technical Report that summarizes evaluations and recommendations on the microvia technology based on our test results.

Top Level Schedule:

Major activities and milestones of the proposal are shown in the following table.  The NASA/JPL and JHU/APL team will conduct weekly telephone conference to ensure adequate information exchange and timely discussions of management of technical, cost and schedule issues.

| Major Milestone | Q1 | Q2 | Q3 | Q4 |
| --- | --- | --- | --- | --- |
| Test board design |  |  |  |  |
| Test board manufacturing |  |  |  |  |
| Development of test plan |  |  |  |  |
| Test fixture, software development |  |  |  |  |
| Environmental tests |  |  |  |  |
| Nondestructive Evaluation |  |  |  |  |
| Report |  |  |  |  |

List of Procurements (over $5K):

In this project, the major procuring cost is $25K, for test boards from two commercial vendors as well as JHU/APL.

Manpower Loading:

|  | Q1 | Q2 | Q3 | Q4 |
| --- | --- | --- | --- | --- |
| NASA/JPL | 0.1 | 0.2 | 0.25 | 0.25 |

Leveraging:

This work will leverage from existing facilities and expertise at NASA/JPL and the PWB facility at JHU/APL, gathered over many years of DOD and NASA technology development and research activities.  No capital equipment will be procured, nor will facilities be significantly developed to perform this effort.

Task Budget:

|  | (FY00) | FY01 | FY02 | FY03 |
| --- | --- | --- | --- | --- |
| Task $ |  |  | $120,000 (total) |  |
| Procurements |  |  | $60,000 |  |

JHU/AP Labor: $48K: PWB procurement: $20K; Supplies: $5K

References:

- MIL-PRF-31032 Performance Specification for Printed Wiring Boards.

- IPC IPC-6012 Standards for Printed Wiring Boards.

- TRW Presentation at the Manufacturing Problem Prevention Program (MP3) workshop, the Aerospace Corporation (ASC) in El Segundo, CA June 27-28, 2000.

- http://www/itri.org/

- http://nmp.jpl.nasa.gov/ds2/tech/microcontroller.html

Attachment

Keywords:

- Microvias

- Blind / Buried Vias

- Low Cost

- High Reliability

- Nondestructive Evaluation

Proposal Abstract:

The team of NASA/JPL and the Johns Hopkins University Applied Physics Laboratory (JHU/APL) proposes to evaluate the reliability of microvia technology (buried and blind vias) in high density printed wiring board (PWB) design.  We will also define criterion for reliable microvia PWB design standards and reliability testing procedures.  This project leverages from previous NASA ATD project conducted at JHU/APL.  To be more focused and effective, we will evaluate microvias in the conventional PWBs with etch-back process only, since this process has been typically applied in space electronics.  The task will also employ novel NDE techniques to inspect microvia PWB, and analytical approaches to acquire in-depth understanding of microvia behavior in temperature cycling environment as well as to predict the reliability of microvias.

Funding Summary:

|  |  | FY01 | FY02 | FY03 |
| --- | --- | --- | --- | --- |
| Task Total |  |  | $120,000 |  |
| Proposing Center | NASA/JPL |  | $ 47,000 |  |
| Supporting Centers | JHU/APL |  | $ 73,000 |  |

Deliverables:

- Qualification Test Matrix  (January, 2002)

- Microvias Test Boards  (April, 2002)

- NDE Procedures  (August, 2002)

- Reliability Assessment Procedures  (August, 2002)

- NASA Technical Report  (September, 2002)