68-Er-166 Review

Drafted by J. Chang, KAERI, 2004.

Files:

ENDF/B-VI: Origin 1988, Res. Param. by Mughabghab[1984] .

JEF:	Copied ENDF/B-V of 1974, latest revision 1988 , Res. Param. by Mughabghab[1984] .

BROND:	Origin 1976, Revision 1989.

- Thermal cross section

The most reliable evaluation for capture cross section is

Mughabghab[1984]	 = 19.6±1.5 b, RI: 96±12 b

s = 14.2±2.1 b, bcoh = 10.6±0.8 fm, R’ = 8.1±0.2 fm

Mughabghab[2003]	 = 19.6±1.5 b, RI: 95±7 b

Holden[1998]	 = 20 b , RI: 96±12 b, b = 10.6±0.2 fm

Knopf[1997]	 = 18±2 , b = 10.52±0.19, R'= 7.6±0.2 fm

Cap	RI	Fast Cap.	Scat.	b.	R	R’

ENDF	19.62	98.92	599.3	15.88	11.18	8.1	8.1

JEF	34.98	140.5	505.0	3.76	5.41	6.63	6.63

BROND	20.6	110.2	646.3	37.12	9.84	7.67	7.67

ENDF and BROND is similar. Bur JEF agrees better with one experimental data by Vertebny[1965].

- Resolved Resonance Parameter

ENDF is based on Mughabghab[1984], and upper limit is 2 keV.

JEF is is based on Mughabghab[1984], and upper limit is 2 keV. Without bound level.

BROND upper limit is 4.2 keV.

- Unresolved Resonance Parameters

Mughabghab[1984]

D0=38±3 eV, 	S0 = 1.6±0.2,	<> = 92±8 meV

D1= ?	 	S1 = 0.94±0.16

D2= ?	 	S2 = 4.7±0.7

ENDF and JEF has NO URR parameters.

BROND uses energy independent URR parameters up to 6 keV.

BROND:	D0 = 38 eV, 	S0=1.762,		<> = 92 meV

D1 = 19 eV, 	S1=0.750,		<> = 92 meV

ENDF has no URR parameter, but agrees well with experimental data as BROND.

BROND is lower in this region.

- Capture (high energy)

ENDF and JEF is same.

BROND is more smooth.

- Elastic

The plot may be wrong.

- Inelastic

ENDF and JEF is same and shows rather flat shape.

BROND show reasonable shape.

- (n,p) and (n,)

ENDF and JEF is missing.

BROND is straightly increasing shape. The (n,) at low energy resonance is neglected.

- (n,2n)

ENDF and JEF are missing.

BROND show reasonable shape.

Recommendation:

ENDF is recommendable for the reactor application.

# References

Vertebny[1965] C,65ANTWERP,,572(186),65)

Mughabghab[1984], Neutron Cross Sections Vol. 1, Part B, Academic Press.

Holden[1998], CRC Handbook of Chemistry and Physics, 78th ed., CRC Press.

Mughabghab[2003], INDC(NDS)-440, 2003.