# Requester:	Danny Cunningham

BP Solar

Date:	December 19, 2002

Area	Temp.	Voc	Isc	FF	Vmax	Imax	Pmax	Aper 

(cm2)	(°C)	(V)	(A)	(%)	(V)	(A)	(W)	(%)

BP Solar	(CdS/CdTe module)

568901

12/17/02	SPIRE 240A	8512.0	24.9	44.98	3.124	66.1	34.21	2.713	92.83	10.91

12/18/02	LACSS SpectroLab X200 storage state	8512.0	25.2	44.83	2.995	67.6	34.58	2.626	90.81	10.7

12/16/02	SOMS OUTDOORS @988 W/m2	8512.0	20.1	44.67	2.931	67.6	34.53	2.563

Normalized and Spectrally Corrected SOMS data		20.1		3.015				91.03	10.7

569401

12/17/02	SPIRE 240A	8512.0	25.0	45.01	3.173	65.8	34.33	2.738	93.99	11.04

12/18/02	LACSS SpectroLab X200 storage state	8512.0	25.2	44.87	3.040	67.9	34.68	2.671	92.61	10.9

12/16/02	SOMS OUTDOORS @1007 W/m2	8512.0	20.4	44.52	3.026	67.6	34.42	2.645

Normalized and Spectrally Corrected SOMS data		20.4		3.053				91.86	10.8

572002

12/17/02	SPIRE 240A	8512.0	25.0	45.27	3.127	67.1	34.47	2.756	95.02	11.16

12/18/02	LACSS SpectroLab X200 storage state	8512.0	25.2	45.20	2.982	69.0	35.18	2.642	92.95	10.9

12/16/02	SOMS OUTDOORS @986 W/m2	8512.0	20.5	45.34	2.907	69.0	35.19	2.585

Normalized and Spectrally Corrected SOMS data		20.5		2.996				93.76	11.0

813104

12/17/02	SPIRE 240A	8512.0	25.0	44.48	3.188	65.5	33.29	2.789	92.86	10.91

12/18/02	LACSS SpectroLab X200 storage state	8512.0	25.2	44.35	3.051	67.0	33.86	2.678	90.67	10.7

12/16/02	SOMS OUTDOORS @985 W/m2	8512.0	18.5	44.43	2.979	67.1	34.18	2.600

Normalized and Spectrally Corrected SOMS data		18.5		3.072				91.65	10.8

815302

12/17/02	SPIRE 240A	8512.0	25.0	44.07	3.173	65.4	32.79	2.787	91.37	10.73

12/18/02	LACSS SpectroLab X200 storage state	8512.0	25.2	43.86	3.055	66.8	33.30	2.689	89.53	10.5

12/16/02	SOMS OUTDOORS @990 W/m2	8512.0	20.6	44.03	2.994	67.0	33.52	2.633

Normalized and Spectrally Corrected SOMS data		20.6		3.071				90.52	10.6

Sample	Description	Aperture area	Total area

(#)	length	width	area	length	width	area

(cm)	(cm)	(cm2)	(cm)	(cm)	(cm2)

568901, 569401& 572002	CdS/CdTe  model#BP990L	152.0	56.0	8512.0	154.9	60.9	9433.4

813104, 815302	CdS/CdTe  model#BP980L	152.0	56.0	8512.0	154.9	60.9	9433.4

Total area is outside edge of glass to outside edge of glass.

Aperture area was measured inside of taped frame to inside of taped frame.

Aperture area was used in the efficiency calculation.

Estimated total uncertainty in the NREL Spire measurement efficiency is ±10%.

Spire 240A measurements were taken with new Peak circuit installed, and running on new NREL software.

The SPIRE 240A monitor calibration was set to 1.203 using the Si reference cell in a module package sn#150576 with a M=0.960.

Estimated total uncertainty of the NREL Large Area Continuous Solar Simulator measurements is ±5%.

The LACSS monitor calibration was set to 103.23 mV using the GaAs reference cell sn#S25 with a M=1.008.

Samples were tested under the LACSS in a storage state condition.

Estimated total uncertainty of the NREL Outdoor measurements is ±5%.

Outdoor sample temperature is measured on the back surface and may not represent the actual junction temperature.

NREL Outdoor (SOMS) Isc, Pmax and Eff measurements are corrected to 1000W/m2 and Spectrally Corrected using an M=0.977 for 12/17/02.

NREL Outdoor (SOMS) measurements are not corrected for temperature.

The solar spectrum that was taken during the outdoor tests are available.

Dark IV's are included.

(Tracking #999)