8/22/07

TD-07-022

LARP Note, Aug 07

LARP TQS02a Test Summary

G. Ambrosio, G. Chlachidze, R. Carcagno, S. Caspi, P. Ferracin, F. Lewis, A. Lietzke, D. Orris, Y. Pischalnikov, G.L. Sabbi, D. Shpakov, C. Sylvester, M. Tartaglia, J.C. Tompkins, G. Velev, A.V. Zlobin

Content:

1. Introduction				  			  2

2. Quench history			  			  2

3. Quenches at temperature between 1.9 and 4.5K		10

4. Ramp rate dependence					11

5. Protection Heater study					12

6. Spot Heater study						14

7. Strain gauge results						15

8. Quench antenna data					25

9. RRR measurement						26

10. Quench origin location					29

11. Magnetic measurement 					31

1. Introduction

TQS02a is a 1m long quadrupole model assembled at LBNL as part of the LARP program. TQS02a uses the same support structure of TQS01 with new coils (made of 54/61 RRP strand).  This report documents the test of TQS02a performed at Fermilab in the Vertical Magnet Test Facility (VMTF) at 4.5 and 1.9 K.  According to a request by LBNL a slow cool down (maintaining T<50 K across the magnet) was executed, starting on the early morning of June 2 to the end of the day on June 3, during which strain gauges and coil segment resistances were continuously monitored. Magnet test started on June 4 and lasted until June 21. The VSDS (Voltage Spike Detection System) was used during the whole test. A detailed analysis of the data recorded by the VSDS is presented in [1].

2. Quench History

The cold test program started at 4.5 K with cold magnetic measurement followed by magnet training at 20 A/s ramp rate. At the beginning of the training the quench detection threshold was set to 500 mV. A series of trips induced by voltage spikes (flux jumps) caused the increase of the detection threshold to 700 mV, then to 1.5 V and finally to 3 V. Subsequently the threshold was lowered to 2V (because of concerns about possible high MIITs), but had to be increased again to 3 V to avoid trips induced by flux jumps.  The first quench occurred at 9902 A. During training at 4.5 K, with 3 V detection threshold, two trips induced by very high voltage spikes occurred at 1737 and 1949 A.

After a series of quenches (from #8 to #16) in coil 20, with quench current varying between 11.1 and 11.8 kA, the quench onset moved to coil 21. Quench #18 started in the so called “pizza box” (a G10 structure containing all coil-to-coil junctions, located on the top of the lead end) close to the splice between coil 20 and coil 21 NbTi leads. This quench occurred at 12.274 A, the highest current reached at 4.5K during the whole test. This quench developed 10 MIITs because of the high quench detection threshold, and the slow propagation. However it didn’t cause any damage to the NbTi cables. At lower temperatures TQS02 reached two times higher currents without quenhes in the “pizza box”. The following quenches showed a fallback (11.4 kA in quench #19), a quick recovery, and a plateau with an average of 12123 A and a slightly negative slop of -22 A/quench.

Subsequently ramp rate studies at 4.5 K were performed, and then the magnet was cooled down to 1.9 K. Tests with 20 A/s ramp rate at 1.9K (from #34 to #45) showed the quench current fluctuating in the range 11.25 kA – 11.95 kA with the exception of quench # 42 that reached 12.39 kA (this quench occurred after magnetic measurement at 1.9K performed after a partial magnet warm-up). All quenches at 1.9K started in coil 21. Quenches from #46 to #48 were performed during magnet warm-up. Ramp #47 started with 40 A/s up to 10 kA, and then 10 A/s. This ramp reached the highest quench current of the whole test (12,467 A). A final series of quenches at 4.5 K with 20 A/s ramp showed a plateau of 11930 A +/- 10A.

Figure 2.1. TQS02a quench history.

TQS02a Quench History table with comments

| File | # | Current (A) | dI/dt (A/s) | tquench | MIITs | Mag Temp Bot L (K) | Mag Temp Top L (K) | Comments |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| tqs02a.Quench.070604130438.013 |  | 1002 | 0 | 0.0017 | 0.17 | 4.424 | 4.421 | darryl couldn't balance cu-i aqd, so the techs will have to look at this. |
| tqs02a.Quench.070604153926.160 |  | 1327 | 50 | -0.4000 | 0.88 | 4.429 | 4.427 | dqd_coil detected a signal - perhaps a spike-induced trip? we were ramping up at 50A/s to perform heater-induced quench. |
| tqs02a.Quench.070604155955.441 |  | 1727 | 20 | -0.0027 | 0.30 | 4.426 | 4.422 | 20 A /s ramp to 5000A to perform heater-induced quench, with threshold raised to 1.5V. DQD coil detection. |
| tqs02a.Quench.070604162531.931 |  | 5003 | 20 | -0.0238 | 2.55 | 4.427 | 4.425 | HFU_1 fired at 300V to induce a quench and capture data at 5000A. We will check signals, which GV and JH conduct magnetic measurements. HFU_2 was in protection mode at 100V, HFU_3 spot heater was "offline" but should have fired from _2 contact closure, at 12V. |
| tqs02a.Quench.070605100858.753 |  | 1705 | 20 | -0.0218 | 0.34 | 4.441 | 4.442 | 2V threshold appears to be unworkable... we tripped off on a voltage spike similar to yesterday's large spike at 1750A. |
| tqs02a.Quench.070605144544.801 |  | 8014 | 20 | -0.0434 | 5.64 | 4.430 | 4.426 | spot heaters in series at 9.6mF, 3.5Ohms resistance total hfu voltage 30V no dump delay; protection heaters at 400V, no p-heater delay |
| tqs02a.Quench.070605155126.832 |  | 8009 | 20 | -0.0357 | 5.07 | 4.428 | 4.432 | the first test at 30V induced a quench only in coil 23. So we raised the voltage to see if we could initiate quenches in all 4 coils. |
| tqs02a.Quench.070605162403.186 |  | 8006 | 20 | -0.0365 | 5.12 | 4.432 | 4.433 | raised the voltage from 50 to 70 V, fired spot heaters to induce quenches, hoping all coils will develop voltage. |
| tqs02a.Quench.070605183235.446 |  | 5004 | 20 | -0.0325 | 2.24 | 4.433 | 4.430 | repeated the heater-induced quench at 5000A, but with hfu_2 triggered at 400V; hfu_1 in protection mode at 400V; hfu_3 simultaneously triggered at 70V. |
| tqs02a.Quench.070605184714.684 | 1 | 9906 | 20 | -0.0148 | 4.88 | 4.439 | 4.436 | protection heaters at 400V, no delay dump 1ms delay spot heater fired at detection, 70V. |
| tqs02a.Quench.070606094913.966 | 2 | 10326 | 20 | -0.0105 | 4.69 | 4.442 | 4.437 | quenched at 10321A, ramp rate 20A/s, T=4.45K. HFU3 was off. |
| tqs02a.Quench.070606102106.918 |  | 1732 | 20 | -0.0192 | 0.29 | 4.443 | 4.441 | trip at 1700 A, ramp = 20 A/s, T = 4.5K |
| tqs02a.Quench.070606111444.461 | 3 | 11165 | 20 | -0.0106 | 5.23 | 4.435 | 4.434 | Ramp 4, rate 20 A/s, I = 11161 A, T = 4.5 K dump 3ms, PH 300V 7 |
| tqs02a.Quench.070606115518.721 | 4 | 11441 | 20 | -0.0085 | 5.07 | 4.436 | 4.436 | ramp 5, I = 11440 A, rate = 20 A/s, T = 4.5 K |
| tqs02a.Quench.070606123347.247 | 5 | 11578 | 20 | -0.0108 | 5.43 | 4.437 | 4.434 | Ramp 6, I = 11575 A, ramp = 20 A/s, T = 4.5 K |
| tqs02a.Quench.070606140258.865 | 6 | 10634 | 20 | -0.0155 | 5.55 | 4.430 | 4.427 | VSDS system appears to be crashed, so we did not get spike data. |
| tqs02a.Quench.070606144702.183 | 7 | 11642 | 20 | -0.0109 | 5.47 | 4.437 | 4.435 | Ramp 8, I = 11637 A, rate = 20 A/s, T = 4.5 Kto |
| tqs02a.Quench.070606152746.043 | 8 | 11602 | 20 | -0.0070 | 4.90 | 4.434 | 4.435 | quench at 11599.2A, ramp rate 20A/s, T=4.45K. Hn�`n�x |
| tqs02a.Quench.070606155359.065 | 9 | 11127 | 20 | -0.0120 | 5.39 | 4.454 | 4.454 | ramp 10, I = 11126 A, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070606162133.230 | 10 | 11848 | 20 | -0.0073 | 4.98 | 4.448 | 4.444 | quench at 11845.6A ramp rate 20A/s T=4.45K |
| tqs02a.Quench.070606164135.111 |  | 1945 | 20 | -0.0122 | 0.33 | 4.450 | 4.448 | tripped at 1949A, ramp rate 20A/s. T=4.45K. |
| tqs02a.Quench.070606170223.671 | 11 | 11499 | 20 | -0.0115 | 5.48 | 4.440 | 4.436 | Ramp 13, I = 11495 A, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070606173608.118 | 12 | 11706 | 20 | -0.0053 | 4.66 | 4.446 | 4.445 | Ramp 14, I = 11700 A, rate 20 A/s, T = 4.5Kƒ÷ |
| tqs02a.Quench.070606180247.881 | 13 | 11521 | 20 | -0.0063 | 4.81 | 4.452 | 4.451 | ramp 15, I = 11515, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070606183249.640 | 14 | 11700 | 20 | -0.0050 | 4.60 | 4.453 | 4.450 | ramp 16, I = 11696 A, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070606190519.154 | 15 | 11808 | 20 | -0.0048 | 5.24 | 4.454 | 4.450 | Ramp 17, I = 11802 A, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070606193546.194 | 16 | 11712 | 20 | -0.0046 | 5.20 | 4.457 | 4.455 | Ramp 18, I = 11710 A, rate 20 A/s, T = 4.5 K |
| tqs02a.Quench.070607085819.744 | 17 | 12072 | 20 | -0.0076 | 6.00 | 4.467 | 4.466 | ramp 19, I = 12069 A, rate = 20 A/s, T = 4.5 K |
| tqs02a.Quench.070607093814.124 | 18 | 12274 | 20 | -0.0339 | 10.07 | 4.452 | 4.455 | ramp 20, I = 12269 A, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070607104128.088 | 19 | 11380 | 20 | -0.0098 | 4.92 | 4.432 | 4.433 | ramp 21, I = 11378 A, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070607112015.464 | 20 | 11974 | 20 | -0.0109 | 6.38 | 4.439 | 4.434 | Ramp 22, I = 11970 A, rate 20 A/s, T = 4.5K |
| tqs02a.Quench.070607114524.375 | 21 | 12165 | 20 | -0.0050 | 5.6 | 4.472 | 4.465 | Ramp 23, I = 12162 A, rate 20 A/s, T = 4.5K |
| tqs02a.Quench.070607121514.882 | 22 | 12153 | 20 | -0.0052 | 5.61 | 4.459 | 4.457 | ramp 24, I = 12146 A, rate = 20 A/s, T = 4.5K |
| tqs02a.Quench.070607135538.210 | 23 | 12139 | 20 | -0.0055 | 5.7 | 4.320 | 4.383 | cool down to 1.9K was aborted because Kinney pump developed a problem, but temperature is slightly cooler than it was earlier. |
| tqs02a.Quench.070607163339.026 | 24 | 12110 | 20 | -0.0046 | 5.61 | 4.410 | 4.410 | several gains were changed to prevent saturation, 21B04_12B05, 21B03_21B04, 21B05_21B06 |
| tqs02a.Quench.070607172917.427 | 25 | 12074 | 20 | -0.0050 | 5.88 | 4.421 | 4.421 | quench at 12070.5A, ramp rate 20A/s, T=4.42K. Dump delay 18 msec (was 13 msec) |
| tqs02a.Quench.070608101421.572 | 26 | 12050 | 5 | -0.0055 | 5.83 | 4.429 | 4.427 | Ramp to 11kAmps at 20Amps/sec then ramp to quench at 5Amps/sece |
| tqs02a.Quench.070608110141.397 | 27 | 11964 | 40 | -0.0070 | 6 | 4.438 | 4.437 | Ramp to quench at 40A/sec |
| tqs02a.Quench.070608112453.473 | 28 | 11717 | 80 | -0.0090 | 6.1 | 4.442 | 4.445 | quench at 11714.4A, ramp rate was 80A/s, T=4.45K. |
| tqs02a.Quench.070608121122.767 | 29 | 12011 | 10 | -0.0056 | 5.82 | 4.452 | 4.446 | quench at I=12008A, ramp rate = 10A/s, T=4.45K. |
| tqs02a.Quench.070608140958.401 | 30 | 11407 | 100 | -0.0028 | 4.78 | 4.426 | 4.423 | ramped at 5A/s to 7500A, then 100A/s to quench (not realizing that 5A/s had already been done). |
| tqs02a.Quench.070609135925.713 | 31 | 10217 | 120 | -0.0048 | 4.68 | 4.421 | 4.421 | Ramp 33, I = 10217 A, rate = 120 A/s, T = 4.5 K |
| tqs02a.Quench.070609143013.717 | 32 | 11844 | 60 | -0.0087 | 6.15 | 4.429 | 4.433 | Ramp 34, I = 11839 A, Rate = 60 A/s, T = 4.5K |
| tqs02a.Quench.070611162130.884 | 33 | 11963 | 5 | -0.0046 | 4.53 | 4.410 | 4.408 | quench at 11956A, ramp rate was 20A/s upto 10kA and then 5A/s till the quench. HFU1/2 both were charged to 200V, delay 0ms. Dump delay 1ms. |
| tqs02a.Quench.070612140759.260 | 34 | 11937 | 20 | -0.0057 | 4.83 | 1.853 | 1.853 | heaters at 200V to keep noise low. ramp rate 20 A/s |
| tqs02a.Quench.070612152045.937 | 35 | 11252 | 20 | -0.0084 | 4.93 | 1.881 | 1.882 | quench current is rather low! appears to be AQD_COIL |
| tqs02a.Quench.070612172710.819 | 36 | 11777 | 20 | -0.0063 | 4.83 | 1.815 | 1.813 | spike system threshold at 150mV. This will be the last quench today, as the gas storage tank pressure is now 150 psi and we need to make liquid. |
| tqs02a.Quench.070618140753.334 |  | 1516 | 20 | 0.0003 | 0.16 | 1.818 | 1.819 | We did a manual trip in order to check that everything is OK after the work done Friday/Monday. |
| tqs02a.Quench.070618143844.917 | 37 | 11446 | 20 | -0.0070 | 4.85 | 1.820 | 1.820 | quench at 11439A, T=1.82K, ramp rate 20A/s. HFU1/2=200V, 0ms delay, dump delay 1ms. |
| tqs02a.Quench.070618155056.289 | 38 | 11947 | 20 | -0.0053 | 4.74 | 1.895 | 1.906 | quench at I=11941A, T=1.9K, ramp rate 20A/s. Ç |
| tqs02a.Quench.070618171826.086 | 39 | 11757 | 20 | -0.0057 | 4.77 | 1.900 | 1.901 | quench at 11731A, T=1.91K, ramp rate 20A/s, many paramet. were tuned for VSDS (Conor knows details). |
| tqs02a.Quench.070618185329.392 | 40 | 11850 | 20 | -0.0059 | 4.78 | 1.886 | 1.887 | quench at 11844A, T=1.89K, ramp rate 20A/s. |
| tqs02a.Quench.070618204435.298 | 41 | 11417 | 20 | -0.0122 | 5.48 | 1.866 | 1.867 | quench at 11411A, T=1.9K, ramp rate 20A/s. |
| tqs02a.Quench.070619162136.084 | 42 | 12391 | 20 | -0.0050 | 4.84 | 1.854 | 1.859 | quench at 12383A, T=1.86K, ramp rate 20A/s. |
| tqs02a.Quench.070619173320.354 | 43 | 12051 | 20 | -0.0053 | 4.75 | 1.931 | 1.932 | quench at 12045A, T=1.94K, ramp rate 20A/s. |
| tqs02a.Quench.070619185157.071 | 44 | 11384 | 20 | -0.0083 | 4.96 | 1.911 | 1.913 | quench at 11374A, T=1.92K, ramp rate=20A/s. |
| tqs02a.Quench.070619202645.177 | 45 | 11751 | 20 | -0.0070 | 4.92 | 1.891 | 1.891 | Quench 45, I = 11741 A, ramp = 20 A/s, T = 1.9K, after sawtooth 0-10.5kA-0 3 times at 80 A/s |
| tqs02a.Quench.070619205921.684 | 46 | 11727 | 20 | -0.0063 | 4.79 | 2.069 | 2.068 | quench at 11716A, T=2.08K, ramp rate 20A/s. |
| tqs02a.Quench.070619212304.332 | 47 | 12467 | 10 | -0.0045 | 4.67 | 2.173 | 2.180 | quench at 12462.5A, T=2.17K, ramp rate 40A/s (upto 10kA) and then 10A/s. |
| tqs02a.Quench.070619220625.464 | 48 | 11966 | 20 | -0.0069 | 4.9 | 2.949 | 3.077 | quench at 11957A, T=2.95K, ramp rate 20A/s. |
| tqs02a.Quench.070620081502.510 | 49 | 11939 | 20 | -0.0069 | 4.88 | 4.440 | 4.437 | Quenching again at 4.5K. I_q=11932.8A, T=4.42K, ramp rate 20A/s. |
| tqs02a.Quench.070620085746.697 | 50 | 11941 | 20 | -0.0066 | 4.77 | 4.445 | 4.441 | quench at 11935.3A, T=4.44K, ramp rate 20 A/s. |
| tqs02a.Quench.070620094054.329 | 51 | 11940 | 20 | -0.0069 | 4.81 | 4.441 | 4.437 | quench at 11933.8A, T=4.44K, ramp rate 20A/s. |
| tqs02a.Quench.070620104514.523 | 52 | 11929 | 20 | -0.0073 | 4.89 | 4.448 | 4.444 | quench at 11924.5A, T=4.44K, ramp rate 20A/s |
| tqs02a.Quench.070620120733.533 |  | 1001 | 20 | -0.6323 | 0.75 | 4.458 | 4.458 | Manual trip at 1000A for Darryl's test. |
| tqs02a.Quench.070620122618.997 | 53 | 11921 | 20 | -0.0067 | 4.78 | 4.451 | 4.452 | quench at 11916.7A, T=4.45K, ramp rate 20A/s. |
| tqs02a.Quench.070620152411.289 |  | 1005 | 20 | 0.0021 | 0.13 | 4.456 | 4.453 | manual trip at 1000A to test noise reduction. |
| tqs02a.Quench.070620171503.734 |  | 11410 | 20 | -0.0024 | 3.83 | 4.522 | 4.536 | Trip at 11400A, T=4.49K. HFU1 fired at 400V. HFU2 in protection mode. |
| tqs02a.Quench.070620182836.832 |  | 8006 | 20 | -0.0130 | 3.48 | 4.447 | 4.505 | manual trip at 8000A, T=4.46K, ramp rate 20A. HFU1 in test mode, HFU2 in protect. mode (400V for both). |
| tqs02a.Quench.070620190124.970 |  | 5007 | 20 | -0.0372 | 2.32 | 4.440 | 4.460 | PHeater study, I = 5000A HFU#1, 400V |
| tqs02a.Quench.070620193005.259 |  | 3007 | 20 | -0.1187 | 1.64 | 4.435 | 4.448 | PHeater study, I = 3000 A, HFU#1 400V |
| tqs02a.Quench.070620200206.825 |  | 11414 | 20 | -0.0064 | 4.38 | 4.427 | 4.453 | PHeater study, I = 11400A, HFU#1 300V |
| tqs02a.Quench.070621075902.153 |  | 8004 | 20 | -0.0171 | 3.8 | 4.426 | 4.427 | Heater study: HFU1/2 capacitor voltage=300V. Ramp to 8000A. HFU1 fired. |
| tqs02a.Quench.070621082344.072 |  | 5002 | 20 | -0.0441 | 2.48 | 4.423 | 4.418 | Heater studies: ramp to 5000A. HfU1 fired (300V), HFU2 (400V) in protection mode. |
| tqs02a.Quench.070621084451.523 |  | 3004 | 20 | -0.1334 | 1.77 | 4.432 | 4.444 | Heater studies: ramp to 3000A, HFU1 (300V) fired, HFU2 (400V) in a protection mode. T=4.43K. Ramp rate 20A/s. |
| tqs02a.Quench.070621093553.536 |  | 10009 | 20 | -0.0193 | 5.31 | 4.416 | 4.413 | Spot heater study: trip induced by spot heater. HFU1/2 (200V) in protection mode, all delays 0ms. HFU3 - 40V. |
| tqs02a.Quench.070621100130.437 |  | 8008 | 20 | -0.0507 | 5.98 | 4.430 | 4.426 | Spot heater study: ramp to 8000A (w ramp rate 20A/s). HFU1/2 (200V) in protection mode, HFU3 (50V) in testing mode. T=4.43K. |
| tqs02a.Quench.070621102520.937 | 54 | 11930 | 20 | -0.0083 | 4.87 | 4.425 | 4.424 | Ramp 68 - quench 54 I = 11927 A, 20 A/s, T = 4.45K |

TQS02a Quench History table with first quenching segments

| File | # | Current (A) | dI/dt (A/s) | tquench | QDC | 1st VTseg | trise | 2nd VTseg | trise | Mag Temp | VSDS run |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  | Bot | Top |  |
| tqs02a.Quench.070604130438.013 |  | 1002 | 0 | 0.0017 | WcoilGnd | V1_TrigCvtB1 | -0.0003 | 23A05_23A06 | 0.0022 | 4.424 | 4.421 |  |
| tqs02a.Quench.070604153926.160 |  | 1327 | 50 | -0.4000 | HcoilHcoil | 22A08_22A09 | -0.0245 | 20B05_20B06 | -0.0055 | 4.429 | 4.427 |  |
| tqs02a.Quench.070604155955.441 |  | 1727 | 20 | -0.0027 | HcoilHcoil | 21A06_21A05 | -0.0046 | 21A08_21A07 | -0.0046 | 4.426 | 4.422 |  |
| tqs02a.Quench.070604162531.931 |  | 5003 | 20 | -0.0238 | HcoilHcoil | 21B01_21B02 | -0.0207 | 21B03_21B04 | -0.0206 | 4.427 | 4.425 |  |
| tqs02a.Quench.070605100858.753 |  | 1705 | 20 | -0.0218 | HcoilHcoil | 22B04_22B03 | -0.0213 | 22A02_22A03 | -0.0210 | 4.441 | 4.442 |  |
| tqs02a.Quench.070605144544.801 |  | 8014 | 20 | -0.0434 | HcoilHcoil | 23A09_23A10 | -0.0448 | 23A07_23A08 | -0.0402 | 4.430 | 4.426 |  |
| tqs02a.Quench.070605155126.832 |  | 8009 | 20 | -0.0357 | HcoilHcoil | 23A09_23A10 | -0.0382 | 23A07_23A08 | -0.0339 | 4.428 | 4.432 |  |
| tqs02a.Quench.070605162403.186 |  | 8006 | 20 | -0.0365 | HcoilHcoil | 23A09_23A10 | -0.0382 | 23A07_23A08 | -0.0336 | 4.432 | 4.433 |  |
| tqs02a.Quench.070605183235.446 |  | 5004 | 20 | -0.0325 | WcoilGnd | 23A05_23A06 | -0.0315 | HP_HN | -0.0291 | 4.433 | 4.430 |  |
| tqs02a.Quench.070605184714.684 | 1 | 9906 | 20 | -0.0148 | HcoilHcoil | 21A08_21A07 | -0.0160 | 21A06_21A05 | -0.0139 | 4.439 | 4.436 | 1 |
| tqs02a.Quench.070606094913.966 | 2 | 10326 | 20 | -0.0105 | HcoilHcoil | 21B05_21B06 | -0.0095 | 21B01_21B02 | -0.0091 | 4.442 | 4.437 | 2 |
| tqs02a.Quench.070606102106.918 |  | 1732 | 20 | -0.0192 | HcoilHcoil | 22B04_22B03 | -0.0098 | 22A02_22A03 | -0.0097 | 4.443 | 4.441 | 3 |
| tqs02a.Quench.070606111444.461 | 3 | 11165 | 20 | -0.0106 | HcoilHcoil | 20B01_20B02 | -0.0106 | Q24P_Q24N | -0.0106 | 4.435 | 4.434 | 4 |
| tqs02a.Quench.070606115518.721 | 4 | 11441 | 20 | -0.0085 | HcoilHcoil | 20A10_20A09 | -0.0091 | 20A08_20A07 | -0.0077 | 4.436 | 4.436 | 5 |
| tqs02a.Quench.070606123347.247 | 5 | 11578 | 20 | -0.0108 | HcoilHcoil | 21B03_21B04 | -0.0105 | 21B01_21B02 | -0.0098 | 4.437 | 4.434 | 6 |
| tqs02a.Quench.070606140258.865 | 6 | 10634 | 20 | -0.0155 | HcoilHcoil | 21B03_21B04 | -0.0171 | 21B01_21B02 | -0.0132 | 4.430 | 4.427 |  |
| tqs02a.Quench.070606144702.183 | 7 | 11642 | 20 | -0.0109 | HcoilHcoil | 22A08_22A09 | -0.0119 | 22A06_22A07 | -0.0113 | 4.437 | 4.435 | 8 |
| tqs02a.Quench.070606152746.043 | 8 | 11602 | 20 | -0.0070 | HcoilHcoil | 20A08_20A07 | -0.0081 | Q24P_Q24N | -0.0063 | 4.434 | 4.435 | 9 |
| tqs02a.Quench.070606155359.065 | 9 | 11127 | 20 | -0.0120 | HcoilHcoil | 20A08_20A07 | -0.0127 | 20A10_20A09 | -0.0105 | 4.454 | 4.454 | 10 |
| tqs02a.Quench.070606162133.230 | 10 | 11848 | 20 | -0.0073 | HcoilHcoil | 20A08_20A07 | -0.0081 | Q24P_Q24N | -0.0053 | 4.448 | 4.444 | 11 |
| tqs02a.Quench.070606164135.111 |  | 1945 | 20 | -0.0122 | HcoilHcoil | 20A08_20A07 | -0.0122 | 20A10_20A09 | -0.0122 | 4.450 | 4.448 | 12 |
| tqs02a.Quench.070606170223.671 | 11 | 11499 | 20 | -0.0115 | HcoilHcoil | 20A08_20A07 | -0.0102 | Q24P_Q24N | -0.0071 | 4.440 | 4.436 | 13 |
| tqs02a.Quench.070606173608.118 | 12 | 11706 | 20 | -0.0053 | HcoilHcoil | 20A08_20A07 | -0.0053 | 20A06_20A05 | -0.0048 | 4.446 | 4.445 |  |
| tqs02a.Quench.070606180247.881 | 13 | 11521 | 20 | -0.0063 | HcoilHcoil | 20A08_20A07 | -0.0077 | 20A06_20A05 | -0.0073 | 4.452 | 4.451 | 15 |
| tqs02a.Quench.070606183249.640 | 14 | 11700 | 20 | -0.0050 | HcoilHcoil | 20A08_20A07 | -0.0052 | 20A06_20A05 | -0.0046 | 4.453 | 4.450 | 16 |
| tqs02a.Quench.070606190519.154 | 15 | 11808 | 20 | -0.0048 | HcoilHcoil | 20A08_20A07 | -0.0048 | 20A06_20A05 | -0.0042 | 4.454 | 4.450 | 17 |
| tqs02a.Quench.070606193546.194 | 16 | 11712 | 20 | -0.0046 | HcoilHcoil | 20A08_20A07 | -0.0050 | 20A06_20A05 | -0.0045 | 4.457 | 4.455 | 18 |
| tqs02a.Quench.070607085819.744 | 17 | 12072 | 20 | -0.0076 | HcoilHcoil | 21B03_21B04 | -0.0073 | 21B01_21B02 | -0.0071 | 4.467 | 4.466 | 19 |
| tqs02a.Quench.070607093814.124 | 18 | 12274 | 20 | -0.0339 | HcoilHcoil | 20A02_20A01 | -0.0309 | 21A01_22A01 | -0.0115 | 4.452 | 4.455 |  |
| tqs02a.Quench.070607104128.088 | 19 | 11380 | 20 | -0.0098 | HcoilHcoil | 21B03_21B04 | -0.0111 | 21B01_21B02 | -0.0087 | 4.432 | 4.433 | 21 |
| tqs02a.Quench.070607112015.464 | 20 | 11974 | 20 | -0.0109 | HcoilHcoil | 21B03_21B04 | -0.0085 | 21B01_21B02 | -0.0074 | 4.439 | 4.434 | 22 |
| tqs02a.Quench.070607114524.375 | 21 | 12165 | 20 | -0.0050 | HcoilHcoil | 21B03_21B04 | -0.0055 | 21B01_21B02 | -0.0043 | 4.472 | 4.465 | 23 |
| tqs02a.Quench.070607121514.882 | 22 | 12153 | 20 | -0.0052 | HcoilHcoil | 21B03_21B04 | -0.0056 | 21B01_21B02 | -0.0046 | 4.459 | 4.457 | 24 |
| tqs02a.Quench.070607135538.210 | 23 | 12139 | 20 | -0.0055 | HcoilHcoil | 21B03_21B04 | -0.0059 | 21B01_21B02 | -0.0052 | 4.320 | 4.383 | 25 |
| tqs02a.Quench.070607163339.026 | 24 | 12110 | 20 | -0.0046 | HcoilHcoil | 21B03_21B04 | -0.0049 | 21B01_21B02 | -0.0041 | 4.410 | 4.410 | 26 |
| tqs02a.Quench.070607172917.427 | 25 | 12074 | 20 | -0.0050 | HcoilHcoil | 21B03_21B04 | -0.0053 | 21A01_22A01 | -0.0043 | 4.421 | 4.421 | 27 |
| tqs02a.Quench.070608101421.572 | 26 | 12050 | 5 | -0.0055 | HcoilHcoil | 21B03_21B04 | -0.0056 | 21B01_21B02 | -0.0052 | 4.429 | 4.427 |  |
| tqs02a.Quench.070608110141.397 | 27 | 11964 | 40 | -0.0070 | HcoilHcoil | 21B03_21B04 | -0.0077 | 21A04_21A03 | -0.0069 | 4.438 | 4.437 | 29 |
| tqs02a.Quench.070608112453.473 | 28 | 11717 | 80 | -0.0090 | HcoilHcoil | 21B03_21B04 | -0.0094 | 21A04_21A03 | -0.0080 | 4.442 | 4.445 | 30 |
| tqs02a.Quench.070608121122.767 | 29 | 12011 | 10 | -0.0056 | HcoilHcoil | 21B03_21B04 | -0.0055 | 21B01_21B02 | -0.0045 | 4.452 | 4.446 | 31 |
| tqs02a.Quench.070608140958.401 | 30 | 11407 | 100 | -0.0028 | HcoilHcoil | 21B01_21B02 | -0.0032 | 23A07_23A08 | -0.0032 | 4.426 | 4.423 | 32 |
| tqs02a.Quench.070609135925.713 | 31 | 10217 | 120 | -0.0048 | HcoilHcoil | 21A01_22A01 | -0.0043 | 23A07_23A08 | -0.0034 | 4.421 | 4.421 | 33 |
| tqs02a.Quench.070609143013.717 | 32 | 11844 | 60 | -0.0087 | HcoilHcoil | 21B03_21B04 | -0.0095 | 21A04_21A03 | -0.0084 | 4.429 | 4.433 |  |
| tqs02a.Quench.070611162130.884 | 33 | 11963 | 5 | -0.0046 | HcoilHcoil | 21B03_21B04 | -0.0049 | 21B01_21B02 | -0.0046 | 4.410 | 4.408 | 35 |
| tqs02a.Quench.070612140759.260 | 34 | 11937 | 20 | -0.0057 | HcoilHcoil | 21B03_21B04 | -0.0064 | 21B01_21B02 | -0.0048 | 1.853 | 1.853 | 36 |
| tqs02a.Quench.070612152045.937 | 35 | 11252 | 20 | -0.0084 | HcoilHcoil | 21B03_21B04 | -0.0092 | 21B01_21B02 | -0.0069 | 1.881 | 1.882 | 37 |
| tqs02a.Quench.070612172710.819 | 36 | 11777 | 20 | -0.0063 | HcoilHcoil | 21B03_21B04 | -0.0073 | 21B01_21B02 | -0.0056 | 1.815 | 1.813 | 38 |
| tqs02a.Quench.070618140753.334 |  | 1516 | 20 | 0.0003 | WcoilGnd | V1_TrigCvtB1 | -0.0003 | 20A02_20A01 | 0.0004 | 1.818 | 1.819 |  |
| tqs02a.Quench.070618143844.917 | 37 | 11446 | 20 | -0.0070 | HcoilHcoil | 21B03_21B04 | -0.0080 | 21B01_21B02 | -0.0053 | 1.820 | 1.820 | 39 |
| tqs02a.Quench.070618155056.289 | 38 | 11947 | 20 | -0.0053 | HcoilHcoil | 21B03_21B04 | -0.0062 | 21B01_21B02 | -0.0043 | 1.895 | 1.906 | 40 |
| tqs02a.Quench.070618171826.086 | 39 | 11757 | 20 | -0.0057 | HcoilHcoil | 21B03_21B04 | -0.0066 | 21B01_21B02 | -0.0045 | 1.900 | 1.901 | 41 |
| tqs02a.Quench.070618185329.392 | 40 | 11850 | 20 | -0.0059 | HcoilHcoil | 21B03_21B04 | -0.0069 | 21B01_21B02 | -0.0049 | 1.886 | 1.887 | 42 |
| tqs02a.Quench.070618204435.298 | 41 | 11417 | 20 | -0.0122 | HcoilHcoil | 21B03_21B04 | -0.0091 | 21B01_21B02 | -0.0077 | 1.866 | 1.867 | 43 |
| tqs02a.Quench.070619162136.084 | 42 | 12391 | 20 | -0.0050 | HcoilHcoil | 21B03_21B04 | -0.0056 | 21B01_21B02 | -0.0046 | 1.854 | 1.859 | 44 |
| tqs02a.Quench.070619173320.354 | 43 | 12051 | 20 | -0.0053 | HcoilHcoil | 21B03_21B04 | -0.0060 | 21B01_21B02 | -0.0043 | 1.931 | 1.932 | 45 |
| tqs02a.Quench.070619185157.071 | 44 | 11384 | 20 | -0.0083 | HcoilHcoil | 21B03_21B04 | -0.0092 | 21B01_21B02 | -0.0066 | 1.911 | 1.913 | 46 |
| tqs02a.Quench.070619202645.177 | 45 | 11751 | 20 | -0.0070 | HcoilHcoil | 21B03_21B04 | -0.0078 | 21B01_21B02 | -0.0056 | 1.891 | 1.891 | 48 |
| tqs02a.Quench.070619205921.684 | 46 | 11727 | 20 | -0.0063 | HcoilHcoil | 21B03_21B04 | -0.0070 | 21B01_21B02 | -0.0055 | 2.069 | 2.068 | 49 |
| tqs02a.Quench.070619212304.332 | 47 | 12467 | 10 | -0.0045 | HcoilHcoil | 20A08_20A07 | -0.0074 | 20A06_20A05 | -0.0073 | 2.173 | 2.180 | 50 |
| tqs02a.Quench.070619220625.464 | 48 | 11966 | 20 | -0.0069 | HcoilHcoil | 20A08_20A07 | -0.0071 | 20A06_20A05 | -0.0066 | 2.949 | 3.077 | 51 |
| tqs02a.Quench.070620081502.510 | 49 | 11939 | 20 | -0.0069 | HcoilHcoil | 21B03_21B04 | -0.0073 | 21B01_21B02 | -0.0066 | 4.440 | 4.437 | 52 |
| tqs02a.Quench.070620085746.697 | 50 | 11941 | 20 | -0.0066 | HcoilHcoil | 21B03_21B04 | -0.0073 | 21B01_21B02 | -0.0056 | 4.445 | 4.441 | 53 |
| tqs02a.Quench.070620094054.329 | 51 | 11940 | 20 | -0.0069 | HcoilHcoil | 21B03_21B04 | -0.0074 | 21B01_21B02 | -0.0056 | 4.441 | 4.437 | 54 |
| tqs02a.Quench.070620104514.523 | 52 | 11929 | 20 | -0.0073 | HcoilHcoil | 21B03_21B04 | -0.0077 | 21B01_21B02 | -0.0074 | 4.448 | 4.444 | 55 |
| tqs02a.Quench.070620120733.533 |  | 1001 | 20 | -0.6323 | HcoilHcoil | V1_TrigCvtB1 | -0.0034 | 21A08_21A07 | -0.0020 | 4.458 | 4.458 | 56 |
| tqs02a.Quench.070620122618.997 | 53 | 11921 | 20 | -0.0067 | HcoilHcoil | 21B03_21B04 | -0.0073 | 21B01_21B02 | -0.0059 | 4.451 | 4.452 | 57 |
| tqs02a.Quench.070620152411.289 |  | 1005 | 20 | 0.0021 | WcoilGnd | V1_TrigCvtB1 | -0.0003 | 23A05_23A06 | 0.0010 | 4.456 | 4.453 |  |
| tqs02a.Quench.070620171503.734 |  | 11410 | 20 | -0.0024 | HcoilHcoil | 21A10_21A09 | -0.0036 | 22B02_22B01 | -0.0024 | 4.522 | 4.536 | 58 |
| tqs02a.Quench.070620182836.832 |  | 8006 | 20 | -0.0130 | HcoilHcoil | 21A08_21A07 | -0.0112 | 20A08_20A07 | -0.0111 | 4.447 | 4.505 | 59 |
| tqs02a.Quench.070620190124.970 |  | 5007 | 20 | -0.0372 | HcoilHcoil | 20A06_20A05 | -0.0393 | 23B03_23B02 | -0.0385 | 4.440 | 4.460 | 60 |
| tqs02a.Quench.070620193005.259 |  | 3007 | 20 | -0.1187 | HcoilHcoil | 20A06_20A05 | -0.1179 | 20A08_20A07 | -0.1179 | 4.435 | 4.448 | 61 |
| tqs02a.Quench.070620200206.825 |  | 11414 | 20 | -0.0064 | HcoilHcoil | 20B03_20B04 | -0.0031 | 20B01_20B02 | -0.0029 | 4.427 | 4.453 | 62 |
| tqs02a.Quench.070621075902.153 |  | 8004 | 20 | -0.0171 | HcoilHcoil | 20A06_20A05 | -0.0150 | 20A08_20A07 | -0.0150 | 4.426 | 4.427 | 63 |
| tqs02a.Quench.070621082344.072 |  | 5002 | 20 | -0.0441 | HcoilHcoil | 21A06_21A05 | -0.0435 | 23B03_23B02 | -0.0428 | 4.423 | 4.418 | 64 |
| tqs02a.Quench.070621084451.523 |  | 3004 | 20 | -0.1334 | HcoilHcoil | 22A02_22A03 | -0.1260 | 23B03_23B02 | -0.1259 | 4.432 | 4.444 | 65 |
| tqs02a.Quench.070621093553.536 |  | 10009 | 20 | -0.0193 | HcoilHcoil | 23A09_23A10 | -0.0195 | 23A07_23A08 | -0.0169 | 4.416 | 4.413 | 66 |
| tqs02a.Quench.070621100130.437 |  | 8008 | 20 | -0.0507 | HcoilHcoil | 23A09_23A10 | -0.0463 | 23A07_23A08 | -0.0417 | 4.430 | 4.426 | 67 |
| tqs02a.Quench.070621102520.937 | 54 | 11930 | 20 | -0.0083 | HcoilHcoil | 21B03_21B04 | -0.0084 | 21B01_21B02 | -0.0074 | 4.425 | 4.424 | 68 |

Figure 2.2.  Quench history during training at 4.5K, at 1.9K, and during temperature dependence study. The marker of each quench shows the coil where it started.

- Quenches at temperature between 1.9 and 4.5K

Three quenches (#46 to #48) were performed during magnet warm up from 1.9K to 4.5K. It should be noted that the magnet temperature was not very uniform when these quenches were performed. Quenches 47 and 48 occurred in coil 20.  Ramp 47 started at 40 A/s up to10000 A and continued up to quench at 10 A/s. The quench current (12467 A) was the highest ever reached over the whole test.

- Ramp Rate Dependence

Ramp rate dependence studies at 4.5K were performed on June 8th and 9th. Current ramp rate was varied from 5A/s to 120A/s. Results are shown in Figure A. Quench current decreases with increasing ramp rate. There were two ramps done at 5A/s rate, at the beginning and at the end of ramp rate study. During this study we did not reproduce the highest quench current (12270A) previously reached with regular ramp rate (20A/s) at 4.5K.

Fig.4.1. Ramp rate dependence of magnet quench current at 4.5K. The highest quench current previously reached at 4.5K is also shown (square marker).

- Protection Heater studies

Protection heater studies were performed at 4.5K after the magnet training was completed at 1.9K temperature. In the TQS02a magnet 2 strip heaters, connected in series, were mounted on the outer layer of each coil (each heater covered one side of the outer layer). Two Heater Firing Units (HFU) were configured for 4.8mF capacitance, each connected to two coil strip heaters in parallel. One HFU was manually fired with the magnet at a constant current to initiate a quench, while second HFU was discharged as a protection heater by the system when the quench was detected. HFUs delay was set to 0ms. HFU1 in a test mode was connected to the strip heaters on coils 20 and 21. Heater studies were performed at 300V and 400V HFU capacitor voltages. Protection heater delays are shown in Figures 5.1 and 5.2. Full markers show the delay to quench start ( = |firing time – quench onset time|). Open markers show the delay to quench detection ( = |firing time|). The delay to quench detection depends on the detection threshold (3 V).

Fig.5.1. Protection heater delay at different current and different HFU capacitor voltage. Full markers show the delay to quench start; open markers show the delay to quench detection (affected by the high threshold)

Fig.5.2. Detail of previous picture showing delays at high current.

- Spot Heater study

Spot heater was mounted on the internal layer of each coil. Initial test of the Heater Firing Units, when we tried to fire all spot heaters together with the protection strip heater, and later the spot heater studies confirmed that spot heater induced quenches were observed only in two out of four coils: 23 and 21.

Spot heater study was done at 4.5K temperature. HFU1 and HFU2 connected to the strip heaters were set in a protection mode with 200V capacitor voltage and 0ms delay. HFU3 was connected to all spot heaters in parallel. Spot heaters were manually fired at 10000A and 8000A magnet current (spot heater capacitor voltage was 40V and 50V respectively). Detection delay time ( = |quench onset time|) was measured as 19.6ms at 10000A and 46.5ms at 8000A. MIITs were 5.3 at 10000A, and 6.0 at 8000A. In both cases first quenching segment was observed in coil 23.

- Strain gauge results

Coils 20,21,22,23 were used in TQS02a, having for the first time Titanium islands instead of Bronze. Similar to previous coils each coil had 3 strain gauges,: two gauges were attached to the inner layer island at the magnet center measuring azimuthal and axial strain and a single axial gauge was placed near the lead end. The gauges where thermally compensated by gauges mounted on stress-free titanium element. Fully compensated strain gauges were used on the shell and the axial tie rods. Measured strain “ε” in two principal directions “z, θ” (and no shear) were converted into stress “σ” using the relationships below with the Modulus, and Poisson ratio for titanium (islands) and aluminum (shell):

.

A comparison of stress in the structure and coils between TQS01,b,c and TQS02a is shown in the table below.

|  | TQS01 | TQS01b | TQS01c | TQS02a |
| --- | --- | --- | --- | --- |
| Maximum current (A) | 10602 (4.4K) 11019 (3.2K) | 9932 (4.4K) | 9570 (4.4K) 10521(1.9K) 9989 (4.4K) | 12269 (4.4K) 12463 (1.9K) 11935 (4.4K) |
| Iss (%) | 87% (4.4K) | 82% (4.4K) | 80-82% (4.4K) 80% (1.9K) |  |
| Shell cold (MPa) -t | +152 | +158 | +142 | +158 |
| Shell cold (MPa) -z | +143 | +140 | +137 | +140 |
| Rods cold (MPa) -z | +113 | +116 | +148 | +118 |
| Island cold (MPa) -t | -198 | -202 | -162 | -142 |
| Island cold (MPa) -z | +34 | +34 | +39 | -87 |

Many more plot files can be found at:

http://supercon.lbl.gov/caspi/download/TQS02a/

The measured strain or stress during the entire test is shown in the following figures:

A typical measured stress of coil 21 during cool-down and warm-up is shown above.

Coils 20,22, and 23 have shown similar behavior.

Axial strain in the island center (see below). The strain in coil 23 developed an “odd” offset below 10K and its absolute value can not be trusted.

Axial strain near the magnet “ends” (above)

.

- Quench Antenna Data

A quench antenna was used during training at 4.5 and 1.9K. The “KEK/HGQ” quench antenna consists of three stationary coil segments, each 0.35 m long and separated by 0.105 m long couplings. Each coil is made with four windings that are sensitive to normal and skew sextupole and octupole magnetic flux changes, at a radius of 23 mm. The probe was positioned in the bore of the magnet so that the second antenna coil, C2, was centered on the magnet coil center. Data analysis showed that windings in C2 recorded flux change signals almost for all quenches, while C1 windings recorded signals for most quenches at 1.9K. Only few signals were recorded in C3. Figure 9.1 shows for every training quench the difference between the time of the first signal in the quench antenna coils (in all windings of C1, C2 and C3) and the time of the quench start according to voltage taps data. This difference is within few msec with very few exceptions. Therefore almost all training quenches started in the magnet body (mostly close to the lead end from quench # 27). Quench antenna was not installed for the quenches 31 and 32 (in preparation to the magnetic measurements).

Figure 9.1  Difference between start of signal in quench antenna coils, and in voltage taps during training.

- RRR measurement

Estimates of RRR in TQS02a coil segments have been made using data captured during the final warm up of the magnet. We started warming the magnet up at about 6:00pm on June 21st reaching 19K temperature at 11:00am on June 22nd and the room temperature (302K) at about 10:00am on June 29th, as shown in Fig.10.1.

Voltages across “fixed” (used for quench protection) and “configurable” (used for quench onset location) voltage tap segments were monitored by the Pentek data loggers, while a current of alternating polarity, +/- 10A, was put through the magnet. We used the RRR-configuration of the amplifier gain for the voltage tap segments (i.e. configuration with increased gains for the “fixed” and “configurable” voltage tap segments). Due to underestimated coil resistance in the configuration file enlarged amplifier gains were set in the RRR-configuration. As a consequence some of the configurable VT signal voltages reached the 5V saturation level by noon of June 26 when magnet was at 180K. To keep the gains unchanged for RRR-measurement we reduced the Kepco trim current from +/- 10A to +/- 2.5A.

Data for all segments are shown in Fig.10.2 and Table 10-I. RRR of inner and outer coil layers are shown in Fig.10.3.

Fig.10.1: Test stand temperatures during the magnet warm up

Fig.10.2: RRR data for different voltage tap segments and coils

Fig.C: 10.3 of inner and outer coil layers

|  | Coil 20 |  |  | Coil 21 |  |  | Coil 22 |  |  | Coil 23 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R(19K) | R(300K) | RRR | R(19K) | R(300K) | RRR | R(19K) | R(300K) | RRR | R(19K) | R(300K) | RRR |
| B12.SnTi |  | 0.387 |  |  | 0.384 |  |  | 0.8456 |  |  | 0.38262 |  |
| B23.Omt | 0.413 | 75.81 | 183.56 | 0.423 | 75.87 | 179.36 | 0.34 | 75.301 | 221.47 | 0.335 | 75.8413 | 226.39 |
| B34.OLS | 0.0115 | 2.08 | 180.87 | 0.0134 | 2.089 | 155.90 | 0.00925 | 2.0534 | 221.99 |  | 1.12396 |  |
| B45.ORE | 0.002715 | 0.465 | 171.27 | 0.002815 | 0.4694 | 166.75 | N/A | N/A | N/A |  | 1.01212 |  |
| B56.ORS | 0.0109 | 1.912 | 175.41 | 0.0113 | 1.9217 | 170.06 | 0.0093 | 1.8906 | 203.29 | 0.00915 | 1.92755 | 210.66 |
| B6A10.Ramp | 0.0157 | 1.17 | 74.52 | 0.0183 | 1.1494 | 62.81 |  | 0.2009 |  | 0.015 | 1.14665 | 76.44 |
| A80.IRS+RE | 0.0097 | 1.703 | 175.57 | 0.0098 | 1.6998 | 173.45 | 0.0075 | 1.6204 | 216.05 | 0.0083 | 1.7011 | 204.95 |
| A68.ILS+LE | 0.0145 | 2.453 | 169.17 | 0.01475 | 2.4436 | 165.67 | 0.011 | 2.4013 | 218.30 | 0.0115 | 2.4801 | 215.66 |
| A56.T2-5 | 0.1095 | 20.122 | 183.76 | 0.109 | 20.086 | 184.28 | 0.0884 | 20.0902 | 227.26 | 0.0888 | 20.0864 | 226.19 |
| A45.T6 | 0.0253 | 5.246 | 207.35 | 0.0287 | 5.2498 | 182.92 | N/A | N/A | N/A | 0.0241 | 5.40218 | 224.17 |
| A34.T7Rs | 0.0114 | 2.121 | 186.05 | 0.0114 | 2.123 | 186.23 |  | 0.1053 |  | N/A | N/A | N/A |
| A23.Imt | 0.364 | 68.422 | 187.97 | 0.362 | 68.443 | 189.07 | 0.295 | 68.3712 | 231.77 | 0.316 | 70.331 | 222.57 |
| A12.SnTi |  | 0.371 |  |  | 1.667 |  |  | 0.3688 |  |  | 0.036351 |  |

Table 10-I: RRR data for all segments

- Quench origin location

Time-of-flight quench-origins were calculated for several quenches during the initial training of TQS02, using the following three times: quench-onset, 1st exit and 2nd-exit (when available).  The time-of-flight distance assumed the known V-tap locations and equal quench-propagation speeds for both quench-fronts. If the time of the 2nd quench-front’s exit was not visible (e.g., when the V-tap DAQ was blinded by the dump-transient voltage) the following quench-speeds were assumed: 20m/s (inner layer), and 10m/s (outer layer).  The following quench-origins were analyzed: Q1,2,3,4,7,8,10,11,15,17,25, 26,27, as indicated in the table below, plotted on a Theta/Z-scaled version of the two pole-turns (Fig. 10.1).

Fig. 10.1: Quench-origin plot for some of TQS02’s early training quenches.  Refer to the table to identify the coil.  The first three training quenches originated in the outer layer ends, close to its transit across the inner pole-island. Middle training quenches occurred in the inner pole turn straight-sections.  4.5K plateau quenches always had multiple starts in the outer layer.  The first onset occurred near the middle of the lead-in side (bottom of plot) a second pole-turn onset originated shortly later just inside the V-tap demarcating the start of the interlayer “Ramp” segment (top left in plot).

- Magnetic Measurements

The field quality magnetic measurements were made with the VMTF vertical drive system and LHC/EMS rotating harmonic coil readout cart. Several data sets were captured:  warm z-scan before cool down, z-scans at 4.5 K and 1.9K. A full cold measurement program is described below. A 0.1 m long tangential probe, with 2 dipole, 2 quadrupole and 1 tangential windings, was utilized. This probe was specially built for these measurements with a radius of 2.17 cm, optimized to the warm finger ID. The positive direction of the z-axis for the scans is pointing from the magnetic center to the lead end, from which the probe was inserted. Each measurement (e.g., at one z-position) contains data from at least 25 full rotations of the probe, and z-scans steps were equal to the length of the probe.

The cold magnetic measurement program at 4.5 and 1.9 K is consisted of the following measurements:

  - Z-scans at 4.5 K:  6.5, 8.0 and 10.5 kA

  - Z-scans at 1.9 K: 12.3 Tm/m (LHC injection, estimated to be 0.583 kA), 100 Tm/m (estimated to be 5.15kA). A measurement at high current (~Iqmax– 0.6kA) was not performed at 1.9 K.

  - Eddy current loops:  20 40 and 80 A/s up to 10 kA with the  probe  positioned in the center of the magnet

  - Dynamic effects measurement, which included a current accelerator profile, similar to the one used in LHC MQXB quads (15 min. duration of the injection plateau and the probe positioned in the center of the magnet).

All magnetic measurement results are presented at 17 mm reference radius, the official radius adopted for LHC.  A detailed magnetic measurements summary is posted at the following URL:

HTTP://tdserver1.fnal.gov/velev/magnets/web/magnets/TQS02/TQS02a_mag_meas.html

Table 11.1 summarizes the quadrupole strength (T*m/m) and transfer function (TF) versus the excitation current, measured when the probe was positioned at the center of the magnet body (z=0 m). The 16% degradation of the TF at high currents is expected due to the iron saturation.

Fig. 11.1 shows the TF versus z coordinate profiles at 0.58, 5.15 and 10.5 kA. The integral magnetic lengths are calculated to be 0.712, 0.723 and 0.735 m at these currents.

| Requested Current (A) | -10 | 10 | 583 | 4000 | 5155 | 10000 |
| --- | --- | --- | --- | --- | --- | --- |
| Measured Current (A) | -10.81 | 10.80 | 583.84 | 3997.74 | 5152.42E | 9995.80 |
| Field (T*m/m) | 0.2336 | 0.2336 | 12.48 | 83.92 | 104.58 | 184.92 |
| TF (T/kA) | 21.71 | 21.62 | 21.38 | 20.99 | 20.29 | 18.50 |

Table 11.1 Strength and TF at different currents in the body of the magnet

Figure 11.1. The magnet TF versus z coordinate at 0.583, 5.15 and 10.0 kA.

Table 11.2 summarizes the harmonics at injection (0.583 kA) and maximum measured current (10.5 kA), averaged over the magnet (left) and for the center body position (right). In general, the field harmonics are in the order of several units. The b5 and b6 at injection are observed to be relatively large, ~ 10 units, similar to TQS01c.

Table 11.2. TQS02 body and average harmonics at different currents

|  | Average | Average | Body only | Body only |
| --- | --- | --- | --- | --- |
| Multipole(units) | Injection | 10.5 kA | Injection | 10.5kA |
| b_3 | 1.71E+00 | 8.50E-01 | 1.90E+00 | 6.16E-01 |
| b_4 | -1.77E-03 | 4.51E-01 | 5.14E-02 | 5.66E-01 |
| b_5 | 7.75E+00 | -3.69E-01 | 7.54E+00 | -7.40E-01 |
| b_6 | -1.29E+01 | 1.72E+00 | -1.29E+01 | 1.85E+00 |
| b_7 | -2.88E-03 | 9.83E-03 | 1.11E-02 | 2.37E-02 |
| b_8 | -6.73E-04 | -2.15E-02 | 2.31E-03 | -1.92E-02 |
| b_9 | -7.62E-02 | 2.29E-02 | -9.43E-02 | 1.12E-02 |
| b_10 | 1.03E-01 | -1.25E-02 | 1.17E-01 | -6.81E-03 |
| a_3 | 3.49E-01 | 2.46E-01 | 5.37E-01 | 4.04E-01 |
| a_4 | -2.15E+00 | 1.13E+00 | -1.99E+00 | 1.44E+00 |
| a_5 | 4.40E+00 | -2.30E-01 | 3.94E+00 | -7.49E-01 |
| a_6 | 4.49E-01 | 1.07E-01 | 3.62E-01 | 9.59E-02 |
| a_7 | -3.79E-02 | -2.50E-02 | -4.78E-02 | -4.20E-02 |
| a_8 | 6.43E-03 | -1.37E-02 | 3.12E-02 | 2.29E-03 |
| a_9 | -3.09E-02 | 9.25E-03 | -4.34E-02 | 6.34E-04 |
| a_10 | 2.55E-03 | 5.24E-03 | 2.96E-03 | 3.56E-03 |

Figure 11.2 shows the dodecapole versus time. The current profile used in this measurement was derived from the profile of production inner triplet LHC quadrupole (LQXB) measurements. The duration of the injection porch was set to 15 min at 12.8 T, accordingly to the LHC specifications. One can observe that the b6 decay and snapback, which are commonly observed in NbTi magnets, are not present (see the time interval from ~700 to ~1600 s).

Current loops at 20, 40 and 80 A/s for TQS02 quadrupole have been executed. The b6 difference between the ramp rate loops is small, indicating small or negligible eddy current effect on the hysteresis loop, similar to what was observed in TQS01c measurements. The b6 hysteresis loops are shown in Figure 11.3.

Figure 11.2. Dodecapole (b6, in units) versus time (s): current profile simulates an accelerator operation.

Figure 11.3. Dodecapole (b6) versus excitation current at different ramp rate 20 (red), 40 (green) and 80 (blue) A/s.

References

- 1. C. Donnelly, G. Ambrosio, G. Chlachidze, S. Rahimzadeh-Kalaleh

“TQS02a Voltage Spike Analysis”,

FNAL TD-07-015, LARP note July 2007

# Text boxes

300 K

4.5 K

1.9 K

4.5 K

300 K