Construction Specification 735 - Concrete Block and Brick Masonry

1.	Scope

The work shall consist of furnishing all required materials and constructing the concrete block and/or brick masonry structures shown on the drawings. Concrete floors, slabs, footings, beams, or similar structural components of composite structures are not included.

2.	Materials

Masonry stone shall meet the requirements of the latest edition of the Alabama Department of Transportation, Standard Specifications for Highway Construction, Section 812, Masonry Stone.

Masonry cement shall meet the requirements of the latest edition of the Alabama Department of Transportation, Standard Specifications for Highway Construction, Section 815, Cement.

Portland cement shall meet the requirements of the latest edition of the Alabama Department of Transportation, Standard Specifications for Highway Construction, Section 815, Cement.

Aggregate for masonry mortar shall meet the gradation requirements of ASTM Specification C-144.

Mortar shall be made by mixing, by volume, one part masonry cement, one part portland cement, five parts mortar aggregate (in damp loose condition), and sufficient water to provide a workable consistency. Mortar that is not used within 2-1/2 hours after mixing shall be discarded.

On-site storage facilities will be such that cements and concrete blocks will be stored and maintained in an air-dry condition.

Written material certifications will not be required unless requested by the Engineer due to reasonable doubt concerning the quality of materials.

3.	Laying

The footing surface shall be cleaned of all unsatisfactory concrete, laitance, coatings, stains, or debris by dry scrubbing with a wire brush or broom, by compressed air, or other methods approved by the Engineer prior to laying the first course of blocks or bricks.

Concrete blocks and brick shall be air dry at the time of placement. Cracked, broken, or chipped blocks or brick shall not be used.

Mortar joints shall be of the thickness required to provide the overall dimensions shown on the drawings. Joints shall be tooled after initial setting and all excess mortar removed to present a finished appearance.

Unless otherwise specified, cores in the stretcher blocks shall be filled after laying with concrete or mortar. The filler shall be thoroughly hand tamped with a steel rod or similar tool to remove air pockets and voids.

4.	Items of work and construction details

The item of work to be performed in conformation with this specification and construction details are:

Work or Material Item, Concrete Block

(1)	This item shall consist of furnishing and installing the 8 in. x 8 in. x 16 in., 8 in. x 8 in. x 8 in. and the 4in. x 8 in. x 16 in. concrete blocks for the 48 in. drop inlets as shown on the drawings.

(2)	Cutting or shaping the blocks to fit the design shall be done by sawing or other methods acceptable to the Engineer.

(3)	All visible corners or edges of the block inlets will be constructed with corner blocks that have smooth flat end surfaces.

(4)	The first course of blocks and steel reinforcing bars will be installed before the footing slab concrete sets up.