July 22, 1994

Contract #TW0592

SPECIAL STANDARD SPECIFICATION

SECTION 09250-S

GYPSUM DRYWALL

Page

PART 1 - GENERAL

1.01	Description Of Work	2

1.02	Design Requirements	2

1.032	Submittals	2

1.043	Quality Assurance	3

1.054	Delivery, Storage And Handling	3

1.065	Project Conditions	3

PART 2 - PRODUCTS

2.01	Manufacturers	3

2.02	Steel Framing Components For Suspended And Furred Ceilings	4

2.03	Steel Framing For Walls And Partitions	4

2.04	Gypsum Board	54

2.05	Trim Accessories	65

2.06	Gypsum Board Joint Treatment Materials	76

2.07	Miscellaneous Materials	76

PART 3 - EXECUTION

3.01	Installation Of Steel Framing	87

3.02	Installation Of Steel Framing For Suspended And Furred Ceilings	87

3.03	Installation Of Steel Framing For Walls And Partitions	97

3.04	Application And Finishing Of Gypsum Board	98

3.05	Methods Of Gypsum Drywall Application	109

3.06	Installation Of Drywall Trim Accessories	1110

3.07	Installation Of Miscellaneous Materials	1210

3.08	Finishing Of Drywall	1210

SPECIAL STANDARD SPECIFICATION

SECTION 09250-S

GYPSUM DRYWALL

PART 1 - GENERAL

1.01	DESCRIPTION OF WORK

A.	Extent of each type of gypsum drywall construction required is indicated on contract drawings.  This section includes the following types of gypsum board construction:

1.	Light-gauge, non-load bearing steel framing members.

2.	Gypsum board screw-attached to steel framing and furring members.

B.	Related Sections:  Sound attenuation blankets are specified in Division 7, Section "Building Insulation".

1.02	DESIGN REQUIREMENTS

A.	Provide partitions and suspended ceilings adequately braced for seismic conditions as identified in Uniform Building Code, Chapter 47, “Installation of Wall and Ceiling Coverings.”

1.032	SUBMITTALS

A.	Product Data:  Submit product information from manufacturers for each type of product specified.

B.	Material Safety Data Sheets (MSDS):  Submit MSDS for all gypsum board products.

C.	Shop Drawings:  Submit details of seismic bracing proposed for use at suspended ceilings and at vertical partitions not braced to structural system.

D.	Submit shop drawings to illustrate each different condition.  Include installation details, inside and outside corners, control joints, penetrations, etc.  Indicate control joint locations on floor plans.

1.043	QUALITY ASSURANCE

A.	Fire-Resistance Rating:  Where gypsum drywall systems with fire-resistance ratings are indicated, provide materials and installations identical with applicable assemblies which have been tested and listed by UL.

B.	Manufacturer:  Obtain gypsum board products from a single manufacturer or from manufacturers recommended by the prime manufacturer of gypsum boards.

Manufacturers offering products which may be incorporated in the work are those who have been in business successfully for at least 5 years without record of product failure.

C.	Products:  All gypsum board products, including joint compounds, tapes, sealants, adhesives, and texturing products shall not contain any asbestos fibers.

1.054	DELIVERY, STORAGE AND HANDLING

Deliver and store materials in manufacturer's original unopened packages, clearly marked with identifying information.  Protect materials as recommended by the manufacturer.

1.065	PROJECT CONDITIONS

A.	Environmental Conditions:  Establish and maintain environmental conditions for application and finishing of gypsum board to comply with ASTM C 840 and with gypsum board manufacturer's recommendations.

B.	Minimum Room Temperatures:  For attachment of gypsum board to framing, maintain not less than 40 degrees F.  For finishing of gypsum board, maintain not less than 50 degrees F for 48 hours prior to application, and continuously thereafter until drying is complete.

C.	Ventilation:  Ventilate building spaces to remove water not required for drying joint treatment materials.  Avoid drafts during dry, hot weather to prevent materials from drying too rapidly.

PART 2 - PRODUCTS

2.01	MANUFACTURERS

A.	Available Manufacturers:  Subject to compliance with all requirements, manufacturers offering products which may be incorporated in the work include but are not limited to the following:

1.	Steel Framing and Furring:

Dale Industries, Inc.

Dietrich Industries

Gold Bond Building Products Division, National Gypsum Co. Unimast, Inc.

United States Gypsum Co.

2.	Grid Suspension System:

Chicago Metallic Corp.

National Rolling Mills Co.

3.	Gypsum Boards and Related Products:

Georgia Pacific Corp.

Gold Bond Building Products Division, National Gypsum Co.

United States Gypsum Co.

4.	Bullnose Corner Bead:

Beadex

2.02	STEEL FRAMING COMPONENTS FOR SUSPENDED AND FURRED CEILINGS

A.	General:  Provide components which comply with ASTM C 754 for materials and sizes, unless otherwise indicated.

B.	Main Runners:  Hot or cold-rolled steel channels with rust inhibitive paint finish.

C.	Hanger Wire:  ASTM A 641, soft, Class 1 galvanized, minimum 9 gauge.

D.	Hanger Anchorage Devices:  Screws, clips, bolts, cast-in-place concrete inserts or other devices applicable to the indicated method of structural anchorage for ceiling hangers.  Size devices for 3 times the calculated load supported, except size direct pull-out concrete inserts for 5 times the calculated loads.

E.	Steel Rigid Furring Channels:  ASTM C 645, hat-shaped, depth of 7/8 inch; mininum 25 gauge thickness, unless otherwise indicated.

F.	Grid Suspension System:  ASTM C 645, manufacturer's standard grid suspension system composed of main beams and cross furring members which interlock to form a modular supporting network.

2.03	STEEL FRAMING FOR WALLS AND PARTITIONS

A.	Steel Studs and Runners:  ASTM C 645, galvanized, 25 gauge thickness unless otherwise indicated.  20 gauge at door jambs and for support of restroom fixtures.

1.	Depth of Section:  3-5/8 inch or as shown on drawings.

2.	Runners:  Match studs; type recommended by stud manufacturer for floor and ceiling support of studs, and for vertical abutment of drywall work at other work.

B.	Steel Rigid Furring Channels:  ASTM C 645, hat-shaped, galvanized; minimum depth of 7/8 inch and minimum 25 gauge thickness, unless otherwise indicated.

C.	Z-Furring Members:  Manufacturer's standard zee-shaped furring members fabricated from hot-dip galvanized steel sheet complying with ASTM A 525, Coating Designation G60; minimum 25 gauge thickness, face flange of 1-1/4 inch, wall-attachment flange of 7/8 inch, and of depth required to fit insulation thickness indicated.

D.	Fasteners:  Type and size recommended by gypsum drywall manufacturer for the substrate and application indicated.

2.04	GYPSUM BOARD

A.	General:  Provide gypsum board of type, edge configuration, and thickness indicated, in maximum lengths available to minimize end-to-end butt joints.

B.	Gypsum Board:  ASTM C 36, and unless otherwise indicated:

1.	Type:  Regular.

2.	Edges:  Tapered.

3.	Thickness:  1/2 inch at ceilings.

4.	Thickness:  5/8 inch at walls.

B.	For interior applications on walls and ceilings, provide the following:

1C.	Fire-Resistive Board:  ASTM C 36, and unless otherwise indicated:

21.	Type:  Type "X".

32.	Edges:  Tapered.

43.	Thickness:  5/8 inch at ceilings and walls.

C.	For applications as Substrate for Exterior Insulation Finish System (EIFS), provide the following:

1.	Walls:  Exterior grade gypsum sheathing

a.	ASTM C 79

b.	Thickness:  1/2 inch

c.	Edge:  T & G

2.	Ceilings:  Exterior grade gypsum ceiling board

a.	ASTM C 931

b.	Thickness: 1/2 inch

c.	Edge:  T & G

D.	For rework at prototyping area

1.	ASTM C 931

2.	Type:  X

3.	Thickness:  5/8 inch

4.	Edge:  T & G

E.	Thermal Barrier:  Where used as thermal barrier under polyisocyanurate insulation, provide the following:

1.	ASTM C 79

2.	Type:  X

3.	Thickness:  5/8 inch

4.	Edge:  Square

D.	Gypsum Backing Board:  ASTM C 442, and use where indicated on drawings or where backing board is not available from manufacturer, gypsum board, ASTM C 36.  Unless otherwise indicated:

1.	Type:  Regular or Type "X" for fire-resistance-rated assemblies.

2.	Edge:  Tapered.

3.	Thickness:  5/8 inch.

E.	Water-Resistant Backing Board:  ASTM C 630, and use where indicated on drawings.  Unless otherwise indicated:

1.	Type:  Regular or Type "X" for fire-resistance-rated assemblies.

2.	Edge:  Tapered.

3.	Thickness:  5/8 inch.

2.05	TRIM ACCESSORIES

A.	Cornerbead and Edge Trim:  Provide cornerbeads, edge trim, and control joints which comply with ASTM C 1047 and requirements indicated below:

1.	Material:  Unless otherwise indicated, galvanized steel with either knurled and perforated or expanded flanges, and beaded for concealment of flanges in joint compound.

2.	Edge trim shapes indicated below by reference to designations of Figure 1 in ASTM C 1047:

a.	"L" Bead

b.	"U" Bead

c.	"LK" Bead

B.	Control Joint:  Provide one piece control joint formed with vee-shaped slot per Figure 1 in ASTM C 1047, with slot opening covered with removable strip.

2.06	GYPSUM BOARD JOINT TREATMENT MATERIALS

A.	General:  Provide materials complying with ASTM C 475, ASTM C 840 and type recommended by the manufacturer for the application indicated, except as otherwise indicated.

B.	Joint Tape:  Paper reinforcing or fiberglass tape.

C.	Setting-Type Joint Compound:  Factory-prepackaged, job-mixed, chemical-hardening powder products formulated for bedding and filling.

For filling joints and treating fasteners and cut edges of water-resistant gypsum backing board, use formulation recommended by gypsum board manufacturer.

D.	Drying-Type Joint Compounds:  Factory-prepackaged, vinyl-based, ready-mix or job-mixed products formulated for taping and topping.

2.07	MISCELLANEOUS MATERIALS

A.	General:  Provide auxiliary materials for gypsum drywall construction which comply with referenced standards and the recommendations of the gypsum board manufacturer.

B.	Gypsum Board Screws:  ASTM C 1002.

C.	Acoustical Sealant:  Water base, non-drying, non-bleeding, non-staining type and permanently elastic.  Comply with requirements specified in Division 7, Section "Joint Sealants", and as recommended by the gypsum board manufacturer for application indicated.

D.	Texturing Products:  As recommended by gypsum board manufacturer for satisfactory "spatter" spray texturing.  Provide other textures as indicated on drawings or schedules.

E.	Corner Guards:  Provide surface-mounted corner guards on all corridor walls and other high impact areas as indicated on drawings.  Where corner guards are required on fire-resistive walls, provide surface or flush-mounted type that are UL listed.

1.	Corner guards shall consist of a continuous extruded aluminum retainer, top and bottom high impact nylon closer caps, and a vinyl/acrylic guard.

2.	Guard length shall be a minimum of 4'-0".

3.	Wall thickness of .110 inch and angle-shaped with 3 inch legs and 1/4 inch radius at corners and ends.

4.	Furnish guard in matte finish from manufacturer's standard color line.  Closure caps shall be of the same color as the guards.  Color to be selected from color selection charts provided by the manufacturer.

F.	Chair Rails:  Provide surface-mounted chair rails on all conference room walls and as indicated on drawings.

1.	Chair rails shall consist of a wood rail painted to match wall.  continuous extruded aluminum retainer, end and corner transitions, and a vinyl/acrylic rail.

2.	Provide rails with a minimum overall height of 3-1/2 inches and overall depth of 7/8 inch.

G.	Bullnose Corner Bead:  Provide nail-on corner bead as manufactured by Beadex.

1.	Style:  Danish N, 1-1/2 Softline.

2.	Size:  1-1/2 inch

PART 3 - EXECUTION

3.01	INSTALLATION OF STEEL FRAMING

A.	Comply with provisions of UBC Articles 4703 and 4704.

BA.	Steel Framing Installation Standard:  Install steel framing to comply with ASTM C 754 and with ASTM C 840 requirements that apply to framing installation.

CB.	Install supplementary framing, blocking and bracing at terminations in the construction and for support of fixtures, equipment services, heavy trim, grab bars, toilet accessories, furnishings, and similar construction to comply with details indicated and with recommendations of gypsum board manufacturer.

DC.	Isolate steel framing from building structure where edges of suspended ceilings abut building structure horizontally at ceiling perimeters, at penetration of structural elements, and where partition and wall framing abuts overhead structure.

ED.	Do not bridge building expansion and control joints with steel framing or furring members.

3.02	INSTALLATION OF STEEL FRAMING FOR SUSPENDED AND FURRED CEILINGS

A.	Secure hangers to structural support by connecting directly to structure where possible, otherwise connect to inserts, clips or other anchorage devices or fasteners as indicated on drawings.

B.	Space main runners 4'-0" and hangers 4'-0" o.c. along runners, unless otherwise indicated.

C.	Installation Tolerances:  Install steel framing components for suspended ceilings so that cross furring members or grid suspension members are level to within 1/8 inch in 12'-0", measured lengthwise on each member and transversely between parallel members.

D.	Grid Suspension System:  Attach perimeter wall track or angle where grid suspension system meets vertical surfaces.  Mechanically join main beam and cross furring members to each other and butt-cut to fit into wall track.

E.	Attach perimeter wall track or  angle wherever support system meets vertical surfaces.

F.	Cross runners supported with 12-gage vertical wires attached to the building structure shall be provided at each end of each surface-mounted lighting fixture.

3.03	INSTALLATION OF STEEL FRAMING FOR WALLS AND PARTITIONS

A.	Install runners (tracks) at floors, ceilings and structural walls, and columns where gypsum drywall stud system abuts other work.

B.	Installation Tolerances:  Install each steel framing and furring member so that the fastening surface do not vary more than 1/8 inch from plane of faces of adjacent framing.

C.	Extend partition framing full height to structural supports or substrates above suspended ceilings, except where partitions are indicated to terminate at suspended ceilings.  Where partitions terminate below ceilings or just above ceiling without extending to structure, provide lateral bracing.  Continue framing for doors and openings, and frame around ducts penetrating partitions above ceiling to provide support for gypsum board.

D.	Space studs and wall furring at 16 inches o.c., except as otherwise indicated.  Attach studs to top and bottom tracks by button punch or screws, except that studs located adjacent to doors, windows, partition intersections or ends, and at corners shall be screwed to tracks.

E.	Frame door openings with vertical studs securely attached by screws at each jamb either directly to frames or to jamb anchor clips on door frame; install runner track sections (for jack studs) at head and secure to jamb studs.

F.	Frame openings other than door openings in same manner as required for door openings, and install framing below sills of openings to match framing required above door heads.

3.04	APPLICATION AND FINISHING OF GYPSUM BOARD

A.	Install walls in strict accordance with indicated UL assemblies.

BA.	Gypsum Board Application and Finishing Standard:  Install and finish gypsum board to comply with ASTM C 840.

CB.	Install ceiling boards in the direction and manner which will minimize the number of end-butt joints, and which will avoid end joints in the central area of each ceiling.  Stagger end joints at least 12 inches.

DC.	Install wall/partition boards vertically to avoid end-butt joints wherever possible.

ED.	Install exposed gypsum board with face side out.  Do not install imperfect, damaged or damp boards.  Butt boards together for a light contact at edges and ends with not more than 1/16 inch open space between boards.  Do not force into place.

FE.	Locate either edge or end joints over supports.  Position boards so that like edges abut, tapered edges against tapered edges and mill-cut or field-cut ends against mill-cut or field-cut ends.  Stagger vertical joints over different studs on opposite sides of partitions.

GF.	Attach gypsum board to framing and blocking as required for additional support at openings and cutouts.

HG.	Form control joints and expansion joints with space between edges of boards, prepared to receive trim accessories.

IH.	Isolate perimeter of non-load bearing drywall partitions at structural abutments.  Provide 1/4 to 1/2 inch space and trim edge with "U" bead trim.  Seal joints with acoustical sealant.  Do not fasten drywall directly to stud system runner tracks.

JI.	Where sound attenuation drywall construction is indicated, seal the work at perimeters, control and expansion joints, openings, and penetrations with a continuous bead of acoustical sealant including a bead at both faces of partitions.  Comply with manufacturer's recommendations for location of beads and close off sound-flanking paths around or through the work.

KJ.	Space fasteners in gypsum boards in accordance with manufacturer's recommendations.

3.05	METHODS OF GYPSUM DRYWALL APPLICATION

A.	Single-Layer Application:  Install gypsum wallboard as follows:

1.	On ceilings, apply gypsum board prior to wall/partition board application to the greatest extent possible.

2.	On partitions/walls, apply gypsum board vertically (parallel to framing), unless otherwise indicated and provide sheet lengths which will minimize end joints.

3.	On Z-furring members, apply gypsum board vertically (parallel to framing) with no end joints.  Locate edge joints over furring members.

B.	Wall Tile Base:  Where drywall is base for thin-set ceramic tile and similar rigid applied wall finishes, install gypsum backing board.

At showers, tubs and similar "wet" areas, install water-resistant backing board.  Apply with un-cut long edge at bottom of work, and space 1/4 inch above fixture lips.  Seal ends, cut-edges, and penetrations of each piece with water-resistant compound before installation.

C.	Acoustical Tile Base:  Where drywall is base for adhesively-applied acoustical tile, install gypsum backing board.

Provide either V-joint type backing board, or tape and finish joints (2 coats unsanded).

D.	Double-Layer Application:  Install gypsum backing board for base layer and gypsum board for face layer.

1.	On ceilings, apply base layer prior to application of base layer on walls/partitions; apply face layers in same sequence.  Offset joints between layers at least 10 inches.

2.	On partitions/walls apply base layer and face layers vertically (parallel to framing) with joints of base layer over supports, and with face layer joints offset at least 10 inches with base layer joints.

3.	On Z-furring members apply base layer vertically (parallel to framing), and face layer either vertically (parallel to framing) or horizontally (perpendicular to framing) with vertical joints offset at least one furring member.  Locate edge joints of base layer over furring members.

E.	Single-Layer Fastening Methods:  Apply gypsum boards to supports with screws.

F.	Double-Layer Fastening Methods:  Apply base layer of gypsum board and face layer to base layer by fastening both base layers and face layers separately to supports with screws.

3.06	INSTALLATION OF DRYWALL TRIM ACCESSORIES

A.	General:  Where feasible, use the same fasteners to anchor trim accessory flanges as required to fasten gypsum board to the supports.

B.	Install metal corner beads at external corners of drywall work.

C.	Install metal edge trim whenever edge of gypsum board would otherwise be exposed or semi-exposed.  Provide type with face flange to receive joint compound except where "U" bead (semi-finishing) type is indicated.

1.	Install "L" bead where work is tightly abutted to other construction.

2.	Install special "LK" bead where other work is kerfed to receive long leg of "L" bead trim.

3.	Install "U" bead where edge is exposed, revealed, gasketed, or sealant-filled (including expansion joints).

D.	Install "U" bead trim where indicated, and where exterior gypsum board edges are not covered by applied moldings.

E.	Install control joints at locations indicated, or if not indicated, at spacings and locations required by referenced gypsum board application and finish standard.

3.07	INSTALLATION OF MISCELLANEOUS MATERIALS

A.	Install each item in accordance with the manufacturer's directions and recommendations.  Use anchors and other fasteners supplied by the manufacturer which match the finish of the items.  Install all items plumb or level.

B.	Mount chair rails at 2'-6 1/2" above finished floor level.

3.08	FINISHING OF DRYWALL

A.	General:  Apply treatment at gypsum board joints (both directions), flanges of trim accessories, penetrations, fastener heads, surface defects, and elsewhere as required to prepare work for decoration.

1.	Prefill any open joints and rounded or beveled edges using type of compound recommended by the manufacturer.

2.	Apply joint tape at joints between gypsum boards, except where trim accessories are indicated.

3.	Finish interior gypsum board by applying joint compound in three coats (not including prefill of openings in base), and sand between coats and after last coat.

B.	Base for Acoustical Tile:  Where gypsum board is indicated as a base for adhesively-applied acoustical tile, install tape and 2-coat compound treatment, without sanding.

C.	Water-Resistant Gypsum Board Base for Ceramic Tile:  Treat joints and fasteners to comply with directions of water-resistant joint compound manufacturer.

1.	In areas to be tiled, treat fastener heads with water-resistant joint compound.

a.	Fill tapered edges in gypsum panels with water-resistant joint compound, embed joint tape firmly, and wipe off excess compound.

b.	Follow immediately with a second coat of water-resistant joint compound over taping coat, being careful not to crown the joint.

c.	Fold and embed tape in all interior angles to form true angle.

2.	In areas not to be tiled, treat fastener heads and embed tape as indicated above, using water-resistant joint compound.  Finish with two coats of joint compound used for regular gypsum board work.

D.	Fire-rated Gypsum Board:  Tape and bed all joints including all layers of multiple layer applications.

E.	Surface Texturing:  All gypsum board surfaces exposed in finish areas shall be textured.  Finish areas are those specified to be painted and as scheduled on the drawings.

1.	Texture shall be a "spatter" spray application unless otherwise approved.

2.	Spray shall be applied to produce a uniform texture without starved spots or other evidence of thin application.

END OF SECTION